## Slide 1
Steffen, CLIC meeting, 14.3.2008
π/2 brazed Cu disc structure

## Slide 2
Steffen, CLIC meeting, 14.3.2008
π/2 brazed Cu disc structure

## Slide 3
π/2 brazed Cu disc structure
Waveguide wall of the input coupler
Power in
Power in

## Slide 4
π/2 brazed Cu disc structure
Input
Damage decreases slightly but does not vanish away completely
Only the last matching iris is significantly less damaged
More melting on the downstream side of the irises
“Pitting” present, possibly due to wire cutting

## Slide 5
2π/3 brazed Cu disc structure
Alberto, CLIC meeting 30.6.2006

## Slide 6
Alberto, CLIC meeting 30.6.2006
2π/3 brazed Cu disc structure

## Slide 7
Waveguide wall of the input coupler
2π/3 brazed Cu disc structure
Power in
Power in
π/2 Cu
π/2 Cu
π/2 Cu

## Slide 8
2π/3 brazed Cu disc structure
Input
Damage decreases but does not vanish away completely
  The decrease is stronger than for π/2 Cu
Less damaged than the π/2 Cu
More melting (perhaps) on the upstream side of the irises
“Pitting” heavily present, possibly due to wire cutting

## Slide 9
π /2 and 2π/3 compared side by side

## Slide 10
π /2 and 2π/3 compared side by side
Input matching irises
Output matching irises

## Slide 11
30HDS11 Small Cu
IMTEC - Cu HDS11 small, 30HDSQ11S.Cu
  Received at CERN in CW44
  RF check in CW45 (they are OK)
  Metrology: CW51 OK
  Burr removal: CW3 (add. step)
  Cleaning: CW04
  SEM: CW05
  Heat treatment: CW06
  SEM: CW08

## Slide 12
30HDS11 Small Cu
After deburring, cleaning and heat treatment
As received
Machining marks “softened” after heat treatment
Machining traces look very smooth
Chip-like burrs are removed
Thick burrs remain (possibly in the high field regions? Input waveguide wall)