## Slide 1: Contrast layers at sub-surface: diamond turned Cu vs annealed Cu
Tomoko Muranaka
Breakdown meeting, 03/09/2013

## Slide 2
Only diamond turned sample, pristine surface
Thin Pt deposited by electron
Thick Pt deposited by Ga ion

## Slide 3
Only diamond turned sample, middle of breakdown area

## Slide 4
Annealed in vacuum sample (without etching),
around a grain boundary
Pt deposited by electron
Pt deposited by Ga ion
Due to misalignment of the system, some part of Cu are remained. Rectangular milling couldn’t be completed in this case.

## Slide 5
Surface of annealed in vacuum sample (without etching)
Milled area

## Slide 6: Summary
The contrast layers are seen at sub-surface area only in the diamond turned sample but not in the annealed sample.
This may indicate a stress-relaxation effect of annealing.