## Slide 1: CERN Nb3Sn Strand Specification, Near Term Procurement and Measurement Plan
Ballarino, L. Oberli, B. Bordini and L. Bottura
Hi-Lumi LHC/LARP Conductor and Cable Internal Review
Ballarino, TE-MSC-SCD

## Slide 2
Conductor for MQXF quadrupole
Double sourcing
  Procurement of PIT and RRP Nb3Sn wire
 Qualification of PIT and RRP Nb3Sn wire
 Development and qualification of PIT and RRP cables
Identical Technical Specification for parallel procurement of PIT and RRP Nb3Sn wire
Procurement of conductor for MQXF started in mid 2012. Experience at CERN with: FRESCA 2 ( strand = 1 m, 40-strand cable) and 11 T Dipole ( strand =0.7 mm, 40-strand cable) Nb3Sn conductor and cables

## Slide 3
Specification – MQXF Strand (35 km+35 km)
1)
2)
3)
1) Selected by magnet designers using past conductor experience
2) Based on characteristics of procured conductor and on conductor R&D activity
(at the time of the procurement experience was on 1 mm and 0.7 mm PIT and RRP strands)
3) From magnet designers (protection) and conductor experience
Minimum Unit Length
400 m
Procurement of 35 km + 35 km of strand

## Slide 4
4)
5)
Specification – MQXF Quadrupole Strand
4) From magnet requirements and conductor experience. Performance specified at 15 T
5) From conductor stability requirements (RRR > 100 on extracted strands) and past experience.
First CERN large procurement with RRR specified to be above 150 – previous orders: RRR > 100
Minimum Unit Length
400 m
Procurement of 35 km + 35 km of strand
Notes: Jc(4.2K,12T)=1424/1472 A/mm2

## Slide 5
Specification – MQXF Strand Specification
Iop_cable = 17460 A
Bpeak = 12 T
361 A
4.2 K, 15 T
632 A
4.2 K, 12 T
Strand Specification
Operation @ 1.9 K
488 A
531 A
436.5 A
P. Ferracin
 18 % Margin on the load line at 1.9 K
Notes: 17320/40=433 A

## Slide 6
Performance of 5 km +5 km MQXF strand
 | RRP 132/169 | PIT 192
Wire diameter | 0.850.003 mm | 0.850.003 mm
Total length | 5 km | 5 km
Unit lengths (m) | 307-979 m 10 ULs, 4 billets | 2500 m /1870 m /734 m 3 ULs,1 billet
Sub-element size | 48 m | 41 m
Ic/Jc (4.2 K, 12 T) |  722 A/2835 Amm-2 |  *590 A/2412 Amm-2
Ic/Jc(4.2 K, 15 T) |  363 A/1425 Amm-2 |  **330 A/1349 Amm-2
RRR | > 180 | > 180
Cu/non-Cu | 1.2-1.35 | 1.33-1.34
* Ic measured on early production 637 A (2648 Amm-2)
** Ic measured on early production 366 A (1521 Amm-2 )
Notes: Short sample measurements refer to different billet

## Slide 7
Past procurement – MQXF Wire
2012 Procurement (5 km+ 5 km)
Conductor for cabling optimization and winding
trials -45 kg
5 km RRP Ti-Ternary 132/169, delivered in Dec 2012
5 km PIT Ta-Ternary 192, delivered in March 2013
Minimum UL=300 m
Jc(4.2 K, 12 T) > 2450 A/mm2
n-value (4.2 K, 15 T) > 30
RRR > 150
Cu-non Cu = 1.2 min, 1.3 max

## Slide 8
2013 Procurement (35 km + 35 km)
Conductor for short model program – 318 kg
35 km RRP 132/169
8 km to be delivered in Nov. 2013 - on track for on time delivery
27 km to be delivered in April 2014
35 km PIT 192
4 km to be delivered in Nov. 2013 – on track for
on time delivery
31 km to be delivered in Febr. 2014
On-going procurement – MQXF Wire

## Slide 9
2014 Procurement (20 km + 20 km)
Conductor for Short Model Program – 182 kg
20 km RRP by first trimester 2015
20 km PIT by first trimester 2015
Short term procurement – MQXF Wire
Procurement of conductor needed
for the short model coil program (6 + 6 coils)
(SMP 550 kg)
In addition: procurement of low-grade (lower cost) PIT and RRP conductor for winding/trials and practice coils– for deliveries as from Jan 2014

## Slide 10
Procurement – MQXF Wire
Procurement plan presented/discussed during CERN-LARP video-conference meeting, Dec 2012 and LARP Meeting, Napa, April 2013
Procured
Ordered.
On-track
Planned
Short Model Program
Planned
Long Prototypes
2012
2013
2014
2015
2016
Cabling trials: 5+5 km
SMP: 35+35 km
SMP: 20+20 km
LP: 200+200 km
2017
Conductor
for series

## Slide 11
2015-2016 Procurement
Conductor for Long Prototypes – 1.8 tons
200 km RRP deliveries 2015 - mid 2016
200 km PIT deliveries 2015 – mid 2016
Short term procurement – MQXF Wire
Last order before
procurement of conductor for MQXF series
SMP + LMP = 2.35 tons of high-grade conductor

## Slide 12
Procured
Ordered.
On-track
Planned
Short Model Program
Planned
Long Prototypes
2012
2013
2014
2015
2016
Cabling trials: 5+5 km
SMP: 35+35 km
SMP: 20+20 km
LP: 200+200 km
2017
Conductor
for series
Procurement – MQXF Wire
Practice coils
SMP: 7+7 km
Practice coils
LMP: 30+30 km
6+6 SMCs
6+6 LMCs
5+5 SMCs (May 2015)
Notes: 6 bobine corte = 40 km; 5 bobine corte = 33 km; 6 bobine lunghe = 180 km

## Slide 13
Procurement of MQXF wire (2012-2016)

## Slide 14
Tests on conductor and cables
Today still extensive tests are needed to qualify newly developed conductor and cables
More measurements are needed to increase statistics - for the MQXF cable wire only 5+5 km of wire was procured till now. Delivery of conductor from first “significant” (35 km + 35 km) order of MQXF strand starts in November 2013
Some discrepancies were found between Ic values provided by wire manufacturers and values measured at CERN – being investigated

## Slide 15
Measurement of wires and cables at CERN
 | Strands | Cables
Critical current* | 1.9 K and 4.2 K, up to 15 T Virgin and extracted strands | 1.9 K and 4.2 K, up to Bext= 10 T (Bpeak  12 T), 32 kA now and 70 kA next year. Ic, stability, MQE, quench propagation, joints,… Effect of transverse pressure
Magnetization | 1.9 K and higher, up to 11 T Virgin and extracted strands | -
Stability (laser) | 1.9 K and 4.2 K, Virgin and extracted strands | -
RRR | Virgin and extracted strands | -
Optical and SEM images, EDS, QC | Virgin and extracted strands Spring-back test | Deformation of filaments QC system of LHC cables
*0.1 V/cm electric field Ic criterion. Range for n-value: 0.1 V/cm- 1 V/cm

## Slide 16
Tests performed at the manufacturer premises
Dimensions
RRR
Sharp bend
Spring back
Rolling
Eddy current
Critical current

## Slide 17
Conclusions
Procurement of conductor for SMCs program has been launched. A procurement strategy has been established in accordance with requirements for coils assembly
CERN will proceed with a double sourcing (PIT and RRP)
CERN procurement is based on RRP 132/169 and PIT 192. Experience at CERN on RRP 132/169 is with the FRESCA 2 and the 11 T Projects – see next presentation