## Slide 1: Past and Present Manufacture and Performance of PIT and RRP132/169
A. Ballarino, L. Oberli, B. Bordini, D. Richter and L. Bottura
Hi-Lumi LHC/LARP Conductor and Cable Internal Review
A. Ballarino, CERN

## Slide 2
Double sourcing
  Procurement of PIT and RRP Nb3Sn wire
 Qualification of PIT and RRP Nb3Sn wire
 Development and qualification of PIT and RRP cables
FRESCA 2. Diameter of strand =1 mm. Procurement started in Marc 2010 it will be completed in Dec 2013
( 170 km tot)
11 T Dipole. Diameter of strand =0.7 mm. Procurement started in May 2010
MQXF Quadrupole. Diameter of strand =0.85 mm
Procurement started in August 2012
Conductor specification and procurement

## Slide 3
 | Sub-element size (m) |  |  |  |  | 
 | Wire  (mm) | RRP 108/127 | RRP 132/169 | RRP 192/217 | PIT 114 | PIT 192
FRESCA 2* | 1 | - | 58 | - | - | 48
Hi-Lumi Quad | 0.85 | - | 48 | - | - | 41
11 T | 0.7 | 46 | 41 | 32 | 44 | -
Smaller sub-element size
Conductor procured for CERN projects
*Fresca 2 conductor: procurement by CERN and CEA – FP7 European Project
RRP
54/61
108/127
132/169
198/217
PIT
114
192

## Slide 4
 | Quantity Procured (km) |  |  | 
 | Wire  (mm) | RRP 132/169 | PIT 114 | PIT 192
FRESCA 2 | 1 | 10+15+18+45 | - | 1+9+15+15+45
Hi-Lumi Quad | 0.85 | 5 + 35 | - | 5 + 35
11 T | 0.7 | 30 + 150 | 3 + 22.4*+ 50 | -
Delivered
In production at OST - on track (38 km Febr. 2014, total quantity by Aug. 2014)
In production at Bruker – on track. Conductor to be delivered in 2013
In production - on track (delivery completed in first trimester 2014)
Conductor procured: RRP 132/169 and PIT
* Additional length of 12.2 km of PIT 192, 0.778 mm diameter, procured by CERN for LARP – shipped by CERN to LBNL in June 2013

## Slide 5
Fresca 2
11 T
Hi-Lumi Quadrupole
PIT (43 %) and RRP (57 %)
1.29 tons RRP 132/169
Quantity of Nb3Sn conductor procured

## Slide 6
Quantity of Nb3Sn conductor procured
2.5 tons

## Slide 7
 |  | Quantity Procured (km) |  | 
 | Wire  (mm) | RRP 132/169 | PIT 114 | PIT 192
FRESCA 2 | 1 | 10+15+18+45 | - | 1+9+15+15+45
Hi-Lumi Quad | 0.85 | 5 + 35 | - | 5 + 35
11 T | 0.7 | 30 + 150 | 3 + 22.4*+ 50 | -
Total length |  | 308 | 75.4 | 125
RRP 132/169, PIT 114 and PIT 192

## Slide 8
Specification – Procured conductor
 |  | FRESCA 2 | 11 T Dipole | Hi-Lumi Quadrupole
Wire  | mm | 1  0.003 | 0.7  0.003 | 0.85  0.003
Sub-element  | m | < 50 | < 45 | < 50
Cu/non-Cu |  | 1.25  0.1 | 1.15  0.1 | 1.1  0.1
Twist pitch | mm | 24  2 | 14  2 | 19  2
Ic(4.2 K) | A | > 873 @12 T | > 438 @ 12 T | > 361 A @ 15 T
Jc(4.2 K) | A/mm2 | > 2500 @ 12 T | > 2450 @ 12 T | > 1340 @ 15 T
n-nalue (4.2 K, 15 T) |  | > 15 | > 15 | > 15
RRR |  | > 150 | > 100 | >150
Unit length | m | > 800 | > 700 | > 400
150 km
35 km
45 km
Quantity of conductor procured

## Slide 9
Billet ID 1.0 mm 132/169 | Jc (4.2 K,15T) A/mm2 OST | Jc (4.2 K,12T) A/mm2 OST | Jc (4.2 K,12T) A/mm2 CERN | RRR CERN
14310 | 1569/1627/1627 | 3020/3047/3026 | 2751/2810/2780 | 296/311/317
14311 | 1698/1624/1627 | 3119/3098/3071 | 2843/2781/2897 | 311/318/304
14312 | 1562/1557/1595 | 2967/2983/3040 | 2738/2739/2799 | 329/335
14108 | 1612/1599/1644 | 3102/3028/3090 | 2749 | 297
14393 | 1609/1641/1655 | 3006/3057/3102 | 2808/2940 | 281/267
14839 | 1540/1579/1599 | 2947/2943/3016 | 2746/2794/2793 | 201/241/218
14840 | 1646/1641/1604 | 3040/3051/3013 | 2743/2833/2800 | 222/250/288
14842 | 1617/1644/1594 | 3025/3058/3026 | 2656/2785/2664 | 222/263/230
Average value | 1613 A/mm2 | 3036 A/mm2 | 2783 A/mm2 | 280
Fresca 2 RRP strand ( = 1 mm)
RRP 132/169
Cu/non Cu values: 1.23 -1.32
50 hours at 650 C
Specified values
> 2500 A/mm2
> 150

## Slide 10
Fresca 2 RRP strand ( = 1 mm)
RRP 132/169
Chart: No. of Pieces
14108 | 3312 | 891 | 781 | 577
14163 | 4246 | 670 | 207 | 188
14310 | 1200 | 654 | 577 | 472
14842 | 1568 | 1199 | 924
14311 | 1154 | 846 | 712 | 581 | 502
14312 | 2475 | 1179 | 533
14393 | 768 | 493
14839 | 2360 | 1219
14840 | 2560 | 1830 | 415
800 m
80 % of Ltot = 35 km delivered in Uls > 800 m

## Slide 11
Billet ID 0.85 mm 132/169 | Jc (4.2 K,15T) A/mm2 OST | Jc (4.2 K,12T) A/mm2 OST | Jc (4.2 K,12T) A/mm2 CERN | RRR CERN
14842 | 1512/1498 | 2888/2900 | 2830/2752 | 160/212
14393 | 1440/1451 | 2881/2877 | 2808/2744 2776/2666 | 232/186 201/196
14310 | 1510/1598 | 2966/3023 | 2757/2820 | 210/215
14839 | 1463/1425 | 2842/2835 | 2800 | 189
Average value | 1490 A/mm2 | 2900 A/mm2 | 2770 A/mm2 | 180
50 hours at 640 C
RRP 132/169
Hi-Lumi quadrupole RRP strand (=0.85 mm)
Cu/non Cu ratio: 1.21 -1.35
Specified values
> 150
> 1340
Verificare

## Slide 12
RRP 132/169
11 T Dipole RRP strand (=0.7 mm)
Billet ID 0.7 mm 132/169 | Jc (15T) A/mm2 OST | Jc (12T) A/mm2 OST | Jc (12T) A/mm2 CERN | RRR
14799 | 1335/1182/1253 | 2669/2456/2530 | 2490/2380/2490 | 175/159 204
14833 | 1226/1244/1218 | 2540/2575/2485 | 2295/2449/2457 | 97/90/101
14841 | 1314/1300/1267 | 2647/2612/2588 | 2402/2470/24322472 | 134/139 121/117
Average value | 1260 A/mm2 | 2567 A/mm2 | 2434 A/mm2 | 134
Cu/non Cu ratio: 1.17 - 1.33
50 hours at 640 C
Specified values
> 2450 A/mm2
> 100

## Slide 13
RRP 132/169
Chart: Strand Diameter (mm)
| 0.7 | 0.85 | 1
Jc(15 T) | 1260 | 1490 | 1613
RRR | 134 | 180 | 280
RRR
4.2 K, 15 T
Sub-element geometrical size (m)
48
58
41

## Slide 14
Chart: Strand diameter (mm)
| 0.7 | 0.85 | 1
Jc(12 T) OST | 2567 | 2900 | 3036
Jc(12 T) CERN | 2434 | 2770 | 2783
RRP 132/169
4.2 K, 12 T
Sub-element geometrical size (m)
48
58
41

## Slide 15
Billet ID 1.0 mm | Jc (15T) A/mm2 Bruker | Jc (12T) A/mm2 CERN | RRR CERN
10503 | 1399 | 2508/2528 | 153/155
11201 | 1410 | 2451/2453/2616 | 160/172/175
10402 | 1353 | 2462/2477/2634 | 103/96/105/135
11302 | 1337 | 2519/2415 | 165
11403 | 1463/1507 | 2512/2507 | 154/173/179/201
23448 | 1403/1433 | 2442/2412 | 225/226/241/201
23258 | 1406/1382 | 2480/2447/24792391/2372/2446 | 159/161/201/209
23728 | 1518/1523 | 2548/2621 | 180/184/154/147
Average values | 1423 A/mm2 | 2478 A/mm2 | 176
Cu/non Cu ratio: 1.23 - 1.32
Fresca 2 PIT strand ( = 1 mm)
PIT 192

## Slide 16
Fresca 2 PIT strand ( = 1 mm)
Chart: No. of Pieces
10402 | 2954 | 1880
10503 | 3162
11201 | 2786 | 2594
11302 | 4903
11403 | 4028 | 1575
23728 | 3085 | 2360
23258 | 1672 | 1133 | 547 | 518
23448 | 881 | 564 | 404
800 m

## Slide 17
PIT 192
Hi-Lumi quadrupole PIT strand (=0.85 mm)
Billet ID 0.85 mm 192 | Jc (4.2 K,15T) A/mm2 Bruker | Jc (4.2 K,12T) A/mm2 Bruker | RRR Bruker
29992 | 1349/1343 | 2395/2412 | 183/193
26279 | 1521 | 2648 | 230
Average value | 1404 A/mm2 | 2485 A/mm2 | 205
Cu/non Cu ratio: 1.33 - 1.34
Production of 5 km
Standard Sn content
> 150
> 1340

## Slide 18
RRP 132/169 and PIT 192
Chart: Strand diameter (mm)
| 0.85 | 0.85 | 1 | 1
RRP 132/169 | 1490 | 2900 | 1613 | 3036
PIT 192 | 1350 | 2414 | 1423 | 2523
12 T
15 T
Comparable performance at 15 T

## Slide 19
Chart: Sub-element geometrical size (m)
| 41 | 48
PIT | 2414 | 2523
 | 1350 | 1423
 | 2567 | 2900 | 3030
RRP | 1260 | 1490 | 1613
RRP 132/169 and PIT 192
12 T
15 T

## Slide 20
Conclusions (1/2)
Main experience at CERN with RRP 132/169 ( 1.3 tons tot) is today based on procurement of conductor for FRESCA 2
A large procurement (150 km) of RRP 132/169 for the 11 T Dipole has been launched – production on track, deliveries expected from Feb. 2014 until Aug. 2014
Experience with the 5 km production of RRP 132/169 for the Hi-lumi Quadrupoles indicates that this conductor meets specification in terms of both Jc and RRR. The RRR measured on the 0.85 mm diameter wire with standard, i.e. not reduced, Sn content is above 180

## Slide 21
Conclusions (2/2)
The - today limited - experience at CERN with RRP 192/217 indicates that RRP 192/217 is still an R&D conductor
In parallel with qualification and procurement of PIT 192, development of Nb3Sn wires of 0.7 mm diameter with smaller (30 m) filaments size and high Jc and RRR is being performed in the framework of a CERN/Bruker EAS R&D Contract