## Slide 1: CERN Cabling Experience FRESCA 2, 11 T Dipole and MQXF A. Ballarino
A. Ballarino, L. Oberli and B. Bordini
17/10/2013
Hi-Lumi LHC/LARP Conductor and Cable Internal Review

## Slide 2
Outline
Fresca 2 and 11 T cables : short overview of geometry and performance
Status of development of MQXF cable
Development of RRP cable
Development of PIT cables
“First generation” cable
Short term planned activity and conclusions
Cable developed at CERN by L. Oberli and A. Bonasia

## Slide 3
Nb3Sn cabling experience at CERN
Fresca 2 cable: 40 strands
 of strand = 1 mm
RRP 132/169
PIT 192
11 T Dipole cable 40 strands
 of strand = 0.7 mm
RRP 54/61, RRP 108/127, RRP 132/169
PIT 114
MQXF Quadrupole 40 strands
 of strand = 0.85 mm
RRP 132/169
PIT 192

## Slide 4
Ic(4.2 K,12 T) | A | 31420
Ic(4.2 K, 15 T) | A | 15170
Iop(1.9 K, Bpeak=13.4 T) | A | 10900 A
n-value(4.2 K, 15 T) | - | > 20
RRR | - | > 100
Cable for FRESCA 2
RRP 132/169
PIT 192

## Slide 5
Strand diameter | mm | 1
Number of strands | - | 40
Cable width | mm | 20.9
Cable mid thickness (50 MPa) | mm | 1.82
Keystone angle | deg | 0
Cable transposition pitch | mm | 120
Aspect ratio | - | 11.48
Packing factor | % | 87.4
Unit length | m | 260
Cable for FRESCA 2
Measured Ic degradation < 5.5 % for cables, with same geometry, made
with PIT and RRP strands. Cables mechanically stables
Without core

## Slide 6
Cable for FRESCA 2
Ic degradation < 5.5 % for cables, with same geometry, made
with PIT 192 or RRP132/169 strands. Cables mechanically stable

## Slide 7
Cable for 11 T dipole
Iop(1.9 K, Bp=11.2 T) | A | 11850
n-value(4.2 K, 15 T) | - | > 20
RRR | - | > 100
RRP 54/61
RRP 108/132
RRP 132/169
PIT 114

## Slide 8
Cable development for 11 T dipole
Strand diameter | mm | 1
Number of strands | - | 40
Cable width | mm | 14.7
Cable mid thickness | mm | 1.25
Keystone angle | deg | 0.78
Cable transposition pitch | mm | 100
Aspect ratio | - | 11.76
Thin edge | mm | 1.149
Thick edge | mm | 1.351
t/2d thin edge | % | 82.5
t/2d thick edge | % | 96.5
Packing factor | % | 87.3
With stainless steel (316 L) core - 12 mm width and 25 m thickness

## Slide 9
Cable for 11 T dipole
Cable ID | Run ID | Length | Width | Mid-thickness at 50 MPa | Keystone angle
H15OC0127A | 86A | 237 m | 14.715 mm | 1.2498 mm | 0.78o
H15OC0127B | 86A | 235 m | 14.717 mm | 1.2491 mm | 0.78o
H15OC0137A | 96A | 218 m | 14.706 mm | 1.2499 mm | 0.78o
Three unit lengths produced for the first 3 CERN 11 T Short Model Coils
RRP 108/127 Cables
In the last two months, development started with cables made from PIT 192 and RRP 132/169 strands:
Degradation < 1.3 % for cables made with RRP 132/169 strands
Same degradation (< 1.3 %) degradation measured on cables made with PIT 114 strands when keystone angle reduced to 0.61o – mid thickness = 1.263

## Slide 10
RRP 208/127 Cables with same geometry and same heat treatment
48h/210C + 48h/400C + 50h/640C
Cable development for 11 T dipole
Degradation of RRR in 11 T cables made from RRP 198/127 strands

## Slide 11
Cable development for MQXF quadrupole
RRP 132/169
PIT 192
Iop(1.9 K, Bp=11.2 T) | A | 17460
n-value(4.2 K, 15 T) | - | > 20
RRR | - | > 100
Stainless steel (316 L) core - 14 mm width and 25 m thickness

## Slide 12
Width : 17.8 mm
Width compaction Cw = - 3.5
Mid-thickness : 1.50 and 1.53 mm
Keystone angle : 0.65 degree
Pitch length : 113 mm (17.5o) and 125 mm (16o)
Cw larger than its value for the FRESCA2 cable (- 4.6) but smaller than its value for the cable for the dipole DS 11 T (- 2.6).
Cable development for MQXF quadrupole

## Slide 13
Cable development for MQXF quadrupole
Production of PIT and RRP cables with identical geometries: width  17.8 mm and  18.1 mm and mid-thickness of  1.5 mm
Variation of keystone angle and twist pitch
Verification of critical current degradation - critical current measurements, optical and SEM analysis – and of winding behaviour – cable mechanical stability

## Slide 14
Mechanical stability Summary
P. Ferracin and S. Izquierdo Bermudez

## Slide 15
Cable development for MQXF quadrupole
RRP 132/169
Sample | Cable ID | Cable width | Mid-thickness | Pitch length | Keystone angle
1 | H16OC0123BA | 17.8 mm | 1.551 mm | 109 mm | 0.66 degree
2 | H16OC0123BB | 17.8 mm | 1.534 mm | 109 mm | 0.67 degree
3 | H16OC0123BC | 17.8 mm | 1.509 mm | 109 mm | 0.65 degree
4 | H16OC0139A* | 17.8 mm | 1.530 mm | 113 mm | 0.50 degree
5 | H16OC0139A* | 17.8 mm | 1.518 mm | 113 mm | 0.54 degree
6 | H16OC0132CA | 18.1 mm | 1.512 mm | 109 mm | 0.62 degree
7 | H16OC0132C | 18.12 mm | 1.512 mm | 95 mm | 0.60 degree
8 | H16OC0132C | 18.08 mm | 1.517 mm | 120 mm | 0.56 degree
During winding tests, all cables were NOT sufficiently mechanically stable
(* better behaviour because of smaller keystone angle – increased compaction
of the thick edge)

## Slide 16
Cable development for MQXF quadrupole
RRP 132/169
17.8 mm wide cable with a keystone angle of 0.65o
Pitch length 113 mm, mid-thick. 1.50 mm: degradation 1.8 % ( - 1.6% to 4.5% ) oil RRR=137
Pitch length 109 mm, mid- thick. 1.534 mm: degradation 0.75 % ( 0% to 3.3% ) oil RRR=112
Pitch length 109 mm, mid-thick. 1.50 mm: degradation 4.1 % ( 2.1% to 6.5% ) oil RRR=122
Pitch length 125 mm, mid-thick 1.50 mm: degradation 2.6 % ( 1.5% to 4% ) no oil RRR=126
17.8 mm wide cable with a keystone angle of 0.58o
Pitch length 125 mm, thickness 1.479 mm: degradation 0.9 % ( -0.3% to 2.8% ) no oil RRR=97
18.1 mm wide cable with a keystone angle of 0.62o
Pitch length 109 mm, thickness 1.512 mm: degradation 1.1% ( - 1.7% to 3.6% ) oil RRR=115
Low-critical current degradation
The larger width does not impact on the degradation
RRR of extracted strands above 100 – RRR of virgin strands > 180

## Slide 17
Cable run 82 fabricated without a core :
Keystone angle 0.64o
Pitch Length of 113 mm,
Mid-thickness of 1.50 mm
Cable run 90 fabricated with a core:
Keystone angle 0.65o
Pitch Length of 109 mm,
Mid-thickness of 1.50 mm
Width = 17.8 mm
Use of oil as lubricant
48h/210C + 48h/400C + 50h/640C
Cable development for MQXF quadrupole
RRP 132/169

## Slide 18
Cable development for MQXF quadrupole
PIT 192
Sample | Cable ID | Cable width | Mid-thickness | Pitch length | Keystone angle | Winding test
1 | H16EC0131AA | 17.8 mm | 1.5418 mm | 109 mm | 0.65 degree | OK
2 | H16EC0131AB | 17.8 mm | 1.523 mm | 117 mm | 0.64 degree | Not OK
3 | H16EC0131AC | 17.8 mm | 1.507 mm | 117 mm | 0.63 degree | Not OK
4 | H16EC0138A | 17.8 mm | 1.531 mm | 109 mm | 0.52 degree | Not OK
5 | H16EC0143AA | 17.8 mm | 1.520 mm | 117 mm | 0.52 degree | Not OK
6 | HE16E0132AA | 18.1 mm | 1.525 mm | 109 mm | 0.57 degree | Not OK
7 | HE16E0132AB | 18.1 mm | 1.540 mm | 95 mm | 0.55 degree | OK
8 | HE16E0132AD | 18.1 mm | 1.520 mm | 117 mm | 0.57 degree | OK
During winding tests, three cable geometries – in red in the table - were
mechanically stable – winding of bare cable with no use of winding tools
and/or binder

## Slide 19
Cable development for MQXF quadrupole
PIT 192
17.8 mm wide cable with a keystone angle of 0.65o
Pitch length 109 mm, thickness 1.507 mm: degradation 6.9 % ( 5.1% to 7.8% ) oil
Pitch length 109 mm, thickness 1.507 mm: degradation 7.5 % ( 6% to 8.8% ) no oil
Pitch length 109 mm, thickness 1.543 mm: degradation 8.9 % ( 7.8% to 10% ) no oil
Pitch length 117 mm, thickness 1.523 mm: degradation 6.8 % ( 5.4% to 8.6 % ) no oil
18.1 mm wide cable with a keystone angle of 0.57o
Pitch length 109 mm, thickness 1.52 mm: degradation 7.8 % ( 6% to 8.6% ) oil
17.8 mm wide cable with a keystone angle of 0.52o
Pitch length 117 mm, thickness 1.520 mm: degradation 4.9 % ( 2.6% to 7.1% ) oil
Pitch length 125 mm, thickness 1.520 mm: degradation 5.8 % ( 4.6% to 7.1% ) oil
Critical current degradation  4.9 % -8.9 % for 17.8 mm wide cable
The larger width does not impact significantly on the degradation
RRR of extracted strands above 100
PL=117 mm

## Slide 20
Cable development for MQXF quadrupole
H16EC0131AE
Limited shearing seen through the sub-elements of the PIT cable.
Cross-section of the PIT 192 cored cables
(17.8 mm, PL = 109 mm, 1.50 mm, 0.65 degree)

## Slide 21
Cable development for MQXF quadrupole
(PL = 113 mm, 1.50 mm, 0.65O)
(PL = 113 mm, 1.52 mm, 0.54O)
Cross-section of the RRP 132/169 cored cables (w=17.8 mm)
Significant shear of
sub-elements

## Slide 22
Cable development for MQXF quadrupole
Cross-section of the RRP 132/169 cored cables (w=18.1 mm)
Thin edge
Thin edge

## Slide 23
Qualification at CERN in FRESCA of two PIT MQXF cables (17.8/18.1 mm width, 117/109 mm twist pitch, 0.63/0.57 keystone angle).
Reached Ic calculated from Ic measured on extracted strands - see next presentation of B. Bordini
Cable development for MQXF quadrupole
PIT 192

## Slide 24
“First iteration” cable geometry
selected for first Short Model Coils
Cable width = 18.15 mm
Cable mid-thickness = 1.55
Keystone angle = 0.55
From previous tables:
PIT 192 cable mechanically stable (average degradation of 7.8 % measured at CERN on strands extracted from cable with 0.57  keystone angle);
RRP 132/169 cable mechanically unstable (average
degradation of 0.9 % measured at CERN on strands extracted from cable with 0.62  keystone angle)

## Slide 25
Remarks/Conclusions (1/3)
The geometry of the “first iteration” cable ended up to be better optimized for PIT – reached acceptable Ic degradation and complete mechanical stability – than for RRP – mechanical unstable cable
The performance of the “first iteration” cable is considered acceptable by magnet designers for the winding of the first short model coils
There are not sufficient results/sufficient understanding today to conclude that mechanical stability of RRP cable cannot be improved – at the benefit of reduced risk during winding of series of coils

## Slide 26
Remarks/Conclusions (2/3)
An activity has started at CERN in order to answer to the following points:
  RRP and PIT are different conductors with different mechanical characteristics. Can we reasonably converge to/adopt an identical cable geometry with acceptable electrical and mechanical performance ?
  Local RRR measurements are needed on extracted strands. How can we correlate the local RRR values, with the stability of the strand/cable and the results of the SEM images (number/quality of sheared sub-elements) ?
  Can we improve the mechanical stability of the RRP cable with a new geometry ? Would that geometry be acceptable for PIT ?

## Slide 27
Remarks/Conclusions (3/3)
Strand (PIT and RRP) for MQXF will be delivered to CERN by end of November 2013. Cabling, heat treatments of extracted strands and cables and various measurements need to be performed
Final deadline set by magnet program (June 2014, see presentation of Paolo and Giorgio) for the definition of the geometry of the “second/last generation” MQXF cable

## Slide 28
Thanks for your attention !