## Slide 1: Magnet Feedback: LARP Long Quadrupole
G. Ambrosio
with contributions by many LARP members
October, 17 2013
QXF Conductor Review

## Slide 2: Outline
Long Quadrupole (LQ) features and conductors
LQS02 conductor related issue
LQS03 conductor related issue
 lessons learnt about conductor

## Slide 3: Long Nb3Sn Quadrupole†
Main Features:
Aperture: 90 mm
Magnet length: 3.7 m
Target:
Gradient: 200 T/m
Goal: Demonstrate Nb3Sn magnet scale up
Parameter at SSL |  | LQS01/02 | LQS03
Strand type |  | RRP 54/61 | RRP 108/127
Jc at 4.2K 12T | A/mm2 | 2670 | 2660
Copper | % | 46% | 55%
Copper RRR in coils |  | > 200 | 70-130
SSL Current 4.6K/1.9K | kA | 13.7/15.2 | 12.9/14.4
SSL Gradient 4.6K/1.9K | T/m | 239/263 | 227/250
† LQ Design Report available online at:
https://plone4.fnal.gov/P1/USLARP/MagnetRD/longquad/LQ_DR.pdf

## Slide 4: LQS02 Conductor related issue

## Slide 5: Ramp Rate Dependence: LQS01b vs. LQS02
LQS01 and LQS02 magnets with the same conductor and coil design show very different ramp rate dependence

## Slide 6: LQS02 “Reverse” Ramp Rate Dependence
Ramp rate dependence was studied at 1.9 K, 2.6 K and 4.6 K
Low ramp rate quenches developed in the OL mid-plane block of coil 13
“Reverse ramp-rate dependence”

## Slide 7: Quenches in Coil 13, OL midplane block
Facts:
Voltage spike at every quench start
Quench started in several segments at the same time
Reverse ramp-rate dependence
Normal temp. dependence
Quenches at lower current during magnetic meas.
Coil 13 OL mid-plane, 10.5 k A
Coil 10 IL pole-turn, at 10.5 k A
G. Ambrosio, et al., “Progress in the Long Quadrupole R&D by LARP”,
IEEE Trans. Appl. Supercond., vol. 22, No. 3, June 2012

## Slide 8: LQS02 Analysis
Holding quenches, Voltage Tap data, Quench Antenna data, and Spike Recording System data confirmed:
The cause is “Enhanced Instability” in one coil
  An unknown “issue” causes a decrease of the stability threshold (Is/2.6) of the conductor in coil 13 OL.
  Possible “issues” are: (i) a local damage or a non-uniform splice forcing more current in a few strands; (ii) a damage of some strands decreasing the local RRR and/or causing filaments merging.

## Slide 9: Notes about Coil 13
By the time we made LQ Coil 13 the fabrication process was well established with small number of nonconformities
Although on Coil 13 inner surface we used three different materials trying to avoid “bubbles”
Lesson learnt:
There are issues that we are not able to detect, which may cause the failure of a coil/magnet
We have unstable conductors
 We need MARGIN!

## Slide 10: LQS03 Conductor related issue

## Slide 11: LQS03 Training History
All quenches started in the pole turn of the inner layer
  Always in the straight section

## Slide 12: LQS03 Temperature Dependence
Holding current at 200 T/m and 4.6 K for 40 minutes w/o quench
200 T/m
After “training”

## Slide 13: LQS03 Analysis
Current limitation independent of temperature
  11.5-11.8 kA
Quench start moving through several segments of 2 coils
No signs of precursors at quench start
One strain gauge showed unloading at 10.6 kA
  Current of quenches #2-#5
 1st possible cause: quenches due to start of unloading
But TQS03 showed more unloading and trained up to 238 T/m
TQS03 RRR > 150; LQS03 RRR > 70
Present understanding: self-field instability with low RRR† triggered by unloading
†E. Takala, et al., “Perturbation Sensitivity of the Magnetothermal Instability”,
IEEE Trans Applied Superc. Vol 22, N. 6, #. 4706106

## Slide 14: LQS03 quench training
Most quenches in Coil #18
Some quenches in Coil #16
One quench in Coil #19

## Slide 15: LQS03 RRR measurements
* RRR = 50 in kinks of one LQS03 extracted strand

## Slide 16: Stability study on RRP 108/127
E. Takala, B. Bordini, L. Rossi, Perturbation Sensitivity of the MagnetoThermal
Instability, IEEE Trans. Appl. Supercond., (2012), Vol 22, No 6, # 4706106
RRR = 50 in kinks of one LQS03 extracted strand

## Slide 17: Lessons Learnt
Issues (in conductor, coil fabrication, magnet assembly) are possible and will happen in the MQXFs
The conductor is NOT intrinsically stable
 we should try to have as much margin as possible
  Will result in better coil yield
Margin is give by:
Higher RRR in coils (minimum: 100, better: 150)
Smaller subelements
Avoiding excessive strand deformation/shear during cabling

## Slide 18: Backup Slides

## Slide 19: LQS02 Test at Fermilab
SSL was computed based on extracted witness sample test results
  LQS02 SSL estimate w/o additional strain: 13.8 kA or 240 T/m at 4.6 K
  Compare to 13.75 kA for LQS01 SSL at 4.6 K
Azimuthal compression of the coil’s pole reached ‑133 ± 28 MPa in LQS02, similar to ‑130 ± 30 MPa in LQS01b
LQS02 was tested at Fermilab in July-August 2011
Voltage tap system in LQ

## Slide 20: LQS02 Quench History
Exceeded 200 T/m at 1.9 K and 2.6 K (only for ramp rates of 100-150 A/s) but failed to reproduce LQS01b performance

## Slide 21: LQS02 quenches in coil 13
All quenches in coil 13 OL mid-plane area showed similar pattern
  Simultaneous start in several segments
  Voltage spikes at the beginning of quench could be indication of decreased conductor stability

## Slide 22: LQS02 quench patterns at high currents
Quench patterns in coil 13 OL mid-plane block (left) and coil 10 pole-turn block (right)
Coil 13 OL mid-plane, 10.5 k A
Coil 10 IL pole-turn, Quench at 10.5 k A

## Slide 23: More checks on conductor stability in LQS02
“Unknown conductor damage” could be a reason for enhanced instability
  Forcing current in a fewer number of strands
Holding quenches: the magnet current increased to 9.4 kA and then held till a quench occurred after 34 s, 57 s and 60 s
All segments have RRR larger than 200, resistance of NbTi-Nb3Sn splices in coil 13 found acceptable 0.8-1 nOhm

## Slide 24: Quench 4 I = 9337 A (ramp 4)

## Slide 25
Better signals by bucking segments in opposite coils;
13b2_b3 – 11 b2_b3
50 ms
Voltage spike captured
250 ms before quench,
~ 50 ms activity

## Slide 26
“Same” spike in other segments
250 ms before quench,
~ 50 ms activity

## Slide 27
Quench antenna segments:
1
2
3

## Slide 28
Quench start in Coil 13:
b4_b5
b3_b4
b2_b3
b1_b2
All segments start in 5 msec range

## Slide 29
Spikes in 13a2_a3:
The quench start looks like the -270 ms voltage spike  same cause

## Slide 30: LQS02
G. Ambrosio, et al., “Progress in the Long Quadrupole R&D by LARP”,
IEEE Trans. Appl. Supercond., vol. 22, No. 3, June 2012
200 T/m
Chart: LQS02 Ramp Rate Dependence vs Temperature
| 20 | 50 | 100 | 125 | 150 | 175 | 250 | 333
4.6K, Coil 13b | 9490 | 9800 | 10530 | 10722
1.9K Coil13b | 10819.6
4.6K Coil 11b | 11090
1.9K Coil10b | 11221
4.6K, RampRate | 10610 | 6745 | 2284.5
1.9K Coil10a | 11814 | 10689.3
2.6K, Coil13b | 10271 | 11170 | 11708
1.9K Coil11a | 11686.1 | 11743.4
2.6K Coil11b | 11090
1.9K RampRate | 8894
2.6K Coil10a | 11574
3.4 K, Coil13b | 9874
“Reverse ramp-rate dependence”
Caused by:
“Enhanced instability”

## Slide 31: LQS03
Test Highlights:
  1st quench at 4.6 K reached 197 T/m (86% ssl)
  1st quench at 1.9 K exceeded 200 T/m (6th quench overall)
  Temperature margin at 200 T/m ~3 K in peak field area
Parameter at ssl |  | LQS01/02 | LQS03 | TQS03
Strand type |  | RRP 54/61 | RRP 108/127 | RRP 108/127
Jc at 4.2K 12T (with SF) | A/mm2 | 2670 | 2660 | 2790
Copper | % | 46% | 55% | 54%
RRR of extracted strands* |  | >150 | 70-150 | 150-190
SSL Current 4.6K/1.9K | kA | 13.7/15.2 | 12.9/14.4 | 13/14.5
SSL Gradient 4.6K/1.9K | T/m | 239/263 | 227/250 | 231/254
* RRR = 50 in kinks of one LQS03 extracted strand

## Slide 32: LQS03 Mechanical Behavior
Strain gauges on structure:
  As expected
  Same prestress as LQS02 (target)
Strain gauges on coils:
  2 lost
  1 unloading at 10.6 kA
  large spread of starting points
    Calibration lost during cool down?
    Issues with thermal compensation?

## Slide 33: LQS03 RRR measurements
All segments

## Slide 34: Possible effect of low RRR - II
Impact of the Residual Resistivity Ratio on the Stability of Nb3Sn Magnets
B. Bordini, L. Bottura, L. Oberli, L. Rossi Senior Member IEEE, and E. Takala
Fig. 1. Sketch representing qualitatively the causes of premature quenches in superconducting magnets affected by magneto-thermal instabilities. In the plot it is reported the current in a strand of the magnet. The acronyms SF and M stand for Self Field and Magnetization respectively.
Fig. 3. Critical current and quench current at 1.9 K. The markers represent the experimental results while the dashed lines are the simulation using the proposed semi-analytical model.