## Slide 1: MM mechanical prototype
Work progress at CERN

## Slide 2: Purpose
Demonstrate feasibility
Setup of basic infrastructure
Gain experience with
  Materials
  Construction/assembly ideas/schemes
  Procedures
  Precision (panel planarity, parallelism of skins, …)
Produce objects that can be measured

## Slide 3: CERN mechanical prototype (1)
Full-wedge small sector quadruplet
  Eta and stereo doublets
Drift gap – 5 mm
Total thickness ~80 mm
Support frame (spacer)

## Slide 4
All panels of equal thickness ~12 mm
  Frame of standard 10 mm Al profiles
  0.4 mm plastic mesh
  9.5 mm foam panel
  Skins – 0.5 mm FR4 segmented into the 8 parts
  Glue – Araldite 2011 – Araldite AY 103-1 + HY 991 – Scotch-Weld DP490
CERN mechanical prototype (2)

## Slide 5: Assembling site
We get new space at Bld. 153-R-030
Iron table 4 x 2.5 m²
Flatness ≤ 20μm

## Slide 6: Vacuum table
On the table was placed thin plastic mesh for pressure distribution
Mesh was covered by 175 μm Mylar foil with the holes
Vacuum

## Slide 7: Vacuum table
On the Mylar was placed 8 pieces of FR4 skin joined by 60 μm Kapton scotch
Skins were sealed with the tape along the perimeter and sucked to the table

## Slide 8
Gluing (1)
Step 1 – 400 μm plastic mesh was glued on the skin
Step 2 – Aluminum frame and foam panels were placed and glued on the mesh

## Slide 9
Gluing (2)
Second skin was placed and sucked on the table
Glue was distributed on the surface
Plastic mesh was wetted by glue and placed on the skin
Prepared “half panel” picked up with the stiff-back structure and placed on the mesh
Calibrated shims were placed under the stiff-back

## Slide 10
Vacuum
Clarinet gas
Skin (G10)
Rohacell honeycomb
Vacuum
Using Stiff-back frame
Glue
Vacuum
Precision shim
Gluing (3)

## Slide 11: First experience (1)
All 5 full-wedge size panels (2 read-out and 3 drift) were glued using different glues and scheme:
The planarity of the panels seems good (visually) – to be measured on the laser interferometer
  Araldite AY103 + HY991 seems more comfortable
  When use Scotch-weld DP490 glue no need of the plastic mesh
Some problems with the gluing
  Some regions where mesh is not glued to the skin, needed injection of the fluid glue

## Slide 12
First experience (2)
Full panel view
Inner structure
Problematic regions

## Slide 13: Panel sag measurements (1)
To measure the sag of the panels, they were places on two ends
The measurements were done for each panel separately with and without additional weight (2.7 kg)
Same measurements were done also for the combination of 2, 3, 4 and 5 panels assembled together

## Slide 14
Panel sag measurements (2)

## Slide 15
Panel sag measurements (3)

## Slide 16
Panel sag measurements (4)

## Slide 17
Weight of the panels

## Slide 18
Prototype assembling
The panel weight varies between 18 and 22 kg
The weight of the assembled prototype including the spacer bars and assembling screws and nuts (100 pairs) –107 kg

## Slide 19
Prototype test
After applying of “extra weight” of 82.1 kg the sag of the assembled prototype increased by 3 mm
Sag came back to the previous value when extra weight has been removed

## Slide 20
Prototype test
Visual inspection shows rather good planarity, to be measured with more precise devises.

## Slide 21
Next step – spacer frame
The spacer frame has been designed and simulated (G. Spigo & M. Ciapetti)
Frame under contraction (Naples, CERN)
From other side of the spacer will be added the dummy wedge with equal weight
To be assembled and tested with prototype in the different orientation for the mechanical deformation, ect…

## Slide 22: Collaborative effort
CERN, Dubna, Lecce …
Drawings and calculations: Lecce and CERN
Infrastructure and tooling: CERN
Technical work: CERN, Dubna, Lecce, Naples + 3 summer students (2 physicist + 1 engineer)