## Slide 2: Highly transparent vacuum chambers
Outline:
Context
Present solutions
New material development
  Alternative to beryllium
  Figure of merit
  Type of material
  Status of different alternatives
Conclusion and next steps
Workshop on Advanced Materials and Surfaces

## Slide 3: Highly transparent vacuum chambers
In high energy physics detectors, transparent vacuum systems are required to:
Reduce the interaction of particles with the matter,
Reduce the activation of the materials,
Reduce the background to the experiments.

## Slide 4: Highly transparent vacuum chambers
Main requirements are:
Vacuum compatibility (leak tightness, low outgassing and permeation),
Temperature resistance (in the range 230 C)
Mechanical stiffness and strength
Transparency of the chamber is defined as:
thickness of the chamber
radiation length
density
Atomic number
Atomic weight

## Slide 5: Present solutions for transparent vacuum chambers Beryllium
Technical difficulties:
Material porosity thin walled vacuum chambers (0.8 mm);
Welding: cracks in welded joints
Beryllium is used for vacuum chambers in the experimental area due to its transparency and stiffness.
Range of geometry:
Thickness: 0.8 mm to 2.6 mm
Diameter: 34.4 to 260 mm
Length: up to 7.3 m
Main drawbacks:
Brittle
Toxicity
A few suppliers, cost

## Slide 6: Present solutions for transparent vacuum chambers Aluminum alloys
Issues: welds, deformation after bake out
Two grades are used for our applications:
2219 for the vacuum chambers, thickness down to 1 mm
5083 for the bellows expansion joints, thickness 0.3 mm, internal diameter ~ 60 mm
Porosities in EB welds between 2219 and 5083 for a bellows
Aluminium bellows
Porosities

## Slide 7: LHC transparent vacuum chambers
Type | Feature | ATLAS | CMS | LHCb | ALICE
Central | Materials | Be/Al | Be/st.st (Be/Al) | Be/Al | Be/st.st (Be/Al)
 | Length (m) | 7.3 | 6.2 | 1.85 | 4.82 (5.50)
 | Int. dia (mm) | 58 (47) | 58 (43.4) | 50-260 | 58 (34.4)
 | Wall (mm) | 0.8 | 0.8 | 1.0 | 0.8
 | Configuration | Cyl | Cone/Cyl/Cone | Cone (UX85/3) | Cyl (Cone/cyl/cone)
Forward | Materials | St.st (Al) | St.st (Al) | Be | Cu/St St
 | Length (m) | 4.2-5.35 | 1.65-7.6 | 3.7-6.05 | 5.0-6.9
 | Int. dia (mm) | 60 – 120 | 55.1-318 | 50-260 | 60-506
 | Wall (mm) | 1 – 2.2 | 1.2-2.8 | 1.0-2.6 | 1.5-2.8
 | Configuration | Cyl | Cone/cyl | cone | Cyl/cone
Characteristics: pre-LS1, (post-LS1), (post-LS2)

## Slide 8: Present solutions for transparent vacuum chambers Supporting system
“old” support to new design
Aluminium to beryllium collar
Stainless steel to CFRE or aramid fibres (Technora) wires
PBI (Celazole) interface pieces (can be used during bake out)
Stainless steel to titanium screws
All polymeric materials have been tested and qualified under radioactive environment.

## Slide 9: New material development for transparent vacuum chambers
Material choice
Transparency is given by:

## Slide 10: New material development for transparent vacuum chambers – Figures of merit
Temperature rise in transient regime:
Thermal fatigue:
Temperature rise in steady state:
Mechanical Stability (buckling):
Several figures of merit, characterizing the material, can be used depending on the final application.

## Slide 11: New material development for transparent vacuum chambers
 | Radiation length [cm] | Young Modulus [Gpa] | X0E1/3
Beryllium | 35 | 290 | 230
Epoxy | 30-36 |  | 
CFRE | 30 | ~ 200 | 175
Carbon | 29 | 35 (GC) | 95
Carbon/Al (60/40) | 17 | 120 (short fibers, randomly oriented) | 84
SiC | 8 | 450 | 61.3
Al2O3 | 7 | 390 | 51
AlLi | 10-11 | 78 | 43
Al | 9 | 70 | 37
Ti | 3.7 | 113 | 18
316L | 1.8 | 200 | 10.5
Figure of merit for thin vacuum chambers

## Slide 12: New material development for transparent vacuum chambers
Figure of merit of different materials, normalized w.r.t. beryllium

## Slide 13: New material development for transparent vacuum chambers
Low Z material for beam pipe
Raw material
Composite material
Structural composite
Carbon (Glassy carbon)
Al alloys
SiC
Carbon reinforcement: long fibers short fibers particulates | Matrix: Aluminium Epoxy + coating
C/C + liner
Sandwich/ Honeycomb composite
As a back-up solution and for very thin chamber
C/C tube and titanium tube set-up

## Slide 14: New material development for transparent vacuum chambers – Structural composite
Case of an external thin leak tight aluminium envelop with internal C/C reinforcement
 | Activation 200 ◦C for 24h | Activation 250 ◦C for 6h
H2 Pumping Speed [l/s] | 310 | 530
Sticking probability [-] | 5.9*10-3 | 1*10-2
 Good vacuum performance:
Outgassing rate ~ 10-12 mbar.l.s-1.cm-2 after bakeout
Compatible with NEG coating
Pumping speed with NEG coating
 Issue with the mechanical behaviour:
Differential thermal expansion  buckling of the thin aluminium envelop
Buckling mode of long tube
Strain concentration
Need to have significant envelop thickness
Either not reliable or not interesting
Internal C/C tube

## Slide 15: New material development for transparent vacuum chambers – Carbon fiber reinforced aluminum
Material obtained by aluminium infiltration of a carbon perform.
Tests on samples from Thales Alenia Space and Dresden University.
 Tentative to find company to try short carbon fibers or graphen in aluminium matrix: not successful (yet).
 Vacuum tests :
Leak tightness
Preliminary outgassing tests promising for unbaked sample
Tube and plates of long carbon fibres in aluminium matrix
 Material not available at the industrial scale.
Reliability with thermal cycles not assessed
Compatibility C/Al: corrosion, cleaning
Outgassing of C/Al composite (4.25 cm2)

## Slide 16: New material development for transparent vacuum chambers – Carbon fiber reinforced epoxy + coating
Long carbon fibres reinforced epoxy resin
Aluminium sputtering coating (up to ~500 nm),
Long carbon fibre epoxy resin with metallic coating
Surface observations
Defects
 Vacuum tests not successful due to pin holes
Try to coat in several steps with intermediate cleaning
Other coating process (ionic liquid)

## Slide 17: New material development for transparent vacuum chambers – Aluminum alloys
New grades with Lithium being qualified: 2050, 2195:
Are grades in 5XXX series with Lithium available?
Small grain size aluminium alloys
Thin walled manufacturing:
Conventional machining
Chemical machining
Transparency
Stiffness
Weld ability
Promising strength
Strength of different aluminium alloys

## Slide 18: New material development for transparent vacuum chambers – SiC
Preliminary results:
SiC and C/SiC are both leak tight
Low outgassing rate for unbaked SiC
Higher outgassing for C/SiC
Small C/SiC plate sample
SiC plate sample
Carbon-fiber reinforced silicon carbide or silicon carbide ceramic are considered:
C/SiC improvement?
Vacuum tests for baked samples
Manufacturing of thin wall
Outgassing curve of SiC materials

## Slide 19: New material development for transparent vacuum chambers – Glassy carbon
Glassy carbon tube
Glassy carbon (GC):
Obtained by the pyrolysis at high temperature of a highly reticulated resin.
Two grades have been considered. Grade K is obtained after a heat treatment at 1000 °C whereas 3000 °C is used for the grade G.
Chemical analyses have been done by EDS. The material is composed of around 98 % (weight) of carbon and 2% of oxygen.

## Slide 20: New material development for transparent vacuum chambers – Glassy carbon
Mechanical properties:
Stiffness:
4 points bending tests on plates equipped with strain gauges
Young modulus and Poisson’s ratio
Strength:
4 points bending tests on bars (avoid chips during cutting)
Compression tests
Weibull’s distribution
 | Young Modulus [GPa] | Poisson’s Coefficient
Grade G | 32.4 ±0.8 | 0.155
Grade K | 32.5 ±1 | 0.17
 | Average strength [MPa] | Standard deviation [MPa} | Weibull shape parameter | Weibull scale parameter [Mpa]
Flexure | 206 | 37 | 5.6-6.3 | 375-416
Compression | 1012 | 73 | 13.5-14.6 | 1587-1644
4 points bending test on plates
Elastic properties
4 points bending test on rods
Survival probability for the bending test

## Slide 21: New material development for transparent vacuum chambers – Glassy carbon
Fracture toughness:
Notched bar under 4 points bending test:
Sample | Groove depth [mm] | Force to failure [N] | Bending stress [MPa] | KIc [MPa.m1/2]
1 | 0.04 | 697 | 123 | 7.8
2 | 0.023 | 973 | 172 | 6.3
3 | 0.049 | 964 | 170 | 13.1
CT specimen: test in preparation
 Two methods will be used to determine the toughness: Maximum force for a given stress intensity factor or load decrease during crack propagation.
 Crack growth test is also foreseen
Notched bar
CT specimen and crack propagation simulation

## Slide 22: New material development for transparent vacuum chambers – Glassy carbon
Transition to metallic parts:
CusilABA inteface layer
Glassy carbon
Ceramic
Soldering with intermediate ceramic part:
Compatible thermal expansion
Higher mechanical strength
Preliminary tests on crucible:
No failure
Initial gaps to be adjusted to have a good flow of the solder
GC crucible soldered with a copper ring

## Slide 23: New material development for transparent vacuum chambers – Glassy carbon
Outgassing rate:
Unbaked material:
Throughput method
Grade K : high outgassing
Grade G : low outgassing
Baked material:
Gas accumulation method
Grade G : outgassing rate of 1.5E-13 mbar l s-1 cm-2
Outgassing curve of unbaked glassy carbon
Outgassing of baked glassy carbon

## Slide 24: New material development for transparent vacuum chambers – Glassy carbon
Possibility to improvement the material properties:
Reinforcement with carbon nanotubes:
mechanical properties ↑
thermal conductivity ↑

## Slide 25: Highly transparent vacuum chambers
Conclusion
Highly transparent vacuum chambers are required in high energy physics domain.
Beryllium and aluminium are two material presently used for vacuum chambers.
Materials, alternative to beryllium, are studied for transparent vacuum chambers.