## Slide 1: Politecnico di Torino: Possible Contributions to WP11 and Work Proposals Lorenzo Peroni, Martina Scapin
Dipartimento di Ingegneria Meccanica e Aerospaziale
EuCARD2 WP11 (Materials for Collimation) kick-off and tasks meeting

## Slide 2: Outline
Development of strength and failure models for relevant materials
Fracture analysis of novel composites materials
Contributions to the development of Equations of State for relevant materials
Contribution to multi-material tests in HiRadMat2

## Slide 3: What do we want to investigate?
r0
Energy deposition shock
Mechanical shock
Equation Of State
isodensity
depth
Development of strength and failure models for relevant materials
Fracture analysis of novel composites materials
Contributions to the development of Equations of State for relevant materials
Mo-GR
Mo
IT180
Cylindrical shockwaves
Reflected shockwaves
Molten zone/plasma
p
r
BEAM
attenuation
Solids
Spall
fracture
Vapour
Gas
SPLASH

## Slide 4: Constitutive material models
Johnson-Cook
Steinberg-Guinan
When the temperature reaches the value of the melting temperature the shear strength of the material model becomes zero and the material starts to be considered like a fluid (pure hydrodynamic behaviour)
These models have typically been tested and calibrated with experiments on Hopkinson bars, Taylor cylinders and with high-explosive (HE)–driven shock or compression waves at pressures up to a few tens of GPa and strain rates of 103 to 105 s-1
For the future, improvement in the material strength model is a fundamental aspect!
Pexpected ~ Edeposited >100 GPa!
Pressure gradients produce plasticity (in ductile material)!
Pure metals data avaliable

## Slide 5: Constitutive material models
Pressure values (spall) and gradients produce fracture (in brittle material)!
The Johnson-Holmquist material model, with damage, is useful to model brittle materials, such as ceramics, subjected to large pressures, shear strain and high strain-rates.
The model simulates the increase in strength shown by ceramics subjected to hydrostatic pressure as well as the reduction in strength shown by damaged ceramics.

## Slide 6: Strength and failure models – SHPB
Compressione/flessione
Trazione
Mini
4 Hopkinson bar systems (tension, compression/bending, miniaturized) with semiconductor straingages and fast data acquisition system (up to 100 MHz)
Standard test (tensile, compression), miniaturized tensile, Brazilian and Spalling test (brittle), triaxiality effects (notched specimens), fracture toughness …
2 high speed video cameras (max 1 Mfps) and a VISAR
Gasgun

## Slide 7: Strength and failure models - Gasgun
Light Gasgun forTaylor, flyer-plate and ballistic impacts tests
Max Bore size 40 mm, accelerating length 4 m
2 high speed video cameras (max 1 Mfps) and 1 VISAR (Velocity Interferometer System for Any Reflector), PVDF sensors

## Slide 8: High speed camera (I)
According to EUCARD2 improvement process of all testing facilities a new high speed camera was acquired
Maxima performances: full resolution 1024 x1024 (7000 fps); maximum frame rate 1000000 f/s (64 x 16 pixels);
Shutter: global electronic shutter up to 369 ns, frame rate independent
Variable Region of Interest (ROI)
Capture 12-bit uncompressed data
20μm pixels ensure best light sensitivity for demanding high-speed or low light applications
8GB memory (standard: 5457 frames or 0.780 s @ maximum resolution)
Gigabit Ethernet interface
Triggering and trigger delay options programmable and selectable

## Slide 9: High speed camera (II)
Video acquisition could be synchronized with data acquisition systems (which generates trigger) and lightening system (flash).
The time between trigger and full light illumination is about 20 ms (using MOF-SET transistors).

## Slide 10: High speed camera (III)
A great number of high resolution images are available for FEM comparison and image analysis
Tensile test at 103 s-1 - duration 300 ms

## Slide 11: Strain-rate & temperature (I)
High strain-rates varying temperature
Quasi-static test
varying temperature

## Slide 12: Strain-rate & temperature (II)
Copper
Copper
Copper
Glidcop
Glidcop
Glidcop
static
static
Static
dynamic
Dynamic
dynamic
e =10%
e =10%
e =10%
e =10%

## Slide 13: Ultra high strain-rate (104 s-1)
Numerical model
Experimental test

## Slide 14: Failure locus: triaxiality effects
For ductile materials, the fracture strain is strongly triaxiality dependent. High strain-rate tests on notched specimens are needed.
R∞
R=2
R=0.8
R=0.4
FEM analysis

## Slide 15: Material models identification
Numerical model
Experimental test
Measured and computed quantities

## Slide 16: Inermet - IT180 (I)
High strain-rate test
Room temperature varying strain-rates
Quasi-static varying temperature
High strain-rates varying temperature

## Slide 17: Inermet - IT180 (II)
Metals produced via powder technology could exhibit brittle behaviour especially at high strain-rates (during the test many waves could travel inside the specimen, with many reflections).
In this condition, even for ductile material, techniques similar to those used for brittle materials could/should be adopted.

## Slide 18: SHPB Spalling test (I)
The SHPB setup is modified in order to allow dynamic tensile tests on brittle material (graphite), to evaluate the failure strain at high strain rates.
The compressive wave reflects on the free surface and turns into a tensile wave.
Specimen motion
Tensile wave

## Slide 19: SHPB Spalling test (II)
The compressive wave (C) of length L is transmitted into the specimen and travels until reaching the free surface
At the free surface the compressive wave is reflected back as tensile wave (T), which grows in amplitude: when T = C, the resultant R = 0 and the specimen is completely unloaded.
When the resultant R = T – C reaches the ultimate stress of the material, it generates a fracture surface.
C
C
T
t1
t2
R
t3
C
T
R
The wave travelling inside the left main fragment is limited in amplitude by the ultimate stress of the material, and cannot generate other fractures (unless inhomogeneities are present). Further fracture could occur in the right fragment.
t4
???
Measuring point on the specimen

## Slide 20: SHPB Spalling test (III)
Evaluation of the failure strain
  Strain gauge is reached by the tensile wave only after fracture has already occurred: given to material damping, the failure strain is therefore higher than what registered by the gauge!
  Failure strain estimated with an exponential model (ε = Ae-Bt)
First compressive wave
Residual strain (plasticity, compaction, damping…)
TENSION
COMPRESSION
Fracture
surface
correspondent
to
the
recorded
signal
Fracture
surfaces
Main
fragment
Measuring point
Damping

## Slide 21: Brazilian test (I)
t/s0
s2/s0
s1
t
s2
F
F
D
Compression
Tension
+1 0 20
s1/s0
Experimental technique, alternative to the classic tensile and compression tests, used for the evaluation of tensile strength of brittle and hard materials (like rocks, glass and ceramics).
Test execution:
Diametric compression of a cylinder (diameter D, thickness t) which generates a maximum tensile stress in the middle of the specimen, perpendicular to the applied load.
The standard test is valid only if the fracture happens/starts in the middle of the specimen
The stress distribution along the diameter in which load is applied is known in case of elastic material behaviour. The stress field is triaxial but the only positive stress (fracture) is the transversal one.

## Slide 22: Brazilian test (II)
SHPB Brazilian test
Pulse shaper
Release valve
Reservoir
Striker
Input bar
Output bar
Accelerating gun
Specimen
DAQ System
Straingage
Straingage
High speed camera
Lightening system

## Slide 23: Spall fracture
When an high intensity compression shockwave reaches a free surface it is reflected has a tensile wave: if the material is still solid, a spall fracture could occur. It is of great interest to determine the spall strength of novel materials.
Typical spall fracture induced by a reflection of waves generated by impact
FREE SURFACE
FREE
SURFACE
The typical technique for spall strength evaluation is the measurement of the free surface velocity (stress related)
spall

## Slide 24: VISAR
A VISAR (Velocity Interferometer System for Any Reflector) measures the velocity of a moving surface by measuring the Doppler shift of laser light reflected off the surface.
Changes in the velocity of the surface produce changes in the wavelength of the reflected light due to the Doppler effect. The interferometer is sensitive to wavelength and converts these wavelength changes to changes in the intensity of several output light signals. These intensities are then recorded by fast photodiodes in a DAQ.
Velocities can be determined with accuracy of ±1% or better, in the range from a fraction of a m/s up to thousands of km/s and with sub-nanosecond time resolution.
The surface observed does not need to be mirror polished and changes in it's reflectivity or in background light have no effect on the velocity. The system requires no calibration and can be considered to be absolute.

## Slide 25: Development of new Equations of State
Carbon
Molybdenum
Due to the mechanical engineering competencies in this field, POLITO could not develop a whole EOS for new materials
Our main actions could be:
Benchmarking and checking of available tables (hydrocodes requirements)
Combining existing EOS to obtain EOS for mixture and composite materials (for example molybdenum-graphite)

## Slide 26: HiRadMat 2
HRMT14 were a successful and novel series of experiment but some improvements could be considered in the second generation of experiments on materials hit by particle beam:
Optimization of the geometry and boundary condition of the specimens (reduction of the dimensions?)
Evaluation of the mechanical quantities to acquire (stress, strain, pressure, velocity , displacements, acceleration…)
Optimization of the beam parameters (number of bunches) in function of the type of material and of the required scenario: high number of bunches on cylinder specimen for tunneling evaluation
Evaluation of thermodynamics variable (temperature)
Electromagnetic disturbs reduction
2

## Slide 27: HiRadMat 2
A great interest from POLITO is the experimental verification of high number of bunches ...

## Slide 28: Next steps (I)
Development of strength and failure models for relevant ductile materials (mechanical tests at different temperatures, strains and strain-rates)
Inermet: improvement of the characterization (compression tests) and extension to ultra high strain-rates in tension
Molybdenum: complete characterization of two alloys (varying temperature and strain-rates) in tension and compression. Failure model definition
Spall strength experiments setup

## Slide 29: Next steps (II)
Fracture analysis of composites materials
Improvement of Hopkinson Bar spalling test for brittle material analysis: test on square section graphite specimens in the next months (specimens ready) with high speed image analysis
Development of a spalling test setup at high temperature
Comparison of results obtained with Brazilian test
Improvement of Brazilian test for very hard materials
Improvement of FE models for advanced results analysis of Spalling and Brazilian tests.

## Slide 30: Politecnico di Torino: Possible Contributions to WP11 and Work Proposals Thank you for your attention
Dipartimento di Ingegneria Meccanica e Aerospaziale
EuCARD2 WP11 (Materials for Collimation) kick-off and tasks meeting

## Slide 31: Politecnico di Torino: introduction, overview of WP8 work and possible contributions to WP11 Backup slides
Dipartimento di Ingegneria Meccanica e Aerospaziale
EuCARD2 WP11 (Materials for Collimation) kick-off and tasks meeting

## Slide 32: WP11 Work - Scenario
MULTI-PHYSICS SOLUTIONS
EQUATIONS OF STATE
MATERIAL ans FAILURE MODELS
EXPERIMENTAL
METHODS
In the material part closest to the beam, the pressure and temperature increase and the materials could melt or vaporize, depending on the loading condition: shockwaves are generated.
The remaining part of the material, which remains solid, is characterized by high values of plastic strain, strain-rate and temperature.
2

## Slide 33: Background: numerical simulations
2004: Target rod hit off-axis by a fast extracted beam of 3.5×1013 p at 400 GeV over an extraction time of 10 ms
2005: Collimator jaw hit by a beam of 3.2×1013 p at 450 GeV over an extraction time of 7.5 ms
2009: Bar (20 mm radius, 1 m long) facially irradiated with 8 bunches of 7 TeV protons (each bunch comprises 1.15x1011 protons)
2012: 3D structure, 7 TeV beam impact, soft-coupled simulations (FLUKA-LSDYNA) with deposition upgrade
Density -10 bunches
Density - 60 bunches
Ansys
Ansys/Analytical
LS-DYNA
A. Bertarelli
A. Dallocchio

## Slide 34: Background: Experimental tests
1998
2003
2013
1 Low energy system
Total length 6 m
Resistive straingages
Straingages amplifier homemade
Data Acquisition system 8bit, 100 MS/s
1 High energy systems (pneumatic, 9 bar)
Total length 8 m
Bars diameter up to 30 mm
Straingages amplifier with high bandwidth (>3 MHz)
Data acquisition systems :
16 bit, 800 kS/s
8 bit, 100 MS/s
5 High energy systems (Gasgun 20-200 bar)
Length 10 m
Semiconductor straingages
2 Fast cameras
Data acquisition systems:
14 bit, 3 MS/s
12 bit 20 MS/s
16 bit 100 MS/s