## Slide 1: EUCARD II - RHP presentation 10/12/2013
RHP-Technology GmbH & Co KG
A-2444 Seibersdorf, Austria

## Slide 2: Overview
Updated of processing technologies available at RHP
Overview on possible geometries and size of parts which can be realized by our available sintering and hot pressing facilities
Overview on possibilities to develop ceramics with customized composition
Possible contribution of RHP

## Slide 3: Hot Pressing Technologies at RHP:
1996 Installation der konventionellen Heißpresse (FCT)
Sample Size
Process Cycle Time
fast
slow
small
large
2009 Installation der direkten Heißpresse Dr. Fritsch
2009 Installation der induktiven Heißpresse (Eigenbau)
2012: Installation einer Einzelsegment Sinterpresse

## Slide 4
3 different pressure assisted Sintering Techniques:
Conventional Hot Pressing: Heating of graphite die using a heating element (indirect)
Direct Hot Pressing or Spark Plasma Sintering (pulsed): Heating of graphite die via current
Rapid Sinter Pressing: Placing of a pre-compacted green part in a permanently heated pressing die
Hydraulic Pressure
Vacuum Chamber
Heating Elements
Graphite Die
Punch
Powder
Punch
Hydraulic Pressure
Atmosphere
Heating Element
Punch
Green part
Punch
Steel die
Power Supply
AC/DC/pulsed
Graphite
Punch
Powder
Graphit e
Electrode
Graphite
Matrize
Hydraulic pressure
Vacuum chamber
Overview: hot pressing technologies
Coventional Hot Pressing
Direct heated hot pressing/
Spark Plasma Sintering
Rapid Sinter Pressing
Notes: Dez-13
4

## Slide 5: Processing steps of Rapid Sinter Pressing
Figure 1: Left image shows the green part and in the right image the automatic handling system is bringing the green part to the permanent heated hot pressing die
Figure 2: The sequence of images shows a) insertion of the green part in the pressing die b) consolidation of the green part and c) ejection of the part after hot pressing
RSP-Technology allows the densification of powders in seconds
RSP uses a permanently heated cavity (e.g. up to 950°C) in which a compacted green part is inserted and densified by pressure (up to 150 MPa)
RSP is a method which is suitable for the manufacturing of parts in large volume

## Slide 6: Parameter Studies: Densification of Copper (I)
By using significant higher pressures compared to conventional hot pressing it is possible to obtain a densification in copper within 10 seconds or less

## Slide 7: „Design“ Possibilities using RSP Technology (I)

## Slide 8: „Design“ Possibilities with RSP Technology (II)
Cu-Mo 30:70 wt%)
Molybdenum
Copper
Copper
Copper
Sandwich Structure
Multilayer Structure
Functionally Graded Structures are also possible

## Slide 9: Typical geometries of hot pressed plates
Rectangular targets
Target/Plate size (examples) for hot pressing and direct hot pressing:
Plates with diameter: 53 mm, 65mm, 76mm, 102mm, 153mm, 175mm, 205mm, 240mm, (for some materials 300 and 350 mm)
Squares mit 40mmx40mm, 62mmx62mm, 140mmx140mm, 150mmx150mm
Rectangular e.g. 171mmx76mm, 182 mm x 91 mm, 320mmx80mm (for materials up to 1.200°C hot pressing temperature)

## Slide 10: TARGETS ON DEMAND
Individual Material Compositions
Single Samples, Prototypes
Small Series
Ceramics, Metals and Composites
Fine-tuned Microstructure
Magnetron Sputtering, Arc-Deposition, Pulsed Laser Deposition, ...
Hard metals, ultrahard coatings, magnetic layers, photovoltaic applications, solid lubricants, advanced ceramics
WC without binder
W, Mo, Nb andTa-Oxide
Ti Carbide, Boride or Nitride
Cr or Ti Silicide
ZnS/SiO2
Sulfides such as MoS2, WS2
Various alloys or metal/ceramic combinations
CUSTOMIZED TARGET MATERIALS

## Slide 11: Advanced Ceramics – Customized products
Materials:
Various Oxide, Nitride, Carbide ceramics in customized shape and size
High temperature borides such as TiB2, ZrB2, HfB2, HfC etc.
Size of up to 300 mm possible
HfO2 target segments with size of 200 mm x125 mm
AlN compound target with size of 300 mm
TiB2 tube
B4C plates

## Slide 12: Target materials for PVD processes
Hot pressed SiC-C Target on Cu backing plate
Hot pressed Boron Target
Tungsten Carbide without binder
Lanthanum Hexaboride
B4C (enriched B10) Target on Cu back plate
AlMgB14 Target

## Slide 13: Density of Borides, Nitrides, carbides

## Slide 14: Thermal Conductivities of Borides, Carbides, Nitrides

## Slide 15: Electrical properties

## Slide 16: Material Combinations : e.g. ZrB2/SiC & HfB2/SiC

## Slide 17: ZrB2/SiC & HfB2/SiC

## Slide 18: Topics
1. Presentation of advanced ceramics produced at RHP Technology (WC, MoC, SiC, TiC, ecc) with specific focus on highly conductive materials
2. Proposals for new heavy and conductive refractory materials (e.g. WC- or Mo2C- based) as an alternative to present tungsten heavy alloys
3. Proposals for other SiC- based materials and their bonding to metallic substrates
4. Type and number of material samples to be produced.

## Slide 19: Possible contributions of RHP
1. Continue Work on Copper-Diamond composites (sandwich structure; include a Mo oder W cladding layer by direct bonding)
2. Prepare ceramic materials/customized composition for screening tests and further characterization
3. Screening of SiC – Metal bonding technology
=> to discuss: type and number of material samples to be produced.
Copper-diamond composites
Cu-Mo-Cu-Mo-Cu Multilayer

## Slide 20: Thank you for your attention!
Further information:
www.rhp-technology.com
DI Dr. Erich Neubauer
RHP-Technology GmbH & Co. KG
Forschungs- & Technologiezentrum, Gebäude CA
A-2444 Seibersdorf
Tel.: 0043-650-9151074
Email: erich.neubauer@rhp-technology.com

## Slide 21: Properties of some UHTCs

## Slide 22: ZrB2 & HfB2