## Slide 1: Overview: HTS4Fusion Workshop

## Slide 2: HTS cables
 | RACC | TSTC | CORC
transposition | complete | partial | partial
Je | high | medium | low
tape consumption | high | low | medium
Three main options of tape alignment
Roebel bars  RACC cable
Twisted stacks of tapes  TSTC
Helical  CORC cable

## Slide 3: HTS cables: topics
Bending
Mechanical properties
Joints & contacts
Automatic manufacturing
Performance at high fields
Scaling to high currents
AC losses

## Slide 4
Roebel Assembled Coated Conductor (RACC) cable

## Slide 5: RACC: perpendicular pressure
Applying pressure on RACC cables
6.7 kN  14 – 43 MPa (contact surface undef.)
10 % reversible Ic reduction
Bayer et al. (KIT)

## Slide 6: RACC: striations
Improving effect of striations
Cu deposition after laser cut
  couples filaments
  higher AC losses (open symbols)
Heat treatment in O2
  decouples filaments
  reduces AC losses (closed symbols)
Goldacker et al. (KIT)

## Slide 7: RACC: round Rutherford
Construction & test of fully equipped 1.4 m model cable
6 Roebel strands, 10 tapes each (4 mm wide, from IRL)
77 K self-field:
  Ic: 2.5 kA
  Jc,e: 1.1 kA/cm-2
  inhomogeneous distribution
  delamination
Goldacker et al. (KIT)

## Slide 8
Twisted Stacked-Tape Cable (TSTC)

## Slide 9: TSTC: Ic(B, T)
Ic at high perp. field and low temp.
better than expectations:
> average Ic of tape * number of tapes * lift factor
Uglietti et al. (CRPP)

## Slide 10: TSTC: bending
Isotropic bending
Easy bending (out of plane): limit: 0.55% strain
Hard bending (in plane): limit: 0.25% strain  1.6 m Ø
   delamination
Uglietti et al. (CRPP)

## Slide 11: TSTC: transverse pressure
Uglietti et al. (CRPP)
Ic vs transverse pressure
Isotropic
Limit in worst case (90 °): 30 MPa
Lower layer of flat cable (15 T, 3 kA per strand): 15 MPa

## Slide 12: TSTC: joints
Fabrication and test of different types of joints
Uglietti et al. (CRPP)

## Slide 13: TSTC: twist windings
BEFORE: bending of TSTC
Hard bending side: 140 mm Ø: 3.6 % irr. degradation
NEW: Stacked-Tape Twist-Winding
Cable follows shape of the curve
   always easy bending side
Takayasu et al. (MIT)

## Slide 14: TSTC: H-channel
Scale-up fabrication of 2 channel TSTC (H-channel)
H-channel reduces self-field effect
Automated production: 4-axis 3D milling machine
Takayasu et al. (MIT)

## Slide 15: TSTC: slotted 5 core CICC
Design of slotted core CICC
Celentano et al. (ENEA)

## Slide 16: TSTC: slotted 5 core CICC
Automated manufacturing
Celentano et al. (ENEA)

## Slide 17
Conductor on Round Core (CORC) cable

## Slide 18: CORC: automated winding
BEFORE: hand winding
irregular tape spacing
  voids in winding pack
  tapes damaged during bending (60 mm Ø: 56 % irr. degradation)
NEW: automated winding machine
controlled tape separation, winding angle & tension
Van der Laan et al. (UC & ACT)

## Slide 19: CORC: bending
Improved cable flexibility
bending to low diameters possible:
  40 mm Ø: 2.5 % rev. degradation
Van der Laan et al. (UC & ACT)

## Slide 20: CORC: terminals & joints
BEFORE: conical or solder filled terminals
Solder filled: high resistivity, small
Conical: Low resistivity, very big
NEW: hybrid type joints
Low resistivity, small
Demountable
36 nΩ
225 nΩ
50-60 nΩ each
170 nΩ total
Van der Laan et al. (UC & ACT)

## Slide 21
REBCO tape
picture: Fujikura

## Slide 22: YBCO tapes: 2014 Amperium
50 % increased Ic @ same price
NEW 2014 products: 4.4 mm wide: >180 A, 12 mm wide: >350 A
Rouse (AMSC)

## Slide 23: YBCO tapes: peeling resistance
Ideal for epoxy impregnated coils
Rouse (AMSC)