## Slide 1: TISD activities during LS1
Update from last report
22 Oct 2013
T. Stora

## Slide 2: Reminder
8B
9C
37K
LIEBE (LBE loop)
ActILab ENSAR (nanoUCx)
Ba beams
Neutron converter
(RILIS in VADIS) molecular beams

## Slide 3
ISOLDE
  Diffusion studies of boron in possible target materials
  Implantation of 10B as 10BF2 into pressed pills of Al2O3, CNT, MgF2[1];
  HV=70kV-80kV
SARAF
  Characterisation of neutron beam
  Implantation of 10B as 10BF2 into Al (200ug/cm2) foil, rcoll=1.5mm,
  HV=32kV
  nBF2+=4*10^16
B
F
+
F
B
F
+
F
[1] J. Vacik et al, On Boron diffusion in MgF2, CP1099, Application of Accelerators in Research and Industry: 20th international Conferene

## Slide 4
4
α detector
Principle
  Irradiation of sample with thermal neutrons:
  For diffusion measurements: Pu-Be Source 1.1*108 n/s @4π, (before moderation )
  Neutron capture cross section of 10B: σth=3840 barn
  Detection of produced 7Li and α from 10B(n,α)7Li
6%: 7Li (1.015MeV + α (1.777MeV)
94%: 7Li (0.840MeV + α (1.470MeV) +γ(0.478MeV)
  10B+n

## Slide 5
Measurement with calibration sample, done with Pu-Be source

## Slide 6
http://www.soreq.gov.il/default_EN.asp
SARAF@Soreq
  Located near Yavne, Israel
  Proton beam (E=1.91MeV) from Soreq Applied Research Accelerator Facility (SARAF) hits liquid lithium target (LiLiT) ,T∼200◦C
  Production of 10-100keV neutrons: 7Li(p,n)7Be
  Irradiation of 10B sample with fast neutrons
  Coincidence detection of produced 7Li and α from 10B(n,α)7Li

## Slide 7
LIEBE: Liquid Lead Bismuth Eutectic Loop target for Eurisol
Validation of the conceptual design of EURISOL direct target by prototyping at Cern-ISOLDE
Diffusion: model from Fujioka et al. (NIM 186 (1981) 409)
Data: Lettry et al. (NIM B 126 (1997) 170)
Motivation: Improvement of yields of short-lived Hg isotopes
Diffusion of isotope when the LBE is on droplets shape which require the use of a grid, a diffusion chamber and a pump to recirculate the liquid.
Total time till the post acceleration: < 300 ms.

## Slide 8
Isolde Front end
Development: integration of a liquid loop target, working at high temperature (from 200 deg C up to 600 deg C) in the Cern-Isolde environment.
Part 1: main part of the target in his confinement
Part 2: pump and engine to recirculate the liquid
Ion Source
Main LBE loop
Heat Exchanger
Feeder tank
Beam
Main part without confinement
Proposed layout:
Main challenges:
  High power deposited on target to be evacuated (HEX to dimension at various T)
  Recirculation of liquid through a compatible LBE pump
  High temperature of use (up to 600 deg C)
  Integration in already existing (relatively small) environment
  Monitoring and control
Proposed design

## Slide 9
Offline tests: Shower formation, pore size and spacing
Model: Shower inside diffusion chamber
Grid: 200μm pore diameter, 300 μm spacing
Grid: 200μm pore diameter, 1 mm spacing
Test stand to investigate shower formation in vacuum
Tests ongoing
LBE shower in air
@ISOLDE-Jan 2014

## Slide 10: nanoTiC - motivation
Chart: Temperature
| 1200 | 1300 | 1400 | 1450
K | 100.0347 | 89.7688 | 88.7633 | 97.4914
Sc | 97.4413 | 96.7691 | 100.3574 | 105.2138
Mg | 95.1796 | 90.7705 | 92.9607 | 100.308
Na | 86.8733 | 77.5087 | 73.6247 | 84.1461
Be | 87.7942 | 84.5397 | 84.7718 | 90.9726
nanoTiC after 5 min
Fractional activity rise at 1450oC is attributed to a an oxide layer in the samples at higher sintering temperatures.
High Melting point – 3160 oC
Sintering studies done, shows that TiC can maintain a submicron structure at least until 1500oC
Operation temperature has to be at least 1500oC (Ca, K, Sc beams)
Release studies
Avoid oxidation of TiC
Improve nanostructure stability => Essencial for good release
TRIUMF shows release of Ca and K from TiC
JPR| 1/3
Notes: No release from TiO2 material | Little release was seen at 10 and 20 min probably due to the defect healing with heat the five min heat treatment | TiC sample after 5 minutes show release (graph made using these values and maximum error | Ca release | Oxidation at 1450C

## Slide 11: nanoTiC – ongoing studies
JPR| 2/3
Powder Suspension
Isopropanol
Polymeric dispersant
Wet mixing
Attrition mill
Zirconia milling elements
Pellet Preparation
Sintering
Drying
Morphology
Density
Porosity
Specific sufrace area
Deagglomerate
Pressing
1500oC for 2 and 10h
Vacuum
Characterization
TiC
Graphite
Carbon Nanotubes
Carbon Black
Study the effect of the different carbon polymorphs
Study the volume ratio of carbon
How to hinder sintering of TiC?
Doping
Add (a higher melting point) second phase
Lower temperature and time

## Slide 12: nanoTiC – results and future studies
TiC + Carbon Black
TiC + Graphite
TiC + Carbon Nanotubes
TiC
Future work:
Release studies
Target prototype
Modeling
JPR| 3/3

## Slide 13
UCX prototype target tests for ActILab-ENSAR
Characterization of conventional UCX using synchrotron-based micro-beam analysis:
  Microscopic morphology – buried porosity & chemistry
  Kinetic stabilization by sub-microscopic UC – UC2 phase competition
  Grain size of material is smaller than previously estimated; global phase transition observed at 2100◦C
  Phase competition between UC and α-UC2 as yet missing explanation of performance and durability of this material
A. Gottberg, et al., submitted

## Slide 14: UCX prototype target tests for ActILab-ENSAR
Release fractions from RaBIT irradiations, ALTO 2013
ISOLDE online tests: Despites major technical difficulties (RFQ, tape station, separator):
record yield of 11Be: 6.0x107 /µC, database: 7x106 /µC (confirmed)
Structure appears to be widely conserved over time and temperature
Repeat tests at ISOLDE and at ALTO within ActILab in 2014
Online tests and synthesis of de-novo designed uranium carbide matrixes:
Different microstructures, densities, grain sizes, crystal structures tested → tailor-made matrix:
Suspension grinding of UO2 powder to 160 nm average particle size
Ultrasound-assisted mixing with multi-walled carbon nanotubes
Pressing to 1.6 g/cm3 pellets
Optimized reactive sintering to mixed uranium carbide inside carbon nanotube matrix
30Na beam intensity evolution
Ch. Lau, et al. , in preparation
A. Gottberg et al. submitted

## Slide 15: UCX Post-Irradiation Studies for ActILab-ENSAR
Post-irradiation analysis:
First analysis of an irradiated UCX target in the history of ISOLDE (important to understand ageing processes and for upcoming waste campaign)
Opening target unit #466 (8.8∙1018 protons in 2011) in inert-gas hot-cell at PSI, 19 mSv/h on contact with Ta beam window
2µm
before irradiation
after irradiation
Pellets appear macroscopically unchanged
Microscopic evolution of pore distribution and grain size under irradiation observable
500 µSv/h on contact with single pellet
Results of synchrotron investigations under analysis
Ceramography and electron micro-probe analysis scheduled for April
Perform full suite of investigations on nano UC

## Slide 16: Proton-to-Neutron Converter Prototype
current design
proton fluence (p/cm2/µC)
neutron fluence (n/cm2/µC)
Operated in October 2012
R. Luis et al., European Physics Journal A, 48 (2012) 90
A. Gottberg et al. submitted to Nucl. Instr. Meth. B (2014)
ISOLDE compatible
geometry optimization
max high-energy neutrons
min proton
in UCx

## Slide 17: Proton-to-Neutron Converter Prototype Online Tests
Strong suppression of contaminations compared to conventional converter confirmed (104 for 80Rb)
Experimental ratio of n-rich species to contamination improved (200 for 80Zn/80Rb)
Poor extraction efficiencies due to low operational temperatures (caused by structural failure)
A. Gottberg et al. submitted to Nucl. Instr. Meth. B (2014)

## Slide 18
Design Study
Beam Energy: 500 MeV;
Beam Intensity: 100μA;
FWHM: 3mm;
Particles per second: 6.242 E14;
UCx density: 3.63g/cm3

## Slide 21
Preliminary Thermal Analysis

## Slide 22
Work in IPNO: Use LaCx as chemical homologue to UCx
La2O3 is very hygroscopic and quicly turns into in La(OH)3
Choice to start with graphite and La(OH)3 :
lanthanum hydroxide stable in the air
strong degassing during sintering = porosity
Synthesis of lanthanum carbide pellets
Smaller beads produce:
Finer powder
Larger pores
Precursor
powder
Grinding
Pressing
Characterisations
He pycnometry
SEM
XRD
Hg porosimetry
Sintering

## Slide 23
Reactions during sintering:
(I)
(II)
La2O3 + 11C → 2 LaC2 + 4 C + 3 CO
La(OH)3 → La2O3 + 3H2O
(I)
(II)
Choice of new outgassing program
reduces the dwell time at high temperature
limit sintering responsible for the decrease of the porosity
limit the change in the microstructure (grain growth ...)
AIMS:
Reducing grain size
Improving homogeneity in shape and grain size
Grinding with planetary mill :
ISOLDE experience with nanoUCx shall be translated to LaCx.
Milled powders would allow to produce smaller grains by two orders of magnitude.
Smaller grains together with carbon nanotubes can be engineered for better preservation of microstrure at high temperature .
Having small grains of the target increases the efficiency of diffusion of the isotope out of the target material.
This program can be used to manufacture LaC2 targets.

## Slide 24
FLUKA simulations of the production of Ba isotopes from LaC2 targets at ISOLDE
LaC2 is a better candidate than UC2
Choice of LaC2 for the production of i.e. neutron-deficient Barium beams
Purchase of material:
Start with La(OH)3 :
lanthanum hydroxide stable in the air
grinding in isopropanol
strong degassing during sintering = porosity
Start with carbon nanotubes :
Size
Thermostability
Diffusion
Grinding equipment (Jar+Beads) in Tungten Cabide:
high density
high hardness and high abrasion resistance
high melting point (2900°C> work temperature ~ 2000°C)
neutron-deficient isotopes of Ba (Cs, Xe, etc.) isotopes LaC2 shows higher production cross-sections thanUCx
For Ba with A<120 the production decreases rapidly and good extraction efficiencies are necessary for decent isotope beams

## Slide 25
Thank you !! Hungry ?