## Slide 1
A method to model the accumulation of oxide charge with fluence in an irradiated MSSD
24th RD50 Workshop, 11-13 June 2014
T. Peltola1), J. Härkönen1), T. Mäenpää1)
1)Helsinki Institute of Physics, CMS Upgrade Project.

## Slide 2
Outline
Motivation & method to determine CCE(x)
  Motivation: why non-uniform 3-level defect model?
  CCE(x): Iteration method
  CCE(x): proton model vs non-unif. 3-l model
Qf(Φ) & c(Φ) modelling
  Measured CCE(x) vs simulation:
    d & η varied
    d = constant
  Qf(Φ) & c(Φ) of region 5 200P MSSD

## Slide 3
Motivation & method to determine CCE(x)

## Slide 4
Non-unif. 3-l model: n-on-p, r5
@ F=1.5e15 cm-2
f = 1 MHz
Φeq=1.4e15 cm-2
MCz200P, region 5
Center of strip
Center of gap
Non-unif. 3-level defect model: Motivation
3-level model within 2 μm of device surface + proton model in the bulk:
Rint (fig. 1) & Cint (fig. 2) in line with measurement also at high fluence & Qf
Non-unif. 3-l model can be tuned to equal bulk properties (TCT, Vfd & Ileak) with proton model → suitable tool to investigate CCE(x)
Figure 2: Cint
Figure 1: Rint
FZ200Y, region 5
Φeq=3e14 cm-2
SiBT measured CCE(x) for proton & mixed fluences (T. Mäenpää):

## Slide 5
40.6%
37.3%
31.1%
25.4%
20.3%
17.5%
CCE loss:
Principle of CCE(x) simulation for given c(shallow acc.) & voltage
5 strip 200P, region 5 @ Φeq =1.5e15 cm-2, V=-1 kV, T=253 K
Acceptor traps remove both inversion layer & signal electrons: better radiation damage induced strip isolation → larger CCE loss between the strips
Increased Qf fills more traps → CCE loss decreases, undepleted region between strips grows
Qf increases
→ Qcoll decreases
Qf increases
→ Qcoll increases
CCE(x) @ Φeq = 1.5e15 cm-2: Iteration method
Space charge dominated region
Oxide charge dominated region
center
strip
2nd
strip
60 μm
0 μm
mip
positions

## Slide 6
CCE(x): proton model vs non-unif. 3-l model
Qf = 1.2e12 cm-2: CCE loss ≈ 15 %
Qf ~ 1.5e12 cm-2: no strip isolation & cluster CCE ~0.5 of expected due to undepleted region produced by high Qf
Center of strip = 0
Center of gap = 60 μm
Non-unif. 3-l model
Proton model
Type of defect | Level [eV] | σe [cm2] | σh [cm2] | Concentration [cm-3]
Deep acc. | EC - 0.525 | 1e-14 | 1e-14 | 1.189*Φ + 6.454e13
Deep donor | EV + 0.48 | 1e-14 | 1e-14 | 5.598*Φ - 3.959e14
Proton model (tuned by R. Eber)
Type of defect | Level [eV] | σe [cm2] | σh [cm2] | Concentration [cm-3]
Deep acc. | EC - 0.525 | 1e-14 | 1e-14 | 1.189*Φ + 6.454e13
Deep donor | EV + 0.48 | 1e-14 | 1e-14 | 5.598*Φ - 3.959e14
Shallow acc. | EC - 0.40 | 8e-15 | 2e-14 | 40*Φ
3-level model within 2 μm of device surface
200P region 5 @ Φeq =1.5e15 cm-2, V=-1 kV, T=253 K
Qf = 1.2e12 cm-2: CCE loss ≈ 41 %
Qf = 2e12 cm-2: increased charge sharing when mip position ≥ 30 μm from center strip, but still producing position information
When strips are isolated both models produce same cluster CCE at the center of the strip

## Slide 7
proton model vs non-unif. 3-l model: electron density
Electron density @ Qf = 1.2e12 cm-2, V=-1 kV from previous slide
Effect of acceptor traps in non-unif. 3-l model is clearly visible:
~5 orders of magnitude difference between models (from n+ to p-stop)
n+
p-stops
n+
center
strip
2nd
strip
Cut @ 50 nm below oxide

## Slide 8
Qf(Φ) & c(Φ) modelling

## Slide 9
Measured CCE(x) vs simulation: d & η varied
200P Region 5: p+ Φeq=3e14 cm-2, V=-990 V, T=253 K
SiBT measured CCE loss(FZ200P/Y, MCz200P) @ V=600 – 990 V: 26.5±1.1%
Double p-stop: dp=1.5 μm=dimplant, wp=4 μm, spacing=6 μm
Two low CCE loss regions observed in Qf scan
Not seen in Φeq=1.5e15 cm-2 CCE loss simulations, because of higher Qf values (1.2e12…2e12 cm-2)
Interpretation: At very low Qf high E produces charge multiplication → additional charge carriers fill traps → CCE loss decreases significantly
Cut @ implant curvature
Charge multiplication region
Oxide charge dominated region
3.1%
→ New approach: keep 3-level region thickness constant & add constant factor to shallow level c
8.5%
Approach:
  Iterate η to find CCE loss within measured error margins @ Qf ~5e11 cm-2
  Change 3-level model thickness to preserve transient signal shape
E(x) between 2nd & center strip for η=40 cm-1, Np=1e16 cm-3

## Slide 10
3-level region: d=2 µm, strip length = 3.049 cm
Φeq≈1.5e15 cm-2 has largest statistics at ~600 V → simulation V adjusted
Φeq=3e14 cm-2
V=-990 V
Φeq =1.5e15 cm-2
V=-608 V
Measured CCE(x) vs simulation: d = constant
Type of defect | Level [eV] | σe [cm2] | σh [cm2] | Concentration [cm-3]
Deep acceptor | EC - 0.525 | 1e-14 | 1e-14 | 1.189*Φ + 6.454e13
Deep donor | EV + 0.48 | 1e-14 | 1e-14 | 5.598*Φ - 3.959e14
Shallow acceptor | EC - 0.40 | 8e-15 | 2e-14 | 40*Φ
Shallow acc. | EC - 0.40 | 8e-15 | 2e-14 | 14.417*Φ + 3.1675e16
Qf=(4.6–6.0)e11 cm-2
Qf=(1.405–1.425)e12 cm-2
Measured CCE loss(FZ200P/Y, MCz200P/Y) @
Φeq (mixed) = (1.4 ± 0.1)e15 cm-2, V = 606 ± 2 V: 30 ± 2 %
Measured CCE loss(FZ200P/Y, MCz200P) @
Φeq (p+) = 3e14 cm-2, V = 600 – 990 V: 26.5 ± 1.1 %
Target Qf ~5e11 and ~1.5e12 cm-2 for given fluences
Measurement: 6 μm resolution

## Slide 11
Qf(Φ) & c(Φ) in p+ irradiated region 5 200P
Fluence [cm-2] | Qf [cm-2] | c(shallow acceptor) [cm-3]
3e14 | (5.3±0.7)e11 | 3.6e16
(1.4±0.1)e15 | (1.415±0.010)e12 | 5.33e16
Qf = 5e10 cm-2
Qf = 2.7e10 cm-2
Qf of non-irradiated 200P from measured initial dip of Cint, that is reproduced by decreasing Qf=2.7e10 cm-2
c(shallow acc.) parametrized by using ‘fixed’ values of Qf → fixed c, parametrized Qf
Increase of the shallow acceptor concentration is found to be ~0.5 of constant factor at the given fluence range
Cint(V)
Cint(V)

## Slide 12
Summary
When position dependency of CCE is modeled by non-unif. 3-l defect model, it is governed by Qf and shallow acceptor concentration
By tuning these two parameters it is possible to reproduce measured CCE loss between strips for given fluence
If one of the parameters is fixed, the other can be solved reliably → potential for Qf(Φ) parametrization
With test values of Qf the shallow acceptor concentration does not have strong dependence on fluence in the range 3e14 → 1.5e15 cm-2

## Slide 13
Backup: SiBT measured CCE loss between strips
Signal loss in-between strips (p=120µm, w/p~0.23)
FTH200N
FTH200P
FTH200Y
MCz200N
MCz200P
MCz200Y
FZ200N
MCz200N
non-irradiated
mixed irradiated 1.5e15neq/cm²
No loss before irrad.; after irrad. ~30% loss; all technologies similar [Phase-2 Outer TK Sensors Review]

## Slide 14
  Backup: Measured Rint
Measurement (W. Treberspurg)
DC-CAP
P and Y types: Rint
109
106
F=5e14 cm-2
F=1e15 cm-2
P and Y types: Rint

## Slide 15
3 strip structure, Vstrip1 = Vstrip3 = 0, Vstrip2 = LV and 0 V
V = -HV at the backplane
Interstip resistance (Rint ) is defined as (Induced Current Method):
Rint is plotted as a function of applied voltage V
Backup: simulated Rint & Cint
1: Vstrip2 = LV 2: Vstrip2 = 0
Vstrip3 = 0
Vstrip1 = 0
Electrical circuit diagram of Rint measurement :
Rint simulation principle
Cint = 2*[AC(1,2)+DC(1,2)+AC(1)DC(2)+DC(1)AC(2)]
Cint simulation principle