## Slide 1: Roebel cable industrial optimization - General Cable Superconductors Dr Nick Long, Robinson Research Institute, Victoria University of Wellington, New Zealand
WAMHTS-1, February 2014
Acknowledgements: Rod Badcock, Kent Hamilton, Chris Bumby, Marc Mulholland, Zhenan Jiang

## Slide 2: Contents
Introduction to Roebel
Design of strands
Punching strands
Testing Ic
Cable assembly
Cable Ic
Mechanical properties
Insulation and reinforcement

## Slide 3: Cable attributes for magnet applications
High current; uniform Ic
Available in long lengths
$/kA-m
Stability (risks of quench, equal current sharing among strands)
Mechanical behaviour
  Ic – stress, transverse and longitudinal
  Bending radii
  Coil manufacture; potting
Manageable AC losses

## Slide 4: HTS Roebel cable
Goals
Develop long length Roebel cable manufacture
Prove applications in high current and/or AC machines
  150 MW generator (Siemens)
  1 MVA Transformer (Robinson Research Institute (ex IRL))
Started R&D at IRL in 2004
Commercialised through General Cable Superconductors

## Slide 5
What is HTS Roebel Cable?
A high capacity winding cable from coated conductor
Continuously transposed
Cables are labelled (no. of strands) / (strand width)
Photo courtesy of Siemens

## Slide 6: Design of strands/cable
Existing designs are a compromise
  Use the wire which was available
    12 mm SuperPower
    10 mm Fujikura and STI (from 2013)
  Keep tool piece manufacture simple
  Minimise problems in automated winding
  Minimise mechanical problems

## Slide 7: Design of strands
Figure – Strands wound together and geometric parameters
Figure – Roebel strand
12 mm
5 mm
6.0 mm
2 mm
30°
300 mm
Parameter | Name | 2 mm Cable | 4.5 mm Cable | 5 mm Cable
LTRANS (=2L) | Transposition length | 90 mm | 300 mm | 300 mm
WR | Strand width | 2 mm | 4.5 mm | 5 mm
WX | Crossover width | 1.7 mm | 5.0 mm | 6.0 mm
“15/5”

## Slide 8: Strand manufacture
Automated multi-strand production
(a)
(b)
(c)
(d)
Formation of Roebel punched strands in 40 mm and 12 mm wide feedstock material.
4 x 5 mm strands in 40 mm wide material,
1 x 5 mm wide strand in 12 mm wide material,
10 x 2 mm strands in 40 mm wide material,
3 x 2 mm wide strands in 12 mm wide material.
Punching
Wire demonstrated: AMSC, SuperPower, Fujikura, STI

## Slide 9: Quality of punching: AMSC wire
Electroplated copper/NiW
Electroplated copper/NiW
AMSC 4 ply Cu/2x NiW/Cu
AMSC 3 ply SS/NiW/SS

## Slide 10: Fujikura: Silver-stabilised punched strand
Ag capping layer
Hastelloy substrate
Ceramic layers
Ag “smearing” occurs over punched edge

## Slide 11: Fujikura Cu-laminated wire – punched strand
Cross section of punched edge from
Cu-laminate stabilised wire (GCS00048):
Copper laminate (stabilizer)
Hastelloy substrate
Ceramic layers
Total thickness: ~200µm

## Slide 12: Wire qualification
Current flow in a wire
Current flow in a Roebel strand
defect
!

## Slide 13: Wire qualification
Scan wire magnetically (penetrated or remanent field)
Quantify uniformity using statistical correlation with an ideal magnetic profile
Correlation along a length of YBCO wire, a minimum Correl can be specified for input wire
Where |Correl | ≤ 1 X is a dataset representing calculated field
Y{y1…yj} is magnetic data across tape
0.000 T
200mm
(a)
(a)
0.023 T
(b)
We use continuous scanning of the Remanent magnetic field to assess tape quality (a) tape with a known defect, and (b) tape with only small scale variability.
Some wire is extremely good !

## Slide 14: Ic measurement of strands
Spiral racetrack former for testing strands up to length 30 m.
Punched strands are moisture sensitive
Heat in dry nitrogen only

## Slide 16: Summary of strand performance
(Je strand) / (Je wire) ~ 90-95%
High minimum value of Correl is necessary but not sufficient condition
 DIc also needs to be considered
 Length of defect important
 Scaling to low T, defects look like a cross sectional loss of conductor
Can we mitigate low Correl values?
  Probably not!

## Slide 17: Cable assembly
Automated planetary wind system for 15/5 cable
Illustration of the assembly process

## Slide 18: Assembly issues
Long length registration of crossovers
  Need high precision for each transposition length in the punching process
  Need tension control on strands in winding
  Difficult to simulate (relevantly) with low cost dummy cables
    Mechanical properties
    Camber

## Slide 19: Ic measurement of cables @ 77 K
15/5 cable from SuperPower wire
Cable details | Cable Ic (A) |  | 
 | Design Ic | Measured | Computed
5/2 | 252 | 203 | 220.1
9/2 | 426 | 318.8 | 339.1
9/2 | 426 | 341.9 | 359.1
15/5 | 1454 | 1100 | 1033
15/5 SRC0024 | 1616 | 1010 | 1109
15/5 SRC0027 | 2093 | 1410 | 1372
Measured Ic has been close to expected Ic
For short length cables accurate Ic measurement is difficult
At 77 K there are strong self-field effects
RRI – 1 MVA Transformer

## Slide 20: Ic measurement of cables @ 4.2 K
15/5 cable from SuperPower wire
From manufacturing perspective cables work as advertised
Measured Ic close to expected Ic (taking into account self-field)
These cables used both ‘CF’ (Cable A) and ‘AP’ (B + C) Superpower wire
Actual strand Ic @ 4 K values were not measured
J. Fleiter et al, Supercond. Sci. Technol. 26 (2013) 065014

## Slide 21: Mechanical properties – longitudinal stress-strain
SuperPower 12 mm wire
Irreversible change @ 840 N (700 MPa).
15/5 Roebel cable
Irreversible change @ 850 N (113 MPa).
Von Mises stress @ 0.4% strain
Roebel 5 mm strand (146 MPa)

## Slide 22: Mechanical properties
Roebel shape weakens structure
  1/6 reversible strain limit of straight wire
Mitigate through
  Potting
  Reinforcement and wrapping
Transverse stress effects
  Again get stress concentration
  Up to 45 MPa without Ic degradation (15/5 cable - CERN)
  Degradation at 10 MPa, (10/2 cable with insulated strands - EPFL)

## Slide 23: Wrapped insulation
Nomex wrapped 12 mm wide cable
Need to include a reinforcing Hastelloy or stainless steel tape
Nomex adds 200 microns total thickness
Roebel cable ready for testing at Siemens Corporate Technology, Germany.

## Slide 24: Winding and Potting coils
Strands need to move during coil winding
  Tight insulation wrapping not advisable
Coated conductor has known interfacial mechanical weakness which can cause problems in potting
  This applies to Roebel as well
  We have damaged cable by using Stycast
Getting complete void filling needs consideration for large coils

## Slide 25: Conclusions
Manufacturing procedures in place for long lengths
Ic performance
  Cables preserve tape performance (~90%)
Quality control
  Measuring magnetic Correl is relatively easy
  Measuring strand Ic is time consuming and adds risk
Cables up to 25 m (15/5 cables) delivered to customers
  We have wound up to 40 m length
Cost ultimately dominated by wire cost
AC loss well characterised (not discussed here)

## Slide 26: Thank you for your attention!