## Slide 1
Conductor on Round Core (CORC) cable development for accelerator magnets
Danko van der Laan
Advanced Conductor Technologies & University of Colorado
Boulder, Colorado, USA
WAMHTS-1, Hamburg, Germany, May 22, 2014
Fraser Douglas
Advanced Conductor Technologies, Boulder, Colorado, USA
Xifeng Lu
University of Colorado,Boulder, Colorado, USA
Ulf Trociewitz and David Larbalestier
Applied Superconductivity Center, National High Magnetic Field Laboratory, Florida State University, FL 32301, USA

## Slide 2: Outline
1. Introduction to ACT and CORC cables.
2. CORC cables for fusion magnets.
3. Mechanical properties of CORC cables.
4. CORC cables for high-energy physics magnets.
5. Production of long, high-quality CORC cables.
6. CORC cable performance projections.

## Slide 3: Advanced Conductor Technologies LLC (ACT)
Advanced Conductor Technologies focuses on the commercialization of high-temperature superconducting Conductor on Round Core (CORC) cables for high-density power transmission and high-field magnets.
Founded in June 2011 as a spin-off from the University of Colorado and the National Institute of Standards and Technology (NIST)
Personnel at ACT:
1. Danko van der Laan, Ph.D.
2. Annemiek Kamphuis, M.Sc.
3. Fraser Douglas Ph.D.
New location:
3082 Sterling Circle Unit B, Boulder, CO 80301 (2851 SF)

## Slide 4: Programs supporting CORC cable development
2. Department of Energy – Office of High Energy Physics
- CORC cables for accelerator magnets
- Phase II SBIR (2 years – April 2014 to April 2016)
- Subcontractor: NHMFL (David Larbalestier and Ulf Trociewitz)
1. Department of Energy – Office of Fusion Energy Sciences
- CORC cable for fusion magnets
- Phase II STTR (2 years – April 2013 to April 2015)
- Subcontractor is MIT (Joe Minervini, Phil Michael and Leslie Bromberg)
3. Navy
- He-gas cooled CORC power transmission cables
- Phase II STTR (2 years – February 2014 to January 2016)
- Subcontractor is CAPS (Sastry Pamidi and Chul Kim)
Advanced Conductor Technologies:
University of Colorado:
1. Department of Energy – Office of High Energy Physics
- support for high-Je CORC cable development
- Base program (3 years – April 2012 to March 2015)

## Slide 5
Conductor on Round Core cables
D.C. van der Laan, SUST 22, 065013 (2009).
CORC cable principle:
Winding many high-temperature superconducting YBCO coated conductors from SuperPower in a helical fashion with the YBCO under compression around a small former.
Benefits:
- Very flexible
- Very high currents and current densities
- Mechanically very strong
- Minimum degradation from cabling (< 10 %)
- Current sharing between tapes possible

## Slide 6
CORC cables for fusion magnets
Cables tested at the NHMFL in 19.8 T background field:
Iquench = 6000 A @ 4.2 K, 19 T
Je = 114 A/mm2 @ 4.2 K, 19.0 T
Ic = 5021 A @ 4.2 K, 19 T, 1 mV/cm
52 YBCO coated conductors, 17 layers, cable O.D. 7.5 mm:
Goal is to reach a cable current >30 kA at 4.2 K and B > 12 T.
ACT: DOE – Office of Fusion Energy Sciences Award DE-SC0007660,
NHMFL: DOE, NSF, agreement DMR-0654118, and the State of Florida

## Slide 7
High-current ramp rates at 19 T
Current ramp rates at
4.2 K, 19 T to 90 % of Iquench:
Phase I STTR DOE - Fusion Energy Sciences Award DE-SC0007660
- 2017 A/s
- 9500 A/s
No effect of high current ramp rates!
Will current distribution become inhomogeneous in
cables with many layers at high current ramp rates?
Cable: 52 CC in 17 layers.

## Slide 8
Ramp rates of 68,000 A/s at 19 T
ACT: DOE – Office of Fusion Energy Sciences Award DE-SC0007660,
NHMFL: DOE, NSF, agreement DMR-0654118, and the State of Florida

## Slide 9
Testing of CORC cables under axial stress
Cable installed with flexible current leads:
Current leads can handle >1500 A at 76 K.
s

## Slide 10
Testing of CORC cables under axial stress
sirr = 228 MPa
sirr = 277 MPa
6 tapes in 2 layers:
12 tapes in 4 layers:
Various options:
3/16” O.D. Cu former, 0.032” wall:

## Slide 11
Testing CORC cables under transverse compression
Phase II STTR DOE - Fusion Energy Sciences Award DE-SC0007660
Compressive stress test facility:
maximum load 10,000 lbs, or 44.5 kN.
anvil lengths 50 mm or 100 mm.
testing at room temperature and 76 K.
sample current exceeding 2 kA.

## Slide 12
Transverse compression test results (Cont.)
Phase II STTR DOE - Fusion Energy Sciences Award DE-SC0007660
CORC cables:
solid stainless steel former
former O.D. 4.8 mm
3 layers
CORC-4:
9 tapes, 0 mm gap, 20 mm Cu
CORC-5:
9 tapes, 0.5 mm gap, 20 mm Cu
CORC-6:
9 tapes, 0 mm gap, 5 mm Cu
Decrease in Ic depends on gap size and copper thickness.
Anvil length: 5 cm.

## Slide 13
Modeling of transverse compressive stress
Phase II STTR DOE - Fusion Energy Sciences Award DE-SC0007660
Maximum compressive stress at 7,500 lbs with 5 cm anvil: 1340 MPa
0.5 mm-wide imprint in 5 cm long brass anvil after 7,500 lbs load suggests a stress of 1.3 GPa!

## Slide 14: CORC cables for accelerator magnets
DOE-High Energy Physics Award DE-SC0009545
Goal 1: Je of > 300 A/mm2 at 20 T at 11 cm bending diameter using basic tape.
Collaborators: David Larbalestier and Ulf Trociewitz (NHMFL)
Goal 2: improve CORC flexibility : Je > 200 A/mm2 at 20 T and at 6 cm bending diameter.
Status at beginning of program (2013):

## Slide 15
CORC Je>100 A/mm2 at 20 T and 6 cm diameter
DOE - High Energy Physics Award DE-SC0009545
Cable:
- 37 YBCO CC, 14 layers
- cable O.D. 6.4 mm
Expected Je = 103 A/mm2 @ 4.2 K, 20 T
Ic = 3989 A (10 cm) 3967 A (6 cm)@ 4.2 K, 15 T (Je=122 A/mm2)
No degradation when bending from 10 cm to 6 cm: Je(20T) = 103 A/mm2!

## Slide 16: Room for improvement
During cable inspection
after test at 19T:
Many damaged tapes in outer
layers due to cable bending!
Caused by loose winding pack.
Winding pack needs to be controlled:
=> Cabling machine is needed.
Ic = 5021 A @ 4.2 K, 19 T
DOE - Office of High Energy Physics grant DE-FG02-12ER41801

## Slide 17
Performance of tapes extracted from CORC cables
52 tape CORC cable:
- 3 mm former
- wound into 11 cm diameter
- tested at 19 T: Ic was 50 % of
projected value.
- Ic(76 K) after test 3300 A
Extracting all tapes from cable
and measure Ic at 76 K:
Outer layers show degradation due to tape kinking.
outside
former
Inner 4 layers show large degradation due to small former.
About 80 % of the tapes near 100 %
Sum of tape Ics 6,100 A!
Low cable performance mainly due to terminations.
DOE - Office of High Energy Physics grant DE-FG02-12ER41801

## Slide 18
CORC cable machine
University of Colorado program sponsored by:
DOE - Office of High Energy Physics grant DE-FG02-12ER41801
Winding of long CORC cables:
winding CORC cables layer-by-layer
accurate control of: 1. tape tension
2. winding angle
3. spacing between tapes
Long, high-quality CORC cables are now available!!!

## Slide 19
CORC cable for CERN order
Cable specification:
12 meter long
38 tapes (4 mm wide, 20 microns of copper)
5 mm diameter former (Al + Cu)
Cable finished Saturday May 17th.
Liquid nitrogen test scheduled first week of June.

## Slide 20
Winding the CERN CORC cable

## Slide 21
Winding the CERN CORC cable (Cont.)

## Slide 22
CORC cable performance projections
Improved Je at 20 T due to winding machine and reduced copper thickness:
Roughly 30 % reduction in cable diameter when using 5 microns of copper and a cable machine.
Roughly 3x improvement of Je at a cable diameter of 6 mm.

## Slide 23
CORC cable performance projections (Cont.)
Improved Je at 20 T due to reduced substrate thickness:
Roughly 50 % improvement of Je when using 30 microns substrate.
CORC cable with 300 A/mm2 is less than 5 mm in diameter!

## Slide 24
Thinner substrates are coming!
http://superpower-inc.com/content/superpower-adds-thinner-substrate-options-superconducting-wire-offerings
“Advanced Conductor Technologies has been eagerly awaiting this new, thinner profile conductor for incorporation into our high current density Conductor on Round Core (CORC) cable,” said Dr. Danko van der Laan, founder and chief executive officer of the start-up company located in Boulder, Colorado…”

## Slide 25
 | O.D. | Tape width | Gap | # tapes | Layer-Ic | Ic (77 K) | Ic (4.2 K, 20 T) | Je (4.2 K, 20 T)
Layer # | [mm] | [mm] | [mm] |  | [A] | [A] | [A] | [A/mm2]
1 | 3.08 | 3 | 0.5 | 2 | 225 | 225 | 432 | 58
2 | 3.16 | 3 | 0.5 | 2 | 225 | 450 | 864 | 110
3 | 3.24 | 3 | 0.5 | 2 | 225 | 675 | 1296 | 157
4 | 3.32 | 3 | 0.5 | 2 | 225 | 900 | 1728 | 200
5 | 3.4 | 3 | 0.5 | 3 | 338 | 1238 | 2376 | 262
6 | 3.48 | 3 | 0.5 | 2 | 225 | 1463 | 2808 | 295
7 | 3.56 | 3 | 0.5 | 2 | 225 | 1688 | 3240 | 326
8 | 3.64 | 3 | 0.5 | 2 | 225 | 1913 | 3672 | 353
9 | 3.72 | 3 | 0.5 | 2 | 225 | 2138 | 4104 | 378
10 | 3.8 | 3 | 0.5 | 2 | 225 | 2363 | 4536 | 400
11 | 3.88 | 3 | 0.5 | 2 | 225 | 2588 | 4968 | 420
12 | 3.96 | 3 | 0.5 | 2 | 225 | 2813 | 5400 | 438
13 | 4.04 | 3 | 0.5 | 2 | 225 | 3038 | 5832 | 455
14 | 4.12 | 3 | 0.5 | 2 | 225 | 3263 | 6264 | 470
15 | 4.2 | 3 | 0.5 | 2 | 225 | 3488 | 6696 | 483
16 | 4.28 | 3 | 0.5 | 3 | 338 | 3825 | 7344 | 510
17 | 4.36 | 3 | 0.5 | 3 | 338 | 4163 | 7992 | 535
18 | 4.44 | 3 | 0.5 | 3 | 338 | 4500 | 8640 | 558
19 | 4.52 | 3 | 0.5 | 3 | 338 | 4838 | 9288 | 579
20 | 4.6 | 3 | 0.5 | 3 | 338 | 5175 | 9936 | 598
CORC cable performance exceeding 600 A/mm2 (20 T)
Based on tapes available within 6 months:
Je (4.2 K, 20 T) > 600 A/mm2 possible in 4.5 mm diameter CORC cable!
Cable bending diameter of 10x cable diameter => 4-5 cm!
30 mm substrate, Ic(77 K, 4 mm) = 150 A, lift factor =2 (Ic(4.2 K,20 T)/Ic(77 K, s.f)

## Slide 26
 | O.D. | Tape width | Gap | # tapes | Layer-Ic | Ic (77 K) | Ic (4.2 K, 20 T) | Je (4.2 K, 20 T)
Layer # | [mm] | [mm] | [mm] |  | [A] | [A] | [A] | [A/mm2]
1 | 3.05 | 3 | 0.5 | 2 | 300 | 300 | 864 | 118
2 | 3.1 | 3 | 0.5 | 2 | 300 | 600 | 1728 | 229
3 | 3.15 | 3 | 0.5 | 2 | 300 | 900 | 2592 | 333
4 | 3.2 | 3 | 0.5 | 2 | 300 | 1200 | 3456 | 430
5 | 3.25 | 3 | 0.5 | 2 | 300 | 1500 | 4320 | 521
6 | 3.3 | 3 | 0.5 | 2 | 300 | 1800 | 5184 | 606
7 | 3.35 | 3 | 0.5 | 2 | 300 | 2100 | 6048 | 686
8 | 3.4 | 3 | 0.5 | 2 | 300 | 2400 | 6912 | 761
9 | 3.45 | 3 | 0.5 | 2 | 300 | 2700 | 7776 | 832
10 | 3.5 | 3 | 0.5 | 2 | 300 | 3000 | 8640 | 898
11 | 3.55 | 3 | 0.5 | 2 | 300 | 3300 | 9504 | 960
12 | 3.6 | 3 | 0.5 | 2 | 300 | 3600 | 10368 | 1019
13 | 3.65 | 3 | 0.5 | 2 | 300 | 3900 | 11232 | 1073
14 | 3.7 | 3 | 0.5 | 2 | 300 | 4200 | 12096 | 1125
15 | 3.75 | 3 | 0.5 | 2 | 300 | 4500 | 12960 | 1173
16 | 3.8 | 3 | 0.5 | 2 | 300 | 4800 | 13824 | 1219
17 | 3.85 | 3 | 0.5 | 2 | 300 | 5100 | 14688 | 1262
18 | 3.9 | 3 | 0.5 | 2 | 300 | 5400 | 15552 | 1302
19 | 3.95 | 3 | 0.5 | 2 | 300 | 5700 | 16416 | 1340
20 | 4 | 3 | 0.5 | 2 | 300 | 6000 | 17280 | 1375
CORC cable performance exceeding 1300 A/mm2 (20 T)
Based on tapes available within 1-3 years:
Je (4.2 K, 20 T) > 1300 A/mm2 possible in 4.0 mm diameter CORC cable!
15 mm substrate, Ic(77 K, 4 mm) = 200 A, lift factor =3 (Ic(4.2 K,20 T)/Ic(77 K, s.f)

## Slide 27
Effect of tape inhomogeneity on CORC cable performance
CORC cable with 12 tapes in 4 layers:
- two tapes with a 2 mm long interruption.
Cable with defects:
Ic = 991 A
n-value = 10.8
Solder-filled cable:
Ic = 1244 A
n-value = 16.8
Current sharing in CORC cables lowers conductor homogeneity and piece length requirements!
DOE - High Energy Physics Award DE-SC0009545
CORC cable performance is largely independent of tape production quality!

## Slide 28
Summary
CORC cables are being developed for three different markets:
1. High-current magnet cables for fusion and scientific magnets.
2. Power transmission cables and magnet feeders and busbars.
3. High-current density cables for HEP magnets:
danko@advancedconductor.com +1-720-933-5674
CORC cable performance improvements:
Je > 300 A/mm2 possible with standard conductor (Ic,tape(20 T) = 150 A
Je > 600 A/mm2 using 30 mm substrate and improved pinning (Ic,tape(20 T) = 300 A
Je > 1300 A/mm2 using 15 mm substrate and improved pinning (Ic,tape(20 T) = 600 A
High-quality CORC cables can now be delivered in long lengths!
Cable concept | Achieved |  | Potential |  | M | stransverse | elongitudinal
 | Iop | Jcable | Iop | Jcable |  |  | 
 | (kA) | (A/mm2) | (kA) | (A/mm2) | (mT) | (MPa) | (%)
CORC | 5 | 114 (19 T) | >10 | >1300 (20 T) | ? | 1000 | 0.6