## Slide 1
Recent results on the development for the SPES target-ion source complex
Cathi Meeting
25 September 2014 ; Barcelona
Alberto Andrighetto
INFN – Laboratori di Legnaro

## Slide 2
Outline
- The SPES RIB production station.
- Laboratories and organization.
- Working groups results.
- Conclusions.
Charge
Breeding
Mass
Separator

## Slide 3
The RIB production area overview
Front end
Wien Filter
RIB Production area
Handling area
Chamber unit storage
AGV
Transition area
90° dipole

## Slide 4
The TIS device
7 UCx coaxial disks:
thickness: 1.3 mm
diameter: 40 mm
Graphite box:
external diameter: 49 mm
average length: 200 mm
3 graphite dump disks
Tantalum tube:
external diameter: 50 mm
thickness: 0.35 mm
length: 200 mm
Ionizer & transfer tube:
thickness: 1 mm
height: 34 mm
Inner diameter: 3 mm
SPES Heater, Ionizer & Chamber
SPES Target :
Optimized for 8 kW power dissipation
(E= 40 MeV, I= 200 μA)
Aluminum target unit

## Slide 5
ILine= 200A -> 600A max
ITarget= 700A -> 1200A max
The TIS on operation

## Slide 6
Wien filter
Triplets
Dignostic box
TIS
The SPES (off-line) RIB station
Evolution of ISOLDE FE6

## Slide 7
The TIS SPES (8) Laboratories
HT LNL Lab
Test Bench LNL Lab
Carbide Chemistry LNL Lab
UCx Chemistry PADOVA Lab
New ‘class A’ LNL Lab
Pavia laser Lab
New LNL laser Lab
Handling LNL Lab

## Slide 8
WG-1: Target and Ion Sources
WG-2: Target Materials
WG-3: Laser
WG-4: Handling
WG-5: Front End
The TIS five Working Groups

## Slide 9
TIS: Definition of the unit device 1/6
Graphite window
Flexible heater
Graphite dump
Thermocouple output (type C)
BNC output (current sensor)
Thermocouple (type C)

## Slide 10
TIS: Ion Source Developments 2/6
The SPES SIS Ion source
WG-01
ionizing cavity
connector
plate
support
thermal screen
Re Ionizing Cavity and Ta Ionizing Cavity
OFF-LINE TESTING
efficiency and emittance measurements with accurate temperature monitoring

## Slide 11
TIS: Ion Source Developments 3/6
The SPES PIS Ion source
WG-01
OPTIMIZED CATHODE GEOMETRY
hot spot close to the anode interface (thermionic electron production)
OPTIMIZED EXTRACTION REGION
low transversal emittance values
(now under testing at LNL)

## Slide 12
> Emittance measurements for SIS and PIS (@ 25kV extraction voltage)
TIS: Ion Source Developments 4/6
WG-01
Chart: electrode - ion source distance (mm)
| 85.3 | 73.699999999999989 | 62.1 | 50.5 | 38.900000000000006 | 27.299999999999997 | 15.700000000000003
emittance RMS | 7.31 | 4.8287 | 5.4297 | 7.4467 | 9.8723 | 13.0907 | 14.9177
PIS (Ar beam)
RMS ≈ 10 π mm mrad (90% ≈ 40 π mm mrad)
Chart: electrode - ion source distance (mm)
| 109.4 | 97.800000000000011 | 86.2 | 74.600000000000009 | 63.000000000000014
emittance RMS | 3.8575 | 2.9645 | 2.872 | 2.63 | 2.8755
SIS (Cs beam)
RMS ≈ 5 π mm mrad (90% ≈ 20 π mm mrad)

## Slide 13
TIS: Ion Source Developments 5/6
Ta - SIS efficiency data (off-line measurements)
> Efficiency measurements for SIS
T = 2200 °C
WG-01

## Slide 14
TIS: Ion Source Developments 6/6
Ionization efficiency measurements for Ar (25 kV)
- Anode voltage = 150 V
- Anode magnetic field ≈ 300 G
- Total beam current ≈ 3 µA
> Efficiency measurements for PIS
WG-01

## Slide 15
1) scaled (d = 13 mm) SiC SPES tested @ ORNL (2007), – 40 MeV, 12 µA p beam, for thermal & release study
2) scaled (d = 13 mm) UCX SPES tested @ ORNL (2010-2011) – 40 MeV, 50 nA p beam, for relase study
 | 2010 Standard UCX | 2011 Low density UCX
Density (g/cm³) | 4.25 | 2.59
Diameter (mm) | 12.50 | 13.07
Thickness (g/cm²) | 0.41 | 0.41
Calculated porosity (%) | 58 | 75
Target: Experimental test 1/4
WG-02
Chart: Graphite Container Temperature
| 300 | 400 | 500 | 550 | 600 | 600 | 650 | 700 | 750
Experimental - With shields | 1173 | 1382 | 1605.3333 | 1734.6667 | 1813 | 1871
FEM - With shields | 1932 | 1815 | 1669

## Slide 16
3) scaled (d = 14 mm) UCX-CNT discs tested @ CERN (2009) and IPNO (2013) for release efficiency studies
Test @ IPNO (2013)
Test @ CERN (2009)
 | UCX-CNT (synthesis at CERN, 2009)
Density (g/cm³) | 1.30
Diameter (mm) | 14.10
Thickness (mm) | 1.30
Calculated porosity (%) | 88
Target: Experimental test 2/4
WG-02
Actilab ENSAR JRA collaboration

## Slide 17
On-line testing of the SPES target architecture @ iThemba (May 2014)
4) Full scale (40 mm.) SiC @ Ithemba, p=66 MeV, 60 microA for thermal dissipation studies
Target: Experimental test 3/4
WG-02
iThemba LABS: funded to build an RIB station like SPES (10 kW multi-foil target)

## Slide 18
On-line testing of the SPES target architecture @ iThemba (2013-2014)
66 MeV, up to 60 A - proton beam on a SiC target (Tmax on SiC =1600°C)
Heater
Power
Beam Power
Target
Temperature
Vacuum
Beam Dump Temperature
Target: Experimental test 4/4
Scattering chamber (build @LNL)
WG-02

## Slide 19
Laser: The LNL Laboratory 1/2
In 2013 a new SPES laser laboratory was build
WG-03
A tunable dye laser system ready for atomic spectroscopy study

## Slide 20
Laser: Activities at LNL 2/2
Design/construction of new
Time of Flight Spectrometer
WG-03
Fiber optic mixer (2 dyes to HCL)
System ready for Ge spectroscopy study.. (Oct ‘14)

## Slide 21
Handling: The SPES overview 1/4
Two systems are foreseen in order to increase the handling security level
Target Front End
Horizontal device
Vertical device
Target chamber unit
WG-04

## Slide 22
Handling: The Horizontal system 2/4
WG-04
< 50 µSv/h
Thanks to L. Sarchiapone

## Slide 23
Handling: The vehicle AGV based 3/4
Devices under construction at the LNL mechanical workshop
WG-04

## Slide 24
Handling: R6D for Puller Handling 4/4
WG-04
Puller
toy

## Slide 25: Front End: Beam transport trace-back 1/5
WG-05
ion source
extraction area
steering area
focusing area
diagnostic area

## Slide 26: Front End: extraction optimization 2/5
l = 4 mm
Φ = 1.5 mm
Tested with a reduction of 40% of emittance
(ε = 6 π mm mrad @ 25 kV)
Main goal: PIS emittance comparable with SIS without losing in efficiency
2) Puller optimization
Source:
PIS
SIS (and LIS)
Quadrupoles:
SIS (and LIS)
PIS (presence of non-linear effects)
Wien Filter:
Mass resolution Transport efficiency
WG-05
Optimization of FE optics in order increase the RIB transport
1) Anode optimization
Old configuration
New configuration

## Slide 27: Front End: design for On-line version 3/5 RAD-HARD version
WG-05
Off-line FE
On-line FE
Critical material List
Teflon with glass fibres -> alumina
Polyethylene -> peek
Viton O-rings -> EPDM
Plastic cable insulator -> air (close the target)
Normal motors -> RAD HARD motors

## Slide 28: Front End: Study on damage 4/5 Use of the LENA (PV) reactor for material testing (collaboration started on June 2014)
WG-05
Reactor for research TRIGA Mark II (250 kW) – LENA since 1965

## Slide 29: Front End: Planning for damage test 5/5 Preliminary program of Italian collaboration: SPES, LENA, INFNPV, UNIBS
WG-05
1. Compilation of materials of interest for the SPES project to be rad-hard tested;
-> working in progress
2. Evaluation by MCNPX, FLUKA codes of the radiation fields and cumulated dose expected on the critical components inside the ISOL bunker -> working in progress
3. Characterization of the obtainable radiation fields in the TRIGA Mark II in order to reproduce as close as possible the expected inside the SPES bunker. -> early 2015
4. Planning of irradiation campaigns at L.E.N.A. reactor on sample of SPES critical materials. . -> early 2015
5. Tests on irradiated samples physical and operational properties of materials corresponding to different levels of irradiated dose; . -> late 2015
6. Post-irradiation study of irradiated samples in order to evaluate the radiation damage (mainly for polymers). . -> late 2015
Possibility to extend the collaboration with external partners (Is fully welcome!)

## Slide 30
SPES
Exotic Beam
UNIPV
UNIPD
UNITN
DIM
DSC
DEI
ION SOURCES
MATERIALS
DIM
DEI
HANDLING
CONTROLS
Conclusions: the collaboration network…
CERN- ISOLDE
GANIL-SPIRAL 2
ORSAY-ALTO
ITHEMBA
ORNL- HRIBF
RISP-KOREA
INFN- Pavia
INFN- Milano
INFN- LNS
INFN- Bologna
INFN- Padova
UNISI
DSF
LASER
Notes: 25/09/2014
30

## Slide 31
Conclusions: the group…
Few results without them…

## Slide 32
Thanks for your attention!
and finally..