## Slide 1
Pei Zhang
(BE-RF-SRF, CERN)
The R&D on HIE‐ISOLDE superconducting quarter‐wave resonators
CATHI Final Review Meeting, 23rd Sep 2014
*This work received support from a Marie Curie Early Initial Training Network Fellowship of the European Community's 7th Programme under contract number PITN-GA-2010-264330-CATHI.

## Slide 2: Outline
Pei Zhang
Page 2
Sep 23rd, 2014
CATHI Final Review Meeting
Cavity frequency tuning strategy & realization
Cavity RF cold test
Multipacting study
Collaboration work with other CATHIers

## Slide 3: HIE-ISOLDE Linac
Pei Zhang
Page 3
Sep 23rd, 2014
CATHI Final Review Meeting
Niobium sputtered on copper
Boost the radioactive beam energy from 3MeV/u to 10MeV/u by using SC linac.
Quarter-wave resonator

## Slide 4: High-β QWR
Pei Zhang
Page 4
Sep 23rd, 2014
CATHI Final Review Meeting
Frequency | 101.28 MHz
Eacc | 6 MV/m
βoptimum | 10.9%
R/Q | 553 Ω
Epeak/Eacc | 5.0
Bpeak/Eacc | 95.6 G/(MV/m)
G=RsQ | 30.7 Ω
U/Eacc2 | 0.207 J/(MV/m)2
Pc at 6MV/m | 10W
|E| field
|H| field
Courtesy M. Fraser

## Slide 5: Cavity production flow
Pei Zhang
Page 5
Sep 23rd, 2014
CATHI Final Review Meeting
Cavity reception
Frequency tuning
Surface treatment
Niobium coating
Cryostat preparation
RF cold test
Cavity storage
Niobium Stripping

## Slide 6: Original frequency tuning strategy
Pei Zhang
Page 6
Sep 23rd, 2014
CATHI Final Review Meeting
Lorentz detuning
Microphonics
Mechanical tolerance (0.1mm)
Cooldown process variability ± 5kHz
Design frequency: 101.28 MHz (4.5K in vacuum)
Large tuning range
Complicated production
High production cost
Tuning system

## Slide 7: New frequency tuning strategy
Pei Zhang
Page 7
Sep 23rd, 2014
CATHI Final Review Meeting
Lorentz detuning
Microphonics
Mechanical tolerance (0.1mm)
Cooldown process variability ± 5kHz
Tuning system
Pre-tuning
Simplified (€ reduction)
Lower Epeak
lower loss on the plate
Max Δf: 42kHz
P. Zhang et al., “Frequency Sensitivity to Cavity Geometry Errors of …”, CERN-ACC-NOTE-2014-0022, 2014.

## Slide 8: Mystery of frequency
Pei Zhang
Page 8
Sep 23rd, 2014
CATHI Final Review Meeting
Cavity heat up to ~630⁰C causes geometry changes
Degreasing
Chemical etching
Influencing variable | Freq. shift
Chemical etching 40’ | -27 ± 3 kHz
Niobium coating | -7 ± 5 kHz

## Slide 9: Frequency tuning
Pei Zhang
Page 9
Sep 23rd, 2014
CATHI Final Review Meeting
The new tuning strategy has been successfully applied.
Resolution: ~0.1 Hz/step

## Slide 10: RF Cold test
Pei Zhang
Page 10
Sep 23rd, 2014
CATHI Final Review Meeting
Cavity reception
Frequency tuning
Surface treatment
Niobium coating
Cryostat preparation
RF cold test
Cavity storage

## Slide 11: Q0 vs. Eacc
Pei Zhang
Page 11
Sep 23rd, 2014
CATHI Final Review Meeting
QP: prototype cavity
QS: series production cavity

## Slide 12: Q0 and Pcav
Pei Zhang
Page 12
Sep 23rd, 2014
CATHI Final Review Meeting
4.77E+8
10 W

## Slide 13: Thermal gradient
Pei Zhang
Page 13
Sep 23rd, 2014
CATHI Final Review Meeting
Thermal gradient: T2 – T1
Surface resistance

## Slide 14: Surface resistance vs. thermal gradient
Pei Zhang
Page 14
Sep 23rd, 2014
CATHI Final Review Meeting

## Slide 15: Surface resistance vs. cool-down speed
Pei Zhang
Page 15
Sep 23rd, 2014
CATHI Final Review Meeting
Thermal gradient [K]: T2 – T1
Cool-down speed [K/min]: average speed from 10.5K to 8.5K

## Slide 16: Study of trapped magnetic flux
Pei Zhang
Page 16
Sep 23rd, 2014
CATHI Final Review Meeting
Horizontal plane
Vertical plane
Total reduction: 625 mG → 180 mG (~70% ↓)
Total enhancement: 625 mG → 1155 mG (~85% ↑)
Trapped magnetic flux causes additional power loss.

## Slide 17: Surface resistance vs. ambient magnetic field
Pei Zhang
Page 17
Sep 23rd, 2014
CATHI Final Review Meeting
 | Rs0 [nΩ] | Rs1 [nΩ/(MV/m)]
QP3.2 | 0.11 | 0.13
QS2.1 | 0.31 | 0.15
For every 1mT ambient magnetic field increment
Ambient magnetic field
 | 0mT | 12mT
QP3.2 | ~11% ↓ | 10% ↑
QS2.1 | ~6% ↓ | 5% ↑

## Slide 18: Multipacting
Pei Zhang
Page 18
Sep 23rd, 2014
CATHI Final Review Meeting
QS1.1
Multipacting seen during every cavity test
- Eacc ~ 1.5 MV/m
- Eacc ~ 0.05 MV/m
MP can eliminated by RF conditioning

## Slide 19: MP by CST Particle Studio
Pei Zhang
Page 19
Sep 23rd, 2014
CATHI Final Review Meeting
1RF
2RF
5RF
10RF
Two MP barriers found
- Eacc ~ 1.2MV/m @ cavity top
- Eacc ~ 0.05MV/m @ cavity body

## Slide 20: MP by SLAC ACE3P suite
Pei Zhang
Page 20
Sep 23rd, 2014
CATHI Final Review Meeting
Two MP barriers found
- Eacc ~ 1.4MV/m @ cavity top
- Eacc ~ 0.05MV/m @ cavity body

## Slide 21
Pei Zhang
Page 21
Sep 23rd, 2014
CATHI Final Review Meeting
Collaboration with other CATHIers

## Slide 22: Field emission (with I. Kobzeva)
Pei Zhang
Page 22
Sep 23rd, 2014
CATHI Final Review Meeting
Electron emission
Energy of the electron hit the bottom plate
Max energy: 880keV
Peak: 830keV

## Slide 23: Aluminium sputtering (with E. Cantero)
Pei Zhang
Page 23
Sep 23rd, 2014
CATHI Final Review Meeting
Beam direction
Aluminium slit
20Ne5+
27Al
Neon beam and aluminium slit are used to measure ion beam size
The contamination of sputtered aluminium atom in the cryo-module

## Slide 24: Aluminium sputtering (with E. Cantero)
Pei Zhang
Page 24
Sep 23rd, 2014
CATHI Final Review Meeting
Fully random emission
Ne beam current: 100pA
Ne sputter on Al yield: 0.109
Average beam size measurement time: 2 min/hour
Time to coat a 1mm2 monolayer Al: ~1 year
Time to coat a 1mm2 monolayer Al inside cavities
- Narrow opening Al incident: 3 years
- Fully random Al incident: 97 years

## Slide 25: Summary
Pei Zhang
Page 25
Sep 23rd, 2014
CATHI Final Review Meeting
New frequency tuning strategy successfully applied
- Mystery of frequency shift unveiled
RF cold test of the cavities smoothly going on
- R&D on cooldown dynamics & flux trapping started
Collaborations with other CATHIers