## Slide 1: Modeling quench propagation in a protection heater covered YBCO coil
Tiina Salmi
Tampere University of Technology (TUT), Finland
The Kyoto Workshop on HTS Magnet Technology for HEP (WAMHTS-2)
Nov 14 2014
Thanks to : A. Stenvall (TUT) ,
G. Kirby (CERN), E. Härö (TUT), J. Van Nugteren (CERN)

## Slide 2: Outline
Purpose of protection heaters and important parameters
Simulation tool
Analyzed cases
Simulated heater delays and quench propagation velocities
Ideas for future heater concepts and conclusion

## Slide 3: Important heater parameters

## Slide 4: Quench protection heaters
After quench detection the magnetic energy (E = I2Lmag/2) must be safely discharged
  Option 1: Extraction via external dump resitor
  Option 2: Internal dissipation via Joule heating in resistive coil segments
Important parameters: Delay time to induce a quench, and the amount of quenched winding
Rdump limited by V:
Large I0, large E  Extract only a small fraction
(LTS) Heaters to quench large fraction of winding for fast I decay and uniform E dissipation

## Slide 5
Heater
Heater
Heater
YBCO cable
Cable insulation
Heater
insulation
Hotspot!
Heat
Heat
Heat
Hotspot!
Hotspot!
Quench propagation
Quench propagation
Delay 1:
A quench intiated under heater
Delay 2:
Entire cable quenched
x
y
z

## Slide 6: Simulation model

## Slide 7: CoHDA: Code for Heater Delay Analysis
Computes heat diffusion from heater to a cable in 2-D (neglect transv.)
Quench when Ic == Iop  Delay 1
  Account for current redistribution
Heat generation due to current in Cu
  Current sharing model with critical surface
Quench propagation between heating stations  Delay 2
Heat generation in heater:
Heat generation in cable:
  T. Salmi et al., Trans. IEEE Trans. Appl. Supercond. 24(4), 2014
  T. Salmi et al., Trans. IEEE Trans. Appl. Supercond. 25(3), 2015
Heat balance eq. to be solved:

## Slide 8: Analyzed cases

## Slide 9: Analyzed cables based on EuCard-2 FM0
  fCu = 0.315
  Acable,ins = 12.2 mm2 fHastelloy = 0.385
  AYBCO = 0.171 mm2 fVoids (epoxy) = 0.1
  fCable ins.= 0.2
Wt = 12 mm
Wx = 5.5 mm
15 Tapes
5.7 mm
Cable 1
7.5 Tapes
11.4 mm
Cable 2
15-tape Roebel cable modeled as stacked tape cable
Conserving Acable and material fractions
Heater
Heater
  G. Kirby and M. Durante, EuCARD2 Milestone report, MS64, 2014

## Slide 10: Simulation domain
dT/dx=0
T = Top
dT/dx=0
T = Top
Imag
Tape width
5.7 mm or 11.4 mm

## Slide 11: Analyzed operation points
6 kA
10 kA
α = 5°
D
B
C
A
CASE | Top (K) | Imag (kA) | B (T) | B angle (α) to ab-plane (°) | Tcs (K)
A | 4.5 | 6 | 15 | 5 | 22.3
B | 4.5 | 10 | 10 | 5 | 22.7
C | 4.5 | 6 | 10 | 5 | 28.8
D | 35 | 6 | 1.5 | 5 | 52.5
  Jc(B,T,α): J. Fleiter (see talk by Glyn yesterday)

## Slide 12: Analyzed heater
State-of-the-art in LTS, typical values:
  25 µm thick stainless steel
  50 µm Kapton
  50 W/cm2 (20 W/mm3) (min.)
  τRC 50 ms (capacitor powered)
Result presented at ASC-2014: In HTS heater like this does not have enough energy to quench for Tcs > ~20 K
Here is analyzed heater with 4 x more E
  50 µm thick stainless steel
  50 µm Kapton
  200 W/cm2 (40 W/mm3)
  τRC 50 ms
  H. Felice et al., IEEE TAS 19(3), 2009
  T. Salmi et al., IEEE TAS 24(3), 2014
  T. Salmi and A. Stenvall, IEEE TAS 25(3), 2015

## Slide 13: Simulation results

## Slide 14: Delay 1 vs. heater coverage
Cable 1
C
B
A
1-D with ” --- ”
Cable 2
C
B
A
Coverage (mm)
Delay 1 (ms)
A: 4.5 K, 6 kA, 15 T (5°): Tcs = 22.3 K
B: 4.5 K, 10 kA, 10 T (5°): Tcs = 22.7 K
C: 4.5 K, 6 kA, 10 T (5°): Tcs = 28.8 K
D: 35 K, 6 kA, 1.5 T (5°) : Tcs = 52.5 K
Need 40 – 80 mm long heating stations (roebel?)
Cable geom. impacts the delay 40-60% !
Heater energy must be related to the cable energy margin
  See extra slides

## Slide 15: Normal Zone Propagation Velocity
Cable 1 ” --- ”
Cable 2 ” __”
C
B
A
I = 6 kA (4.5 K)
B = 10  15 T
NZPV = 0.3  0.5 m/s
B = 10 T (4.5 K)
I = 6  10 kA
NZPV = 0.3  0.8 m/s
Geometry does not matter
Consistent with other studies
A: 4.5 K, 6 kA, 15 T (5°): Tcs = 22.3 K
B: 4.5 K, 10 kA, 10 T (5°): Tcs = 22.7 K
C: 4.5 K, 6 kA, 10 T (5°): Tcs = 28.8 K
D: 35 K, 6 kA, 1.5 T (5°) : Tcs = 52.5 K

## Slide 16: Delay 2 vs. heater period
C
B
A
C
B
A
Cable 1
Cable 2
Period (mm)
Delay 2 (ms)
Max 120 – 150 mm period
  Or > 300 K under heater
  Coverage min 30-50% (compare to 10-30% in LTS)
If protected with heaters, better to find a way to cover all with the heater!
A: 4.5 K, 6 kA, 15 T (5°): Tcs = 22.3 K
B: 4.5 K, 10 kA, 10 T (5°): Tcs = 22.7 K
C: 4.5 K, 6 kA, 10 T (5°): Tcs = 28.8 K
D: 35 K, 6 kA, 1.5 T (5°) : Tcs = 52.5 K

## Slide 17: Ideas for future heaters and conclusions

## Slide 18: Ideas for alternative heaters 1/2
Fig. From Wikimedia commons, authored by Christian Barth
Example:
If the pink was a heater
Coverage for the blue
Coverage for the green
1. Heater co-wound as one of the strands,
or as a wider strip on the cable wide side
+ Good heater contact with cable
+ Need less heater power
- Still need insulation between heater and other strands
- May require ”take-outs” from the middle to limit the voltage

## Slide 19: Ideas for alternative heaters 2/2
2. Several shorter ”layered” heaters on top of the coil
First Kapton
PH1: Stainless steel
Second Kapton
PH1: Current route (copper)
PH2: Stainless steel
PH2: Current routes
+
-
+
-
+ Can make several short heaters with high power (and low voltage) to cover a long coil
+ PH current leads only at coil ends
- Need many HFU’s
- Less uniform trace thickness

## Slide 20: Conclusion
The CoHDA simulation tool now includes also quench propagation in a YBCO cable
Analysed heater delays in FM0 cable
  Modeling roebel cable as stacked tape
    Dimensions impact on heater delay time but not on NZPV
Seems that with a powerful heater cables can be quenched, but the quench propagation is so slow that it is better to try to cover the entire cable with heater and not rely on heating stations
  Needed delays depend on J, L and detection time
Must investigate also other protection options than heaters
Future work will consists of interfacing the heater model to a current decay model for a comprehensive quench protection analysis

## Slide 21
Two geometries tested in 3.3 m long LARP LHQ 15 T Nb3Sn quadrupole coil.
Cov.
Cov.
Per.
Per.
Cov.
Per.
Examples of heater geometries

## Slide 22: Design plot to estimate delay 1 vs. Tcs
100 W/cm2 (148 ms)
50 W/cm2 (>300 ms)
200 W/cm2 (22 ms)
300 W/cm2 (39 ms)
Heater powered with a square pulse.
Pulse width so that T max. in heater is 300 K.
Example Tcs
Delay 1, when heater powered with 100 W/cm2 (tpulse = 148 ms)
Cable 1, Top = 4.5 K

## Slide 23: Enthalpy vs. Temperature margin
Heater energy must be related to the cable energy margin

## Slide 24: Current ”redistribution”
We go through cable segments column by column
1,1
2,1
N,1
. . .
. . .
i,j
Ti,j
QUENCH = 0
tdelay1 = -1
DO j = 1, K
ISC,j = 0
DO i = 1, N
ISC,j = ISC,j + JC (B, Ti,j) * Aelem
IF (ISC,j ≤ Iop) QUENCHj = 1
END DO
IF (tdelay1 = 0) tdelay1 = time
ICu,j = Max (0, Iop - ISC,j)
END DO
Aelem = AYBCO/N
. . .
1,2
1,K
. . .
. . .
N,K

## Slide 25: Heat generation
1,1
2,1
N,1
. . .
. . .
i,j
Ti,j
Vtot = 0
DO j = 1, K
JCu,j = ICu,j / Acu
Vk = JCu,j * ρCu,i=N/2,j * Δx
fgen = Iop * Vku / (ACable* Δx)
Vtot = Vtot + Vk
END DO
. . .
1,2
1,K
. . .
. . .
N,K
Δy
Δx
Δx and Δy constant in cable
Acable =
Acu/ fCu

## Slide 26
Record the time of first heat generation (TqVT)
Do all combinations of VT’s
(Consider only VT’s where heat generation)
For all VT’s
Is Joule heat generated at the location of the VT?
YES
Compute the quench propagation velocity between VT’s
NO