## Slide 1: Reduction of internal porosity in 2212 round wires with overpressure (OP) processing
Maxime Matras
J. Jiang, N. C. Craig, P. Chen, F. Kametani, P. J. Lee, U. P. Trociewitz, H. Kandel, C. Scheuerlein* , E. E. Hellstrom, and D. C. Larbalestier
Applied Superconductivity Center, National High Magnetic Field Laboratory, Florida State University
*CERN

## Slide 2
Why do we need overpressure (OP) processing to make 2212 wire a candidate for high field applications?
  To increase JE by densification of the 2212 filaments
When and how does conductor densification occur?
  High densification is reached homogeneously above 800°C
How much reduction in diameter does OP produce?
  About 4% decrease in diameter
What is the effect of OP on coil? (Peng Chen - NHMFL)
Can we densify 2212 wires before winding?
  Cold isostatic pressing is one option
What length of conductor does not densify in case of seal failure?
Driving questions

## Slide 3
Cross section as-drawn 37x18 (W13)
Kametani et al., Supercond. Sci. Technol. 24, 075009 (2011)
Filaments from wire quenched in the melt
As-drawn filaments are 60±5 % dense (PIT process)
40±5 % gas bubbles after 2212 melts
Bubbles block current transport
Wire expands at high temperature
As-drawn wires are only 60% dense
Problems:
Filament cavity and 2212 powder have different volumes
Internal gas causes Ag creep at high temperature (T. Shen)

## Slide 4
Closed ends 1 atm: gas trapped
<60% dense
Overpressure (OP) densifies 2212 wires
Courtesy Dr C. Scheuerlein
Closed ends 100 atm OP:
0.8 mm diameter closed ends 8 cm long samples
Courtesy Dr C. Scheuerlein
Assumption: closed ends short samples behave the same as long coil length
100 atm closed ends
Densification
1 atm closed ends
expansion
As-drawn 60% dense

## Slide 5
Overpressure (OP) densifies 2212 wires
Courtesy Dr C. Scheuerlein
Courtesy Dr C. Scheuerlein
Problems at 1 atm:
Filament cavity and 2212 powder have different volumes
Gas causes Ag creep, further dedensifying the 2212 and causing local eruptions
With 100 atm OP
Volume of filament cavity is reduced and match closer 2212 powder volume
OP stops gas expansion.

## Slide 6
Dense filaments are the key for high JE
Closed ends 1 atm (coil behavior)
150 A/mm2
Closed ends 100 atm (coil behavior)
JE 6x
Experiment done on short wires (8cm long) (37x18)
917 A/mm2
[4.2K, 5T]
OP at 100atm makes 2212 a candidate for high field applications.
35 m long 10 bar samples fell on the curve and many more coils are coming (Peng Chen talk)
JE is calculated from diameter of OPed wires. What about JC?
( 611 A/mm2 20 T)

## Slide 7
Dense filaments are the key for high JE
Experiment done on short wires (8cm long)
JC is calculated using the as-drawn wire filament cross sectional area (60% dense filaments)
JC increases (actually it triples) with decreasing wire diameter as full physical connectivity occurs.
Cross section
as-drawn 37x18 (0.8mm diameter)
[4.2K, 5T]
[4.2K, 5T]

## Slide 8
When does densification occur?
Special heat treatment:
Densification is reached at about 821°C for 2h.
50 atm and 100 atm show similar results.
Filaments densify before 2212 melts
Before 2212 melts
After 2212 melts

## Slide 9
Special heat treatment:
821C - tmax
50 atm
No change in filament shape after densification
Filaments densify before 2212 melts
3.75 ± 0.13%
Densification occurs within 2 h
86.7 ± 1.7% dense filament from 2h
0.17h (10 min)
2h
For large size magnet, high densification is expected to be homogeneously reached for the whole winding pack before melting the 2212.

## Slide 10
100atm 821°C-12h
4.2 % decrease in wire diameter at 100 atm
4.2 ± 0.3%
100 atm OP significantly decreases the wire diameter.
Issue:
For magnet construction, this change in diameter poses an interesting challenge. (See Peng talk).
As-drawn
100 atm full heat treatment

## Slide 11
CIPing densifies wires at room temperature
2.1 %
Results:
Half of the OP densification can at least be reached at room temperature using a CIPing pressure of 20.4katm (300kpsi).
4.2 %
Average as-drawn diameter
Average diameter 100atm OP HT
CIPed at 20.4 katm
Goal:
We want to decrease wire diameter at room temperature before winding magnet to anticipate the diameter shrinkage of the wire during the 100 atm OP HT.

## Slide 12
Wire fully densifies about 1 m in from the open end
2.2 m long sample fully heat treated at 100 atm
Both ends open (worth case)
1 extra meter needs to be added to coil terminals when OP processed
1 m
1 m

## Slide 13
Wire densification with overpressure is the key for high JE and high Jc.
Filaments densify before 2212 melts, starting at about 800°C, high density (87%) occurring at about 821°C within 2 h.
Wire diameter decreases by 4.2 ± 0.3% at 100 atm.
CIPing at 20.4katm provides decrease in diameter of at least 2.1%.
Without seal, wire fully densify about 1 m in from the open end.
Conclusion

## Slide 14
Collaborations with Y. Huang, H. Miao, S. Hong, and J. A. Parrell of Oxford Superconducting Technology
Technical support from B. Chew, W. L. Starch, V. S. Griffin, and J. Craft at FSU.
Support by BSCCO strand and cable collaboration (BSCCo), a grant of the US Department of Energy and by the NHMFL, which is supported by the NSF under NSF/DMR-1157490 and by the State of Florida.
Acknowledgement

## Slide 15: Thank you for your attention
This is a Sub-title