## Slide 1: DESIGN OPTIONS FOR SEPARATION DIPOLES AND QUADRUPOLES
E. Todesco
CERN, Geneva Switzerland
Revised version 16 May
Acknowledgements: L. Bottura, R. Tomas, R. Martin
CERN, 15th May 2014
Future circular colliders - magnets

## Slide 2: SEPARATION DIPOLE
Today we have 26 T m
  At 7 TeV, 8.3*14.3=119 T m give a kick of 2 p/1232 = 5.1 mrad
  26 T m gives 1.1 mrad kick
  Beam separation is 192 mm, so distance D1-D2 is 96/1.1= 87 m
For HL LHC we aim going to 35 T m, 1.5 mrad
  distance D1-D2 reduced to 96/1.5= 64 m
For FCC
  Energy from 7 to 50 TeV : *7.14
  Beam separation from 192 to 300 mm: *1.56
  But D1-D2 distance is doubled , i.e. from 87 to 174 m: /2
  Needed kick is 26*7.14*1.56/2=145 T m [R. Tomas proposal]
  I would also consider the option of 290 T m, giving a D1-D2 space of 87 m

## Slide 3: SEPARATION DIPOLE
D1 is a single aperture magnet
  Resistive for LHC – 80 mm aperture
  5.6 T for HL LHC, in Nb-Ti – 150 mm aperture
  We can consider a Nb3Sn version, with 15 T short sample and 12 T operational field
    This is 1 T more than the 11 T
    Should be achievable with 40 mm coil, four layers of 10 mm cable
  In this case length is also 12 m –still reasonable
    In case of short lay out with 87 m between D1 and D2 two modules of 12 m could be considered
  Aperture is between 40 and 60 mm probably closer to 40 mm (iteration is needed with optics)
    Not so challenging

## Slide 4: RECOMBINATION DIPOLE
D2 is a double aperture magnet
  Superconductive for LHC – 80 mm aperture, 3.5 T
  For HL LHC, in Nb-Ti, 105 mm aperture, 4.5 T (in progress)
    Limit is field quality due to cross talk
  We can consider a Nb-Ti option with 6 T, very conservative
    Separation is larger, 300 mm so 6 T should not be a problem
    Two moduls of 12 m long magnets
    Aperture required is 40 mm
  We can consider a more challenging Nb3Sn version, with 12.5 T short sample and 10 T operational field
    Should be achievable with 30 mm coil, two layers of 15 mm cable
    Field quality will be difficult, spool pieces needed (but not so difficult to do)
    In case of shorter lay out, two modules of 12 m length needed

## Slide 5: QUADRUPOLES
We provide a second guess on the possible relation gradient vs aperture, cased on scaling [E. Todesco, L. Rossi, PRSTAB 9 102401 (2006)]
  40 mm aperture: 470 T/m (peak field 10.7 T)
  50 mm aperture: 400 T/m (peak field 11.4 T)
  60 mm aperture: 350 T/m (peak field 12.0 T)
With hypothesis of present Nb3Sn performance, 50 mm of coil (possibly 4 layers) – this is a challenging option
  With two layers, 30 mm
  one has 10% less
    40 mm 430 T/m
    50 mm 370 T/m
    60 mm 325 T/m

## Slide 6: QUADRUPOLES
We provide a second guess on the possible relation gradient vs aperture, cased on scaling [E. Todesco, L. Rossi, PRSTAB 9 102401 (2006)]
  70 mm aperture: 310 T/m (peak field 12.5 T)
  80 mm aperture: 280 T/m (bore field 12.9 T)
  90 mm aperture: 260 T/m (bore field 13.2 T)
With hypothesis of present Nb3Sn performance, 50 mm of coil (possibly 4 layers) – this is a challenging option

## Slide 7: CELL QUADRUPOLE
LHC: 220 T/m, 3.15 m integrated gradient 700 T
From 7 to 50 TeV: * 7.14
From L=100 to L=200 m (cell length) : /2
Needed gradient: 2500 T
  So, with 470 T/m we will have 5.3 m in the short option
  Or with 430 T/m we will have 5.8 m in the long option