## Slide 1
Conductor for LHC Upgrades
ASC 2014
13 August 2014
A. Ballarino
Ballarino, B. Bordini, L. Bottura, L. Rossi
CERN, Geneva

## Slide 2
Large Scale Productions
LHC  1200 tons of Nb-Ti
 200 kg of HTS (Bi-2223)
ITER PF and CC coils
 200 tons of Nb-Ti
TF and CS coils
 500 tons Nb3Sn
Hi-Lumi LHC 11 T Dipoles, IR Quadrupoles
 25 T tons Nb3Sn
+  5 tons for CERN development program
+  5 tons for LARP development program*
* Arup Ghosh, BNL
6000 tons of Nb3Sn for 16 T FCC
2000 tons of HTS for 20 T FCC
Notes: 1200 ton = 7600 km
ITER: larger production of Nb3Sn strand ever

## Slide 3
Series Quadrupoles
LS3 (2023)
Series 11 T Dipoles
LS2 (2018)
Series 11 T Dipoles
LS3 (2023)
Total procurement = 30 t
 5 t for magnet short models and prototypes
Dual sourcing
Nb3Sn Procurement for Hi-Luminosity LHC

## Slide 4
FRESCA 2 dipole – Magnet for upgrade of cable test facility – FRESCA . Block dipole, 13 T, 100 mm bore
Diameter of strand =1 mm. Procurement (CERN and CEA, Eucard 1) started in March 2010 and it was completed in Dec 2013 ( 170 km tot)
11 T Dipoles for LHC
Diameter of strand =0.7 mm. Procurement started in May 2010
Hi-Lumi Quadrupoles for LHC
Diameter of strand =0.85 mm. Procurement started in August 2012
Nb3Sn Conductor Procurement at CERN

## Slide 5
JC (kA/mm2)
Dfil (m)
RRR (-)
Performance
Peak field
Cost
Stability Protection
Magnetization Field Quality
Stability
2.5
2
1.5
3
3.5
1
4
200
150
100
50
10
20
50
100
target
Dream wire
target performance:
Jc > 3 kA/mm2
Dfil < 20 m
RRR > 150
Hi-Luminosity wire
specification:
Jc > 2.45 kA/mm2
Dfil < 50 m
RRR > 150
+ Mechanical properties for cabling
Nb3Sn Conductor Specification

## Slide 6
Hi-Luminosity LHC Nb3Sn Wire - Specification

## Slide 7
Hi-Luminosity LHC Nb3Sn Wire – Measured Performance

## Slide 8
 | Sub-element size (m) |  |  |  |  | 
 | Wire  (mm) | RRP 108/127 | RRP 132/169 | RRP 192/217 | PIT 114 | PIT 192
FRESCA 2* | 1 | - | 58 | - | - | 48
Hi-Lumi Quad | 0.85 | - | 48 | - | - | 41
11 T | 0.7 | 46 | 41 | 32 | 44 | -
Smaller sub-element size
*Fresca 2 conductor: procurement by CERN and CEA – FP7 European Project
RRP
54/61
108/127
132/169
198/217
PIT
114
192
Hi-Luminosity LHC Nb3Sn wire

## Slide 9
Chart: Applied Field, [T]
11 T Nb3Sn Dipole Strand ( = 0.7 mm)
fil_PIT=44 m
fil_RRP=41 m
Flux Jump Amplitude  12 mT
T = 1.9 K
Measurements by D. Richter
M-loop width (0.5 T, 1.9 K) < 30 mT
Max spread around average  4.5 %
300 mT

## Slide 10
Chart: Sub-element geometrical size (m)
| 41 | 48
PIT | 2414 | 2523
 | 1350 | 1423
 | 2567 | 2900 | 3030
RRP | 1260 | 1490 | 1613
RRR > 100
Jc vs  of filaments
Mesurements performed at CERN

## Slide 11
+ Smaller filament size
(_filaments  20 m)
+ RRR > 150
Nb3Sn for LHC High Energy Upgrade

## Slide 12
YBCO Conductor
Bruker Tape, Eucard 2,

## Slide 13
YBCO Cables
Measurements at CERN
Eucard 2 activity
Roebel cable by KIT

## Slide 14
To get there….
  Nb3Sn (16 T magnets )
  Increase Jc in high fields
  Develop wire architectures that meet the characteristics required for accelerator quality magnets (reduce filaments size for field quality, assure stability requirements (RRR), guarantee mechanical properties as needed for cabling, winding and operation in a magnet assembly)
  HTS (20 T magnets)
  Assure Je at 4.5 K and in high (20 T) fields
  Reduce (or cope with…) conductor anisotropy (REBCO tape)
  Develop and demonstrate high current HTS cables
  Understand and handle quench performance and quench protection (first on strands and cables and after on magnets)
  Study and demonstrate field quality - for tape and wire geometry. Improve conductor geometry as needed – striation for tape, smaller filament size for wire ….
Eucard 2 Program

## Slide 15
Conclusions
In order to make a high-energy superconducting machine possible, conductors need to undergo a sustained and intensive program of R&D including:
development of materials that meet the desired characteristics for accelerator quality magnets;
work with conductor manufacturers to ensure that the developed strands are also of a sufficiently robust quality for large scale production (i.e. good yield)
.

## Slide 16
Thanks for your attention !