## Slide 1
Ramesh Gupta
BNL, NY USA
BNL High Field and
HTS Magnet Program
H T

## Slide 2: HTS Magnet Program at BNL
HTS magnet R&D over a wide range:
  High field, Medium field and low field (high temperature)
  Many geometries – racetrack, cosine theta, solenoid
Number of HTS coils/magnets designed built & tested:
  Well over 100 HTS coils and well over 10 HTS magnets
Type of HTS used:
  Bi2223, Bi2212, ReBCO, MgB2 – wire, cable, tape
Amount of HTS acquired:
  ~50 km (4 mm tape equivalent)
Or recent activities have been largely on magnets with ReBCO
  (yet one Bi2223 and one MgB2 magnet is ready for testing)

## Slide 3: Superconducting Magnetic Energy Storage (SMES)
High field large aperture HTS solenoid with huge stresses
Key Target Parameters: 25T, 100mm, 1.7MJ, 12mm ReBCO
Funded by arpa-e as a “high risk, high reward” project
Ramesh Gupta, BNL, Aug 2014
Notes: 3

## Slide 4
2 pancakes
1140 A, 4K
HTS Magnet Test Results (BNL/ABB/SuperPower/Houston)
100 mm bore ReBCO ARPA- E SMES Coil
46 pancakes
350 A, 27K, 12.5 T
R. Gupta, BNL, Aug 2014
Peak fields higher
12 pancakes
760 A, 4K, 11.4 T

## Slide 5: High Field HTS Magnet- PBL/BNL SBIR
Field on axis: 15.7 T
Field on coil : 16.2 T
(original target: 10-12T)
Overall Jo in coil:
>500 A/mm2 @16 T
Aperture = 25 mm
Highest field all HTS solenoid
*Credit to SBIR/STTR office for this and SMES work which was the result of this

## Slide 6: 2G HTS Quad for FRIB Fragment Separator Region
Important: Magnet for a real machine- baseline design of FRIB

## Slide 7: Large Temperature Margins (only possible with HTS)
Provides robust operation against local and global heat loads

## Slide 8: Advanced Quench Protection Electronics
Detects onset of pre-quench voltage at < 1mV and with isolation voltage > 1kV allows fast energy extraction

## Slide 9: Protection of HTS Magnet During an Operational Accident Near Design Current
175A
185A
Design: 210 A in SP Coils
Ringing in power supply made situation worse
90mV

## Slide 10: Magnet Designs for FCC

## Slide 11
Cos (q) Coil - PBL/BNL STTR#1
(12 mm, one block, 77 K)
BENEFITS of Kapton-CI:
No epoxy/adhesive to HTS tape (prone to degradation by epoxy)
Standard insulation in magnets
Cured coil can be handled easily
Makes good coil (including ends)
No measurable degradation@77 K

## Slide 12
Cos (q) Coil - PBL/BNL STTR#2
(4 mm, goal: full coil, 4 K test)
Future Plan (Phase I & Phase II)
No measurable degradation@77 K
Construction and 4 K test of full cos (θ) coil in next few months
R&D to develop base technology for accelerator magnets in next few years (includes measuring and finding ways to deal with magnetization)
Use these magnets in an accelerator in next few decades

## Slide 13: High Field 2-in-1 Common Coil Dipole Design for Colliders
A conductor friendly design
  Suitable for HTS coils – Roebel cable?
  Unfavorable orientation wrt field
      However, think long term. Will Ic remain so anisotropic forever?
Beam #1
Coil #1
Coil #2
Beam #2
Highest field R&W
Nb3Sn dipole
HTS tape common coil dipole

## Slide 14: A Coil Design with Overpass/Underpass Ends Optimized for ReBCO Tape
No need for lifting the ends and no reverse curvature
  Less strain on the conductor but winding more complicated
Align ReBCO tape parallel to the field for
  Higher Jc
  Lower magnetization (will depend on the thickness and not on the width)
R. Gupta, et al., “Next Generation IR Magnets for Hadron Colliders,” ASC2002
Solenoid
Type Ends

## Slide 15: Magnet R&D for FCC

## Slide 16: Common Coil Dipole at BNL for Testing HTS Insert Coils as in a Hybrid Magnet
BNL has a unique 10+ T Nb3Sn common coil dipole with large open space to test HTS coils in background field.
Provides fast turn around and economic R&D as no disassembly/assembly of the magnet is required
HTS coil become a part of the hybrid magnet test (~15 T)
High current 2212 coil

## Slide 17: A Warm bore Cryo-cooled Magnet with 6 HTS coils
Evening: Switch ON; Morning: COLD
Suitable for various studies
Quench studies
Measure magnetization induced harmonics
  as a function of time
  as a function of temperature
  as a function of field
BNL has about 50 HTS coils available for various studies; about 30 with ~100 meters of HTS
Consider utilizing this asset

## Slide 18: Summary
Yet a long way to go before HTS magnets can be used in HEP accelerators, HTS magnet technology has made a major progress over last decade. (I’m personally optimistic).
BNL has been active on developing HTS magnet technology and has made many significant demonstrations. BNL is looking forward to offer its unique and substantial experience to future HTS magnet R&D for FCC.
However, we are more than HTS‘R’US (of which I’m proud of). We also have active programs on LTS magnets (our bread-and-better), and are the one US facility with working superconducting accelerator magnets.