## Slide 1
PHYSICAL AND CHEMICAL CHARACTERIZATION OF A DEPOSIT OF CHROMIUM OXIDE
Manon DURAND
Chemistry Laboratory (TE-VSC-SCC)
Student in Chemistry Engineer School (ESCOM)

## Slide 2: Table of contents
Introduction
Establishment of the analytical methods and parameters
Heat treatments
Conclusion

## Slide 3: Introduction
Injection Kicker Magnets
electromagnetic devices composed of 4 magnets and 4 pulse generators
guide, maintain and focus the particle beam on its near-circular orbit
installed on the injection points of LHC
0,12Tesla in less than 900ns, for about 8ms.
Vacuum chamber

## Slide 4: Introduction
Problem with electron clouds
vacuum chambers in alumina
high SEY ~ 9-10
adverse effects: increase in pressure
          rise of temperature of the cold magnets
          instabilities, loss of beam.
(by F. Ruggiero)

## Slide 5: Introduction
Topic of the internship FINAL AIM: SEY reduction 1,4
Mike Barnes (TE-ABT-FPS)
Dr. Sudarshan, The Effect of Chromium Oxide Coatings on Surface
Flashover of Alumina Spacers in Vacuum (1976).
Objectives:
  Establishment of analysis methods - FT-IR spectroscopy
  - Thermal analysis
  - X-Ray diffraction (EN-MME-MM)
  - SEY measurements
  2. Heat treatments at different temperatures.
CrO3
Cr(VI)
Cr2O3
Cr(III)
>500°C
Intermediary reductions
Oxygen release

## Slide 6
Establishment of the analytical
methods and parameters

## Slide 7: Thermal Analysis
Differential Scanning Calorimetry
Total mass loss: 30% > 23% (theory: 4CrO3  2Cr2O3 + 3O2)
Evaporation?
Closed crucible with pure CrO3
Sample mass before analysis: 3,5mg
Sample mass after analysis: 2,5mg
Temperature range: 20°C  550°C
Heating speed: 5°C/min
Gaz : nitrogen, 50mL/min
270°C

## Slide 8: Thermal Analysis
Thermogravimetry
Total mass loss: 35% > 23% Evaporation?
Mass loss (1st reaction): ≈17%
Crucible with pure CrO3
Sample mass before analysis: 9,4mg
Sample mass after analysis: 6,1mg
Temperature range: 20°C  550°C
Heating speed: 5°C/min
Gaz : nitrogen, 50mL/min
1h45
270°C
17%

## Slide 9: Thermal Analysis
Total mass loss: 30% > 17% Reaction + Evaporation?
 Characterisation of the Cr(VI) thermal reduction.
 Restart of the thermobalance.
Crucible with pure CrO3
Sample mass before analysis: 3,5mg
Sample mass after analysis: 2,5mg
Temperature range: 20°C  270°C
Heating speed: 5°C/min
Isothermal duration : 5h
Gaz : nitrogen, 50mL/min
5h50

## Slide 10: FT-IR Spectroscopy
Attenuated Total Reflectance (ATR)
+ Fast, non-destructive.
- Unsuitable for in-situ analysis in vacuum chambers.
CrO3
Cr2O3
H2O

## Slide 11: FT-IR Spectroscopy
Transmission
+ Suitable for in-situ analysis.
Characterisation of the oxides.
- Samples storage (CrVI and KBr hygroscopic).
CrO3
Cr2O3
H2O
Sample
I source(x)
I (x)

## Slide 12: FT-IR Spectroscopy
Diffuse Reflectance
+ Suitable for analysis of residues in crucibles.
Characterisation of the oxides.
- Apparatus limitation (minimum wavelength: 600cm-1).
 Characterisation of the chromium oxides.
Transmittance (%)
H2O
CrO3
H2O
Cr2O3

## Slide 13: X-Ray Diffraction
(Floriane Leaux, Gonzalo Arnau Izquierdo (EN-MME-MM))
 Characterisation of the chromium oxides.
Pure Cr2O3
Standard library Cr2O3 (CrIII)
Pure CrO3
Standard Library CrO3 (CrVI)

## Slide 14: SEY Measurements
- Alumina - Sand-blasted, nickel-coated
and glided copper
(Holger Neupert, Valentin Nistor (TE-VSC-SCC))
SEY ≈9-10
SEY ≈1,8

## Slide 15
Heat treatments

## Slide 16: Samples before treatment
CrO3(aq) 10% (w/w) coating (Cr(VI))
(1h dipping + 1h drying (120°C))
FT-IR spectroscopy
X-Ray diffraction
SEY measurements

## Slide 17: 260°C for 4hours
FT-IR spectroscopy
X-Ray diffraction (EN-MME-MM)
SEY measurements
KBr+ CrO3 tablet
 Decrease in SEY.
Inapplicable solution
(hydroscopic).
CrO3 (240°C - 14H00)
Insoluble phase + liquid phase
Standard Library Cr3O8 (Cr5.33)
SEY ≈2
SEY ≈1,8

## Slide 18: 350°C for 72hours (backout simulation)
FT-IR spectroscopy
X-Ray diffraction (EN-MME-MM)
SEY measurements
KBr+ CrO3 tablet
Creation of Cr(III).
 Unstable solution.
CrO3 (350°C - 72H00)
Standard Library Cr2O3 (CrIII)
Standard Library Cr2O5 (CrV)
SEY ≈2
SEY ≈1,7

## Slide 19: 550°C for 72hours
FT-IR spectroscopy
  X-Ray diffraction (EN-MME-MM)
SEY measurements
 Inhomogeneous coating.
 Presence of Cr(III).
Transmittance (%)
Pure CrO3
CrO3 (550°C - 72H00)
Standard Library Cr2O3 (CrIII)
SEY ≈4
SEY ≈1,5

## Slide 20: Conclusions
Analytical methods and parameters established.
Several solutions to control coatings in the vacuum chambers.
Cr(III) seems to be a stable solution.
Improvements:
Study homogeneity of the coatings.
Identify intermediary oxides, create a FT-IR data base.
Study the influence of number of backouts for the Cr2O3 concentration.

## Slide 21: Acknowledgements
- Paolo Chiggiato (TE-VSC)
- Mauro Taborelli (TE-VSC)
- Benoit Teissandier (TE-VSC)
- EN-MME: F. Leaux, G. Arnau.
- Polymers Laboratory
- TE-ABT: L. Ducimetiere, M. Barnes.
- TE-VSC: C.Charvet, D. Letant-Delrieux, F. Fesquet, H. Neupert, L. Bardo, P. Maurin, R. Setnescu, R. Leber, V. Nistor.

## Slide 22
THANK YOU FOR YOUR ATTENTION