## Slide 1
Pablo Fernández-Martínez, D. Flores, V. Greco, S. Hidalgo, A. Merlos, G. Pellegrini and D. Quirion
IMB-CNM (CSIC), Barcelona (Spain)
Design and Fabrication of an Optimal Peripheral Region for the LGAD
This work is supported by RD50 Collaboration

## Slide 2
Talk Outline
Critical aspects of the LGAD design
Optimization of the multiplication junction
Optimization of the junction edge termination
Optimization of the periphery
New production run
Conclusions

## Slide 3: Critical aspects of the LGAD design
Core Region  Uniform electric field, high enough to activate mechanism of impact ionization (multiplication)
Termination  High electric field confined in the core region
Periphery  (Dead region) Charges should not be collected. Reduction of the leakage currents
Electric Field @ 400 V
N+
P
π

## Slide 4: Core region: Optimization of the Multiplication layer
Gain = 2÷4
Run 6474
Wafers have different gains:
  Good uniformity of gain over the wafer.
Doping profile of the P and N+ diffusions is crucial

## Slide 5: Optimization of the Junction Edge Termination
3 Designs have been analyzed
Three Requirements:
  VBD_Core(1D) < VBD_Termination
  Electric Field Uniformity
  Compatible with segmentation
Notes: En esta tesis se han evaluado tres estrategias para implementar la terminación.

## Slide 6: Junction Edge Termination: Deep N-type diffusion
  The electric field peak is reduced at the JTE curvature
  The highest electric field value is located at the main junction (1D)
   multiplication control
Ec value at the JTE junction is not as low, so the breakdown can be localized at the main junction

## Slide 7: Junction Edge Termination: Deep N-type diffusion
Runs 6474 & 7062
P-type multiplication layer
Metal
N-Type Diffusion (JTE)
SiO2/Si3N4
Passivation
VBD > 1100 V

## Slide 8: Junction Edge Termination: Segmented devices
Deep N-type diffusion works properly for pad devices
In segmented devices N+ electrode extension seems more convenient
Electric Field in two adjacent strips

## Slide 9: Design of the Device Periphery
Peripheral region should ensure the voltage capability as well as limiting the leakage current.
  After the full (vertical) depletion is reached, a fast lateral depletion of the lowly doped substrate takes place.
A C-Stop located too close to the edge termination can degrade the voltage capability
A deep P+ diffusion (C-Stop) is needed in the die periphery to avoid the depletion region reaching the unprotected edge
C-Stop
C-Stop
C-Stop

## Slide 10: Optimization of the periphery: Guard Ring
Good isolation should be ensured
Guard ring confines the detection area
Biased guard Ring around the detection region.
  The ring is independently biased to extract the surface component of the current
  Voltage capability is preserved (same curvature as JTE)

## Slide 11: Optimization of the periphery: Positive oxide charges
Surface leakage currents
Field oxides grown in wet conditions (H2 + O2) typically have a positive charge density in the range of 5e10 cm-2
  Surface inversion of the substrate and modification of the depletion dynamics.

## Slide 12: Optimization of the periphery: Strategies
Positive oxide charges (radiation induced or technologically originated) induce surface inversion of the substrate  Current path towards the collector electrode.
Boron blanket implant
Same implant
P-Spray: Counteracts the inversion
P-Stop: cuts the current path off

## Slide 13
Low Current Devices
High Current Devices
High Voltage Capability (Breakdown > 1100 V) in all wafers
Leakage current varies from some 10 nA to more 100 µA in devices within the same wafer
Electrical Characterization: Yield
VBD > 1100 V
Guard Ring is short-circuited with N+ electrode (inefficient P-Spray)
Run 6474
LGAD Wafer (W8 – High Boron Implant)

## Slide 14
New Fabrication Run
Top Distribution
Back Metallization

## Slide 15
New Fabrication Run
9 LGAD Pad Detectors
  3 (8 x 8 mm multiplication area)
  6 (3 x 3 mm multiplication area)
9 PiN Detectors
  3 (8 x 8 mm active area)
  6 (3 x 3 mm active area)
4 LGAD pStrips Detectors
  32-160-50-06-24
  32-160-62-06-12
  64-80-10-06-24
  64-80-22-06-12
2 PiN pStrips Detectors
  32-160-50-06-24
  64-80-10-06-24
1 FEI4 compatible pStrip Detector
1 Pixelated LGAD Detector (6 x 6 pixels)
1 Pixelated PiN Detector (6 x 6 pixels)
3 LGAD for Timing Applications
  200 um to chip edge
  250 um to chip edge
  800 um to chip edge
1 Specific Test Structure (SPR,SIMS,XPS)
IJS Ljubljana
INFN Torino
LAL Orsay
113 Structures
  47 (10 x 10 mm, total area)
  66 (5 x 5 mm, total area)

## Slide 16
New Fabrication Run: LGAD & PiN pad Detectors
LGAD 1,4,7
LGAD 2,5,8
LGAD 3,6,9
LGAD & PiN Pad Detectors
  Multiplication Area
    8 x 8 mm (Type 1, 2, 3)
    3 x 3 mm
    Termination: * P-Stop + N-Guard Ring (Type 3, 6, 9)
    * P-Stop + N-Guard Ring with JTE (Type 2, 5, 8)
    * JTE + P-Stop + N-Guard Ring with JTE (Type 1, 4, 7)
    * Field Plate 10 µm, 0 µm (Type 7, 8, 9)
Field Plate
Field Plate

## Slide 17
New Fabrication Run: LGAD & PiN strip Detectors
32.160.62.06.12
32.160.50.06.24
64.80.22.06.12
64.80.10.06.24
4 LGAD pStrips Detectors
  32-160-50-06-24
  32-160-62-06-12
  64-80-10-06-24
  64-80-22-06-12
2 PiN pStrips Detectors
  32-160-50-06-24
  64-80-10-06-24
Key Legend
  AA-BB-CC-DD-EE
  AA, Channels Number
  BB, Pixel Size
  CC, Multiplication Width
  DD, P-Stop Width
  EE, P-Stop Position

## Slide 18
LGAD and PiN Pixelated Detectors
1 Pixelated LGAD Detector (6 x 6 pixels)
1 Pixelated PiN Detector (6 x 6 pixels)
IJS Ljubljana

## Slide 19
LGAD for Timing Applications
3 LGAD for Timing Applications
  200 um to chip edge
  250 um to chip edge
  800 um to chip edge
INFN Torino

## Slide 20
Specific Test Structure. SRP, SIMS, XPS
Field Plate
Field Plate
N-Well
L1 P-Stop, C-Stop Well
L2 P-Well (P Multiplication)
L3 JTE
L4 N-Well
L4 + L2 N-Well over P-Well
L4 + L3 N-Well over JTE
2.75 mm
3.65 mm
LAL Orsay

## Slide 21
Conclusions
Optimization of the LGAD peripheral region is crucial for the detector performance
  Edge termination techniques confine the high electric field into the multiplication area and give voltage capability to the detector
  Structures within the peripheral region avoid high leakage currents and degradation
Deep N-diffusion termination technique has proved good performance
P-Spray technique has shown poor effectiveness
New production run at the IMB-CNM include pad and segmented (strip and pixel) designs with an optimized peripheral region based on the P-Stop technique.
300 µm-thick prototypes with the new mask set is now in production. A 200 µm-thick run is on going.

## Slide 22
Thank you
Questions?

## Slide 23
Back up Slides
Just in case

## Slide 24: Optimization of the Multiplication layer
Small variations in the Boron implant dose (~ 2 × 1012 at/cm2) lead to large changes in Gain and Breakdown values
Higher Boron implant Dose:
  Higher Gain
  Lower Breakdown
P-type multiplication layer determines both Gain and Breakdown
Effective charge and doping value at the junction determine the Gain

## Slide 25
Charge Collection Measurements: Electrons (mips)
LGAD diodes with different values of the doping dose of the p-type multiplication layer.
Wafers have different gains:
      Good uniformity of gain over the wafer.
      Very good stability of some diodes up to >1000 V.
Gain = 2÷4
Gain = 8÷20
W7  1.6 × 1013cm-2
W8  2.0 × 1013 cm-2
G. Kramberger,
24th RD50 Workshop, Bucharest
Medium Boron Implant
High Boron Implant
Run 6474

## Slide 26: Edge Termination: Why is needed?
The N+ shallow contact and the P-multiplication layers have to be locally created with a lithography mask
  The electric field at the curvature of the N+/P junction is much higher than that of the plane junction (where Gain is needed)
  Avalanche at the N+/P curvature at a very low reverse voltage (premature breakdown)
Shallow N+ and P-multiplication layers self aligned
High electric field peak at the curvature
Notes: Ruptura prematura, porque se alcanza el campo crítico de ruptura en la curvatura.

## Slide 27: Design of the Edge Termination: Critical Electric Field
P-Multiplication layer
P-Substrate
Extrapolated values
B. Jayant Baliga (2008): Fundamentals of Power Semiconductor Devices

## Slide 28: Junction Edge Termination: Floating Guard Ring
The N+ shallow diffusion is used to implement a floating guard ring.
  The lateral electric field distribution is smoothed leading to two peaks (main junction and floating guard ring)
  The electric field peak and the risk of avalanche breakdown at the curvature of the main junction is reduced. Optimization of the guard ring location is needed.
The lower Ec value at the ring junction can lead the termination to breakdown

## Slide 29: Junction Edge Termination: N+ Extension
The N+ is used to extend the N+ beyond the edge of the multiplication layer
  Phosphorous diffuses more in the very lowly doped substrate (higher curvature radius and voltage capability).
  The electric field rapidly increases at the plain junction (multiplication).
The lower Ec value at the overlap junction can lead the termination to breakdown

## Slide 30: Junction Edge Termination: Junction Termination Extension
N+ electrode
N Diffusion (JTE)
Lowly doped N-type Deep diffusion (JTE) around the curvature of the main junction
  Additional (specific) photolithographic step
  The addition of a Field Plate moderates the electric field at the JTE curvature
Field Plate
P type multiplication layer
P type (π) substrate
Resistivity ~ 10 KΩ·cm
P+ electrode
Notes: Finalmente, la terminación JTE es la que mejores resultados nos ha dado

## Slide 31
Capacitance humps are related with the depletion of the periphery
Run 6474
Implementation: Problems at the peripheral region
Moderate reduction
Run 7062
Leakage current is mostly generated at the periphery