## Slide 1: TPA-TCT A novel Transient-Current-Technique based on the Two Photon Absorption process 25th RD50 Workshop @ CERN
P. Castro1, M. Fernández1, J. González1, R. Jaramillo1, M. Moll2, R. Montero3, F. R. Palomo4, I. Vila1
1Instituto de Física de Cantabria (CSIC-UC)
2CERN
3Universidad del Pais Vasco (UPV-EHU)
4Universidad de Sevilla (US)

## Slide 2: Scope of this talk
Here, this talk focused on the experimental results from the first proof-of-concept measurement to study the TCT currents induced by TPA in an RD50-like non-irradiated standard PiN diode.
More details on the basics of the TPA process can be found in this talk by F.R. Palomo (link)
More details on the code TRACS (TRansient Current Simulator) used to compute the theoretical current waveforms in P. de Castro talk (link)

## Slide 3: Outline
Motivation and challenges for a TCT technique based on the Two- Photon- Absortion (TPA) process.
Femto-second laser setup:
  Signal size and shape vs. laser power.
  Determining the charge carriers generation volume.
Experimental data vs. simulation for a z-scan in a PiN diode.
Conclusions and outlook

## Slide 4: Motivation for a TPA-based TCT technique
TPA-TCT is a way to generate very localized electron-hole pairs in semiconductor devices (microscale volume).
TPA-TCT simplifies the arrangement to inject light into the device and the unfolding of the device internal Electric field and other relevant parameters of the theoretical model.
"A picture is worth a thousand words”
TPA-TCT could provide a novel experimental tool for studying the currently under development small pixel size detectors.

## Slide 5: TPA-TCT Proof-of-concept Challenges
Confirm the generation of TPA induced current in a silicon diode with the appropriate laser power.
Determine the dimensions of the charge-carrier’s generation volume.
Compare the experimental TCT current waveforms against the theoretical simulated current waveforms (access its potential as experimental tool to discriminate between different theoretical models).

## Slide 6: Experimental arrangement (1)
Laser
l  1300 nm
P  50-100 pJ
DT  240 fs
Rate  1 kHz
Df  11 nm
Microfocus
X100 Objective
f 100 mm lens
2.5 GHz DSO
OSC
AMP
SSA
&
FROG
OPA
IF
IA
VNDF
PD
CCD
L
FSW
RL
BS
BS
OBJ
TS
S
DO
DUT
TB
Sourcemeter
Pulsed femto laser (at normal incidence) entering the diode junction side (conventional top-TCT configuration)
FEMTO LASER
OPTICAL BENCH
READ OUT

## Slide 7: Experimental Arrangement (2)
DUT CNM N-IN-P DIODE
LGAD PIN REFERENCE DIODE
Ref - W9F9

## Slide 8: Evidence of TPA-TCT (1)
Z-Scan: vertical displacement of the DIODE perpendicularly to the laser beam (z axis)
Diode
Displacement
TPA -> Charge vs z -> plateau (Observed behavior)
SPA (Standard TCT) -> Charge vs z -> no z dependence.
80 x nindex_Si  280 um

## Slide 9: Evidence of TPA-TCT (2)
Pure quadratic dependence between the Signal Charge and the laser power.

## Slide 10: Which is the adequate laser power ?
Similar pulse shapes for laser pulses up to a power of 60-80 pJ, for higher power values TCT waveform gets wider and wider (likely due to plasma effects).
Seconds
35 pJ
47pJ
59 pJ
82 pJ
147 pJ
223 pJ

## Slide 11: TPA-TCT Proof-of-concept Challenges
Confirm the generation of TPA induced current in a silicon diode with the appropriate laser power.
Determine the dimensions of the charge-carrier’s generation volume.
Compare the experimental TCT current waveforms against the theoretical simulated current waveforms (assess its potential as experimental tool to discriminate between different theoretical models).

## Slide 12: TPA-Induced charge-carriers volume
The laser’s volume of excitation ( e-h pair creation) is fully determined by the laser parameters (l and W0) and the TPA cross-section in Silicon (b)
In our case, l and b are known, a fit of the raising edge of the charge z-scan profile determines W0
beam waist from the fit
w0 = 0.95±0.05 um

## Slide 13: TPA-Induced Charge-carriers volume (2)
Simulation
Simulation

## Slide 14: TPA-TCT Proof-of-concept Challenges
Confirm the generation of TPA induced current in a silicon diode with the appropriate laser power.
Determine the dimensions of the charge-carrier’s generation volume.
Compare the experimental TCT current waveforms against the theoretical simulated current waveforms (assess its potential as experimental tool to discriminate between different theoretical models).

## Slide 15: TCT Waveforms: 20um focus depth
NOT a fit just a simulation normalization
Single Photon Absorption red laser TOP-TCT (hole injection)
CNM N-IN-P DIODE
LGAD PIN REFERENCE DIODE
Ref - W9F9 (500 V bias)

## Slide 16: TCT Waveform: 97 um focus depth
Electrons and holes TCT current contribution distinct from the TCT current shape.
NOT a fit just a simulation normalization
CNM N-IN-P DIODE
LGAD PIN REFERENCE DIODE
Ref - W9F9 (500 V bias)

## Slide 17: TCT Waveform: focus depth 160um
Around the minimal pulse width, similar arrival times for electrons and holes
CNM N-IN-P DIODE
LGAD PIN REFERENCE DIODE
Ref - W9F9 (500 V bias)

## Slide 18: TCT Waveform: focus depth 237um
TCT wavefrom gets wider again, trailing edge dominated by electrons now.
CNM N-IN-P DIODE
LGAD PIN REFERENCE DIODE
Ref - W9F9 (500 V bias)

## Slide 19: TCT Waveform: focus depth 278um
SPA - red laser bottom-TCT like signal (electron injection)
CNM N-IN-P DIODE
LGAD PIN REFERENCE DIODE
Ref - W9F9 (500 V bias)

## Slide 20: TPA-TCT: Distinct Electron & Hole dynamics
Out of the box simulation (no fit): 500 V, RC 17pC, Laser waist 0.95 um, Vdep 50 Volts
Excellent agreement between data (left) and TRACS simulation.
Holes
Electrons
junction
Ohmic contact

## Slide 21: TPA-TCT Proof-of-concept Challenges
Confirm the generation of TPA induced current in a silicon diode with the appropriate laser power.
Determine the dimensions of the charge-carrier’s generation volume.
Compare the experimental TCT current waveforms against the theoretical simulated current waveforms (assess its potential as experimental tool to discriminate between different theoretical models).

## Slide 22: Conclusions and Outlook
We have completed the successful proof-of-concept of a novel Transient-Current-Technique based on the Two-Photon-Absortion (TPA) process
Excellent agreement between the experimental data and the simulation points to its potential as tool for disentangling different theoretical models.
Opens up the possibility of a new range of opportunities for boosting the scope of TCT techniques:
  More accurate 3D mapping of Efield.
  Simpler unfolding methods.
  More accurate study of pixelated sensors.
  Less relevance of metal-induced beam reflections.
But, still a lot of work and challenges ahead to make it a reliable, accessible and practical diagnostic tool.

## Slide 23: THANK YOU !

## Slide 24: Generation Volume (knife-scan)
Diode
Displacement
Laser waist < than 1 um (accuracy limited by motor displacement resolution)