## Slide 1: Laboratory performance and industrial quality: Pump diodes for High-Energy Lasers
Speaker Martin Wölz

## Slide 2: Outline
JENOPTIK AG
Research-to-industry transfer: Diode Lab GmbH
Laser diodes for HEC-DPSSL
Laser diode stacks
Outlook: mass production

## Slide 3: JENOPTIK AG History
Ernst Abbe Innovator and reformer; in 1867 scientific director of and in 1875 partner in the Zeiss workshop
Carl Zeiss University mechanic and entrepreneur; founded the workshop for precision mechanics and optics in Jena in 1846
1945/46: Transfer of patents and dismantling of parts of the company by the U.S. and Soviet armies.
1946: A new Zeiss Company is founded in Oberkochen.
The Zeiss plant in Jena, East Germany, is converted into state property.
Carl Zeiss Jena GmbH gives rise to the creation of Jenoptik GmbH.
  17,000 employees are dismissed
  Demolition, renovation and development of former Zeiss production sites
1991
1996/1998
In 1996 Jenoptik GmbH was converted into a joint stock corporation.
Going public: June 16, 1998
1945 - 1948
1846/1866
Notes: 3

## Slide 4: JENOPTIK AG Divisions and Business Units
Optical Systems
Industrial Metrology
Traffic Solutions
Defense & Civil Systems
Corporate Center
Optics
Micro Optics
Optoelectronic Systems
Roughness and contour measurement
Form measurement
Dimensional measurement
Equipment
Service Providing
Mechatronics
Sensor Systems
Corporate Center
Lasers & Material Processing
Lasers
Laser Processing Systems
Key Figures 2013
 | Sales (M€) | EBIT (M€) | Employees
Jenoptik Group | 600.3 | 52.7 | 3433
Lasers & Optical Systems | 224.7 | 24.6 | 1391

## Slide 5: JENOPTIK Division: Lasers & Material Processing Business Unit: Lasers
Lasers
Laser Processing Systems
Epitaxy
Mounting
Processing
JENOPTIK Diode Lab GmbH
Berlin
Notes: 5

## Slide 6: Introduction Semiconductor laser diode bar
Diode laser
fill factor = emitter width / pitch
Notes: 1) beam divergence:
slow axis – lateral / fast axis – vertical
2) fill factor
Herstellung:
  Großserienproduktion
  Methoden und Geräten der Siliziumtechnologie (Speicher- und Prozessorproduktion)
  Hoher Automatisierungsgrad
  Geringer Personalaufwand
  Hoher F&E Aufwand
  Umfangreiches technologisches „Know-How“ notwendig
  Hochtechnologie - Produkt

## Slide 7: Outline
JENOPTIK AG
Research-to-industry transfer: JENOPTIK Diode Lab GmbH
Laser diodes for HEC-DPSSL
Laser diode stacks
Outlook: mass production

## Slide 8: Research-to-industry transfer JENOPTIK Diode Lab GmbH
1997 Joint diode laser development
2002 Formation of JENOPTIK Diode Lab GmbH - transfer research results into production - employees from FBH join new company - FBH shares clean-room facilities
2004 8 types of high-power diode lasers qualified for production decision to build independent production facility
2006 20 employees
2007 Start of production
2009 Acquisition of TES AG epitaxial services
2014 47 employees
leader in laser diode development
JENOPTIK Laserdiode GmbH
experienced in LD packaging,
test and qualification
Public projects
BRIMO
HEMILAS
Recruiting
Development contracting
Notes: aus Vortrag 12.1.2010
  Zusammenarbeit FBH – JENOPTIK AG seit 1997
    Ferdinand-Braun-Institut: Dem weltweit führenden Institut auf dem Gebiet der Laserdioden – Entwicklung
    JO Laserdiode GmbH: Eine Firma mit exzellenter Erfahrung in der Montage, Test und Qualifikation von Hochleistungs-Laserdioden
    Ergebnis: Entwicklungsmuster mit hervorragenden Eigenschaften
  2002: Entscheidung der JENOPTIK AG zur Gründung einer eigenen Firma:
    Ziel: Weiterentwicklung der Forschungsmuster zu Produkten
    Februar 2002: Gründung der JENOPTIK Diode Lab GmbH
Von 2002 bis 2004: Produktentwicklung
  Enge Zusammenarbeit mit FBH und der JENOPTIK Laserdiode GmbH
  Nutzung des Reinraum und der technologischen Ausrüstung des FBH in 2 Schichten
  Mit unseren eigenen Mitarbeitern (aus Industrie und FBH)
  Mit unserem eigenen technologischen Equipment für kritische Prozess-Schritte
  Erfolgreicher Abschluss der Produktentwicklung und Qualifizierung von 8 verschiedenen Typen von Hochleistungs- Laserdioden
2004 Entscheidung zum Aufbau einer eigenen Fertigungsstätte
2005 Entscheidung zur Standortwahl zu Gunsten des WISTA-Standortes
2007 Fertigungsaufnahme in neuer Fertigungsstätte
2009 Kauf und Integration des Zulieferers TES AG

## Slide 9: Epitaxy Capabilities at JDL
9
    Two multiwafer planetary reactors
        12 x 3" or 4"
        8 x 3" or 4"
    Layer characterisation: HRXRD, C-V profiling, EL, PL, SEM, (SIMS)
    Foundry services
    Certified to ISO 9001:2008

## Slide 10: Reproducibility Electro-optical characteristics
wafer-to-wafer wavelength reproducibility: better than 1 nm

## Slide 11: Reproducibility Electro-optical characteristics
Stability over 2.5 years : σ slope ± 1 % σ Ith ± 3 %
808 nm, 50% FF, 1.5 mm
M. Zorn et al., Proc of SPIE 7918-27 (2011)

## Slide 12: Reproducibility Reliability
808nm, 50%, 2mm
27000 h min. lifetime (95% of devices degrade less than 20%)
45000 h MTTF
20% degradation limit

## Slide 13: Jenoptik Diode Lab GmbH (JDL) Semiconductors: Laser Bars & Single Emitters
Laser epitaxial structure design
InGaAlAsP / GaAs-Epitaxy (MOVPE)
GaAs-process line
Facet-Coating process
Single Emitter (SE) and Laser Bar
Wavelength: 760 nm – 1060 nm
Power range - Single emitter CW: 12 W - Bar CW: 200 W - Bar QCW: 500 W (QCW = Quasi Continuous Wave, pulsed operation)
Bare bar sale
laser diode bars
Notes: 13

## Slide 14: Outline
JENOPTIK AG
Research-to-industry transfer: Diode Lab GmbH
Laser diodes for HEC-DPSSL
Laser diode stacks
Outlook: mass production

## Slide 15: What can we do for high energy class lasers?
  Mason et al., 7th HEC-DPSSL Workshop (2012)
  Mercury design
  10 J, 10 Hz: DiPOLE prototype
    Yb:YAG 200K, 940nm, 1.2ms QCW
    40 kW pulse power from 192 bars
  100 J …
  Erlandson et al., Opt. Mater. Express 1, 1341 (2011)
  LIFE pump architecture
    200 J, 10 Hz: ELI Beamlines L3
    Nd:glass RT, 880 nm, 300µs QCW
    3.2 MW pulse power, ca. 10.000 bars
Increase the power density of QCW bars !
Notes: from HEC-DPSSL 2014
Today you have heard news about two projects than relied initially on laser bars from Jenoptik Diode Lab:
1) this morning Marco Hornung: POLARIS status (aktive 25er Stacks)
2) after lunch Klaus Ertel: DiPOLE status (passive 8er Stacks)

## Slide 16: JDL New generation QCW bars Reducing semiconductor “cost per Watt”
New chip generation (NG) vertical design
Targets
  increased Pop per chip area
  decreased “cost per Watt”
Vertical structure (epitaxy) designed by FBH: Pietrzak et al., Proc. of SPIE 896528 (2014)
  better carrier confinement  high internal efficiency ηi  higher Pop
  thick waveguide  narrow fast axis divergence
Chart: resonator length (mm)
| 0.6 | 1 | 1.5 | 2 | 3.5
QCW 75% NG | 500
QCW 75% | 300
CW 50% | 80 | 120 | 160
CW 30% | 40 | 50 | 80 | 120

## Slide 17: New generation quasi-CW 880 nm Bars (II) Better efficiency  reduced “cost / Watt”
phenomenological model (char. Temp.) Erbert et al., Top. Appl. Phys. 78, Springer (2000)
input parameters T0, T1
Chart: resonator length (mm)
| 1 | 1.5 | 2 | 2.5 | 3
100W | 0.056588 | 0.06979 | 0.055645 | 0.036785
300W | 0.03784 | 0.0645 | 0.0688 | 0.0645
500W | 0.006632 | 0.051832 | 0.0672 | 0.069912 | 0.066296
Notes: Pop ↗, L(ηmax) ↗

## Slide 18: New generation quasi-CW 880 nm Bars (II) Better efficiency  reduced “cost / Watt”
recall phenomenological model based on char. Temp.
input parameters T0, T1
new generation (NG) structure has efficiency maximum for smaller chip
Chart: resonator length (mm)
| 1 | 1.5 | 2 | 2.5 | 3
100W | 0.056588 | 0.06979 | 0.055645 | 0.036785
300W | 0.03784 | 0.0645 | 0.0688 | 0.0645
500W | 0.006632 | 0.051832 | 0.0672 | 0.069912 | 0.066296
100W NG | 0.10775 | 0.15961 | 0.14075 | 0.12284 | 0.10303
300W NG | 0.062324 | 0.14582 | 0.15945 | 0.15519 | 0.14497 | 0.13219
500W NG | 0.11428 | 0.14926 | 0.15913 | 0.15644 | 0.14837

## Slide 19: New generation quasi-CW 880 nm Bars (III) Power-voltage-current characteristic
Pop = 500 W
Iop = 450 A
Sop = 1.211.17 W/A
WPEmax = 59.5%
WPEop = 55%
75% FF, L=1.5 mm (37 Emitters, W = 190 µm)
JDL-BAB-75-37-880-TE-500-1.5

## Slide 20: New generation quasi-CW 880 nm Bars (IV) Far-field profiles
Measured at: I= 400A (300µs, 10ms, T=25°C)
Fast axis:
qFWHM = 20.5°
q95% = 47.0°
Slow axis:
qFWHM = 8.3°
q95% = 10.0°

## Slide 21: New generation quasi-CW 880 nm Bars (V) Lifetime test
device under test: JDL-BAB-75-37-880-TE-500-1.5 on microchannel cooler
conditions: 485A, 300µs, 100Hz (3% d.c.), 25°C
0.8 Gshots as of Oct, 2014, ongoing
Chart: Test time (h)
| 0 | 24 | 100 | 400 | 700 | 1300 | 1600
BT_000259 F3504-2 | 512.2475 | 508.487 | 510.373 | 505.4492 | 507.866 | 507.6705 | 504.9248
BT_000689 F3504-2 | 499.8096 | 497.3344 | 495.8448 | 491.453 | 492.0968 | 491.1644 | 488.021
BT_000312 F3504-2 | 506.84 | 505.5632 | 506.669 | 501.8984 | 500.4407 | 501.7967 | 503.8532
BT_000697 F3504-2 | 506.5208 | 496.024 | 487.647 | 488.483 | 489.8213 | 487.416 | 488.406
BT_000678 F3504-2 | 509.2 | 509.0735 | 510.4075 | 505.4036 | 502.373 | 504.6854 | 504.9248
BT_000631 F3504-2 | 508.3106 | 506.8742 | 507.9344 | 503.3335 | 504.1132 | 506.9882 | 500.0565
BC_1013101 F3504-2 | 511.0124 | 505.2658 | 502.5086 | 472.6944 | 488.494 | 487.0944 | 490.199
BC_1013652 F3504-2 | 516.054 | 514.329 | 512.6426 | 508.6526 | 511.856 | 509.576 | 509.519
BC_1013107 F3504-2 | 516.859 | 515.0765 | 512.995 | 509.2568 | 512.4944 | 510.3056 | 505.3336
BC_1013648 F3504-2 | 517.089 | 515.5365 | 513.9495 | 512.2322 | 510.0776 | 512.255 | 509.3366
BC_1013451 F3504-2 | 516.1805 | 512.369 | 510.8072 | 512.0042 | 510.3284 | 509.5532 | 510.0548
BC_1013111 F3504-2 | 516.5255 | 509.006 | 513.961 | 509.519 | 509.7014 | 506.4523 | 510.0776

## Slide 22: Outline
JENOPTIK AG
Research-to-industry transfer: Diode Lab GmbH
Laser diodes for HEC-DPSSL
Laser diode stacks
Outlook: mass production

## Slide 23: Diode Laser Stacks
  Used in direct applications, laser pumping, medical and research applications
  4 to 25 laser bars vertical 2 to 4 bars horizontal
  cw power per bar: 50 – 80 W l 808 nm 50 – 120 W l 9xx nm
  qcw power per bar: 100 – 300 W l 808 & 9xx nm
  Capacity: thousands p.a.
Features
Vertical Diode Laser Stacks
qcw Stacks
Horizontal Diode Laser Stacks
Notes: 23
23

## Slide 24
Passively cooled QCW laser diode stacks
CTE-matched
JenLas® QCW
QCW, quasi continuous wave, pulsed operation, t ≈ ms
Semiconductor laser in stationary operation
Low duty cycle  thermal equilibrium not reached  high pulse power
New cost-efficient mounting technology
Flexible arrangement of laser emitters
Catalog product
Lab demonstrator

## Slide 25: Passively cooled laser diode stacks for pulsed operation
880 nm QCW bars
8 x in series
next generation JenLas® QCW stack technology
tp = 300µs
DC 1% 3% 6% 10%
Chart: 8x JDL-BAB-75-37-880-TE-500-1.5, tp=300µs, vary duty cycle
| 28.14 | 50.66 | 75.11 | 82.82 | 90.1 | 97.4 | 104.6 | 111.78 | 124.47 | 149.06 | 173.67 | 198.29 | 222.43 | 246.62 | 273.63 | 302.08999999999997 | 325.33 | 351.03 | 377.01 | 402.23 | 428.38 | 454.37 | 479.98 | 505.08
Leistung 1% | 4.7 | 105.8 | 324.8 | 397.8 | 464.8 | 529.8 | 595.8 | 662.8 | 774.8 | 994.8 | 1220.8 | 1450.8 | 1670.8 | 1890.8 | 2120.8 | 2330.8 | 2550.8 | 2780.8 | 3000.8 | 3210.8 | 3420.8 | 3640.8 | 3840.8 | 3990.8
Leistung 3% | 2.79 | 51.37 | 255.7 | 315.37 | 375.37 | 432.03 | 498.7 | 558.7 | 652.03 | 852.03 | 1048.7 | 1252.03 | 1448.7 | 1642.03 | 1835.37 | 2032.03 | 2222.03 | 2418.7 | 2605.37 | 2788.7 | 2972.03 | 3148.7 | 3322.03 | 3505.37
Leistung 6% | 3.17 | 47.3 | 91.13 | 133.47 | 174.8 | 214.8 | 256.47 | 451.47 | 643.13 | 841.47 | 1034.8 | 1231.47 | 1419.8 | 1604.8 | 1786.47 | 1969.8 | 2136.47 | 2319.8 | 2469.8 | 2619.8 | 2769.8 | 2903.13 | 3036.47 | 3153.13
Leistung 10% | 2.68 | 9.55 | 173.16 | 233.16 | 285.16 | 338.16 | 390.16 | 442.16 | 528.16 | 697.16 | 860.16 | 1022.16 | 1192.16 | 1342.16 | 1492.16 | 1622.16 | 1762.16 | 1872.16 | 1982.16 | 2072.16 | 2152.16 | 2192.16 | 2202.16 | 2152.16
Effizienz 1% | 0.013903 | 0.16952 | 0.34498 | 0.38111 | 0.40726 | 0.42722 | 0.44524 | 0.46122 | 0.48009 | 0.50636 | 0.52501 | 0.53794 | 0.54404 | 0.54712 | 0.54524 | 0.53577 | 0.53611 | 0.53432 | 0.53003 | 0.52558 | 0.5265 | 0.53013 | 0.50511 | 0.49898
Effizienz 3% | 0.0089102 | 0.091944 | 0.30123 | 0.33753 | 0.36736 | 0.38983 | 0.41408 | 0.43108 | 0.45318 | 0.48518 | 0.5065 | 0.51984 | 0.529 | 0.5353 | 0.53869 | 0.53958 | 0.53379 | 0.52905 | 0.52451 | 0.52029 | 0.51539 | 0.51058 | 0.5118 | 0.51669
Effizienz 6% | 0.01 | 0.083846 | 0.14645 | 0.19641 | 0.23593 | 0.2693 | 0.29834 | 0.39115 | 0.44324 | 0.47611 | 0.49482 | 0.50855 | 0.51559 | 0.52048 | 0.52212 | 0.51826 | 0.50894 | 0.50537 | 0.49679 | 0.48925 | 0.48146 | 0.47247 | 0.46866 | 0.46769
Effizienz 10% | 0.0091991 | 0.018458 | 0.22551 | 0.27285 | 0.30546 | 0.33376 | 0.35716 | 0.37614 | 0.40297 | 0.4389 | 0.46134 | 0.47401 | 0.48589 | 0.48857 | 0.48888 | 0.48499 | 0.48169 | 0.46555 | 0.45539 | 0.44192 | 0.42869 | 0.40931 | 0.38674
limit
thermal roll-over
operating point

## Slide 26: Outline
JENOPTIK AG
Research-to-industry transfer: Diode Lab GmbH
Laser diodes for HEC-DPSSL
Laser diode stacks
Outlook: mass production

## Slide 27: Outlook: mass production GaAs-based laser diodes
Laser confinement nuclear fusion schemes challenge laser diode supply world-wide
Lesson learned from red LED ramp-up: world-wide capacity can be doubled in two years if supported by demand (or by government programs)
Chart: year
| 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020
InGaAlP LED / year | 905625 | 905625 | 1207500 | 1207500 | 1690500 | 2113125 | 3622500 | 4528125 | 6037500 | 5735625 | 6218625 | 6762000 | 6339375
LIFE one-time demand | 454500 | 454500 | 454500 | 454500 | 454500 | 454500 | 454500 | 454500 | 454500 | 454500 | 454500 | 454500 | 454500
High-Power Laser capacity | 81000
HiPER one-time demand | 20250 | 20250 | 20250 | 20250 | 20250 | 20250 | 20250 | 20250 | 20250 | 20250 | 20250 | 20250 | 20250

## Slide 28: Summary
Jenoptik Diode Lab GmbH FBH spin-off development, production and bare bar sale
new 500W laser bars for QCW operation
next generation laser diode stacks
  JenLas® QCW
  standard layout available summer 2015
880 nm