## Slide 1: Xband accelerating structures review 24-25.11.2014
N. Catalan Lasheras

## Slide 2: Goals of the review
Describe/put together existing manufacturing steps
  Conditions, procedures, tests, etc.
Verify and agree on the procedures
Bring short term modifications
  To be implemented already in 2015
Propose longer term modifications, studies or R&D efforts
  There was not be time for discussing all in detail but we eleborated a list of potential directions to explore
  Work to be done in coordination with other CLIC-RF work packages

## Slide 3: Participants
31 participants including outside laboratories
D. Schulte, CERN/ABP
PH. Lebrun, S. Stapnes, CERN/DG
S. Atieh, A. Cherif, G. Favre, M. Garlache, A. Perez Fontenla, CERN/MME
M. Aicheler, O. Brunner, N. Catalan Lasheras, M. Filippova, A. Grudjev, D. Gudkov, S. Lebet, A. Olyudnin, C. Rossi, A. Solodko, I. Syratchev, J. Vainola, A. Xydou, B. Woolley, W. Wuensch, CERN/RF
M. Taborelli, M. Thiebert, CERN/VSC
F. Toral, L. Sanchez. Ciemat, Spain
T. Higo, T. Abe, KEK, Japan
M. Franzi, J. Weng, SLAC, USA
23 talks plus discussions
2 long days

## Slide 4: Program of the review
Introduction to the review. N. Catalan Lasheras
Manufacturing workflow and status of the procedures. A. Solodko
…..
Tolerances coming from alignment. D. Schulte
Tolerances coming from RF. A. Grudjev
Manufacturing for High-Gradient. W. Wuensch
Ultra precision machining and built to cost disk optimization. S. Atieh
How do we measure/accept the disks, shape. Roughness. A. Cherif
…..
Review of SLAC and KEK etching procedures. J. Wang
Current cleaning and etching procedures followed at CERN. M. Taborelli
Heat treatment study results, burrs and roughness. A. Perez Fontenla
Role of oxidation in bonding . M. Taborelli
…..
Assembly and alignment procedure. M. Aicheler
Cell to cell alignment on GLC structures. T. Higo
Brazing/bonding sequence. S. Lebet, A. Solodko
Bonding dependence from weight and roughness. A. Xydou
H2 diffusion bonding against vacuum brazing. T. Higo
…..
TD26CC plans from CIEMAT. L. Sanchez
MTF. M. Filippova
RF measurements and tuning. R. Wolf, B. Wooley
Baking requirements. M. Taborelli
Systematic analysis done on existing samples. A. Perez Fontenla
…..
Manifolds assembly. D. Gudkov
SiC to copper brazing. A. Solodko

## Slide 5: Baseline manufacturing flow
RF DESIGN
ENGINEERING DESIGN (3D models, 2D drawings)
QUALITY CONTROL AT FACTORY
CONFORM
NOT CONFORM
QUALITY CONTROL AT CERN
PRELIMINARY RF CHECK
LEAK TIGHTNESS TEST
RF CHECK AND TUNING
INSTALLATION
PACKAGING AND SHIPPING
BRAZING OF COUPLERS, TUNING STUDS, COOLING CIRCUITS
ULTRA PRECISION MACHINING
ASSEMBLY OF COUPLERS (brazing, machining)
DIFFUSION BONDING OF DISC STACK
BAKING
(vacuum 650 °C,
10 days)
RF DESIGN
ENGINEERING DESIGN (3D models, 2D drawings)
QUALITY CONTROL AT FACTORY
CONFORM
NOT CONFORM
QUALITY CONTROL AT CERN
PRELIMINARY RF CHECK
LEAK TIGHTNESS TEST
RF CHECK AND TUNING
INSTALLATION
PACKAGING AND SHIPPING
CLEANING
(LIGHT ETCHING)
Add a final dimensional control

## Slide 6: Requirements from luminosity. D. Schulte
See. N. Galindo Munoz talk
See A. Solodko talk

## Slide 7: Tolerances coming from RF. A. Grudjev
a
b
r
d
s
be
ae
l
e=ae/be
Sensitivity study for undamped cell.
Riccardo Zennaro, “Study of the machining and assembly tolerances for the CLIC accelerating structures”, EUROTeV-Report-2008-081, (2008)
Jiaru Shi, Alexej Grudiev, Walter Wuensch, “Tuning of X-band traveling-wave accelerating structures”, NIMA 704 (2013)
Sub micron precision is required if no tuning is applied and no temperature correction is allowed
Only systematic errors considered. Random errors being studied

## Slide 8: Conclusions from RF tolerances
Sensitivity studies hints to sub-micron accuracy
  Only systematic errors
  Damping waveguides to be considered
2B is the parameter most critical for input couplers
Tuning could correct 10 MHz but is not the baseline of CLIC.
  Prototypes need to be produced according to the baseline aiming at no tuning.
  Tuning will be used as a measure of accumulated errors and assembly quality
  eventual feedback to RF design and beam dynamics if not achievable.
We should try to correlate tuning to disk geometry. Action?
  Not all data available for all disks
  One attempt was done in the past without success. (EDMS1291907)
Stay at submicron tolerance in the shape
Study random manufacturing errors.
Systematic deformations?

## Slide 9: Taking shortcuts. W. Wuensch
High power breakdown behaviour of a pair of electrodes seems to be similar to that of an accelerating structure once the “appropriate” scaling laws are applied… work in progress
We could “judge” changes or improvements in the current procedure using sample electrodes.
surface treatment, cleaning, etching, degassing, etc

## Slide 10: Shape accuracy. S. Atieh
Not a problem. Well within reach in critical areas!

## Slide 11: Achieved Flatness. S. Atieh
  Seems to be ok for closed waveguide but not for open waveguide.
  Disks are saddle-shaped for open waveguides
2008
2009
2010
2011-2012

## Slide 12: Achieved Flatness II
  Outliers are measured in free state for damping waveguides
    Could come from the free-state requirement
Chart: 
Need to compare between free state and vacuum chuck and change specifications if necessary

## Slide 13: How do we measure/accept the disks? A. Cherif
Metrology and SEM analysis done only on spare disks
Parts arrival
Cleaning by TE/VSC
Temperature stabilization inside the laboratory
Program construction
Measuring setup
Tool calibration
Measurements
      Characteristics on the drawing
      Iris
      Cavity
      Flatness
      Concentricity
Roughness
      Mitutoyo
      Veeco
Results on EDMS

## Slide 14: How do we measure/accept the disks? A. Cherif
Lost of effort on reducing dimples by CMM
  Probe marks
From 4.7 to 0.08 um!

## Slide 15: Discussion on machining and acceptance
Some metrology needs to be done for all pieces including reference outside surface and shape.
Sharp edge. Machining sequence to be stated in the technical specs to chose the orientation of burrs. Action: Said.
Can we accept a larger roughness in the cell wall? Action: Alexej
Burrs, scratches, contamination and indents. How small can we visually detected 10-100um? Action: Andrej.
Flatness should be not relaxed but measurements checked.
  Measurements with the vacuum chuck to be compared with the “free state” Action Ahmed
Changing R05 to 1.0 or 2.5 to be studied Action: Alexej
Shall we tight the tolerance for OD to +/1um? And the shape?
Review disks conditioning

## Slide 16: Surface issues for RF structures in SLAC. J. Wang
Surface roughness after etching
Etching for removing slight contamination and fluids
Not justified for diamond-turned pieces

## Slide 17: Study of heat and chemical treatments effects on the surface of ultra-precision machined discs for CLIC. A. Perez Fontenla
  The presence of steps (µm) was confirmed in all discs, before and after etching; The discontinuity before etching is smaller on discs annealed for a longer time or higher T (nr 4 & 5);
Etching increases drastically roughness and is worse in low temperature samples
Burrs are removed by etching.

## Slide 18: Role of oxidation on bonding. M. Taborelli
Surface diffusion more important than bulk diffusion. H2 may speed up the process.
Oxidation reduces adhesion force.
Oxidation appears in less than an hour.
Unlike vacuum, heating in H2 will reduce oxidation
Beware of carbon contamination which will not be removed
1040 degrees will eliminate oxide in open surfaces. What about bonding surfaces?

## Slide 19: Discussion on surface treatment
No etching should be done on disks anymore.
  Only solvent cleaning.
  Thus no dimples should be allowed in the RF part larger than? Ra?
  Burrs and machining steps need to be under control
Test on oxide to be prepared. XPS measurements of oxide layer growth.
  Bonding cycle on oxidised samples to assess the bonding quality and the “deoxidising” capacity of the heating cycle. Action: Mauro, Serge.
Handling from the reception of the disks needs to be reviewed. Action Nuria
  Beware of Carbon contamination
Stress relieve temperature much lower than in SLAC, KEK and CIEMAT. Is this a concern? Action Said

## Slide 20: Assembly and alignment procedure. M. Aicheler
Manual stacking made against a UP machined V-block using tuning holes or machined line
Manual stacking against automatic stacking
Measured before and after bonding

## Slide 21: Cell to cell alignment on GLC structures. T. Higo
OD is the key for measurements need to be fully measured.
Stacked manually against a V-block.
Hold during transport to the oven.
Later used pre-bonding at low temperature ~150 degrees before releasing fixture

## Slide 22: Some (really) typical results
Cell to cell alignment < 1um
Smooth shape. Large bow
Bonding slippage < 1um
Very good cell to cell alignment.
Lots of measurement points
Bow can be easily corrected

## Slide 23: Discussion on bonding/brazing
Clear and detailed procedures for bonding/brazing
Bonding dependence on weight studies
  See A. Xydou presentation
Vacuum brazing used at lower frequency. Single cell study In KEK. Waiting for the results
No big changes in the procedure in the short term
  Could be worth to study different atmosphere in electrodes?
New smaller tooling to avoid leaving the cleanroom. Action Serge

## Slide 24: RF X-band previous projects @ CIEMAT
TBL PETS
Buncher
Microtron
Precision machining
Precision joining
Vacuum brazing
Precision assembly
Low power RF tests
Bead pull and tuning

## Slide 25
Plans for CLIC structures: TD26CC
Tuning at CERN
Disc machining
Parts machining
Bonding
Brazing
Leak testing
Assembly
CIEMAT will manufacture a TD26CC structure according CERN procedures
Scope of the collaboration

## Slide 26: New workflow steps. M. Filippova
Manufacturing Step Main Catalogue Data:
Applicable Standard EDMS document № where the corresponding step procedure is attached
Results  EDMS document № of the corresponding result report
Some step data fields to be implemented individually for some steps according to table 3, column “Manufacturing step catalogue data”.
Dimensional control
MTF. Maria Filippova

## Slide 27: Responsibilities
Write procedure
After each manufacturing step:
Close the MTF step
Attach result file
Open Non conformity in not ok
Define manufacturing sequence
Approve procedures
Coordinate between steps
Discuss and decide on NC actions

## Slide 28: RF measurements. B. Woolley, R.Wegner
4 Port VNA
TWS input ports
contact thermometer
TWS output ports
V-block
discs clamped together
clamping device
high-quality measurement cables
RF Measurements and Tunning. A. Olyunin, R. Wegner, B. Woolley

## Slide 29: Tuned structure and tuning record
RF Measurements and Tunning. A. Olyunin, R. Wegner, B. Woolley

## Slide 30: Discusion and Conclusions
Use the same pins for all structures.
Verify that tuning is preserved during manufacture
Need statistical study of tuning for all structures up to know
  To validate the CLIC baseline (no tuning)
  To evaluate the assembly quality,
No correlation found between tuning records and disks/cells geometry errors.
  Possibly most errors are produced by assembly
  TBC. Only one structure has been done.
  See A. DeGiovanni talk
RF Measurements and Tunning. A. Olyunin, R. Wegner, B. Woolley

## Slide 31: Baking requirements
H2
H2
Changes after 8h are only in 1e-10 of concentration!

## Slide 32: Degassing data from PSI structure

## Slide 33: Discussion on baking
According to simulations work 10 hours would be sufficient to eliminate H2 in the copper bulk.
  Sample is thin (1cm) and may not be representative?
Data from PSI structure seems to indicate that degassing is not that fast.
  Significant reduction after 12 hours
Refurbished degassing oven in building 101 has been equipped with gas analyser. Action Ivo
  Data to be taken on the next cycles. TD26CC on January
  With and without structure

## Slide 34: Manifolds assembly. D. Gudkov
+
Serge Lebet, Vadim Soldatov

## Slide 35: Alternatives to manifolds. Discussion
First of this kind in CLEX now.
TD24_SiC being manufactured slightly differently
Putting manifolds and SiC in vacuum tank could also be a possibility
Integrated disks
  Very accurate shape of the external reference is a bigger problem for these disks.
  First samples arrived
Study is under way
Waiting for TD24_SiC experience

## Slide 36: Needs for SiC to Cu joining
AS with damping material
RF GATE VALVE
Crack
Undergoing study by Igor and Anastasiya

## Slide 37: Conclusions
Procedures are now fully known and justified. Ongoing with the authors.
Industry-ready specs need to include a clear QA
Some conslusions and follow-ups
  Immediate changes, to be implemented from next year
  Follow-up items to be defined during the following months
  Long term studies
We make prototypes to prove CLIC baseline
  No compromises
  Conditioning is as important as hig gradient
Faster feedbak
  Changes that may impact bonding quality will be tested in simple disks in the oven.
  Changes that may impact high gradient will be first tested on electrodes
Larger and faster interaction with other work packages

## Slide 38
Thanks!