## Slide 1: PHIN Results
Christoph Hessler, Eric Chevallay, Steffen Doebert, Valentin Fedosseev, Irene Martini, Mikhail Martyanov
CLIC Workshop 2015, CERN
27.01.2015

## Slide 2: Motivation for a CLIC Drive-Beam Photoinjector
A conventional system (thermionic gun, sub-harmonic buncher, RF power sources) is not necessarily more reliable than a photoinjector. At CTF3 e.g. the availability of the CALIFES photoinjector is high.
With a photoinjector in general a better beam quality can be achieved than with a conventional system.
Conventional system (thermionic gun, sub-harmonic buncher) generates parasitic satellite pulses, which produce beam losses.
  Reduced system power efficiency
  Radiation issues
These problems can be avoided using a photoinjector, where only the needed electron bunches are produced with the needed time structure. → Has been demonstrated for the phase-coding in 2011.
M.Csatari Divall et al., “Fast phase switching within the bunch train of the PHIN photo-injector at CERN using fiber-optic modulators on the drive laser”, Nucl. Instr. And Meth. A 659 (2011) p. 1.

## Slide 3: Challenges for a CLIC Drive-Beam Photoinjector
Achieve long cathode lifetimes (>150 h) together with high bunch charge (8.4 nC) and high average current (30 mA)
Produce ultra-violet (UV) laser beam with high power and long train lengths (140 µs)
  UV beam degradation in long trains
  Thermal lensing and heat load effects?
High charge stability (<0,1%)
→ Vacuum improvement, new photoemissive materials, new cathode substrate surface treatment
→ Usage of Cs3Sb cathodes sensitive to green light → New UV conversion schemes with multiple crystals
→ Study the dynamics of laser system with full CLIC specs
→ Feedback stabilisation, new laser front end
Photocathode R&D
Laser R&D
Photoinjector optimization and beam studies

## Slide 4: Challenge to Verify Feasibility of Drive-Beam Photoinjector
CLIC requirements far beyond PHIN specs:
One PHIN run per year with 3 cathodes to test. → No statistics possible under these conditions!
Photocathode lifetime measurements require long measurement periods, which are in general not available to the extend as needed.
Different macro-pulse repetition rates: 0.8 – 5 Hz (PHIN) 50 Hz (CLIC)

## Slide 5: Recent R&D Activities at PHIN
Since a strong negative impact on vacuum level is expected for CLIC parameters, the vacuum level in PHIN has been improved and its impact on photocathode performance studied:
  Lifetime studies with Cs2Te cathode under improved vacuum conditions.
  Lifetime studies with Cs3Sb cathodes and green laser light under improved vacuum conditions.
Focus on Cs3Sb cathodes sensitive to green light:
  Lifetime measurements.
  RF lifetime measurements.
  Dark current studies.
Long-term measurement with Cs2Te under nominal operating conditions (2.3 nC, 1.2 µs)
Studies for AWAKE project:
  Emittance measurement with low intensity beam to investigate PHIN’s suitability for AWAKE.
  QE measurement of copper cathode for defining QE requirements for AWAKE.

## Slide 6: Improvement of Vacuum in PHIN
1/e lifetime 185 h
1 nC, 800 ns, l=524 nm, Cs3Sb
1/e lifetime 26 h
1 nC, 800 ns, l=262 nm, Cs3Sb
7e-10 mbar
1.3e-10 mbar
Dynamic vacuum level:
4e-9 mbar
Static vacuum level:
2.2e-10 mbar
March 2012
March 2011
Activation of NEG chamber around gun
Installation of additional NEG pump
<2e-10 mbar
2.4e-11 mbar
July 2013
1/e lifetime ?

## Slide 7: Photocathodes Used during PHIN Run 2014
Number | Material | Age | QE in DC gun | QE in PHIN
#198 | Cs2Te | New cathode, produced 05.03.2014 | 14.8% after production | ~10%
#199 | Cs3Sb | New cathode, produced 27.5.2014 | 5.2% after production | 4.9%
#200 | Cs3Sb | New cathode, produced 7.8.2014 | 5.5% after production | 3.9%
6A56 | Cu | Copper plug (Diamond powder polished) used for RF conditioning | 2e-4 after PHIN run | 3e-4
In 2014 the initial QE of Cs2Te and Cs3Sb cathodes in PHIN was in reasonable agreement with the measurements in the DC gun.
QE of Cu cathode was too high compared with best literature values (1.4e-4) . Maybe contaminated with Cs.
Test for
AWAKE

## Slide 8: Lifetime Measurement with Cs2Te Cathode
Under improved vacuum conditions:
Double exponential fit represents well the data
Lifetime similar to previous measurement.
Cs2Te is not ultra-sensitive against non-optimal vacuum conditions
Dynamic pressure: 3e-10 mbar 1.5e-9 mbar
2014
2011
2.3 nC, 350 ns, Cs2Te #185
2.3 nC, 350 ns, Cs2Te #198
t2 = 300 h

## Slide 9: Lifetime Measurement with Cs2Te Cathode
Under nominal operation conditions (2.3 nC, 1.2 µs)
Strong pressure increase. Heating of (uncooled) Faraday cup?
1/e lifetime still 55 h
2.3 nC, 1.2 µs, Cs2Te #198

## Slide 10: Lifetime Measurement with Cs3Sb Cathodes
Under improved vacuum conditions
Data can be partially fitted with a double exponential curve, with similar lifetime as 2012, however, measurement time is too short for reliable fit.
Klystron trip and phase jump changed slope drastically.
Dynamic pressure: 2.5 - 5e-10 mbar ~9e-10 mbar
2.3 nC, 350 ns, Cs3Sb #189
1/e lifetime 168 h
2.3 nC, 350 ns, Cs3Sb #199
2014
2012
t2 = 154 h

## Slide 11: Lifetime Measurement with Cs3Sb Cathodes
Under improved vacuum conditions:
Despite better vacuum level the lifetime is significantly shorter.
Strong QE decrease started after a phase jump.
Dynamic pressure: 2.3e-10 mbar
1/e lifetime 185 h
7e-10 mbar
1 nC, 800 ns, Cs3Sb #200
1 nC, 800 ns, Cs3Sb #189
2014
2012
t = 47.6 h

## Slide 12: Lifetime Dependence on Vacuum
Cs2Te yields better than Cs3Sb, but not drastically better.
Measurements with different beam parameters but similar vacuum conditions yielded similar lifetimes. → It seems that lifetime is mainly determined by vacuum level. But the vacuum level is also a function of beam parameters.

## Slide 13: RF Lifetime of Cs3Sb Cathodes
Fresh cathode
Cathode #200 (Cs3Sb)
Used cathode
Cathode #199 (Cs3Sb)
Fast and slow decay visible as during beam operation.
In both cases longer lifetimes as during beam operation.
Lower vacuum level than during beam operation.
Dynamic vacuum level: 2.5e-10 mbar
Dynamic vacuum level: 3e-10 mbar

## Slide 14: Dark Current Measurements
Field emission contribution from gun cavity (Cu) and cathode.
Cs3Sb cathodes (F~2 eV) produce higher dark current than Cs2Te (F~3.5 eV) and copper (F~4.5 eV). → Higher vacuum level for Cs3Sb than Cs2Te under same beam conditions.
The low dark current measured with copper confirms that the major contribution is coming from the cathode.

## Slide 15: Cathode Surface Studies
Surface analysis of photocathode materials with XPS and their impact on the cathode performance in collaboration with TE/VSC has started.
  New UHV carrier vessel was commissioned to transfer cathode from production laboratory to the XPS set-up:
  XPS measurement allows material characterization of the surface. Together with qualitative elemental composition also chemical and quantitative information can be obtained (not straightforward):
  Easy case: Cu (slightly oxidized)
  Complex case: Cs3Sb
Peaks overlap!
Courtesy Irene Martini

## Slide 16: Upgrade of Laser System
Installation of new 500 MHz fiber front end with CLIC specs for PHIN. Decoupling PHIN and CALIFES laser systems, but keeping the possibility to switch back to the old front end for PHIN.
Delivery of new front end delayed, but expected in the coming weeks.
Preparation work (re-arrangement of current laser system) has started.
Planned studies:
  Stability studies with new front end with improved stability.
  Studies of heat-load effects and thermal lensing in laser rods at 50 Hz rep rate.
  In parallel further studies on new harmonics generation schemes with multiple crystals to solve problem with UV generation for 140 µs long trains.

## Slide 17: Outlook: Plans and Ideas for PHIN
Cathode lifetime studies with 2.5 µs long pulse trains (double of nominal PHIN train length) and tentatively 5 Hz repetition rate: → “old” 1.5 GHz time structure needed for obtaining conclusive results. → Vacuum window needed. → Long and probably painful RF conditioning required. → Using Cs2Te cathodes.
Measurement of RF lifetime of Cs2Te cathode
Study of impact of the longer bunch spacing with new laser front end on the photocathode lifetime. → Measurements with 1.05 µs (=3*350 ns) and 2.3 nC with Cs2Te
Study of charge stability with the new laser system.
Study the effect of surface roughness on cathode lifetime (Electro-polished cathode plugs).
Study the performance of three components cathodes in PHIN (e.g. K2CsSb).
Re-measure QE of uncontaminated copper cathode for AWAKE.
 Many interesting ideas for a further PHIN run in 2015!

## Slide 18: Ideas for Future CLIC Photoinjector Developments
It is clear that this question cannot be answered alone by extrapolating from PHIN experiments.
To verify feasibility of photocathodes for CLIC specifications, at some point a RF gun with full CLIC specs must be built.
If the environment will be not suitable for standard photocathodes, are there any fundamentally new ideas which could potentially solve the problem?
The main concern about a CLIC drive beam photoinjector is: Will the high bunch charge and average current create conditions (e.g. vacuum level), which are deadly for the photocathode?

## Slide 19: Protective Layers for Photocathodes
Protective layer of alkali-halides (NaI, CsI, CsBr) can increase resistivity against oxidation:
Buzulutskov et al., Nucl. Instr. and Meth.
A 387 (1997) 176
Graphene (2D material, monolayer) as a chemically inert diffusion barrier to prevent oxidation:
Works for metals. Is it also suitable for photocathodes?
S. Chen et al., ACS Nano 5 (2011) 1321

## Slide 20: Diamond Photocathodes
Chemical stable photocathode
Survives air-exposure
High QE, however in the deep UV (<190 nm), not achievable with conventional laser sources.
A.S. Tremsin, O.H.W. Siegmund,
Diamond & Related Materials 14 (2005) 48–53
Potential solution (first proposed by H. Tomizawa et al (JASRI/SPring-8)): Z-polarized laser beam:
High Z-field (few GV/m) reduces work function due to Schottky effect.
Excitation with longer wavelength could be possible.
H. Tomizawa et al., Proc. LINAC2012, 996

## Slide 21: Diamond-Amplified Photocathodes
Concept developed at BNL: Diamond as a secondary electron emitter.
Due to robustness of diamond long lifetimes with high current seems to be reachable.
[1] X. Chang et al., PRL 105, 164801 (2010)
In test setup at BNL a 35% probability of electron emission from the hydrogenated diamond surface was measured with an emission gain of 40 [1].
However, slow charging of the diamond due to thermal ionization of surface states cancels the applied field within it. → Generation of long pulses might be problematic.
Complicated setup (DC and RF acceleration)

## Slide 22: Acknowledgement
Controls: Mark Butcher, Mathieu Donze, Alessandro Masi, Christophe Mitifiot
Beam instrumentation: Thibaut Lefevre, Stephane Burger
Vacuum: Berthold Jenninger, Esa Paju
RF: Stephane Curt, Luca Timeo
Wilfrid Farabolini
CTF3 operators
XPS studies: Holger Neupert, Valentin Nistor, Mauro Taborelli, Elise Usureau
Collaborators at LAL and IAP-RAS
… and many others
… and thank you for your attention!

## Slide 23
Backup Slides

## Slide 24: Layout of PHIN
FCT: Fast current transformer VM: Vacuum mirror SM: Steering magnet BPM: Beam position monitor MSM: Multi-slit Mask OTR: Optical transition radiation screen
MTV: Gated cameras SD: Segmented dump FC: Faraday cup

## Slide 25: PHIN and CLIC Parameters
Parameter | PHIN | CLIC
Charge / bunch (nC) | 2.3 | 8.4
Macro pulse length (μs) | 1.2 | 140
Bunch spacing (ns) | 0.66 | 2.0
Bunch rep. rate (GHz) | 1.5 | 0.5
Number of bunches / macro pulse | 1800 | 70000
Macro pulse rep. rate (Hz) | 5 | 50
Charge / macro pulse (μC) | 4.1 | 590
Beam current / macro pulse (A) | 3.4 | 4.2
Bunch length (ps) | 10 | 10
Charge stability | <0.25% | <0.1%
Cathode lifetime (h) at QE > 3% (Cs2Te) | >50 | >150
Norm. emittance (μm) | <25 | <100

## Slide 26: Photocathode Lifetime Studies 2013
Lifetime studies under improved vacuum conditions were already planned for 2013, however due to many problems no comparable lifetime measurement could be performed at that time.
Problems in 2013 among others: “unknown” beam instrumentation, low initial QE, fast QE decrease, QE jumps, 24h drifts.
Problems with photocathodes could be potentially traced back to a wrong surface finishing of the cathode substrates and have been solved in 2014.
Photocathode surface after usage

## Slide 27: Emittance Measurements for AWAKE
Laser beam size: ~ 1 mm sigma, charge 0.2, 0.7, 1.0 nC, energy 5.5 – 6 MeV
Normalized emittance for 0.2 nC: 3.2 mm mrad ( big errors !)
Charge dependence is roughly sqrt as it should be
En(0.2 nC): 3.2 mm mrad
En(0.7 nC): 4.6 mm mrad
En(1 nC): 5.5 mm mrad

## Slide 28: QE Measurement for AWAKE
Copper plug 6A56:
  QE(DC-gun) = 2e-4
  QE(PHIN) = 3e-4
QE of Cu cathode was too high compared with best literature values (1.4e-4).
Possible explanation: Contamination with Cs. The plug was located in photocathode preparation chamber during a bake-out.
Copper plug 6A46 has not been in preparation chamber during bake-out and has a QE (DC gun) = 3e-5.
It is planned to test 6A46 also in PHIN.