## Slide 1: Electro-Optic development for short bunch length monitoring
David Walsh, ASTeC
Steven Jamison, Edward Snedden,
Allan Gillespie, Thibaut Lefevre

## Slide 2: Outline of Talk
Requirement/Aims
EO Techniques
Our new technique: EO Transposition
System Design and Testing
  Predicting EOT signal level
  Status of EOT monitor construction
  EOT + FROG results!
Resolution (Materials)

## Slide 3: Requirement and Aims
CLIC project targets
Non-invasive
Single shot
Diagnostic target resolution ~20fs rms (Bunches ~150fs rms)
EO diagnostics: (encoding of Coulomb field into a laser field)
Advantages
Scales well with high beam energy
  Particle methods get impractical (size, beam dumps)
Non-destructive
  Bunches can still be used
  Live feedback
Challenges
Unreliability, maintenance and cost of suitable ultrashort pulse laser systems
Temporal resolution
We aim to improve on the resolution and the robustness of EO diagnostics

## Slide 4: Current EO Techniques
Coulomb field of relativistic bunch
probe laser
non-linear crystal
Standard Description
Coulomb field flattens transversely, and defines charge distribution
Pockels effect induces polarization ellipticity
Technique borrowed from THz electro-optic sampling where (tprobe << tTHz)
Spectral Decoding
Chirped optical input
Spectral readout
Uses time-wavelength relationship
~1ps
Temporal Decoding
Long pulse + ultrashort pulse as gate
Spatial readout (cross-correlator crystal)
Uses time-space relationship
~150fs

## Slide 5: Physics of EO Transposition
More Rigorous Description – nonlinear frequency mixing
S.P. Jamison Opt. Lett. v31 no.11 p1753
EOT pulse
t
E
Coulomb field
Optical field in
t
t
E
E
~50fs
Time Domain
Intensity
Intensity
ν
few mm
tens μm
820nm
Coulomb field
EOT spectrum
circa 20nm
Intensity
~820nm
Optical field
ν
ν
Frequency Domain

## Slide 6: Characterisation of Transposed Pulse
Considerations: * needs to be single shot
* autocorrelation not unambiguous – no shorter reference pulse available
* low pulse energy
Solution: Grenouille (frequency resolved optical gating), a standard and robust optical diagnostic.
Retrieves spectral intensity and phase from spectrally resolved autocorrelation.
=
Spectrum
Spectral Phase
The most sensitive “auto gating” measurement
Self-gating avoids timing issues (no need for a fs laser)
Requires minimum pulse energy of ~1 μJ
“Carrier” frequency
Can’t measure
What we want to know
<-Fourier->
Can be retrieved!
4.5 fs
pulse
Baltuska, Pshenichnikov, and Weirsma, J. Quant. Electron., 35, 459 (1999).

## Slide 7
Nanosecond
Laser System
Stretcher
Comp-
ressor
BBO
DIY
GRENOUILLE
Generation
1000x Amplification
(NCOPCPA)
Measurement
Coulomb field
GaP
¼λ plate
& polariser
Beam
dump
Beam
dump
Pulse Evolution
time
amplitude
nanosecond probe
“transposed pulse”
stretched
amplified
recompressed
532nm
10mJ
10ns
~800nm
10ns
1mJ
Nanosecond laser derived single frequency probe brings reliability
“Electro-Optic Transposition” of probe encodes temporal profile
Non-collinear optical parametric chirped pulse amplification (NCOPCPA) amplifies signal
Full spectral amplitude and phase measured via FROG
Coulomb field, and hence bunch profile, calculated via time-reversed propagation of pulse
EO Transposition System

## Slide 8: EOT System Build Status
Sirah Cobra Dye laser
6 ns, 3 mJ, linewidth < 2 GHz
Continuum Surelite YAG
~ 4.5 ns, 150 mJ, seeded
Jitter < 0.3 ns r.m.s.
M2 = 1.6
Primary laser systems finally delivered end of Nov 2014– Characterisation largely complete
All other components ready (except camera for FROG) and can now be integrated, characterised, and made robust
Dye laser not proposed for the final design – possibility of building a seeded OPO

## Slide 9: Characterisation of EO Transposition
Δν ~44GHz
Δ t ~10ps FWHM
Femtosecond laser-based test bed
Femtosecond laser pulse spectrally filtered to produce narrow bandwidth probe
Auston switch THz source mimics Coulomb field.
Well-characterised spectral and temporal profile.
Switchable diagnostics – Balanced sampling, Crossed Sampling, and Autocorrelation (spectrally resolved!)

## Slide 10: Experimental System
Balanced
detectors
Autocorrelator
Crossed
Polariser
And
Spectrometer
Pmt &
Lock-in
4-f filter
THz Source and interaction point

## Slide 11
Input pulses
Optical probe length Δt ~ 10 ps
Optical probe energy S ~ 28 nJ
THz field strength E ~ 132 kV/m
Leaking probe
| |2
Transposed Pulse Measurements
Spectral Measurement
Autocorrelation
(<0.5 nJ)

## Slide 12: Extrapolation to bunch parameters
Scaling factors
Pulse energy of ~15nJ is predicted.
1μJ required for the commercial single-shot FROG, “Grenouille”.
is the EO crystal length, is the nonlinear coefficient
CLIC Example:
Pulse energy 1mJ
Pulse duration 10ns
“Typical” nanosecond pulse
laser as probe
Coulomb field for target CLIC
bunch parameters (CDR)
Bunch length 44μm
Bunch charge 0.6pC
Property | Factor of improvement
 | x36
 | ÷1002
 | ÷22
 | x1862
Overall | x31
Property | Factor of improvement
 | x36
 | ÷1002
 | ÷22
 | x1862
Overall | x31
24.5 MV/m
100 kW
Method can be used to estimate applicability to other beams
– left as an exercise for the listener!
Total energy in EOT Pulse ~470pJ

## Slide 13: FROG Measurement
Delay
Frequency
Experimental Spectrogram
Recovered Spectrogram
0.55 ps pulse measured with a 10 ps, transform limited, probe!
PCO dicam pro
ICCD camera
256x frame integration
30x software averaging

## Slide 14: New THz Measurement Scheme
Delay (60 ps window)
This looks like a spectrogram!
(an absolute phase FROG!)
This is a FROG where both SFG and DFG mechanisms are present and spectrally overlap, a FROG algorithm was modified to account for this.
Essentially, the interference pattern between SFG and DFG in the trace reveals the absolute phase.
Theory extended to optical pulses
and is being published (on Arxiv now)
arXiv:1501.04864 [physics.optics]

## Slide 15: Temporal Resolution
EO transposition scheme is now limited by materials:
Phase matching and absorption bands in ZnTe/GaP.
Other materials are of interest, such as DAST or poled polymers, but there are questions over the lifetime in accelerator environments.
Collaborative effort with MAPS group at the University of Dundee on development of novel EO materials
Potential to produce an enhancement of nonlinear processes through metallic nanoparticles.
THz field induced second harmonic TFISH enhancement being investigated.
Surface nonlinear effects…
A key property of the EO Transposition scheme may be exploited
FROG (Grenouille) retrieves the spectral amplitude and phase
At frequencies away from absorptions etc. the spectrum should still be faithfully retrieved
Potential to run two, “tried and tested”, crystals with complementary response functions side by side to record FULL spectral information!

## Slide 16: Spectral Compositing of Multiple Crystals
Phasematching not the whole story
  Dips caused by absorption near phonons
  Phase distortion near absorptions become very large
  Distortions in c(2) near absorptions
Discard data around the absorption lines
Fill in the blanks with different crystals
(10 mm thicknesses)
Basic numerical study is promising.
Not yet demonstrated for THz…
(insufficient bandwidth)

## Slide 17
Thank you for your attention

## Slide 18: Chirped Pulse Optical Parametric Amplification
Very small Phase and Amplitude distortions can be calculated (and so can be removed)
Bandwidth very broad >50THz
Tested using stand-ins for pump and signal – picosecond laser system and Ti:Sapphire laser
Pulse spectrum maintained
Heavily attenuated
800nm, 50fs pulse
20mm BBO
θ = 23.81
α = 2.25
532nm, ~300MW/cm2
optic axis
θ
α
Photodiode or
Spectrometer
Gain of >1000x verified
Pump derived from 50ps pulse laser

## Slide 19
Time response & spectrum of field dependent on spatial position, R: dt ~ 2R/cg
 ultrafast time resolution needs close proximity to bunch
(N.B. equally true of CTR, CDR, Smith-Purcell, Electro-Optic, etc.)
Common Problem - Field at Source
20 fs
Field radiated or probed is related to Coulomb field near electron bunch
20fs electron bunches, 200fs separation, g =1000
High g is an advantage!
20fs resolution only obtainable
For >1GeV beams

## Slide 20
LATTE Lab
The Laboratory for
Laser, Terahertz and Terawatt Experiments
in accelerator applications
Lab overview
Longitudinal Profile Monitor CLIC-UK project
UV diagnostics and novel EO materials
TW laser system: to be commissioned. Output available in lab
High power, adjustable temporal profile and polarisation state THz sources >1 MV/m
Core laser sources (lockable to RF):
Ti:Sapphire - 81 MHz, <50 fs, 400 mW or 1 kHz, <50 fs, >1 mJ
OPA - 1 kHz, 570 nm to 12 µm, 1 µJ to 270µJ (λ dependent)

## Slide 21: Stretcher and Compressor Design
GVD = 5.6x106 fs2
Calculations indicate nanosecond
level jitter has negligible effect
Pulse | Properties | Peak Power
532nm Pump | 10mJ, 10ns Gaussian temporal profile | 1x106 W
800nm EO Transpostion Signal | Amplified signal energy > 1 μJ, ~50 fs | 20x106 W
As above but stretched GVD = 5.6x106 fs2 | > 1 μJ, ~310 ps | 3.2x103 W
>Pump! Not possible
Conjugate Stretcher and Compressor designs
1m
1m
0.5m
All gratings
G=1200 lines/mm
Θdeviation~15°
OK, will not distort