## Slide 1: MQXF Goals & Plans
G. Ambrosio
MQXF Conductor Review
November 5-6, 2014
CERN

## Slide 2: Outline
Scope
MQXF Main Requirements & Lengths
MQXF Main Design Features
Schedule
Strand overview
Cable overview
Past Experience
Agenda

## Slide 3: Scope
MQXF: new quads for ATLAS and CMS IRs
  Critical component for the High Luminosity LHC

## Slide 4: MQXF Main Requirements
140 T/m in 150 mm coil aperture
Q1/Q3 length: 8 m
Q2 length: 6.8 m
Max outer diameter: 630 mm
1.9 K operating temperature
Radiation strength: > 25 MGy (no problem for conductor)
Field quality: see next presentation
ATLAS
CMS

## Slide 5: MQXF Lengths
 | Short model | Q1/Q3 (half unit) | Q2
Magnetic length [m] | 1.2 | 4.0 | 6.8
“Good” field quality [m] | 0.5 | 3.3 | 6.1
Cable unit length per coil [m] | 150 | 450 | 710
Strand per coil [km] | 6.5 | 18.9 | 30

## Slide 6: MQXF Main Design Features
Same design for Q1/Q3 and Q2s:
Two-layer coils
  Without internal splice
  With one wedge per layer
Al shell structure preloaded by bladders and keys
  Segmented Al shell
Axial preload by tie-rods
Quench protection by active heaters
  and possibly CLIQ

## Slide 7: MQXF Schedule
Short model program: 5 CERN-LARP models, 2014-2016
  Coil fabrication started in 02-03/2014
  First magnet test (MQXFS1) in 07/2015 (3 LARP coils, 1 CERN coil)
Long prototype program: 2 (CERN) + 3 (LARP) models, 2015-2018
  Coil fabrication starts in 2015: 02 (LARP), 10 (CERN)
  First magnet test in 08/2016 (LARP) and 07/2017 (CERN)
Series production: 10 (CERN) + 10 (LARP) cold masses, 2018-2021
  Coil fabrication starts in 01/2018; First magnet test in 10/2019
  US-HiLumi contribution contingent on proven baseline by Jan/Mar 2016

## Slide 8: MQXFS Coils
MQXFS1 coils are in progress both by LARP and CERN:
MQXFS coil #2 by LARP
to be tested in mirror structure

## Slide 9: MQXF Strand - Overview (from CERN technical specification document)
0.85 mm strand
Filament size <50 μm
  OST 132/169: 48-50 μm
  Bruker PIT 192: 42 μm
Cu/Sc: 1.2  0.1  55% Cu
Critical current at 4.2 K and 15 T
  361 A at 15 T (632 A at 12 T)
Bruker PIT strand, 192
OST RRP strand, 132/169
US baseline: RRP 132/169
Based on ~20 yr. experience by CDP, LARP, Base Programs
The PIT conductor is back-up / alternative option
More details in Arup’s talk
CERN baseline: 50% RRP and 50% PIT
More details in Amalia’s talk

## Slide 10: MQXF Cable - Overview
40-strand cable
Mid thickness
  1.525 mm
  tolerance: +/- 0.010 mm
Width
  18.150 mm
  tolerance: +/- 0.050 mm
Keystone angle
  0.55 deg.
  tolerance: +/- 0.1 deg.
Pitch length
  109 mm
SS core 12 mm wide and 25 μm thick
Same baseline for Q1/Q3 and Q2s:
Coils with these cable parameters are being fabricated by CERN & LARP for the 1st short model (MQXFS1)
to be tested in Summer 2015
RRP cable

## Slide 11: Past Experience - Risk Reduction
Conductor and magnet parameters have been selected taking into account many years of conductor development and magnet R&D in the US and at CERN

## Slide 12
Overview of LARP Magnets
SQ
SM
TQS
LR
LQS
HQ
TQC

## Slide 13
High Field Quadrupole (HQ)
Goal: demonstrate all performance requirements for Nb3Sn IR Quads in the range of interest for HL-LHC (magnetic, mechanical, quench protection etc.)
Main design parameters and features in the latest models tested (HQ02a/b):
Conductor and cable | 
Strand diam. (mm) | 0.778
Cu/Sc | 1.2
No. strands | 35
Cable width (mm) | 14.8
Cable thickness (mm) | 1.375
Keystone angle (deg.) | 0.75
Short Sample Performance |  | 
Param. | 4.5K | 1.9K
Iss [kA] | 16.4 | 18.2
Bpk [T] | 12.9 | 14.2
Gss [T/m] | 186 | 205
Al shell
Coil
Bladder
locations
Alignment key
Iron yoke
Al
collar

## Slide 14
HQ02 Results
Accelerator Quality
Order of magnitude reduction of dynamic effects (ramp rate, field quality) with cable core
Quench performance
HQ02a: operational gradient (80% SSL) with no training
HQ02b: fast training to 95% level with 200 MPa pre-load
Quench protection
380K quench temperature without degradation
Successful first test of the CLIQ system in Nb3Sn
250K
320K
380K

## Slide 15
HQ02 RRR
Note: Coil #15 extracted strands showed RRR as low as 50
Coil #15
Coil #16
Coil #20
Coil #17

## Slide 16: Agenda
Start Time | Duration |  | Speaker(s)
9:00 | 0:20 | Welcome and review charge | Lucio/Apollinari
9:20 | 0:30 | MQXF goals and plans | Giorgio
9:50 | 0:30 | MQXF Design and Conductor Requirements | Paolo
10:20 | 0:30 | Mechanical stability and QXF coil winding | Paolo/Giorgio
10:50 | 0:20 | Coffee break | 
11:10 | 0:45 | Conductor Technical Specifications | Amalia/Arup
11:55 | 0:25 | MQXF RRP-Strand for Q1/Q3 | Arup
12:20 | 0:25 | MQXF RRP-Strand for Q2 | Bernardo
12:45 | 1:30 |  | 
14:15 | 0:30 | MQXF Cable for Q1/Q3 | Dan
14:45 | 0:30 | MQXF Cable for Q2 | Luc
15:15 | 0:25 | PIT Strand & Cable for Q2 | Amalia
15:40 | 0:30 | Lessons Learnt from CERN experience | Luc
16:10 | 0:20 | Coffee break | 
16:30 | 0:30 | Lessons Learnt from LARP experience | Arup/Dan
17:00 | 0:25 | US-HiLumi Conductor Procurement | Arup
17:25 | 0:25 | HiLumi Conductor Procurement | Amalia
17:50 | 1:00 | Closed Session | 
18:50 |  |  | 

## Slide 17: Agenda II
Start Time | Duration |  | Speaker(s)
9:00 | 0:20 | QA/QC plans for Q2 Strand | Bernardo
9:20 | 0:20 | QA/QC plans for Q2 Cable | Christian
9:40 | 0:40 | QA/QC plans for Q1/Q3 Conductor | Ian
10:20 | 0:15 | Coffee break | 
10:35 | 0:20 | Summary | Paolo/Giorgio
10:55 | 0:45 | Questions from Committee | 
11:40 | 1:00 | Closed session | 
12:40 | 1:30 |  | 
14:10 | 3:00 | Closed session | 
17:10 | 1:00 | Close-out | 
18:10 |  | ADJOURN | 

## Slide 18: Nomenclature
MQXF production magnet for HiLumi
MQXFS short model (a.k.a. SQXF)
MQXFL long prototype (a.k.a. LQXF)
TQ 90 mm short (1m) quadrupole
LQ 90 mm long (3m) quadrupole
HQ 120 mm short (1m) quadrupole

## Slide 19: Back up Slides

## Slide 20
HQ02b Quench Performance
Significant improvement of training rate above 15 kA, reaching 95% of 1.9K SSL
~230 A/quench
~30 A/quench
H. Bajas, G. Chlachidze, M. Martchevsky,
F.Borgnolutti, D. Cheng, H. Felice, et al.