## Slide 1: MQXF RRP® Strand for Q1/Q3
A. K. Ghosh
MQXF Conductor Review
November 5-6, 2014
CERN

## Slide 2: Outline
Introduction
RRP® Strand
RRP® 108/127 Strand for MQXFS1
  Design change for RRR Control
RRP® 132/169 MQXF strand
Present status of wire performance
  Comparison of vendor and LARP data on Ic
  Ic and RRR optimization
Strand Magnetization
Cable and Insulation
RRR of Extracted strand
Summary

## Slide 3: Introduction
The 1st Short model MQXFS1 magnet is using coils made with 108/127 strand.
Subsequent Short model and Long prototype MQXF magnets will use 132/169 design wire (smaller filament diameter)
For the MQXF Q1/Q3 Magnets we will most likely use RRP® wire from Oxford Superconducting Technology
Strand diameter 0.85 mm
  Ti-Ternary Nb3Sn
Cable is a 40- strand Rutherford Cable with stainless steel core

## Slide 4: RRP® strands with smaller filaments
  Smaller sub-elements can minimize flux jumps and improve stability.
  Filament Magnetization decreases
Smaller Filament Size
Courtesy of Jeff Parrell (OST)
169

## Slide 5: Sub-element (Filament) diameter Ds
Cu/Non-Cu=1.2 , 45.5% SC
R=Cu/Non-Cu=1.2 , 45.5% SC, 54.5 % Cu
0.85 mm strand with132 filaments has the same sub-element size as the 0.778 mm wire with 108 filaments that is used in HQ
Table of Sub-element diameter in mm

## Slide 6: Ti-Ternary 108/127 Strand Production
From prior experience we found that RRR is not well controlled in the “standard” RRP-wire. (details in a later presentation by A. Ghosh and D. Dietderich)
For the LARP order of 410 Kg which used 12 billets, OST introduced a small design change in the sub-element
  This production was used to resolve RRR control
  6 billets use standard Tin content (Nb/Sn ratio=3.4)
  6 billets use 5%-Reduced Tin content (Nb/Sn ratio=3.6)
Reduced Tin has significant impact on the RRR of the copper.
    Side-effect: Marginal decrease in Jc.
Piece lengths have been very good; some billets drew down in a single piece.

## Slide 7: MQXF Strand Specification
Process | RRP® or PIT Nb3Sn
Strand Diameter, mm | 0.850 ± .003
Ic(15 T) at 4.2 K, A | > 361
n-value | > 30
Ic(12 T) at 4.2 K, A (Reference Only) | (> 632 )
Ds, µm (sub-element diameter) | < 50
Cu : Non-Cu volume Ratio | 1.2 ± 0.1
RRR (after full reaction) | ≥ 150
Twist Pitch, mm | 19 ± 2
Twist Direction | Right-hand screw
Strand Spring Back, deg. | < 720
Magnetization Width at 3 T, 4.2 K, mT | < 300
Minimum Piece length, m | TBD for Q1/Q2/Q3

## Slide 8: Specification for MQXF Strand LARP-M-8007 Rev.0
132/169
Nb/Sn ratio > 3.4 to meet RRR
Jc(15 T) > 1400 A/mm2
Process | Ti-Ternary RRP® Nb3Sn
Strand Diameter, mm | 0.850 ± .003
Ic(15 T) at 4.2 K, A | > 361
n-value | > 30
Ds, µm (sub-element diameter) | < 50
Cu : Non-Cu volume Ratio | 1.2 ± 0.1
RRR (after full reaction) | ≥ 150
Twist Pitch, mm | 19 ± 2
Twist Direction | Right-hand screw
Strand Spring Back, deg. | < 720
Magnetization Width at 3 T, 4.2 K, mT | < 300
Minimum Piece length, m | 550
High temperature HT duration, h | ≥ 48

## Slide 9: RRP 132/169 strand for MQXF short model magnets
LARP had an existing PO of 255 Kg (~55 km) for 108/127 under specification LARP-M-8004-Rev. B
Contract was revised to change design to 132/169
Process | Ti-Ternary RRP® Nb3Sn
Strand Diameter, mm | 0.85 ± .003
Ic(15 T) at 4.2 K, A | > 361
Ic(12 T) at 4.2 K, A | > 684
n-value | > 30
Ds, µm (sub-element diameter) | < 60
Cu : Non-Cu volume Ratio | > 1.1
RRR (after full reaction) | ≥ 150
Twist Pitch, mm | 14 ± 2
Twist Direction | Right-hand screw
Minimum Piece length, m | 750
High temperature HT duration, h | ≥ 48
Exception:Ic(15 T) > 350 A

## Slide 10: RRP 132/169 strand for MQXF model magnets
LARP had an existing PO of 255 Kg (~55 km) for 108/127 under specification LARP-M-8004-Rev. B
  This was converted to 132/169- strand with “reduced-Sn”, using Nb Type-1.
  Exception to Ic (15 T) specification: 350 A (compared to 361 A)
  Strand qualified using HT schedule: 210C/48h + 400C/48h + 665C/50h
  9 billets were made
  Ic, RRR and Cu/non-Cu measurements made at OST for samples taken from the front-end and back-end of each billet.
  Ic and RRR measurements made at BNL using samples reacted with the same nominal HT schedule

## Slide 11: MQXF strand 132/169, “reduced-Sn”, OST data 210C/48h + 400C/48h + 665C/50h
Exception to LSL
UCL-Upper Control Limit
LCL – Lower control limit
LSL – Lower specification limit
AVG – Average
s – Std. Dev
Ic-AVG needs to be increased in production to meet LSL of 361 A

## Slide 12: RRR of the billets with the same HT
    RRR is well above specification minimum of 150
Average RRR | 315
± s | 32

## Slide 13: Cu/Non-Cu ratio
Average Cu/Non-Cu | 1.21
± s | 0.035

## Slide 14: Comparison of BNL and OST data
 | Ic(15T) BNL | Ic(15T) OST | Ic(12T) BNL | Ic(12T) OST | Ic(15T)_OST/ Ic(15T)_BNL | Ic(12T)_OST/ Ic(12T)_BNL | RRR BNL | RRR OST
Average | 374 | 370 | 692 | 687 | 99.0% | 99.3% | 288 | 315
s | 15 | 15 | 19 | 20 | 1.0% | 1.0% | 38 | 32
H, T | Ic_OST | Ic_BNL | n_OST | n_BNL
11.0 |  | 819 |  | 52
12.0 | 681 | 678 | 50 | 46
13.0 | 557 | 558 | 48 | 46
14.0 | 447 | 450 | 46 | 41
15.0 | 352 | 355 | 44 | 35
16.0 | 269 |  | 34 | 
OST and LARP measurements are very consistent
Samples were reacted and measured at each facility
Round Robin Test of samples reacted at BNL

## Slide 15: Optimizing 132/169 for MQXF
Specification Limits
    There is headroom in RRR to increase Ic by using longer times at 665 oC or slightly higher temperature 670 oC
    Or by adjusting the Nb/Sn ratio

## Slide 16: Longer times at 665 oC
665 C | 50 h | 100 h
Average, A | 374 | 388
s, A | 17 | 17
3.7 % Increase in Ic

## Slide 17: Magnetization of MQXF 132/169
ΔM = 238 mT at 3 T, 1.9 K
ΔM expected to be ~ 200 mT at 3 T, 4.5 K
X. Wang
Measurements performed at OSU
By M. Sumption and X. Xu
ΔM

## Slide 18: Magnetization of 0.85 mm,108/127 and 132/169 at 1.9 K
Magnetization scales with filament diameter
108/127 Scaled by 89%
Strands have same Jc and Cu/Non-Cu ratio
X. Wang
Measurements performed at OSU
By M. Sumption and X. Xu

## Slide 19: Cable Insulation at LARP
Insulation is braided directly on cable
  New England Wire Technology (NEWT)
Using S-2® glass (from AGY) with 933 Silane sizing
  48 carriers
  2 ply yarn, twist pitch 75 mm
Several lengths of QXF cable has been insulated
  Using braiding parameters to yield target specification of 0.145  0.005 mm thickness
  10-stack measurements at 5 MPa are used to determine insulation thickness
  Thickness can be readily adjusted to meet any change to present specification.
Each Cable length ~ 170 m | Measurement at 5 MPa |  | 
~170 m | mm |  | 
Cable ID | Ist Cycle | 2nd Cycle | 3rd Cycle
1050Z | 0.142 | 0.140 | 0.140
1051Z | 0.143 | 0.140 | 0.138
1053Z | 0.154 | 0.149 | 0.147
1055Z | 0.148 | 0.145 | 0.143
1057Z-A | 0.149 | 0.146 | 0.145
1057Z-B | 0.149 | 0.146 | 0.145

## Slide 20: Summary
The “reduced-Sn” design change increases RRR manufacturing margin with minimal loss of Jc.
  Implemented for all billets in process and future procurements.
RRP® 132/169 wire can meet strand specs
  Manufacturing margin in Ic needs to be increased by good control of the Nb/Sn ratio, and by reaction optimization
LARP plan implements 132/169-strand in MQXFS2 magnet and all MQXFL prototypes.
Strand procurement has been planned to meet cable manufacture and coil winding schedule. (Later Presentation)
Specification and Production QA plan and documents is being finalized this fiscal year for pre-production lots and preparing for issuing call for RFP(Request For Proposal) for the production.

## Slide 21
End of Presentation