## Slide 1: Conductor Technical Specification
Ballarino, B. Bordini, L. Oberli (CERN)
A. Ghosh (LBNL)
HL-LHC/LARP International Review of
Superconducting Cable for the
HL-LHC Inner Triplets Quadrupoles (MQXF)
Ballarino
5th November 2014

## Slide 2
Introduction
Functional specification that defines wire performance and qualification tests to be performed at the contractor’s premises
  CERN specification addressed to two manufacturers (OST, USA and Bruker EAS, Germany). Two different technologies of Nb3Sn wire procured (RRP and PIT)
  LARP specification addressed to one manufacturer
  (OST, USA). RRP wire procured

## Slide 3
Functional Specification document independent on wire technology
Layout of wire proposed by the company
No changes in wire layout after start of wire production – formal approval requested
Introduction

## Slide 4
Strand Diameter | mm | 0.850 ± 0.003
Ic(15 T) at 4.2 K | A | > 361
n-value | - | > 30
Ic(12 T) at 4.2 K, A (Reference Only) | A | (> 632 )
Ds (sub-element/filament diameter) | m | < 50
Cu : Non-Cu volume Ratio |  | 
min | - | 1.1
max | - | 1.3
RRR (after full reaction) | - | > 150
Twist Pitch | mm | 19 ± 2
Twist Direction | - | Right-hand screw
Strand Spring Back, deg. |  | < 720
Magnetization Width at 3 T, 1.9 K | mT | < 330
Minimum Piece length | m | 800 m for Q2
 |  | 500 m Q1 and Q3
Nb3Sn wire Characteristics and Performance

## Slide 5
Strand Diameter | mm | 0.850 ± 0.003
Ic(15 T) at 4.2 K | A | > 361
n-value | - | > 30
Ic(12 T) at 4.2 K, A (Reference Only) | A | (> 632 )
Ds (sub-element/filament diameter) | m | < 50
Cu : Non-Cu volume Ratio |  | 
min | - | 1.1
max | - | 1.3
RRR (after full reaction) | - | > 150
Twist Pitch | mm | 19 ± 2
Twist Direction | - | Right-hand screw
Strand Spring Back, deg. |  | < 720
Magnetization Width at 3 T, 1.9 K | mT | < 330
Minimum Piece length | m | 800 m for Q2
 |  | 500 m for Q1 and Q3
Nb3Sn wire Characteristics and Performance
1)
1) Selected with magnet designers on the basis of past experience

## Slide 6
Chart: Peak Field, (T)
| 16 | 15 | 14 | 13.37547011764706 | 12.44771423529412 | 11.52663470588235 | 10.615071470588241
Ic(1.9 K) | 444.2067 | 549.7223 | 671.6633 | 757.1657 | 899.1648 | 1060.2963 | 1242.8806
Ic(4.22 K) | 280.7368 | 360.8317 | 454.6497 | 562.0554 | 685.7059 | 827.3926 | 989.6731
Ic(1.9 K) with 5% degradation | 421.9964 | 522.2362 | 638.0802 | 719.3074 | 854.2066 | 1007.2815 | 1180.7365
Magnet Load-Line | 0 | 436.5 | 488 | 531 | 585.7856
Magnet Operating Point | 436.5
Ic(4.22 K, 15 T)= 361 A | 360.8317
Magnet Critical Current @ 1.9 K | 542
 19 % Margin on the load line at 1.9 K
Iop_cable = 17460 A
Bpeak = 12.07 T
Nb3Sn for MQXH magnet

## Slide 7
Strand Diameter | mm | 0.850 ± .003
Ic(15 T) at 4.2 K | A | > 361
n-value | - | > 30
Ic(12 T) at 4.2 K, A (Reference Only) | A | (> 632 )
Ds (sub-element/filament diameter) | m | < 50
Cu : Non-Cu volume Ratio |  | 
min | - | 1.1
max | - | 1.3
RRR (after full reaction) | - | > 150
Twist Pitch | mm | 19 ± 2
Twist Direction | - | Right-hand screw
Strand Spring Back, deg. |  | < 720
Magnetization Width at 3 T, 1.9 K | mT | < 330
Minimum Piece length | m | 800 m for Q2
 |  | 500 m for Q1 and Q3
2)
2) Based on layout of procured conductor

## Slide 8
Chart: Applied Field, [T]
fil_PIT=41 m
fil_RRP=48 m
T = 1.9 K
Measurements by D. Richter, CERN
Magnetization of Nb3Sn wire
Ds < 50 m
RRP: 280 mT
Jc(4.2K)=2800 A/mm2

## Slide 9
Strand Diameter | mm | 0.850 ± .003
Ic(15 T) at 4.2 | A | > 361
n-value | - | > 30
Ic(12 T) at 4.2 K, A (Reference Only) | A | (> 632 )
Ds (sub-element/filament diameter) | m | < 50
Cu : Non-Cu volume Ratio |  | 
min | - | 1.1
max | - | 1.3
RRR (after full reaction) | - | > 150
Twist Pitch | mm | 19 ± 2
Twist Direction | - | Right-hand screw
Strand Spring Back, deg. |  | < 720
Magnetization Width at 3 T, 4.2 K | mT | < 300
Minimum Piece length | m | 800 m for Q2
 |  | 500 m for Q1 and Q3
3)
3) From conductor stability requirements (RRR > 100 on extracted strands)

## Slide 10
Conclusions
Common CERN/LARP performance specification agreed
with magnet designers
Specification used by CERN for the past procurement of
Nb3Sn strand for MQXF – see next presentations
Two wire layouts proposed by the wire manufacturers: RRP 132/169 (procured by CERN and by LARP) and PIT 192 (procured by CERN) – see next presentations