## Slide 2: Rad-hard warm magnets
P. Fessia, N. Mariani, A. Sanz Ull, D. Tommasini and the whole TE-MSC-MNC section
Presented by P. Fessia
Contributions on the LHC from
Fluka analysis: Francesco Cerutti, Anton Lechner, Eleftherios Skordis
Collimation input: Rodrick Bruce, Stefano Redaelli, Belen Maria Salvachua Ferrando, Elena Quaranta
MNC team: Paolo Fessia, N. Mariani, Pierre Alexandre Thonet, D. Tommasini
Power Converter: Hugues Thiesen
Optics: Massimo Giovannozzi
MME design office: L. Favre, T. Sahner
VSC: E. Page, N. Zelko
Magnetic Measurement team: M. Buzio

## Slide 3: LHC→HL-LHC→FCC
LHC
30-50 MGy
HL-LHC
250-300 MGy
FCC
Where ?

## Slide 4: LHC or re-acting

## Slide 5
Point 7
MQW: Magnet Quadrupole Warm
MBW: Magnet Bending Warm

## Slide 6: Identified Failure modes
Degradation of the insulation system due to radiation leading to inter turn short or shorts to ground
Degradation of the mechanical shimming performed with ambient temperature cured resins
Degradation of the insulation system due to radiation leading to inter turn short or shorts to ground
Remark magnet build with no coil on the mid plane and therefore out from the expected zone of highest losses

## Slide 7: Type of deposition map
Dose (MGy)
Normalization: 1.15 1016 p (30-50 fb-1 ).
Computations with E 6.5 TeV relaxed collimator settings
Dose (MGy)

## Slide 8: Radiation resistance dose estimation
Degradation of mechanical properties appears and it can be measured before degradation of electrical properties
But …
What is the effect of the insulation thickness on the degradation ?
We know that exposure to air during irradiation should make the larger the damage.
How much ?
Worth re-evalauting the correlation between electrical and mechanical properties degradation
Actions of the fillers on the radiation resistance
Results mechanical test of the irradiated used resin or similar one
Value of mechanical load in the insulation
Estimation of the level of resistance of the insulation system to radiation

## Slide 9: Point 3 and 7 coil magnet damage estimation
MQW | MBW
From 10 to 20 MGy | From 40 to 60 MGy
From 20 to 50 MGy | From 60 to 80 Mgy
Larger than 50 MGy | Larger than 80 MGy
IP 7
IP 3

## Slide 10: Preparing HL-LHC or acting

## Slide 11: MQW shielding

## Slide 13: MQW shielding effect on the coil
Normalization: 1.15 1016 p (50 fb-1 )
Beam 2
Beam 2
Reduction Factor 3 on most exposed magnet with the hardest spectra. It shadows 20 % the radiation on the following magnet
Reduction Factor 4 on less exposed magnet with the softer spectra.

## Slide 14: Point 3 and 7 coil magnet damage estimation with shielding green arrow installed LS1 yellow arrow foreseen for LS2
MQW | MBW
From 10 to 20 MGy | From 40 to 60 MGy
From 20 to 50 MGy | From 60 to 80 Mgy
Larger than 50 MGy | Larger than 80 MGy
IP 7
IP 3
R

## Slide 15: MQW Life Test to the HL-LHC era
Experimental activities:
Measure of coil-coil displacement to identify eventual mechanical degradation (12 positions)
Measure of Temperature evolution (20 positions)
Measure of coils longitudinal and transversal deformation (8 positions)
Electrical verification of the magnet at regular intervals with two complete certifications (at 50% and 100% of foreseen life cycle)
Coil-coil relative displacement
Estimation of mechanical induced damage on LHC Warm Quadrupoles
Temperature probes and strain gauges
Reproduction of electromagnetic induced stresses on coils, spacers and magnet’s frame to assess life expectation of installed magnets with respect to cyclic loads during LHC operations.
Work performed in collaboration with: CERN Mechanical Laboratory, CERN Polymer Laboratory and CERN Design Office.
Imposed load: 4 power cycles every LHC physics run, ~47’000 cycles expected up to HL-LHC era end.

## Slide 16: MQW Life Test: first results
Preliminary results up to 25’000 cycles (half of foreseen magnet’s life)
Chart: Strain Gauges S1a and S1b
| 42041 | 42042 | 42044 | 42052 | 42053 | 42054 | 42056 | 42057 | 42059 | 42060 | 42061 | 42062 | 42063 | 42065 | 42066 | 42067 | 42068 | 42069 | 42071 | 42072
S1a - Longitudinal Deformation | 3.968 | 3.671 | 3.662 | 3.263 | 3.564 | 3.665 | 3.993 | 3.416 | 3.472 | 3.594 | 3.294 | 3.443 | 3.616 | 3.772 | 3.462 | 3.905 | 3.98 | 3.534 | 3.535 | 3.737
S1b Transversal Deformation | 4.469 | 4.054 | 4.205 | 3.799 | 4.364 | 4.243 | 4.43 | 4.213 | 4.257 | 4.418 | 3.745 | 4.188 | 4.606 | 4.095 | 4.163 | 5.039 | 4.379 | 4.65 | 4.499 | 4.3
Chart: Displacement Sensor 67-C
| 42041 | 42042 | 42044
06-11/02/2015 | 0.00997 | 0.0102 | 0.01006
17-23/02/2015 | 0.01016 | 0.01016 | 0.01028 | 0.01002 | 0.01013
23-26/02/2015 | 0.01058 | 0.01015
26/02-04/03/2015 | 0.00983 | 0.00917 | 0.01021 | 0.0105 | 0.01092
04-10/03/2015 | 0.00961 | 0.01011 | 0.00948 | 0.00963 | 0.00985
67_C | 0.00997 | 0.0102 | 0.01006 | 0.01016 | 0.01016 | 0.01028 | 0.01002 | 0.01013 | 0.01058 | 0.01015 | 0.00983 | 0.00917 | 0.01021 | 0.0105 | 0.01092 | 0.00961 | 0.01011 | 0.00948 | 0.00963 | 0.00985
Very stable signal with few oscillations mostly due to T effect.
No influence of em fields or hysteresis effects.
Displacements constant since beginning of test.
Coils Strains giving regular and strong signal.
MQW 038 is well behaving through the endurance test, which is now prosecuting the road to 50’000 cycles (end of HL-LHC era)!

## Slide 17: MQW/MBW Coils Insulation Resins Characterization
Additional activities to predict the long term behaviour of the materials used for MQW (and MBW) magnets, including:
Mechanical tests,
Electrical tests,
Microstructural analysis…
All evaluated as a function of received dose (irradiation campaign under preparation)!
Flexural Tests plots courtesy of O. Sacristan De Frutos (CERN Mechanical Laboratory).
Fracture Surface of MQW coils insulation resin sample showing fibres detachment.
Metallographic sample of type E glass fibres embedded in MQW epoxy resin.

## Slide 18: FCC and HL-LHC development or pro-acting

## Slide 19
for HL-LHC and FCC
Know better
Know before
Known margin

## Slide 20: Know better: resin testing from present to future
Presently used insulations systems and new insulation systems

## Slide 21: Monitoring the health of the magnet: DS R&D
Displacement measured through “Home made CuBe beam based displacement sensors”, in the following DS.
DS are made of a CuBe plate, instrumented with strain gauges and mounted on a support structure in 3D printed polymer.
The DS is then calibrated and inserted inside the magnet along the interstitials between coils up to 1.5 m depth.
Final accuracy achieved ~0.5 microns for excursions of ~4 mm.
 The technology can be implemented in different situations by ad hoc designs of the main body and of the CuBe plate geometry…
High demanding requirements:
High precision and reproducibility over a long number of cycles;
No influence from Temperature and EM fields;
Capable to slide in the small interstitial between MQW coils, adapting to irregular surfaces and locations…
Strain gauges
3D printed body
CuBe plate
Measuring pins
Final sensor inserted between coils 6-7
30 mm

## Slide 22: Know margin: rad hard insulation schemes
22
Hitachi cables used in KEK & PSI: square shape, Cu cladding, different dimensions available. [1]
ITER cables: round shape, tailored design for different machine areas.[2]
Possible schemes
Non organic insulations
Organic insulations
Cyanate Esther compounds
E glass fibre
S glass fibre
High radiation hard epoxy with mica

## Slide 23: Known margin: the whole magnet
mechanical systems to allow fast or remote handling, alignment, connection and disconnection.
for reliable, radiation hard, fast electrical fittings, compatible with remote handling
reliable, radiation hard, fast hydraulic fittings, compatible with remote handling

## Slide 24: Plug in magnet for tunnel installation

## Slide 25: Conclusion
The development of rad-hard magnets for FCC is a continuum of the LHC Consolidation program and of the HL-LHC development program. The Three projects are synergic and build one on the other
A rad hard coils does not mean a rad hard magnet: electrical connection, hydraulic connections and manipulation have to be intimately integrated to provide an homogenous product. CERN needs partners in order to develop the adequate answers in the different fields