## Slide 1
BINP
Cold test stands
for cryogenic beam vacuum Qualification
Alexander Krasnov
Budker Institute of Nuclear Physics (BINP), Novosibirsk, Russia
E-mail address: a.a.krasnov@inp.nsk.su
FCC week, Washington 25.03.2015

## Slide 2
BINP
a.a.krasnov@inp.nsk.su
- Motivations
- Historical tour: measurements made at BINP for SSC and LHS cold beam vacuum
- What we have to know else
- Parameters of perspective SR beam lines at BINP for vacuum cold stands
- SEY measurements in presence of strong magnetic field
FCC week, Washington 25.03.2015

## Slide 3
BINP
a.a.krasnov@inp.nsk.su
FCC hh
1E14 eV
2E-4 eV
T=2K, High field superconducting magnets
FCC energy scale
1E-2 eV
Condensation energy of hydrogen
1 eV
Binding energy of atoms in molecules
1E4 eV
Synchrotron radiation,
Electrons in e-clouds
FCC week, Washington 25.03.2015

## Slide 4
BINP
a.a.krasnov@inp.nsk.su
Initial surface condition
after pumping at RT down to 1e-4 ÷ 1e-5 Torr :
30 ÷ 100 ML of
Chemically bound: MxOy, Mx(OH)y, Mx(HOC3)y, carbon clusters
Physically adsorbed: H2O, organics
SR provoke dissociation of the molecules.
Note 1: Evaporating 0.1% of 1ML cause gas density increase on 100 time more of acceptable level!
Note 2: Life time of Physically adsorbed molecules on a surface can by evaluated from Frenkel equation:
FCC week, Washington 25.03.2015

## Slide 5
BINP
a.a.krasnov@inp.nsk.su
Ec = 20 ÷ 500 eV (SSC – 300 eV, LHC – 46 eV,
First SR beam lines at BINP for cold vacuum tests
FCC week, Washington 25.03.2015

## Slide 6
BINP
a.a.krasnov@inp.nsk.su
Stand for testing of prototype chambers for SSC cold beam vacuum
FCC week, Washington 25.03.2015

## Slide 7
BINP
a.a.krasnov@inp.nsk.su
H2 dynamic pressure vs photon dose
100 h
T=1.9K
ID=50mm
39mm
Beam screen
T=5
¸
20K
OD=49mm
Cooling tubes
slots
He
He
Long term prognosis for CO, CO2, O2 ?
FCC week, Washington 25.03.2015

## Slide 8
BINP
a.a.krasnov@inp.nsk.su
One of prototype chamber with beam screen for LHC cold beam vacuum
Long term prognosis for CO, CO2, O2 ?
FCC week, Washington 25.03.2015

## Slide 9
BINP
a.a.krasnov@inp.nsk.su
One of first prototype chamber with beam screen for LHC cold beam vacuum
Long term prognosis for CO, CO2, O2 ?
FCC week, Washington 25.03.2015

## Slide 10
BINP
a.a.krasnov@inp.nsk.su
Dynamic pressure of H2 vs temperature inside simple tube with TiZrV getter film.
SR photon flux 4E10 ph/s, Ec=4.5 keV
·
5
0
1
0
0
1
5
0
2
0
0
2
5
0
3
0
0
T
e
m
p
e
r
a
t
u
r
e
[
K
]
1
E
-
1
2
1
E
-
1
1
1
E
-
1
0
P
2
[
Торр
]
FCC week, Washington 25.03.2015

## Slide 11
BINP
a.a.krasnov@inp.nsk.su
Installation for investigation photo-desorption of condensed gases
FCC week, Washington 25.03.2015

## Slide 12
BINP
a.a.krasnov@inp.nsk.su
Photo-desorption of condensed gases
FCC week, Washington 25.03.2015

## Slide 13
BINP
a.a.krasnov@inp.nsk.su
Indirect photon fluxes hitting of internal surface was decreased by a factor of 4 at least
Two benefits:
0.02÷0.03
0.5
SR
Slots
Electron cloud consideration
(started too late)
Decreasing of photoelectrons contribution in e-clouds from roughly 20% to 5%
Mitigation of recycling of condensed molecules: helps for surface conditioning
FCC week, Washington 25.03.2015

## Slide 14
BINP
a.a.krasnov@inp.nsk.su
Electron cloud consideration
A thermo-cycling might be needed
T=1.9K
ID=50mm
Screen for e-cloud
p+
Slots
Cooling tubes
T=5
¸
20K
OD=49mm
Saw tooth
γ
γd
e-
e-ph
e-
FCC week, Washington 25.03.2015

## Slide 15
BINP
a.a.krasnov@inp.nsk.su
What we have to investigate by testing of FCC cold beam chamber prototypes:
First stage
Dynamic pressure in presence of SR (Ec up to 4.5 keV) in temperature range 40 ÷ 80K. Transparency of BS.
Possible pressure raise during thermo-cycling after accumulating a photon dose. Definition suitable temperature range
Azimuthal distribution of photoelectrons
Specular SR reflecting, distribution of diffusely scattered photons
SEY of cold surface in presence of strong magnetic field (up to 13T)
Add at second stage
SEY in situ
XPS (Auger) in situ (surface element analysis)
Ion desorption under SR
FCC week, Washington 25.03.2015

## Slide 16
BINP
a.a.krasnov@inp.nsk.su
Parameter | BEP |  | VEPP-3 |  | NISSI |  |  |  | 
 |  |  |  |  | Normal dipole |  |  | Super-bend | 
 | min | max | min | max | min |  | max | min | max
E [GeV] | 0,2 | 0,9 | 0,3 | 2 | 0,4 |  | 2 | 0,4 | 2
SR critical energy [keV] | 0,014 | 1,3 | 0,016 | 5 | 0,028 | 3,5 |  | 0,13 | 16
SR incident angle [mrad] | 10 (5) |  | 10 |  | 10 |  |  | 10 | 
SR flax on testing chamber [ph/m/s] | 3E16 (1,5E15) | 4E17 (2E17) | 1,6E15 | 3E16 | 3E16 | 3E17 |  | 2,7E16 | 2E17
SR max power on testing chamber [W/m] | 30 (15) |  | 7,7 |  | 58 |  |  | 160 | 
Sample chamber possible length [m] | 1 (in 2015) 2 (in 2016) |  | 1,5 |  | 3 |  |  | 3 | 
Available [year] | from 2015 |  | 2015 ÷ 2017 |  | from 2020 |  |  | from 2020 | 
Parameters of available and potentially available SR beam lines for vacuum investigations at BINP
FCC week, Washington 25.03.2015

## Slide 17
BINP
a.a.krasnov@inp.nsk.su
SEY at magnetic field
Set-up for RT experiments
Element (from left to right) | ID [mm] | Length [mm] | Gap with right element [mm]
C | - | - | 0.25
M | 0.5 | 2 | 3
D | 4.5 | 1 | 1
BM1 | 4 | 10 | 0
Drift tube | 7 | 325 | 1
BM2 | 7 | 59 | 2 ÷ 3 (to sample)
“C” – thermo-cathode
“M” – modulator
“D” – diaphragm
“BM1, BM2” – beam monitors
“S” – sample
“SM” – sample manipulator
Parameters
-Energy of primarily electrons: 50 ÷ 1500 eV
-Primarily beam pulse current: up to 200 µA
-Primarily electron beam pulse duration: 1 ÷ 10 ns.
-Beam diameter: ~ 1.5 mm
-Maximum magnetic field: 0.05 T
-BM1, Drift tube, BM2 bias: -600 ÷ +600 V
FCC week, Washington 25.03.2015

## Slide 18
BINP
a.a.krasnov@inp.nsk.su
First experimental results
Primary
Secondary
Secondary - Primary
BM1
BM2
S
FCC week, Washington 25.03.2015

## Slide 19
BINP
a.a.krasnov@inp.nsk.su
C
D
M
BM1
Drift tube
BM2
B
10
325
60
S
First experimental results. SEY
FCC week, Washington 25.03.2015

## Slide 20
BINP
a.a.krasnov@inp.nsk.su
Flat
C
D
M
BM1
Drift tube
BM2
B
10
325
60
S
FCC week, Washington 25.03.2015

## Slide 21
BINP
a.a.krasnov@inp.nsk.su
SEY vs extracting bias Ubm2
C
D
M
BM1
Drift tube
BM2
B
10
325
60
S
FCC week, Washington 25.03.2015

## Slide 22
BINP
a.a.krasnov@inp.nsk.su
C
D
M
BM1
Drift tube
BM2
B
10
325
60
S
Energy distribution
z
0
Ubm1=Udrift=Ubm2=5V
where Ez=Esz+Ubm2 and delay t’ is defined as:
FCC week, Washington 25.03.2015

## Slide 23
BINP
a.a.krasnov@inp.nsk.su
C
D
M
BM1
Drift tube
BM2
B
10
325
60
S
Energy distribution
FCC week, Washington 25.03.2015

## Slide 24
BINP
a.a.krasnov@inp.nsk.su
The installation provides adequate measurements of SEY in the present of magnetic field
Effective reflectivity of secondary electrons cannot be measured ( electron density has to be decreased by a factor of 100 )
Mitigation of effective SEY by a grooved surface more stronger than it was predicted. If its space charge effect, the application of grooves should significantly decrease saturation density of e-cloud
Conclusion
FCC week, Washington 25.03.2015

## Slide 25
BINP
a.a.krasnov@inp.nsk.su
SEY
Installation into superconducting solenoid to provide experiments at magnetic field up to 10 Tesla
Installation of photo-cathode to avoid electromagnetic excitation and increase beam diameter up to 4 – 6 mm to decease electron density by a factor of 100 at least
systematic measurements samples with special coatings and surface treatments
Conclusion/ proposals for future
FCC week, Washington 25.03.2015

## Slide 26
BINP
a.a.krasnov@inp.nsk.su
Thanks a lot to
Vadim Anashin, Vincent Baglin, Bernard Henrist, Jose Miguel Jimenez, Oleg Malyshev, Paolo Chiggiato, Roberto Cimino for collaboration work and helpfull discussions
Thank for your attention!
FCC week, Washington 25.03.2015