## Slide 1
Transnational access to TRIGA _Mark III reactor
at Jožef Stefan Institute, Ljubljana

## Slide 2: Why reactor?
neutrons cause damage also in HEP experiments!
NIEL concept is not valid!
high fluences possible at reactor

## Slide 3: TRIGA reactor Training Research Isotope General Atomics
Built in 1966 (General Atomics), reconstructed in 1991
250 kW maximum power, can be regulated to few W
flux scales with power
agreement between simulated and measured fluxes within few percents
measured damage factor for fast (> 0.1 MeV) neutrons is 0.90 ± 0.05
calculated damage factor is 0.88 ± 0.05
there are also epithermal and thermal neutrons (2-3 x flux of fast neutrons), contribution to NIEL only 1-2%
TID is about 1 kGray for 1014 neqcm-2 at 250 kW
equivalent flux is 1.69 1012 ncm-2s-1 in small tube (1016 in 100 min)
equivalent flux flux is 3.05 1012 ncm-2s-1 in large tube
accuracy of equivalent fluence is ± 10%
maximum uninterrupted irradiation time is 16h.
highest fluence for AIDA 1017 cm-2
web page http://www-f9.ijs.si/~mandic/ReacSetup.html

## Slide 4
The reactor research centre is a part of Jožef Stefan Institute,

## Slide 5
Large tube
Small tube

## Slide 6
flux per unit of lethargy (ln E)
L. Snoj et al. Applied Radiaton and Isotopes 70 (2012) 483-488
elliptic large tube (axis 7 x 5cm)

## Slide 7
no cooling of samples during irradiation
water temperature stabilized to 20±2oC
annealing times long compared to irradiation time
Temperature during irradiation:

## Slide 8
Chart: 410 Irradiation units - 2 years
Chart: 39 Projects - 2 years
Chart: 
Chart: 
Irradiation units/year | 140 | 270 | 170 | 29
Chart: 
Irradiations | 90 | 167 | 95 | 37
600 units delivered
389 irradiations

## Slide 9
More than 30 publications related with AIDA irradiations at JSI published before March 2014
Chart: 
| ATLAS | CMS | RD50 | BELLE II | LHCb | OTHERS
 | 260 | 146.5 | 76 | 19 | 19 | 88.5
Sharing of reactor units between experiments

## Slide 10: Conclusion:
reactor proved to be useful tool to study of radiation damage
plan for irradiations was 100% fulfilled