## Slide 1
Neutron Converting Thin Films
Activities in Linköping
PVD of 10B4C
CVD of B4C
Coating production
Gd thin film work so far
Carina Höglund
carina.hoglund@esss.se

## Slide 2: Thin films at Linköping University
Thin Film Physics division in Linköping:
~60 persons (26 PhD students)
  Hard and low-friction coatings
  Energy materials
  Power electronics & wide-band semiconductors
  Gas and chemical sensors
  Conducting polymers
  Neutron-detecting films
Materials Research at IFM (~250 persons) Interdisciplinary, involving industry and institutes
State-of-the-art laboratories
Integrating experiments, theory, and modeling
Spin-offs include Ion Bond, Thin Film Electronics, Impact Coatings, n-Works
2
Analysis techniques:
TEM, SEM, EDX, XRD, ERDA, RBS, AES, XPS, ToF-SIMS, AFM, STM, etc…

## Slide 3: Magnetron sputtering of 10B4C
2-side coated substrates  3-fold rotation
Good adhesion on Al, Si...  >1 mm on Al, Si, Al2O3, etc
High density  97% of bulk
Maximize amount of 10B 79.3 at.% of 10B
Minimal amount of impurities  H + N + O only ~1 at.%
Thickness control and uniformity  Understood and under control
Neutron radiation hard  Survive 1014 neutrons/cm2
Large area depositions  Coated >100 m2 in May 2014 for IN5 demo
3
10B4C
Si
1 mm
ToF-ERDA
SEM

## Slide 4: CVD of B4C
Not a line of sight technique  Complex geometries
Demands on a CVD process:
Low temperature, < 600 °C
No corrosive gases
Easy up scaling
Organoboranes:
Very reactive – low process temperature!
- Trimethyl borane (TMB): B(CH3)3 - Triethyl borane (TEB): B(C2H5)3
Al-substrates
H. Pedersen, C. Höglund et al., Chem. Vap. Dep. 18, 221 (2012)
Plasma enhanced CVD
Carrier gas (H2 or Ar)
TEB
Ar carrier gas/plasma gas
TMB
Thermal CVD

## Slide 5: IN5 segment
Collaboration ESS – LiU – ILL
0.8 x 3 m2 detector area
27 000 blades with 10B4C (>100 m2)
Expect 60% efficiency @2.5 Å
Deadline September 2014
 Mass production test!
5

## Slide 6: Coating production
LiU
”ESS”
New facility
New colleague - Linda
2014-2016: Up-scaling
Capacity for >1000 m2 of 10B4C per year (ESS needs >6000 m2)
6

## Slide 7: Gd compounds for n-detection
Problem: Oxidization
Can we find a stable and conducting compound?
Gd is known to oxidize severely
A GdN thin film of ~200 nm is fully oxidized within 12 h
Possible solution:
Stabilize GdN by alloying with a chemically, mechanically,
and/or thermally more stable nitride!
Consider TM1−xGdxN, with TM = Ti, Zr, Hf
7

## Slide 8
B. Alling, C. Höglund et al., Appl. Phys. Lett. 98, 241911 (2011)
TM1−xGdxN from first principles (TM = Ti, Zr, Hf)
Ti  Phase separation
Zr, Hf  Readily mix
Magnetron sputtering
Solid solution of Zr1-xGdxN?
Oxidation resistance?
Material to consider for neutron detectors?
8

## Slide 9
Deposition of Zr1-xGdxN
Reactive magnetron sputter epitaxy (MSE)
UHV conditions: pbase = ~10-8 Torr
Seed and capping layers (when used): ZrN
9

## Slide 10: Zr1-xGdxN solid solution Oxidization
No capping or seed layer
Substrate temperature 400 °C
Oxidization level measured with RBS after:
 <2 weeks
 3-4 months
Very little Gd results in oxidization
Capping and seed layer needed for long time stability
10

## Slide 11
Thank you for your attention!
carina.hoglund@esss.se