## Slide 1: Trends in MONOLITHIC DETECTORS and ADVANCED CMOS MANUFACTURING W. Snoeys ESE Seminar October 14th 2014
walter.snoeys@cern.ch, PH-ESE-ME, CERN

## Slide 2: MONOLITHIC DETECTORS : definition
Readout circuit
Collection electrode
Sensitive layer
High energy particle
yields 80 e-/h+ pairs/μm in Si
Integrate readout with the silicon sensor
  Advantages in integration, cost, potentially strong impact on power consumption and material budget
  in two experiments: DEPFET in Belle-II and MAPS in STAR
  not yet in LHC, adopted for ALICE ITS upgrade, considered for CLIC/ILC

## Slide 3: Traditional Monolithic Active Pixel Sensors
cfr. M. Winter et al
RESET
Example: three transistor cell
COLUMN BUS
ROW
SELECT
    Commercial CMOS technologies
    No reverse substrate bias:
      Signal charge collection mainly by diffusion
      more sensitive to displacement damage
    Only one type of transistor in pixel (twin well)
    Rolling shutter readout
      very simple in-pixel circuit (3 or 4 transistors)
      pixel size: 20 x 20 μm2 or lower
      serial, row-by-row, not very fast
  Main challenge for improvement: need combination of:
  tolerance to displacement damage (depletion)
  integration of complex circuitry without efficiency loss
  commercial technology

## Slide 4: MAPS SENSOR CHIP in STAR experiment
First MAPS system in HEP
MIMOSA28 (ULTIMATE) chip
IPHC Strasbourg :
Twin well 0.35 μm CMOS
High resistivity (> 400 Ωcm) 15 μm epi
Readout time 190 μs
TID 150 krad
NIEL few 1012 1 MeV neq/cm2
MIMOSA28
(ULTIMATE)
Data taking March-June 2014

## Slide 5: THE ALICE ITS UPGRADE PROJECT
Replace the inner tracking system with an entirely new detector in 2017-2018
Improve
  impact parameter resolution by a factor 3 in rφ, 5 in z
  standalone tracking resolution and pT resolution at low pT
  New Layout 7 layers, 12.5 Gpixels in ~ 10 m2
  X/X0 0.3 %
  Pixel size: O(30x30) μm2
  Inner layer radius 22 mm
Parameters
  Chip: 15 mm x 30 mm x 50 μm
  Spatial resolution ~ 5 μm
  Power density < 100 mW/cm2
  Integration time < 30 μs
  Max required radiation tolerance : TID 700 krad & NIEL1013 1 MeV neq/cm2
ALICE-TDR-17/CERN-LHCC-2013-024
Thin sensors, high granularity, large area, moderate radiation
 Monolithic silicon pixel sensors

## Slide 6: ALICE MONOLITHIC ACTIVE PIXEL SENSOR
Technology choice
TJ 180 nm CMOS imaging process
Deep Pwell
Gate oxide < 4 nm good for TID
6 metal layers
  15…40 μm 1…8 kΩcm epitaxial layer
  Epi not fully depleted unless …
  (AC coupling, high fields, Dulinski, Kachel et al)
Chip development
Since end 2011, 4 MPWs and 3 engineering runs, 4th submitted now.
Two internal pixel chip architectures: ALPIDE and MISTRAL
Small scale prototypes for sensor optimization and radiation tolerance verification Full scale prototypes recently fabricated: lab and beam tests ongoing also on:
      irradiated
      thinned (50 μm) devices
      thinned devices mounted on flex

## Slide 7: NOTE: WAFER SCALE INTEGRATION by STITCHING
Courtesy: N. Guerrini & R. Turchetta, Rutherford Appleton Laboratory
RAL group designed many sensors in this technology
For the moment stitching not exploited for the ALICE ITS upgrade

## Slide 8: RADIATION TOLERANCE
Example: SNR of seed pixel measured with MIMOSA-32 ter at the CERN-SPS
at two operating temperatures, before and after irradiation
with the combined load of 1 Mrad and 1013 1 MeV neq/cm2

## Slide 9: MISTRAL
FSBB/MISTRAL
Rolling shutter: evolution of STAR like development
FSBB/MISTRAL functional
  lab tests promising, ENC 15-20e
  preparing for test beam
Beam test results from smaller scale prototype:
Efficiency above 99 % with fake hit rate below 10-5 achievable

## Slide 10: ALPIDE
  In-pixel amplifier/comparator ~ 40nW (~5mW/cm2) allows architectures other than rolling shutter
  Hit driven readout (priority encoder)
  Full scale prototype for the ALICE ITS: chip size: 3 x 1.53 cm2
                ~ 500 000 pixels of 28 x 28 μm2
3 cm
1.53 cm

## Slide 11: ALPIDE: priority encoder
.…..
STATE
VALID
ADDRESS
Zero-suppression
PIXEL Front-end
PIXEL Front-end
Periphery Digital Readout
RESET
STATE
RESET
SYNC
10
512
512
512
512
STATE
PIXEL Front-end
PIXEL Front-end
RESET
STATE
RESET
512
512
512
512
CLOCK
TRIGGER
0
511 double columns
512 rows
BAIS
DATA
Pulse
DACs
VALID
ADDRESS
SYNC
10
Zero-suppression

## Slide 12: ALPIDE pixel
11 µm
Sensor
Front-end
28μm
28μm
Priority encoder
Pixel layout
Analogue output of one pixel under 55Fe
Shaping time ~ 2 μm
~ 600 mV
(result from small scale prototype)

## Slide 13
THINNED ALPIDE SOLDERED ON FLEX
Thinning and soldering do not affect the performance of the chip
Band structure reflects different design options in the prototype chip
Noise << Threshold spread ~ 18 e

## Slide 14: ALPIDE test beam results
5 – 7 GeV pions at CERN PS
Telescope of 7 planes
Zero substrate bias
Sector 2 (diode reset and 2 μm spacing)
99% efficiency at fake hit rate of 10-5 achievable (only 20 pixels masked)
~ 5.5 μm spatial resolution (including tracking error of ~ 3 μm)

## Slide 15: SENSOR OPTIMIZATION: IMPORTANCE OF Q/C
If thermal noise from the input transistor dominant, for a given S/N and bandwidth:
m = 2 for weak inversion
P = analog power
Q = collected signal charge
C = input capacitance
Q/C is THE figure of merit for a sensor
Changes with different design options in the sensor
Has a direct system impact, more margin with back bias

## Slide 16: DETECTION EFFICIENCY AS A FUNCTION OF HIT LOCATION WITHIN PIXEL
Better efficiency for lower threshold
Lower efficiency for higher threshold, start losing hits in the pixel corners

## Slide 17: CLUSTER SIZE AS A FUNCTION OF HIT LOCATION WITHIN PIXEL
Larger cluster size for lower threshold
Smaller cluster size for higher threshold, charge sharing starts in the corners
Good telescope resolution needed for these plots

## Slide 18: FULL DEPLETION FOR RADIATION HARDNESS
All circuitry in the collection electrode
  Can be done in any CMOS technology with deep Nwell (triple well)
  Apply high reverse substrate voltage (eg -60 V)
  Well protects transistors from HV
  Charge is collected by drift, good for radiation tolerance
  Risk of coupling circuit signals into input
In-pixel circuit simple in small collection electrode for low C by
    ‘rolling shutter’ readout as in MAPS,
    special architectures (eg LePIX), or
    use it as smart detector in hybrid solution (cfr ATLAS, I. Peric)
NMOS in Pwell
Deep Nwell collection electrode
Pwell
PMOS in Nwell
P-substrate
I. Peric

## Slide 19: CAPACITIVELY COUPLED PIXEL DETECTOR (CCPD)
I. Peric
Early example next page
Now versions with FEI4 (eg CPPM GF)

## Slide 20: EFFICIENCY and RADIATION TOLERANCE OF CCPD
I. Peric, CPIX14
CLICPIX: M. Benoit, CPIX14
Similar developments: SLAC/UCSC (0.35 μm) J. Segal et al.

## Slide 21: Deep N-band as collection electrode
Better shielding from circuit, but large C
Dario Gnani LBNL

## Slide 22: FULL DEPLETION WITH JUNCTION ON THE BACK
Psubstrate
Pwell Collection Electrode
Nwell with circuitry
Back side N diffusion
Need full depletion
Double-sided process for junction termination, not really compatible with standard foundries
Vnwell = 0 V
Vnwell = 2 V
C. Kenney, S. Parker (U. of Hawaii),
W. Snoeys, J. Plummer (Stanford U) 1992
Only a few V on the Nwell diverts the flow lines to the collection electrode

## Slide 23: OTHER WAYS TO OBTAIN JUNCTION ON THE BACK
Several other developments (eg T. Obermann(Bonn) with ESPROS)
Also epitaxial layer and substrate of opposite type (R. Turchetta)
In general:
      Watch die edge/junction termination
      Radiation tolerance to be investigated/confirmed
Example: post CMOS wafer thinning & back-side processing
S. Lauxterman CPIX14
Finished CMOS wafer on high resistivity
Wafer thinned to 50 um
Thinned wafer with anti-reflective coating
Chip mounted in camera
Image (raw data)

## Slide 24: Silicon On Insulator (SOI) Y. Arai et al.
  Impressive development
  Now looking at double SOI for radiation tolerance and better back gating properties
  Bias on middle silicon can be used to compensate radiation induced threshold shifts (to 10 Mrad)
  New people in the collaboration:
  N. Teranishi, S. Kawahito, I. Kurachi
  Other presentation on SOI: T. Kishishita, CPIX14 (rad tol transistors ok, leakage current issue)

## Slide 25: CONCLUSIONS and OUTLOOK
  Radiation tolerant particle sensors can now be produced in CMOS technologies at lower cost than traditional sensors
  Analog active sensor and modified digital readout chip
    cfr ATLAS HV/HR CMOS collaboration
    maintain high Q/C, minimize cross-talk and increase density
    can choose a different CMOS technology for both
    cheap bonding or gluing in combination with capacitive coupling
    Rad tolerant to 1015 neq/cm2, more development needed
  Integrate the full readout into the sensor:
    further advantages in terms of assembly, production cost and Q/C
    adopted for ALICE ITS upgrade with full-scale prototypes in test:
      MISTRAL: rolling shutter, more conservative and mature
      ALPIDE: front-end with data driven readout, more aggressive
        Perspective for 20-30 mW/cm2 and a few μs integration time
      Beam tests: good position resolution and detection efficiency
      Tests on irradiated devices ongoing, expect to meet requirements

## Slide 26: CONCLUSIONS and OUTLOOK
  Full depletion for higher radiation tolerance
    Junction on the front: in principle possible, but requires high circuit well voltage and ac coupling. Easier with simple circuit.
    Circuit in collection electrode: radiation tolerance demonstrated to ~ 1015 neq/cm2, but need simple circuit to maintain reasonable C.
    Junction on the back side: need full depletion, but double sided processing incompatible with standard foundries. Some processing alternatives become available, but radiation tolerance still needs verification
  Power consumption
    ALPIDE prototype reaches about 100 mV divided over a few pixels
    ~ 300 mV on a single pixel would practically eliminate analog power: it would be sufficient to “turn on” a transistor
    Need more work on architectures to reduce digital power
    Power for transmission of data off-chip may well become dominant

## Slide 27: THANK YOU and also to ALICE ITS and CERN collegues and to people providing material and suggestions for this presentation More on ESSCIRC/ESSDERC later Presentations in Bonn CPIX14.org
walter.snoeys@cern.ch, PH-ESE-ME, CERN