## Slide 1
(TISD) Beam developments
‏
Thierry Stora

## Slide 2
Beam developments in the past 5 years
X3-10
VADIS
Purification of 80-82Zn,130Cd
with quartz
(Hads)‏
1st Fe RIB
X5 30Na Re ion source
X10 20,21Mg
sub-m SiC
Au beams
by laser ionis.
48Cr
x250
44TiF3+
X5 VADIS
Nano
CaO
Y2O3
9Be(n,a)6He
17C as CO+
Helicon Ion source
Molten salt
target
Purif Fr, Ra
With LIST
70+Ni beams
Molecular beams
Nano UCx
Purification of lanthanide beams 140Nd, 140-142Sm:
GdB6 ion source cavity + RILIS

## Slide 3
Update of the database
Update of yield data following recent developments and publications
Graphical restoration (lost with new ISOLDE website)
Cloned database for data update and analysis of the problems

## Slide 4: Yield data update
Hayley Osman – Summer Student Project 2014, T. Mendonca
2 Years of E-logs (~1,500 entries)
184 Unpublished yield entries
200+ Publications reviewed
205 Yield entries

## Slide 5: List of beams under development (Group for Upgrade of Isolde)
8B
9C
37K
Pb/Bi target for EURISOL (LIEBE project)
nano-UCx (ActILab-ENSAR)
refractory molecular beams combined with RILIS
New neutron converter (with TRIUMF)
Ba beams

## Slide 6: 8B molecular beams
K. Baechmann. Chemical Problems of the On-Line
Separation of Short-Lived Nuclides. Forschungs-
bericht K70-28, BMBK-FB-L70-28, 1970. (EMIS !)

## Slide 7: Beam development

## Slide 8: 8-B from Boron fluoride
M. Gai et al.
Target 499:carbon nanotubes
cold transfer line, VADIS
SF6 into container
Positron activity corresponds to 3*102 1/uC
Proof that activity originates from 8B still pending

## Slide 9: Titanium Carbide-Carbon Composites Results of TiC nanostructural studies (37K)
Mixing TiC and Carbon (diferente vol. ratios)
Material Microstructure Study
TiC + MWC nanotubes
Test for nanostructure stability at 1500, 1650 and 1800oC
TiC + Carbon black
TiC +Graphite
Main quality parameters:
High surface area
High porosity (>30%)
Nanometric TiC grains
Keep these parameters at the highest possible temperature
Fast diffusion and release of exotic isotopes
PhD Joao Pedro Ramos

## Slide 10: Titanium Carbide-Carbon Composites Release studies and target prototype
Release studies and target prototype
The three most promising material nanostructures were selected, irradiated and studied in terms of release.
TiC + Carbon black (50 vol.%) nanostructure, which was stable up to 1800oC, was selected to produce a full target prototype.
Target going online today!

## Slide 11
Context of the Project
RNB intensities mainly depends on the target performances
UCX target high performances are crucial for next generation facilities:
 Better understanding material properties  release kinetics
+ Studying new synthesis techniques
Task #1: Synthesis of new actinide targets
Task #2: Characterization of new actinide targets
Task #3: Actinide targets properties after irradiation
Task #4: Online Tests of Actinide Targets
Project submitted with a budget request of 460 K€,
but finally initiated with 336 K€.
CERN | GANIL | INFN | IPNO | PSI
113 K€ | 38 K€ | 72 K€ | 55 K€ | 58 K€
From C. Lau
Last week IPNO
EURISOL Town meeting

## Slide 12
two orders of magnitude
Composing a Recipe for Nano-Grained UO2
Synthesis of de-novo designed uranium carbide matrixes:
Different microstructures, densities, grain sizes, crystal structures tested → tailor-made matrix:
Suspension grinding of UO2 powder to 160 nm average particle size
Wet-mixing with multi-walled carbon nanotubes
Ultrasound drying of mixture and pressing to 1.6 g/cm3 pellets
Fast reactive sintering to mixed uranium carbide in carbon nanotube matrix
30Na yield evolution under irradiation
Online tests in November
A. Gottberg et al.

## Slide 13: LaC2–MWCNT Spallation Target Material (Ba beams)
La(OH)3 particle size reduction by suspension grinding
FLUKA Production Yields
after comparing all RE as possible spallation target nuclei
Lanthanum Hydroxide Nanopowder
Ultrasound-Dispersed Multi-Walled Carbon Nanotubes
2 µm
500 nm
2 µm
200 nm
LaC2-MWCNT Nano Composite (After Carbo-Thermal Reduction)
Microstructure of UC2-MWCNT nano composite currently under investigation
After 10 days at 1900°C
After 10 days at 1900°C
Online tests in November
J. Guillot, et al.
J. Guillot, Wonjoo Hwang, A. Gottberg

## Slide 14: Molten salt unit NaF520 (IS509)
21.6 cm
T. Mendonca et al.
……….
……….
……….
Pump
Heat
Exchanger
Protons
7 mA, 160 MeV
18Ne 1013/s
Transfer line to ion source
Irradiation chamber
Diffusion chamber
NaF:LiF
700ºC

## Slide 15
Results from 2012 confirmed this year with new target unit
Molten salt unit NaF520 (IS509)
11C as CO+ beam at intensity >1e8pps.

## Slide 16: LIEBE project
Electromagnetic pump
Proton beam
Irradiation volume
Diffusion chamber
Transfer line
Courtesy of V. Barozier and M. Delonca
Reference isotope 177Hg (T1/2=130 ms)
Diameter/thickness shape: 100 μm
Sphere: 0.57
Cylinder:0.44
Foil:0.26
Design review in summer 2014

## Slide 17: Prototyping phase of the LIEBE target
What is the proper spacing with LBE?
Grid samples
4 grids to be tested (different spacing from 1 mm up to 0.4 mm), holes diameter of 0.1 mm.
6 showers per grids
Vacuum pump
Camera
LBE liquefying

## Slide 18
Prototype phase started. Droplets 100mm grid 0.4mm confirmed.
Online likely shifted to 2016
LIEBE project

## Slide 19: VADIS + RILIS Online with Liquid Pb Target
These measurements were obtained with a standard VADIS under normal operating conditions
 More optimization possible
T.D. Goodacre, B. Marsh, et al.

## Slide 20: In conclusion
The TISD activity is ongoing and requests are prioritized through the GUI meeting
The TISD « team » will renewed to a large extent (Tania and Joao Pedro will still be there
next year, new fellow and PhD expected).
Some very exciting results : going nano, confirmed molten salt, high power molten target loop,
VADLIS, maybe 8B…
Some ISOL technical development activities relevant to ISOLDE will be ongoing
within a starting MEDICIS PROMED H2020 Marie Curie ETN network,
ie with Prof Novozelov (not necessarily at CERN, distributed throughout the network).