## Slide 1
LHCb SciFi
The new Fibre Tracker for LHCb
Christian Joram
CERN PH/DT
ECFA High Luminosity LHC Experiments Workshop - 2014
  The LHCb SciFi project: Brazil (CBPF) - China (Tsinghua) - France (LPC, LAL, LPNHE) - Germany (Aachen, Dortmund, Heidelberg, Rostock) - Netherlands (Nikhef) - Poland (Warsaw) - Russia (PNPI, ITEP, INR, IHEP, NRC KI) - Spain (Barcelona, Valencia) - Switzerland (CERN, EPFL) - UK (Imperial College)

## Slide 2
Scintillating fibre tracking: more than 30 years of history in HEP
UA2 upgrade, CHORUS, D0, ATLAS ALFA + many small scale experiments
high geometrical flexibility (planar, barrel, …) and in principle "edgeless"
good tracking performance (shit < 100 mm), potentially high speed
very low and uniform material budget
Evolution of optical readout technology
image intensifiers (II) + CCD  (MA)PMT/HPD  VLPC  SiPM
very fast (LHC speed) readout is now possible
Unfortunately little progress in
scintillating fibres: few suppliers, limitations in light yield, attenuation length, rad. hardness
assembly technologies: no company produces high quality fibre mats
 building a SciFi tracker is a labour-intense adventure
R.C. Ruchti
Annual Review of Nuclear and Particle Science, 1996

## Slide 3
Outline
The LHCb SciFi Tracker
The main challenges
  Fibres with high light yield and attenuation length
  Building large-size detector modules
  Radiation damage to scintillating fibres
  Optimised SiPM detectors and their radiation hardness
  Fast readout with manageable data volume
  Integration (incl. operation at -40 °C)

## Slide 4
LHCb Tracker Upgrade TDR
CERN/LHCC 2014-001
LHCb TDR 15
The current
Outer Tracker (OT) = Straw tube gas detectors (Ø 4.9 mm)
Inner Tracker (IT) = Silicon mstrips (pitch = 200 mm)
will be replaced by a single fast and light technology:
SciFi tracker = scintillating fibres with SiPM readout.
Current LHCb
IT + OT  SciFi
Reminder:
LHCb upgrade for running after LS2 (≥2020, 50fb-1)
(see talk by G. Passaleva, yesterday)

## Slide 5
Main requirements on the SciFi tracker
Detector intrinsic performance: measure x,x' (y,y') with
high hit efficiency(~99%)
low noise cluster rate (<10% of signal at any location)
sx < 100μm (bending plane)
X/X0 ≤ 1% per detection layer
Constraints
40MHz readout
geometrical coverage: 6(x) x 5(y) m2
fit in between magnet and RICH2
radiation environment:
      ≤ 1012 1MeV neq / cm2 at the location of the
      photo-detectors
      ≤ 80Gy at the location of the photo-detectors
      ≤ 35kGy peak dose for the scintillating fibres
low temperature operation of photodetectors
LHCb FLUKA simulation

## Slide 6
Technology: Fibres and photodetectors
The SciFi tracker is following the technology developed by the Aachen group for the PERDaix detector (prototype balloon experiment)
B. Beischer et al., A 622 (2010) 542–554
G.R. Yearwood, PhD thesis, Aachen, 2013
PERDaix: 32 mm wide bi-layer module in stereo geometry.
Hits consist of clusters with typical size = 2.
Allows for good resolution from COG and suppression of noise (= single hit pixel in 1 channel).
4 64-ch. SiPM arrays
5 staggered layers of Ø250 mm fibres form a ribbon (or mat)
Readout by arrays of SiPMs. 1 SiPM channel has the similar width as fibre pitch (~250 mm) and extends over the full height of the mat (~1.5 mm).

## Slide 7
1 module
2 x ~2.5 m
2 x ~3 m
readout
readout
10 or 12 (almost) identical modules per detection plane
fibre ribbons (mats) run in vertical direction.
fibres interrupted in mid-plane (y=0) and mirrored
fibres read out at top and bottom
photodetectors + FE electronics + services in a “Readout Box”
Very light and uniform material distribution
~540 mm
T1
T2
T3
General layout of the detector
3 stations with 4 planes each X-U-V-X, stereo angle ± 5° (prel.)
X/X0 = 2.6% per station

## Slide 8
Main specifications of the SciFi tracker
Some rough numbers
3 M fibres (2.5 m long)
Total fibre length ~10,000 km of fibres (+ spares)
600 000 readout channels
item | specs
Scint. fibre | 0.25 mm Ø, double cladded, blue emitting. Baseline Kuraray SCSF-78 MJ
Photodetector | SiPM array, 128 ch., pitch 0.25 mm
Module dimensions | (2 x 250) x 54 cm, 40 mm thick, one end mirrored
Active surface | ~360 m2
Radiation | Non-uniform, up to 30 kGy, 1012 n/cm2
Readout | 3-thresholds, clustered, 40 MHz
Environment | SiPM at -40°C, rest at ambient T
2 x 250 cm
54 cm
SciFi module

## Slide 9
Challenge 1: Fibres with long attenuation length and high light yield
We are currently observing attenuation lengths
which are lower than for fibres bought in 2010.
Possible causes identified at recent meeting with
Kuraray in Japan. Expect improved batch in few weeks.
We aim for Latt > 3.5 m
Kuraray SCSF-78 MJ
Attenuation Length
Normalised @ 100 cm
Scintillation light yield
of one 0.25 mm fibre ,
measured by a PMT
The scintillation yields appear to be ~OK.
Chart: Distance (cm)
| 60 | 90 | 120 | 150 | 180 | 210 | 240
2010 "DO" 1000ppm | 2.024 | 1.768 | 1.514 | 1.372 | 1.215 | 1.096 | 0.9534
2010 "AC" 1000 ppm | 1.969 | 1.595 | 1.366 | 1.221 | 1.102 | 0.9775 | 0.8958
2013 1000ppm | 1.84 | 1.54 | 1.28 | 1.19 | 1.05 | 0.89 | 0.83
2014 1000ppm | 1.848 | 1.552 | 1.3 | 1.103 | 0.959 | 0.821 | 0.732
FIT 2010 DO: 2.39e(-0.0038x) | 2.3924 | 2.1369 | 1.9087 | 1.7049 | 1.5229 | 1.3602 | 1.215 | 1.0853 | 0.96937
FIT 2010 AC: 2.26e(-0.0040x) | 2.2571 | 2.0028 | 1.7771 | 1.5769 | 1.3992 | 1.2415 | 1.1016 | 0.9775 | 0.86736
FIT 2013: 2.26e(-0.0043x) | 2.2618 | 1.9891 | 1.7494 | 1.5385 | 1.3531 | 1.19 | 1.0466 | 0.92042 | 0.80948
FIT 2014: 2.49e(-0.0053x) | 2.4901 | 2.124 | 1.8117 | 1.5453 | 1.3181 | 1.1243 | 0.959 | 0.818 | 0.69773
Points at 60 cm not included in fit.
(cladding light , helical paths)
Extrapolation of the fits to d=0: same yield within ±5%
Kuraray SCSF-78 MJ
Scintillation Yield

## Slide 10
We are also exploring a new scintillation material
Nanostructured Organosilicon luminophores (NOLs)
activator
Spectral
shifter
L
(α, β or γ-
radiation)
Е
L = 1 - 2 nm << R
Patent RU 2380726 (2010)
Chemical coupling of activator and WLS molecules increases scintillation yield.
Light output is 90-120% of that of anthracene ,
i.e. 50% higher than in standard plastic scintillator (like BC-408).
So far only tested on scintillator tiles, not on fibres!
Radiation hardness ?
To be tested!
Material is highly interesting for inner region of SciFi tracker (strong 'natural' attenuation + high ionising dose).
Kuraray and ISPM have started to collaborate on the development of NOL based fibres. We expect first samples in about 1 month.
(Institute of Synthetic Polymeric Materials, Russia, S. Ponomarenko)
polystyrene matrix
S.A. Ponomarenko, Nature Scientific Report, 8 Oct 2014, doi:10.1038/srep06549

## Slide 11
Fibre mats are produced by winding fibres, layer by layer, on a fine-pitch threaded wheel
p = 270 mm
~150 mm
~ Ø 900mm
addition of very fluid epoxy glue, TiO2 loaded
Fibre winding (at Univ. of Dortmund)
Dedicated machine, in-house production
feeder
Test winding (at Univ. of Aachen)
Use of a large CNC lathe.
Challenge 2: Geometrical precision
After partial polymerisation, the mat is cut and flattened for full polymerisation.
~ 2800 mm
~ 150 mm

## Slide 12
An important parameter: Fibre diameter (non-)uniformity
Over 99.9% of the length, the fibre diameter is within 250 ± few mm
~4 M measurements along 12.5 km fibre
(1 point every 3 mm), performed with a LASER micrometer.
However, typically once per km, the fibre diameter increases beyond acceptable limits (~300 mm).
Bump problem addressed together with Kuraray. Expect improvement in coming few months.
Plots by
P. Hebler,
Dortmund.
Bumps distort local winding pattern.
Occasional bumps can in principle be eliminated during winding, but this is time consuming.

## Slide 13
before irradiation
after irradiation
0 kGy
3 kGy
at 6.25 Gy/s
22 kGy
at 1.4 Gy/s
Ll = 439 cm
Ll = 422 cm
Ll = 126 cm
Ll = 52 cm
Complex subject. Literature relatively poor and contradictory  We perform our own irradiation tests under conditions which come close to the ones met in the experiment.
Ionising radiation degrades transparency of polystyrene core (shorter att. length), but doesn't affect scintillation + WLS mechanism.
Example: LHCb irradiation test (2012)
  3 m long SCSF-78 fibres (Ø 0.25 mm), embedded in glue (EPOTEK H301-2)
  irradiated at CERN PS with 24 GeV protons (+ background of 5·1012 n/cm2)
Challenge 3: Radiation damage to scintillating fibres

## Slide 14
Max. signal loss in region around beam pipe (35 kGy) of 27%
There is no well-established model to describe L(D)/L0 = f(Dose)
Hara model:
describes our high dose data well, but has some weaknesses (can’t include D=0, can become negative)
We are currently preparing several low-dose (1 kGy) irradiations to improve data situation.
Hara model 
K. Hara et al., NIM A411 (1998), no. 1 31 .
L(D)/L(0) = a+ b log(D)
More irradiations were performed at KIT (Karlsruhe) 10 MeV protons and in-situ in LHCb cavern.
L(D) 

## Slide 15
We co-develop with Hamamatsu (JP) and KETEK (DE) 128-channels SiPM arrays, with very similar dimensions.
Photon detection efficiency
PDE = QE · egeom · eavalanche
2 x 64
channels
=f(OV)
egeom can be optimised by increasing the pixel size.
eavalanche can be increased by higher OV.
Both effects must be counter-acted by efficient trenches to control pixel-to-pixel cross-talk.
PCB
Flex cable
  Challenge 4: Optimised SiPM detectors and their radiation hardness

## Slide 16
PDE and cross talk measurements at CERN and EPFL
Chart: KETEK 2012 W1-3B-1
Chart: KETEK 2014 C4-W3-c3-ch16
Chart: Over voltage (V)
| 2 | 3 | 4 | 5
Cross talk | 0.0028 | 0.00696 | 0.0148 | 0.0181
Chart: Over voltage (V)
| 1.5 | 2.5 | 3.5 | 4
Cross talk | 0.017779 | 0.038344 | 0.07338 | 0.089883
(X-talk and after
pulses removed)
(X-talk and after
pulses removed)
with trenches
with trenches
with new trenches
Received very recently also new Hamamatsu devices (under test)!
Expected scintillation spectrum after full dose in mid-plane

## Slide 17
Dark counts are primary noise source.
Keep pixel-to-pixel cross-talk low  avoid double-noise hits (which can seed noise clusters)
Hamamatsu 2013 technology (single channel devices)
The SiPMs suffer mainly from the neutrons (NIEL)
The SiPMs are exposed to 1.2·1012 n1Mev.eq. /cm2 (50 fb-1)
A detailed FLUKA simulation showed that shielding (Polyethylene with 5% Boron) can halve this fluence  tests so far done for 6·1011/cm2 .
The SiPMs need to be cooled. Our default working point is -40°C. Noise reduced by factor ~64.
Scaled to 0.33 mm2
6·1011 n/cm2

## Slide 18
~0.6 M channels
40 MHz readout rate
Signal propagation time up to 5m · 6ns/m = 30ns  some spill over to next BC
No adequate (fast, low power) multi-channel ASIC available
LHCb develops its own ASIC, called PACIFIC, with 64 channels (130 nm CMOS, TSMC)
3 hardware thresholds (=2 bits)
seed
neighbour
high
plus a sum threshold (FPGA) are a good compromise between precision (<100 mm), discrimination of noise and data volume.
Compared to analog (6 bit) readout, expect resolution to degrade from ~50 to 60 mm. Marginal impact on p-resolution.
P ~ 8 mW/channel
Zin ~20-40 W
ff ~ 250 MHz
Challenge 5: Fast readout with manageable data volume

## Slide 19
Challenge 6: Integration (incl. operation at -40 °C)
SiPM cooling pipes
Insulation
(Rohacell with Mylar µ alu layer)
Hybrid connectors
Mounting flange
The principal integration element is the Read Out Box (ROB) at the end of every module.
Ensure precise optical coupling of cold SiPMs to fibres
House warm electronics
Ensure gas & light tightness and insulation.
Couple to mechanical frame structure.
Illustration of 'cold' part of ROB
Cooling pipe
fibres
SiPM
Coolant: C6F14 or Novec 649
~54 cm
Heat load / ROB
~ 20 W

## Slide 20
Where do we stand and what can we expect?
Non-irradiated 2.5 m long 5-layer mat + 2011 technology SiPM array,
measured with 1.5 MeV e- in lab (from energy filtered Sr-90 source).
SiPM
mirror
 measured in lab (Sr-90 e-)
 expected gain from non-irradiated 6-layer mat, 2014 SiPM technology, H.E. hadrons
Chart: d (mm) from SiPM
| 2405 | 2200 | 1970 | 1800 | 1600 | 1400 | 1200 | 1000 | 800 | 600 | 400
Mean Vs X | 11.3219 | 11.7475 | 12.1171 | 12.0232 | 11.9294 | 13.1831 | 12.9577 | 12.6988 | 14.7551 | 15.7828 | 15.6055
Fit | 10.9652 | 11.3561 | 11.8112 | 12.1594 | 12.5821 | 13.0195 | 13.4721 | 13.9405 | 14.4251 | 14.9266 | 15.4455
Fitting | 20.2634 | 20.9858 | 21.827 | 22.4704 | 23.2516 | 24.0599 | 24.8964 | 25.7619 | 26.6576 | 27.5844 | 28.5434
after irrad | 12.9733 | 13.922 | 15.0473 | 15.9225 | 17.0015 | 18.1364 | 19.3296 | 20.5838 | 21.9019 | 23.2867 | 24.7414
Expected loss due to radiation damage (50 fb-1)
We expect this performance to be sufficient to guarantee 98-99% hit efficiency anywhere and after full radiation dose.
We just had 1 week of successful test beam at CERN H8. Full size fibre mats + latest SiPM technology.
Analysis in progress.

## Slide 21
Status and Outlook
Learned how to make 13 cm wide and >2.5 m long fibre mats. Current focus: machining and precision assembly of mats on panels. Several fibre mats successfully tested in H8 (1 week ago).
128-ch. SiPM arrays from KETEK successfully tested, but packaging needs to be improved. Increased PDE and(!) reduced XT.
New arrays from Hamamatsu just arrived, but already used in beam.
Single channel of PACIFIC successfully tested. 8-channel version fabricated, but had a minor design flaw. Full scale (64 ch.) prototype ASIC in 2015.
Efforts for overall detector design, Readout Box, mechanics now in full swing. Lots of challenges like beam pipe hole, cooling (insulation, condensation).
Starting to prepare tooling, logistics and QA. Mass production of fibre mats and modules will require sustained efforts (4 winding centres) and tight quality control.
 Start of fibre mat and module production around end 2015.
 Detector to be ready for installtion around mid 2018.
Fibre modules
SiPMs
RO electronics
Design
Production