## Slide 1: D1 Development Status
T. Nakamoto
KEK
CERN-KEK Committee
21 November 2014, KEK

## Slide 2: Participants & Supports
KEK
T. Nakamoto, M. Sugano, S. Enomoto, H. Kawamata,
Q. Xu (left March 2014), N. Higashi, N. Okada, R. Okada,
Y. Ikemoto, M. Iio, T. Ogitsu, K. Sasaki, N. Kimura, M. Yoshida, A. Yamamoto.
CERN
E. Todesco, A. Musso, G. Kirby, F. Savary, A. Ballarino,
P. Fessia.

## Slide 3
Layout of IR Magnets
HL-LHC
Nominal LHC
NC D1
IT Quads. w/ Nb3Sn
SC D1
HL-LHC
Nominal LHC
IT Quads.& D1
Long Straight Section
Crab Cavity
D2
Q4
Corrector
Package
Q1
Q2a
Q2b
Q3
Aperture increase in IT Quads:70mm150mm Large bore also for the new D1
Replacement of current NC D1 by SC D1: Shortening magnet length by 15m
Making room for new crab cavities

## Slide 4: NC vs SC
 | Beam separation dipole, D1 | 
 | LHC | HL-LHC
Aperture | 52mm gap | 150mm
Nominal Field (Peak Field) | 1.4 T | 5.6 T (6.5 T)
Magnetic Length | 3.4 m x 6 ~21m | 6.27 m
Stored Energy | 0.014 MJ/m | 0.34 MJ/m

## Slide 5: Latest Design Parameters of D1
Stress management
High saturation, stray field, flux return cryostat
Radiation resistance, cooling capability
Coil ID: 150 mm
Integrated field:35 T m (26 Tm at present LHC)
  5.59 T at 12 kA. Lcoil=6.3 m
Top: 1.9 K by HeII cooling
Op. point (2D coil): 75 %
Coil layout: 1 layer of 15.1 mm cable
  Better cooling. Saving space for iron yoke.
Conductor: Nb-Ti LHC MB outer cable
Structure: Collared yoke structure by keying
  RHIC dipole, LHC MQXA, J-PARC SCFM
  Enhancing iron material for stray field issue
Field quality: < 10-4 at Rref = 50 mm
Cold mass OD: 550 +10 x 2 = 570 mm
Cryostat OD: 914 mm, same as MB cryostat
Radiation, energy deposition:
5
13
8
4
44 turns
135 W in total, 2 mW/cm3 at local peak, Radiation dose >25 MGy

## Slide 6: 2m-long Model Magnet - Overview
Shell: SUS304L
Horizontal split iron yoke:
low-carbon steel (EFE by JFE steel)
Collaring keys
f60 mm HX hole
Notches and f 34 mm holes for iron saturation effects
Same outer-interface for J-PARC SCFM jigs
4 split stainless steel spacer collars: NSSC130S
NbTi SC cable (LHC MB outer) + Apical insulation
Radiation resistant GFRP (S2 glass + BT resin) wedges
Brass shoes
Single-layer coil, 4-split spacer collars, collared yoke by keying
HeII cooling channel

## Slide 7: Deliverables
One 2m long model magnet will be built and tested at KEK.
The second model development is also planned.
Design parameters | Production | 2-m model
Field integral | 35 T•m | 10.3 T•m
Magnetic length | 6.27 m | 1.85 m
Coil mechanical length | 6.46 m | 2.00 m
Magnet mechanical length | 6.96 m | 2.50 m
Cold mass weight | 12 tons | 3.8 tons
Cable unit length per coil | 568 m | 175 m

## Slide 8
Mechanical Analysis: Yoking
Mechanical analysis during the assembly process, cooling and excitation using ANSYS has been completed
Highest stress arisen at key slots in the yoke < 220 MPa
 The assembly scheme would be feasible
UX = 0
UY = 0
Collar
Coil
Yoke
0.5 unit
thickness
Remove load from the yoke shoulder and insert the load-key; The gap between top and bottom yokes keep closed at both ends.
Stress in the yoke
Key insertion

## Slide 9
Mechanical Analysis: Coil Stress
UX = 0
UY = 0
Collar
Coil
Yoke
Pole
Mid-plane
Coil stress during yoking: 100 MPa
Excitation

## Slide 10
Magnetic Design by ROXIE:
Variation of multipole coefficients
Nominal current
Nominal
current
b3
b3
b5 ~ b13

## Slide 11
Magnetic Design by ROXIE:
Transfer Function
Nominal current
Transfer function starts to decrease at 6 kA and the value at the nominal
current is lower by 10% than one at low field

## Slide 12
Magnetic Design by ROXIE:
Possible Error Sources
Impact of possible design changes
Diameter and position of HX holes (-5.1 units)
Shape of cryostat (Elliptical cryostat option)
(-2 units)
Systematic errors
Packing factor of iron yoke (-1.2 units)
Relative permeability of stainless steel collar (-0.6 units)
Mispositioning of coil blocks during yoking
(-1 unit)
Random geometric error
ID890 mm x 1112 mm,
t=12 mm, elliptical
Thanks to Susana Izquierdo Bermudez
for her technical support in ROXIE
(Change of b3 by each factor)
A
B
C
D
55mm
12mm
33mm
32mm
33mm
9mm
5mm
54mm
20mm
Yoke
Collar

## Slide 13
Coil End Design by ROXIE
Old version
Coil end found in practice
winding
(2-m test coil)
Modified design
End spacer
made using a 3-D
printer
Due to insufficient length between straight section to end,
cables at the coil end tend to be inclined
to relieve strain energy
 Difference in height between end spacer and cables
Coil end will be modified to have longer length
Length of each coil block is being optimized to minimize multipole coefficients

## Slide 14
Quench Protection Study with Rdump=75 mW
Rdump=75 mW: Already implemented for the MB circuit in the LHC
Quench detection threshold: 0.1 V, 10 msec
Cable resistance was neglected in calculation of detection time & time constant of
current decay, t  A conservative scenario
Quench starts around lead out (B ~ 0 T)  Worst case
Peak temperature at Bpeak
(at Imax=13kA) = 305 K
Further study will be made with 3D field map soon.
QPH would not be necessary in the production magnet, but it will be decided after quench test using 2-m model magnet.
Calculation condition

## Slide 15: SC Cable Supply & Schedule
Delivery Date | Objective | Requirement | Remark
Feb. 2013 | 10 stack meas. (a piece length > 0.3 m) | ~50 m w/ MB type insulation | Both MB inner and outer cables w/ MB type insulation
Jan. 2014 May 2014 | 1 practice coil* + 2 real coils for the 1st 2-m long model + 1 spare coil | 220 m** x 4 | LHC MB outer cables w/ MB type Apical insulation
April. 2015 | 2 practice coils + 2 real coils for the 2nd 2-m long model | 220 m x 4 | LHC MB outer cables w/ MB type Apical insulation
JFY2016 (prospect) | 6 or 7 full-scale magnets + 4 practice/spare coils | 600-640 m x 18 | LHC MB outer cables w/ MB type Apical insulation
Done!!
NbTi LHC MB outer cable supplied by CERN for the new D1 .
TBD

## Slide 16: GFRP End Spacers, Wedges
GFRP: MGC BT2160/2170 + S2 glass by ARISAWA
  Radiation resistance beyond 50 MGy
  similar modulus as G10: 29 GPa
  But 30 % higher mechanical strength
End-spacers: manufactured in-house
  Design by ROXIE
  Modeling with NX, Drawing with Solid Edge
  CAD/CAM CATIA V5
Wedges
Adhesion: Cyanate Ester (MGC BT2160RX)

## Slide 17
Cable: NbTi MB cable with APICAL and PIXEO insulation supplied by CERN
Coil configuration:
- Single layer coil
- 44 turns, 4 coil blocks
- Coil length: 2020 mm (between the end saddles)
- 2D cross-section optimized for HX-hole of 50 mm (old version)
Wedge(GFRP)
MP shim(GFRP)
Pole shim (GFRP)
Ramp box
Center post
Mandrel
Pushing bar
Coil Structure

## Slide 18
Layer Jump
2D cross-sections of the layer jump
Coil layer at the straight section
Collar layer at the lead end
Pole turn
Ramp box was designed in such a
way that the layer jump turn go out uprightly
Ramp box
A
B
C
A
B
C

## Slide 19
Coil Size Control at Curing
Final size of coil is determined by yoking
Pressure applied to coil
Curing: 50 MPa
Yoking: 100 MPa (max)  80 MPa
From the results of 10 stack measurement (22 cables),
coil after curing should be larger by 0.9 mm
than the final size
Forming block
Mandrel
Pushing bar
Curing pressure
0.9mm-thick shim
0.9 mm-thick shims were inserted
and coil was compressed until the gap
was closed
Gap

## Slide 20: Test Coil Fabrication
Demonstration of coil fabrication with a first 2m (test) coil.

## Slide 21
Temperature Trend at Curing
Max. temperature could be controlled at 190 - 210oC (< 220oC)
150oC
180oC
190oC
Expected temperature profile was realized
F-E
M
F-W
NN
N
M
S
SS
Temperature profile to harden cyanate ester (150oC x 4h + 180oC x 8h) was obtained
as expected
Bonding of polyimide insulation
Hardening of cyanate ester

## Slide 22
Coil after Curing
The gap between the end saddle and
the cable was closed after curing
Hard BT resin + S2 glass GFRP can
be accommodated to the cable
Bonding between the cable and
the wedges is sufficiently strong
Effectiveness of heat treatment
profile is verified

## Slide 23
Electrical Tests for QA
No ground fault throughout winding and curing
No change of cable resistance (for 44 turn)
No damage of cable insulation checked
by a bundle of fine Nb-Ti filaments
No turn-turn insulation failure at least
up to 1 kV (Surge test)
Coil inductance: 2.26 mH
(calc. value = 2.28 mH)
Electrical soundness of the coil
was confirmed
After winding | 242.9 mW
Under curing pressure, before curing | 242.5 mW
After curing | 242.2 mW
Surge test

## Slide 24
Coil Size Measurement
Pushing bars with strain gauges
50 ton hydraulic press
Coil pressure up to 90 MPa
Continuous measurement using the 5.4 m-long bench
Two pushing bars each having 5 x 20mm-wide fingers
4 x linear gauges to measure coil deformation
Similar apparatus as CERN (Thanks to G. Kirby)
R5
R4
R3
R2
R1
L5
L4
L3
L2
L1
Maximum pressure to compress the coil to the final size was measured

## Slide 25
Preliminary
Coil Size Measurement: Results of Test Coil
Measured maximum pressure: 80 – 92 MPa
(After correction considering machine
deformation: 90 – 100 MPa)
The size of our test coil is almost
as designed
Coil pressure – deformation
Results for adjacent 5 sections
Final size
Oversize
Coil stress at the final size along the coil length
Dot: Results for each 20 mm
Line: Average for every100 mm
R
L
R5
R4
R3
R2
R1
1-m Straight section

## Slide 26: Ground Insulation
Ground Insulation: same concept as MQXA
  4 layer of 0.125 mm thick Polyimide insulation (Upilex-RN)
  Large shrinkage of the coil during the assembly should be taken into account.
Brass shoes to intervene laminated collar sheets and the insulated coil.
Collaring mandrel ensuring the proper coil form.
Concept and design checked by the practice model.

## Slide 27: QPH & Spot Heater
QPH might not be necessary for the D1 because peak temperature is estimated to be 300K by a conservative scenario.
Quench Protection Heater (0.25 mm think) for model magnet R&D
  Still searching for manufacturer in Japan.
  Possibility of supply from CERN
  Necessity??
Spot heaters will be implemented in the model magnet for the quench protection study.
  higher field at the straight section
  lowest field at the coil end (probably at lead-out)
CLIQ might secure the quench protection?
  Experimental study with the 1st model magnet

## Slide 28: Requirement for Cooling
New 2 HX holes: f60 @R=190
Collar lamination w/ 0.2mm gap by emboss
Longitudinal grooves on collar: d2 x w20, both sides of triangle notch.
Yoke packing factor of 98 %
Free area: 153 cm2
Yoke 98%
Collar 96%
Heat Exchanger
Heat Exchanger
Suggestion by Rob:
2 x f57 HeII HXs
Radial gap of 4 % up to HX holes.
Longitudinal free area >100cm2

## Slide 29
Collars
Stainless steel: NSSC 130S (same as YUS130S)
  12 tons of NSSC-130S sheets (2.3mm & 2.6mm thick) delivered. This can cover the model magnet development and >30% of the 7-m long full-scale magnets production.
  Specification, once set for the LHC MB, is fulfilled. Very low permeability of 1.002 confirmed at RT/4.2K.
4-way split collar concept for the dipole coil to avoid the unwanted warp at the fine-blanking process.
  Collars work as spacers between the coil and the yoke.
  A sub-stack of the collars is laminated by the 2.3mm thick “fixing collar” and the 2.6mm thick “spacer collar”. Similar with MQXA.
  Four sub-stacks are connected by lock pins and provide the coil pre-stress below 5 MPa.
  Emboss of 0.2mm
Procurement of fine-blanking dies is on-going.
Radiation resistant GFRP collar at lead end, same design concept as the J-PARC SCFM.
Odd layer
Even layer
e.g.) GFRP collar to clamp the ramp box and the lead-out on the single layer coil for J-PARC SCFM.

## Slide 30
Collaring Press and Mandrel
Horizontal collaring press in preparation.
  coil pre-stress below 5MPa.
  coil deformation controlled by the collaring mandrel.
Demonstration of collaring mandrel
  3D rapid prototyping.
  Main mandrel can be removed by using “Flat Roller” after yoking.

## Slide 31
Yokes
Low carbon steel: EFE by JFE steel
  15 tons of EFE sheets (5.6mm & 6mm thick) delivered for the model magnet.
  Another 15 tons will be procured within this year.
  Y.S.: > 240 MPa. Magnetic property: OK.
Yoke is locked by 3 keys at each side. The coil pre-stress of 90-100 MPa will be given by the yoking.
Mechanical short model study: Demonstration of mechanical structure
  Concept of 4-way split collars and pre-alignment feature.
  Increase of thickness difference (5.6mm & 6.0mm): help for yoke stacks assembly.
  Coil pre-stress measurement at assembly and cool-down to LN2 temperature
For model magnet:
  KEK placed an order of fine-blanking dies. Yoke stacks will be delivered by Feb. 2015.
  Holes on the yoke sheet are not finalized and will be machined for the model magnets.
assembly of top and bottom yoke stacks for J-PARC SCFM

## Slide 32
Presses, Jigs
3.6 m long hydraulic press for coil curing and yoking is ready.
Yoking jig
(J-PARC SCFM)
Forming block
3500 tons hydraulic press

## Slide 33: Preparatory Work for Cold Tests
Modification and procurement of the cryostat for
“12 kA, 150 mm aperture” D1 magnet.
  Old Spec. of 9m-deep vertical cryostat: 7.5kA, 70 mm aperture dedicated for MQXA.
  New header w/ larger warm bore.
New 15 kA CLs to be delivered in March 2015
Upgrade of PC and bus lines. (7.5 kA >> 15 kA).
  New 15kA-DCCT procured by KEK is being calibrated at CERN.
  New dump resistor of 75 mW with grounding at the middle.
New DAQ systems
New header, cold tube, quench antenna
New 15kA bus lines
New 15kA-CLs

## Slide 34: Deliverables and Near-term Plan
One 2m long model magnet will be built and tested at KEK.
The second model development is also planned.
Up to now, 2m long test coil fabricated. Coil size measurement done.
Dec. 2014 A short mechanical model
April 2015 1st 2m long model
  Field optimization by ROXIE and end spacer design are underway.
  Coil winding would start at Jan. 2015.
June 2015 Commissioning of test stand
  A new header (cryostat flange) for D1. To be inspected by local government.
  A new pair of 15kA CLs
  Upgraded 15kA P/C and buses
Sep. 2015 Cold test of 1st model
Dec. 2015 2nd 2m long model
Feb. 2016 Cold test of 2nd model

## Slide 35: Accounting & Budget for D1 model R&D
 |  | JFY2013 Accounting |  | JFY2014 Budget | 
 |  | Prediction | Inventory on order | Proposal | Min. Req.
Income | Carry over from the last year | 8.40 | - | 0 | 0
 | CERN-KEK Budget | 21.17 | - | 21.10* | 21.10*
 | KEK (ATLAS-J + ? ) | 85.00 | - | 126.00 | 80.00
 | Total | 114.57 | - | 147.10 | 101.10
Expenditure | Conceptual Design | 0.00 + 1 FTE | - | 0.00 + 0.2 FTE | 0.00 + 0.2 FTE
 | Engineering (CAD support) | 7.52 + 1 FTE | - | 7.00 + 1 FTE | 7.00 + 1 FTE
 | Materials for D1 model magnet | 52.81 | 34.60 | 55.00 | 44.50
 | Test stand | 44.97 | 7.50 | 47.00 | 25.00
 | Technical support | 5.41 | 2.21 | 12.00 | 12.00
 | Travel & others | 3.87 | 1.00 | 5.00 | 2.60
 | Carry over to the next year | 0 | 0 | 21.10 | 10.00
 | Total | 114.57 | 45.31 | 147.10 | 101.10
Unit: MJYen (~10kCHF)
* Assuming 100 JYen=1 CHF
55.00
+22.29
82.6

## Slide 36: Accounting (Not finished yet)
2013 and 2014
CERN-KEK Budget
KEK (ATLAS-J + ? )
Note:
CERN-KEK Budget for 2015 was transferred Aug. 2014.
No budget remains.

## Slide 37: Summary
KEK has been engaged in the FP7 HiLumi-LHC design study. R&D of the beam separation dipole magnet, D1, including the 2-m model is underway.
  Coil ID of 150 mm
  35 Tm w/ nominal field of 5.6 T at 12kA under 2 mW/cm3 (local peak), 25MGy
Conceptual design is mostly completed and the 1st test coil was fabricated at KEK. Coil size measurement results showed that the coil was made as designed.
The 1st 2m model will be fabricated spring 2015 and the cold test is anticipated in September 2015.