## Slide 2: IC Technologies
Michael Campbell
PH Department
CERN

## Slide 3: Acknowledgements
J. Alozy
M. Barbero
S. Bonacini
J. Christiansen
F. Faccio
E. Heijne
K. Kloukinas
X. Llopart
A. Marchioro
S. Michelis
W. Snoeys

## Slide 4: Disclaimer
This talk is focussed on mainstream microelectronics technologies
It does not address projects with special requirements such as
  DC-DC
  MAPS, HR/HV CMOS
  Bipolar etc

## Slide 5: Outline
Introduction
Challenges for microelectronics at HL-LHC
Common Foundry access – status
  IBM
  TSMC
IP block sharing
Interconnect
Future technologies

## Slide 6: Introduction
Rad tolerant ASICs are one of the key enabling technologies of the LHC
In particular, ASICs designed for radiation tolerance in 250nm CMOS played a major role

## Slide 7
pixel
detector
beam pipe
Si strip
tracker
e-CAL
TRT
h-CAL
muon chambers
Some of the ASICs in ATLAS
FE-I3 pix det
28 000 chips
80 M segments
1.7 m2 Si sensor
ABCD Si det
50 000 chips
6 M segments
60 m2 Si sensor
ASDBLR TRT det
38 000 chips
DTMROC TRT det
19 000 chips
ASD muon det
148 000 chips
Total ATLAS
100 million sensor cells
appr. 800 000 chips
majority ASICs
Chips to scale 1 cm
E. Heijne

## Slide 8
pixel
detector
Total CMS
appr. 1 million chips
of which 700 000 ASICs
MAD muon det
181 000 chips
25 000 m2 gas-filled
APV25 Si det
110 000 chips
9.3 M segments
198 m2 Si sensor
PSI46 pix det
16 800 chips
66 M segments
1 m2 Si sensor
QIE8 calorimeter
220 400 chips
beam pipe
Si strip tracker
e-CAL
h-CAL
muon chambers
Chips to scale 1 cm
Some of the ASICs in CMS
E. Heijne

## Slide 9: Introduction
Rad tolerant ASICs are one of the key enabling technologies of the LHC
In particular, rad hard by design deep sub micron 250nm CMOS played a major role
ASICs will continue to be key components for HL-LHC
However, a number of challenges have to be faced when keeping up with the evolution of the technology

## Slide 10: Challenges for ASICs for HL-LHC
Higher hit rates
Higher radiation hardness
Higher trigger rate or trigger-free operation
Minimise material/power consumption
High dynamic range design in sub-100nm processes
Dealing with pile up – sub ns time stamping

## Slide 11: Moore’s law of pixel readout chips
Chart: CMOS process [nm]
| 600.0 | 250.0 | 250.0 | 130.0 | 130.0 | 65.0 | 250.0 | 250.0 | 250.0 | 130.0
 | 0.013841 | 0.17521 | 0.18182 | 0.56198 | 0.89256 | 1.7578 | 0.07 | 0.02 | 0.06 | 0.2
Clicpix (2013)
Timepix3 (2013)
Medipix3RX (2011)
Timepix (2006)
Medipix2 (2002)
Medipix1 (1998)
FEI4
(2011)
Alice1LHCb
(2000)
FEI3
(2006)
PSI46
(2005)
11
Unfortunately, the cost of a mask set also increases exponentially
X. Llopart, W. Snoeys

## Slide 12: Following Moore’s law @ LHC – some practical challenges
Technical:
  Large variety of transistor devices available
  Large choice of metal stacks
  Increased simulation/layout complexity
  Power density challenge
  Design manual scaling
  Wafer diameter increases to 300mm
Organisational:
  Mask set in 65nm costs are O(CHF1M)

## Slide 13: Some lessons from the first generation of LHC ASICs
The selection of a CMOS process must be based as much on the commercial viability of the foundry/process as on the elegance of the technical solutions it offers. This impacts yield (cost) and long term accessibility.
Collaboration between groups works best if based on a common technology platform
Duplication of design effort - while valuable for training purposes - was probably a little excessive
The choice of readout architecture should allow for short-comings in simulated data.

## Slide 14: Outline
Introduction
Challenges for microelectronics at HL-LHC
Common Foundry access – status
  IBM
  TSMC
IP block sharing
Interconnect
Future technologies

## Slide 15: CERN Supported Technologies in 2014-2015
Legacy technology: IBM CMOS6SF 250nm
Mainstream technology: IBM CMOS8RF 130nm
Alternate technology: TSMC CMOS 130nm
Advance technology: TSMC CMOS 65nm
S. Bonacini, K. Kloukinas

## Slide 16
News on Access to IBM technologies
Commercial contract will be assigned to MOSIS
Favourable pricing conditions (NRE & production runs)
MOSIS guarantees 6 month advance notice in case of a decision to discontinuity the service
Confidential Disclosure Agreements (CDA) remain valid
CERN continues to support the 130nm Mixed Signal Design Kit
Foundry access
  MPWs, Engineering & Production runs via MOSIS
    Design data submitted directly to MOSIS
    Design submission technical support by MOSIS
  Coordination and Purchase orders by CERN
S. Bonacini, K. Kloukinas

## Slide 17: Very recent news on IBM foundry
IBM issued a press release on Monday 20th October announcing that Global Foundries will take over their microelectronics business
IBM will pay $1.5bn over 3 years
For the time being the impact (if any) of this acquisition on our agreement with MOSIS to access the IBM process(es) is unknown

## Slide 18
IBM 130nm supported process and metal stacks
18
STI
poly
M2
M1
M3
LY
E1
MQ
M1
W
M2
M3
MQ
MA
MQ
LY
poly
M2
M1
M3
M1
W
M2
M3
W
E1
MA
passivation
M1
W
M1
W
mimcap
M4
M4
M4
CMOS8RF-DM (3-2-3 BEOL)
95% of designs
CMOS8RF-LM (6-2 BEOL)
Specific mixed signal design kits available for both stacks
More info:
http://support-ictech-mpws.web.cern.ch/support-ictech-mpws/index.htm
M1
M4
MQ
E1
MA
G. Pares. CEA-LETI
S. Bonacini, K. Kloukinas

## Slide 19
IBM 130nm IP blocks available via CERN
Standard cell library from foundry (173 kgate/mm2)
Standard I/O library from foundry
High-density standard cell library (1.5V and 1.2V, 345 kgate/mm2)
LVDS and SLVS drivers/receivers
SRAM generator (40MHz, dual-port synchronous)
eFuse (1- and 8-bit; 3.3V-10mA-burn in <1ms for 8 bits)
Bandgap (current-mode, output 597 ± 4 mV over p,V,T)
ePLL (40, 80, 160 or 320 MHz input and output, 1.2V or 1.5V supply)
eCDR (as ePLL above, but data input and clock output)
ADC (preliminary. 1 kS/s, 12 bit, 32 channels, 1.5V supply, fees apply)
DAC (8-bit, current output, 40nA LSB)
* Blocks are supplied ‘as is’ for HEP experiments
S. Bonacini, K. Kloukinas

## Slide 20: Access to TSMC technologies
Data and technical support
  Institute should contact IMEC to sign an NDA
    IMEC has a list of CERN collaborating institutes
    IMEC will distribute the Mixed Signal design kit and provide users with design kit maintenance and technical support
  No access fees. Pay-per-use scheme.
    A 7% fee is applied on the fabrication cost (prototyping, production).
    This fee covers part of the Mixed Signal Design Kit development and maintenance costs
    Projects that make use of the Mixed Signal Design Kit must seek fabrication services exclusively via CERN and IMEC service
Foundry services
  Institute should contact CERN to inform about submission plans
  CERN will make an effort to coordinate submissions to share prototyping costs
  CERN will issue the purchase orders to IMEC
  CERN will receive the fabricated chips and distribute them to designers
S. Bonacini, K. Kloukinas

## Slide 21: TSMC Non Disclosure Agreement (NDA) and Master Technology Usage Agreement (NDA-MTUA)
3-party NDA: TSMC- IMEC – Institute
  Permitting the distribution of technology information from IMEC to institutes, including layouts of std. cell libraries
  Permitting institutes to exchange technical data and work in collaboration
Covers both 65nm and 130nm processes
Use restrictions:
  automotive applications
  medical applications except for medical imaging systems
  any military applications
  nuclear materials related to defense system or power systems
  aerospace application except fundamental scientific research and dosimetry
Sale of chips is permitted except for banned applications
Export control restrictions
  Comply with all applicable national export control laws, regulations, and rules
  Institutes that will receive silicon from CERN must sign and return to CERN a “Letter of Compliance Concerning Deep-Submicron Technology Circuits”
All NDAs issued by IMEC are identical. Neither IMEC nor the foundry are willing to negotiate 35+ times with all single Institutes
S. Bonacini, K. Kloukinas

## Slide 22: TSMC 130nm supported process and metal stacks
STI
poly
M2
M1
M3
M6
M7
M5
M1
W
M2
M3
M5
RDL
M6
M5
M6
poly
M2
M1
M3
M1
W
M2
M3
W
M7
RDL
passivation
M1
W
M1
W
mimcap
M4
M4
M4
Flavour: CM013G
Mixed Signal option
Transistors: Native (zero-vt), high-, low,
std-Vt devices (+ultra-high)
MIM capacitors (1.5 fF/um2)
MOM capacitors
Ultra-thick metal (UTM)
Triple well / deep n-well
8-inch and 12-inch fabs available
8 metals (5-thin, 1-thick, 1-UTM, RDL)
Closest metal stack to legacy 130nm process (DM 3-2-3)
Metal pitch of TSMC process is different from IBM process !
Mixed signal design kit is under development - delivery expected end of 2014
S. Bonacini, K. Kloukinas

## Slide 23: TSMC 130nm IP blocks (under development)
Submitted June 2014: (to be tested)
  High-density standard cell library (CERN)
  Bandgap, based on DTNMOS (CERN)
Work in progress:
  SRAM generator (CERN)
  ePLL (40, 80, 160 or 320 MHz input and output, 1.2V supply) to be submitted Dec.2014 (CERN)
  Analog buffer, rail-to-rail (NIKHEF)
  SLVS I/O pads (Univ. Sao Paulo)
S. Bonacini, K. Kloukinas

## Slide 24
TSMC 130nm Radiation tolerance measurements
IBM 130nm
TSMC 130nm
Standard NMOS Vt shift
S. Michelis
.1 1 10 100
Dose (Mrad)
0.01 0.1 1 10 100 1000
Dose (Mrad)
DVt (mV)
-160 -120 -80 -40 0
DVt (mV)
-80 -60 -40 -20 0

## Slide 25: TSMC 130nm Radiation tolerance measurements
IBM 130nm
TSMC 130nm
Standard NMOS Off leakage current
Although leakage current peaks at 2MRad (increase of 4 orders of magnitude) this goes back to the nA level after a few hours of room temperature annealing
S. Michelis
0.1 1 10 100
Dose (Mrad)
0.01 1 10 100 1000
Dose (Mrad)
Ileak (nA)
0.1 1 10 100 1000
Ileak (nA)
0.1 1 10 100 1000

## Slide 26
TSMC 130nm Radiation tolerance measurements
IBM 130nm
TSMC 130nm
Standard PMOS Vt shift
The Vth shift for Pmos is limited to 5-30mV at 400Mrad. It seems a bit better than IBM
S. Michelis
0.1 1 10 100
Dose (Mrad)
0.01 0.1 1 10 100 1000
Dose (Mrad)
DVt (mV)
0 20 40 60 80 100
DVt (mV)
0 5 10 15 20 25 30 35

## Slide 27: TSMC 65nm supported process and metal stacks
STI
poly
M2
M1
M3
M5
M6
M4
M1
W
M2
M3
M4
RDL
M5
M4
M5
poly
M2
M1
M3
M1
W
M2
M3
W
M6
RDL
passivation
M1
W
M1
W
mimcap
Two metal stacks
  6+1 metals (“CERN metal stack”)
      4-thin, 1-thick, 1-UTM , RDL
  9+1 metals (compatible with IMEC mini@sic)
      7-thin, 1-thick, 1-UTM , RDL
“Special” metal stacks can be made available
  This will require a one-time-charge of
  15-20KEuro + annual maintenance
  Institutes can always get organized to share
  costs of special PDKs among themselves.
Two standard cell libraries
    9-tracks, standard-Vt
    7-tracks, high-Vt (Low Power)
Mixed-signal design kit is being distributed by IMEC to TSMC-IMEC NDA signatories
S. Bonacini, K. Kloukinas

## Slide 28: TSMC 65nm Radiation tolerance measurements
Vth decrease of 20 mV for low dose level (10 Mrad)
Vth increase of 150 mV for 1 Grad
T = -25°C
T=100°C
T = 25°C
0.01 0.1 1 10 100 1000
Dose (Mrad)
DVt (mV)
-100 0 100 200 300 400
DVt (mV)
-100 0 100 200 300 400
Standard NMOS Vt shift
20 30 40 50 60 Annealing (days)
M. Barbero, J. Christiansen

## Slide 29: TSMC 65nm Radiation tolerance measurements
T = -25°C
T=100°C
T = 25°C
Standard NMOS transconductance
0.01 0.1 1 10 100 1000
Dose (Mrad)
20 30 40 50 60 Annealing (days)
D transconductance (%)
-50 -40 -30 -20 -10 0 10
D transconductance (%)
-50 -40 -30 -20 -10 0 10
M. Barbero, J. Christiansen

## Slide 30: TSMC 65nm Radiation tolerance measurements
+20°C
-15°C
65% max
<30% max
40 days
Standard NMOS Ion
30 days
Pre-irrad
(0Mrad)
1Grad
M. Barbero, J. Christiansen

## Slide 31: TSMC 65nm Radiation tolerance measurements
DVt (mV)
0 100 200 300 400 500
DVt (mV)
0 100 200 300 400 500
20 30 40 50 60 Annealing (days)
0.01 0.1 1 10 100 1000
Dose (Mrad)
T = -25°C
T=100°C
T = 25°C
Standard PMOS Vt shift
M. Barbero, J. Christiansen

## Slide 32: TSMC 65nm Radiation tolerance measurements
0.01 0.1 1 10 100 1000
Dose (Mrad)
20 30 40 50 60 Annealing (days)
D transconductance (%)
-80 -60 -40 -20 0
D transconductance (%)
-80 -60 -40 -20 0
T = -25°C
T=100°C
T = 25°C
Standard PMOS transconductance
M. Barbero, J. Christiansen

## Slide 33: TSMC 65nm Radiation tolerance measurements
<50% max
100% max
+20°C
-15°C
40 days
Pre-irrad
(0Mrad)
1Grad
Standard PMOS Ion
M. Barbero, J. Christiansen

## Slide 34: IP Block sharing
During LHC-1 sharing of blocks was mostly within sub-detector groups or from CERN to outside institutes.
Licensing was based on ‘gentlemen’s agreements’
Significant duplication of effort
RD-53 have agreement between member institutes but limited to RD-53 efforts
For a more general purpose repository there is a need to solve the ‘engineer at the University of Saint-Genis’ problem

## Slide 35: Interconnect technologies
Al wire bonding remains the dominant means of I/O from chips
Flip chip is common on high volume consumer goods
Through Silicon Vias (TSVs)are being used in some special applications (such as smartphone camera assemblies and DRAMs) but such processes are difficult or impossible to access in smaller volumes
TSV-last processing starts to become viable:

## Slide 36: Through Silicon Vias
TSV first – VIAs are drilled prior to the fabrication of the CMOS transitors
TSV middle – VIAs are drilled after CMOS definition (Front End Of Line) but prior to metal definition (Back End of Line)
TSV-last – VIA’s are drilled on finished wafers

## Slide 37: TSV-last from LETI on Medipix3RX
G. Pares. CEA-LETI

## Slide 38: Wafer map before and after TSV processing
J. Alozy

## Slide 39: First TSV plus edgeless Si assembly
J. Alozy

## Slide 40: Future CMOS technologies
Industry is already in production at 16nm
Some upcoming technical challenges:
  28nm - High K metal gates
  20nm - SiGe strained devices
  16nm – FINFETs
HEP specific challenges
  radiation tolerance
  Front end design density
  Access ($$$)

## Slide 41: Future CMOS technologies
Industry is already in production at 16nm
Some upcoming technical challenges:
  28nm - High K metal gates
  20nm - SiGe strained devices
  16nm – FINFETs
HEP specific challenges
  radiation tolerance
  Front end design density
  Access ($$$)
Poly Si gate
1.2nm SiO2
Si substrate
Intel 65nm
Tahir Ghani, Intel

## Slide 42: Future CMOS technologies
Industry is already in production at 16nm
Some upcoming technical challenges:
  28nm - High K metal gates
  20nm - SiGe strained devices
  16nm – FINFETs
HEP specific challenges
  radiation tolerance
  Front end design density
  Access ($$$)
Gate electrode
Hi-K dielectric
Si substrate
Tahir Ghani, Intel

## Slide 43: Future CMOS technologies
Industry is already in production at 16nm
Some upcoming technical challenges:
  28nm - High K metal gates
  20nm - SiGe strained devices
  16nm – FINFETs
HEP specific challenges
  radiation tolerance
  Front end design density
  Access ($$$)
SiGe
SiGe
Source
Drain
Gate
Tahir Ghani, Intel

## Slide 44: Future CMOS technologies
Industry is already in production at 16nm
Some upcoming technical challenges:
  28nm - High K metal gates
  20nm - SiGe strained devices
  16nm – FINFETs
HEP specific challenges
  radiation tolerance
  Front end design density
  Access ($$$)
Tahir Ghani, Intel

## Slide 45: Conclusions
Microelectronics technologies are one of the foundation technologies for present and future HEP experiments
As a community we are best served by using a limited number of common platforms
65nm CMOS is becoming a new ‘hard’ node
We could (and must) get better organised for IP block sharing
New interconnect approaches might provide novel solutions for detector and module design

## Slide 46: Thanks for your attention!
S. Procz