## Slide 1
Avinash Joshi1, L. M. Pant2 & A. K. Mohanty2
1Alpha Pneumatics, Thane, Maharashtra
2Nuclear Physics Division, Bhabha Atomic Research Centre, Mumbai
Reactive Ion Etching of GEM foils

## Slide 2
The Triple GEM for the CMS Muon System

## Slide 3
Present process of GEM foils making involves Photolithography and Chemical / Electrochemical etching of copper and polyamide layers
Uniformity and reproducibility of etching are governed by :
Rate of a chemical reaction : function of ratio of activities (Concentration)
of reactants to products
Transport factor : ratio of partial pressure of a reactant
reaching the surface through boundary layer
to the partial pressure of reactant in gas mix
Activity at reaction surface : function of diffusivity of Reactant Species
(inward) and Products Species (outward)
through the boundary layer
Flow of reactants & products : across boundary layer is controlled by the
thickness of boundary layer.
Present GEM fabrication process

## Slide 4
Reactant and products are in liquid state
Reaction rates are highly sensitive to temperature and concentration of reacting species
Solvent is needed to activate and transport the reacting species
Boundary layer is thick and the layer thickness is few microns
The supply of the reacting species to the reaction surface becomes lesser as the holes become deeper
This problem becomes very prominent when hole diameter is nearer to boundary layer thickness
Inner surface of the etched hole has undercutting, because of isotropicity
Disadvantages of Liquid Etching

## Slide 5
Gas Phase reaction - clean and precise
Features having Very Large aspect ratio can be etched
Photo-resist mask can be removed by Ashing under O2 plasma
Instant Change of etchants by switching gases through MFC control channels
Galvanic protection possible to avoid over-etching of front copper layer.
Etch process can be sequenced and programmed to etch multiple layers, in succession
End point detection by OES (optical emission spectroscopy) is possible
Surface passivation of exposed etched surface by oxygen plasma
Excellent control over Differential etch rate between Copper and Polyimide
DC bias : controlled ion energy for directional etching
Very little undercutting
It is possible to etch copper and Kapton in – situ
Plasma Etching : Advantages over Liquid Etching

## Slide 6
1) RF Power density
2) Gas Mixture component types
3) Gas mixture Ratio
4) Pressure
5) Substrate Temperature
6) Electrode spacing : 19 mm with GEM foil at ground
Plasma Etching : Process variables

## Slide 7
Plasma Etching at Alpha Pneumatics, Thane Factory
RF Supply @ 13.56 MHz
RF matching network
(capacitively coupled plasma)
457 mm
175 mm
Tuning the plasma
Process Chamber with
Pirani Gauge & Baratron
Applied
Power (W)
Reflected
Power (W)

## Slide 8
with O2 (100%) with SF6 (100%)
RF Plasma at 0.4 to 1.0 Torr : 19 mm electrode spacing

## Slide 9
SEM photograph of plasma etched silicon grooves with large aspect ratio (L/a)
a = 15 m
L = 90 m

## Slide 10
Etch rate of polymide versus SF6 concentration in O2
Ref : “Dry Etching of Polyimide in O2-CF4 and O2-SF6 Plasmas” Guy Turban and Michel Rapeoux , Journal of Electrochem. Soc. Solid State Science and Technology, p 2231-2236, Nov. 1983

## Slide 11
Chart: 
| 0 | 8 | 20 | 30 | 45 | 60 | 80 | 90 | 100
Reference | 0.1 | 0.3 | 0.5 | 0.3 | 0.5 | 0.6 | 0.5 | 0.3 | 0.1
Experimental | 0 | 0.2 | 0.3 | 0.2 | 0.3 | 0.4 | 0.3 | 0.2 | 0.05
Etch rate of polymide versus SF6 concentration in O2
Ref : “Dry Etching of Polyimide in O2-CF4 and O2-SF6 Plasmas” Guy Turban and Michel Rapeoux , Journal of Electrochem. Soc. Solid State Science and Technology, p 2231-2236, Nov. 1983
Etch Rate : m / min 
percentage of SF6 in O2 

## Slide 12
Gas Pressure : 0.6 torr
For Polyimide (Kapton)
a) SF6 : 6.0 SCCM (20%)
b) O2 : 24.0 SCCM (80%)
c) RF Power Density : 0.6 to 1.2 W/cm2
d) Maximum Etch Rate Achieved : 0.3 m/min
For Copper
a) SF6 : 24.0 SCCM (80%)
b) O2 : 6.0 SCCM (20%)
c) RF Power Density : 0.6 to 2.0 W/cm2
d) Maximum Etch Rate Achieved : 0.05 m/min
e) Substrate Temp : 25OC/Start, 35OC/End
f) Duration : 10.0 min
Etching Parameters

## Slide 13
Courtesy : Shuvendu, ASD-BARC
P0
Rejected Polyimide foil from CERN with
Cu already patterned at 70 m diameter
50 m of polyimide
5 m of Cu
100 nm of Chromium
70 m diameter in Cu
SEM view
70 m
140 m

## Slide 14
 18 m deep trench in Polyimide in 48 minutes
under SF6 (20%) + O2 plasma
SEM view
Glass
Mask
Polymide

## Slide 15
Courtesy : Shuvendu, ASD-BARC
P9
 24 m deep trench in Polyimide in 60 minutes under SF6 (20%) + O2 Note , there is no undercutting
SEM view
50 m of polyimide
5 m of Cu
100 nm of Chromium
70 m diameter in Cu
24 m

## Slide 16
50 m of polyimide
5 m of Cu
100 nm of Chromium
70 m diameter in Cu
30 m
Courtesy : Shuvendu, ASD-BARC
 30 m deep trench in Polyimide in 60 minutes
under SF6 (20%) + O2 plasma
SEM view

## Slide 17
Polyimide etched to a depth of 50 m in 120 minutes
under SF6 (20%) + O2 plasma
50 m of polyimide
5 m of Cu
100 nm of Chromium
70 m diameter in Cu
45 m

## Slide 18
EDAX measurement of surface chemistry showing
presence of Cu and Cr in the bottom layer
5 m of Cu
70 m diameter in Cu
50 m of polyimide
100 nm of Chromium

## Slide 19
EDAX measurement of surface chemistry showing
absence of Cr in the bottom layer
reverse concentration : SF6 (80%) + O2 (20%) flash for a couple of minutes
5 m of Cu
70 m diameter in Cu
50 m of polyimide
100 nm of Chromium

## Slide 20
Etching of Copper on Polyimide
SF6 (90%) + O2
Cu intact
due to mask
Cu intact
due to mask
0.2 m of Cu
etched from
unmasked surface

## Slide 21
5 m etching of Copper on Polyimide (5000 X)
SF6 (90%) + O2
Courtesy : Shuvendu, ASD-BARC
Cu
Polymide
SEM view
Glass
Mask

## Slide 22
1) Cl2 gives better results than SF6
2) With SF6 + O2 mixture, higher surface temperature
(214OC) is required to evaporate the products
3) Etch rates of 0.5 m/min (x10)have been achieved
under Cl2 + O2 plasma and UV irradiation
Cl2 as an alternative to SF6

## Slide 23
Artwork and Mask making : Image of GEM foil mask

## Slide 24
Artwork and Mask making : 1/100th part of artwork
Drawing prepared in Auto Cad 2004 platform
Front and Back side contact /proximity masks
Total 591000 elements per mask
Single reticule of 185 mm x 175 mm size
Present Status :
Artwork prepared by us, which has been okayed by CERN
We are in touch with emulsion mask makers from US and commercial negotiations are going on to prepare emulsion and chrome type contact masks.

## Slide 25
An etch rate of 0.5 m/min for Polymide and 0.05 m/min for Cu has been demonstrated
Possible modifications / Etchants for future RIE processes for GEM
Gases : SF6, CF4 , O2 ,CH2FCF3 (R134a) , Cl2, Argon and Nitrogen, Organometallics
SF6 and CF4 more suitable than R134a as Fluorine yield is significantly higher
Cl2 and O2 plasma etch copper but does not affect Polymide
SF6 and O2 plasma etch PMMA but does not affect copper but etch rate is very poor
Power density of 0.5 Watt/cm2 is adequate
CCP or ICP methods can be used for large area
Process of RIE under UV radiation to facilitate CuClx evaporation
We are using CCP technique (@13.56 MHz)
Summary and Outlook

## Slide 26
1) “Dry Etching of Polyamide in O2-CF4 and O2-SF6 Plasmas”
Guy Turban and Michel Rapeoux , Journal of Electrochem. Soc. Solid State Science and Technology pp2231-2236 Nov. 1983
2) “ Dry Etching of Copper Using Plasma” by Kejun Xia
Semiconductor TCAD Lab. Auburn University, AL,
Oct 19, 2003
3)“Plasma etching of copper films at low temperature”
P.A.Tamirisa et al , Microelectronic Engineering, Volume 84, Issue 1, January 2007, Pages 105–108
References

## Slide 27
Dr. Padmakar Tillu for providing high purity SF6 gas
Dr. S.C.Purandare (DCMP – TIFR) for SEM studies
Shivendu (ASD-BARC) for optical images
Acknowledgements