## Slide 1
Target and Ion Source Development
Report 2014
Alexander Gottberg
Target Materials
  UCX
  LaC (n-def. Ba, Cs, In, Xe)
  TiC (n-def. K, Sc, Ca)
  MWC nanotubes (B, Be)
  LiF:NaF (Ne, C, O)
Target Concepts
  Liquid Salt (diffusion of Ne)
  Liquid Loop Targets (LIEBE)
  Boron Beams
  Combining VADIS and RILIS

## Slide 2
Target Materials

## Slide 3: ISOL Target Materials
Germanium (Ge)
Tin (Sn)
Ce3S4
TeO2:KCl:LiCl
NaF:LiF
Lead (Pb)
Lead-Bismuth (Pb:Bi)
Gold (Au)
Lanthanum (La)
Lanthanum:Thorium alloy
Lanthanum:X alloys
Uranium-Chromium
Bismuth (Bi)
Praseodymium (Pr)
Neodymium (Nd)
Terbium (Tb)
Gd:Cu
Er:Cu
Pr:B
Uranium (U)
ThF4:LiF
Titanium (Ti)
Niobium (Nb)
Zirconium (Zr)
Tantalum (Ta)
Tungsten (W)
Molydenum (Mo)
Iridium (Ir)
Vanadium (V)
Hafnium (Hf)
Silicon layers (Si)
Thorium layers (Th)
Thorium/Niobium (Th/Nb)
Tin/Graphite (Sn/C)
Platinum/Graphite (Pt/C)
Plutonium (Pu)
ISOL Target Materials
Solid Metals
Carbides
Others
Molten
Oxides
Uranium Carbide (UCx) *
Carbon (C) *
Aluminium Carbide (Al4C3)
Calcium Carbide (CaC2)
Lanthanum Carbide (LaC2) *
Thorium Carbide (ThC2)
Silicon Carbide (SiC) *
Titanium Carbide (TiC) *
Vanadium Carbide (VC)
Scandium Carbide (ScC2)
Zirconium Carbide (ZrC)
Gadolinium Carbide (GdCx)
Curium Carbide (CmCx)
Beryllium Oxide (BeO)
Magnesium Oxide (MgO)
Aluminium Oxide (Al2O3) *
Calcium Oxide (CaO) *
Yttrium Oxide (Y2O3) *
Cerium Oxide (CeO2)
Thorium Oxide (ThO2) *
Hafnium Oxide (HfO2) *
Zirconium Oxide (ZrO2)
Barium Oxide (BaO)
Titanium Oxide (TiO2) *
Strontium Oxide (SrO)
Lanthanum Oxide (La2O3)
Uranium Oxide (UO2)
BaB6
BaZrO3
CeB6
CeS
Zr5Ge3
Hf3Si3
Hf5Ge3
Hf5Sn3
Ta5Si3
CaB6
BN
CeS
Zr5Si3
Zr5Ge3
AlN
Na-zeolite
Ca-zeolite
Tl-zeolite
commonly or recently used at ISOLDE
* engineered advanced micro or nano structure

## Slide 4: UCx as Benchmark for ISOL-Facilities Worldwide
Chart: 
| Ta | Ti | Y2O3 | UC | HfO | Pb | CaO | ZrO | ThC | Sn | Ir/Ta/W | SiC
 | 42 | 9 | 30 | 396 | 6 | 21 | 39 | 15 | 27 | 15 | 6 | 12
Actinide targets at ISOLDE in 2011 (2010)
249 shifts out of 396  68% of total (72%)
13 new units (12 new, 2 old)
FLUKA production rates in UC2 by 2 μA X 1.4 GeV protons [1/s]
1· 1010
1· 1012
1· 1011
1· 109
1· 108
1· 107
1· 106
1· 105
1· 104
1· 103
1· 102
1· 101
Neutrons
Protons

## Slide 5: UCx Post-Irradiation Studies
Post-irradiation analysis:
First analysis of an irradiated UCX target in the history of ISOLDE (important to understand ageing processes and for upcoming waste campaign)
Opening target unit #466 (8.8∙1018 protons in 2011) in inert-gas hot-cell at PSI, 19 mSv/h on contact with Ta beam window
2µm
before irradiation
after irradiation
Pellets appear macroscopically unchanged
Microscopic evolution of pore distribution and grain size under irradiation observable
500 µSv/h on contact with single pellet
Further results of synchrotron investigations under analysis
Ceramography and electron micro-probe analysis on-going

## Slide 6
two orders of magnitude
Composing a Recipe for Nano-Grained UO2
Synthesis of de-novo designed uranium carbide matrixes:
Different microstructures, densities, grain sizes, crystal structures tested → tailor-made matrix:
Suspension grinding of UO2 powder to 160 nm average particle size
Wet-mixing with multi-walled carbon nanotubes
Ultrasound drying of mixture and pressing to 1.6 g/cm3 pellets
Fast reactive sintering to mixed uranium carbide in carbon nanotube matrix
30Na yield evolution under irradiation
Online tests in November

## Slide 7: Small Grain Target Materials – so far...
  The ideal target material, for release of, alkali, alkaline-earth and noble gases, was defined:
  Nanometric/submicron grain size
  High porosity (>30%)
  Macroporosity (>100nm)
  No closed porosity
  Sub-micrometric SiC showed improved release rates of short-lived Mg
  1-50 µm SiC considered in the past as a useless target material in terms of release
  Uranium carbide targets are, by far, the most used at ISOLDE.
  Very porous structure (75%)
  Much less prone to sinter than conventional UC2 targets (micrometric UC2 + Graphite)
  Release rates on many isotopes improved.
Sub-micron Silicon Carbide
Uranium Carbide – CNT Composite
𝑈𝑂2+6𝐶→𝑈𝐶2+2𝐶+2𝐶𝑂
T. Stora, S. Fernandes, S. Mathot, and P. Bowen, “Nanostructured Target for Isotope Production,” WO 2010/034364 A12010.
Patent
  UO2 (120 nm) + MWCNT
Calcium Oxide
up to 1800oC
UO2 (micron sized) milled
Three more this year…

## Slide 8: LaC2–MWCNT Spallation Target Material
La(OH)3 particle size reduction by suspension grinding
FLUKA Production Yields
after comparing all RE as possible spallation target nuclei
Lanthanum Hydroxide Nanopowder
Ultrasound-Dispersed Multi-Walled Carbon Nanotubes
2 µm
500 nm
2 µm
200 µm
LaC2-MWCNT Nano Composite (After Carbo-Thermal Reduction)
Microstructure of UC2-MWCNT nano composite currently under investigation
After 10 days at 1900°C
After 10 days at 1900°C
Online tests in November
J. Guillot, et al.

## Slide 9: Titanium Carbide-Carbon Composites Results of TiC nanostructural studies
Mixing TiC and Carbon (different vol. ratios)
TiC + MWC nanotubes
Test for nanostructure stability at 1500, 1650 and 1800oC
TiC + Carbon black
TiC +Graphite
Main quality parameters:
High surface area
High porosity (>30%)
Nanometric TiC grains
Keep these parameters at the highest possible temperature
Fast diffusion and release of exotic isotopes
J.P. Ramos, et al.

## Slide 10: Titanium Carbide-Carbon Composites Release studies and target prototype
The three most promising material nanostructures were selected, irradiated and are studied in terms of release.
TiC + Carbon black (50 vol.%) nanostructure, which was stable up to 1800oC, was selected to produce a full target prototype.
Target going online Today
J.P. Ramos, et al.

## Slide 11
Production of Boron Beams

## Slide 12: Boron Beams Offline
Determination of suitable target operation parameters
6%: 7Li (1.015MeV + α (1.777MeV)
94%: 7Li (0.840MeV + α (1.470MeV) +γ(0.478MeV)
10B+n0
Release studies from different materials using neutron activation
Ch. Seiffert, et al.

## Slide 13: Boron Online
Target unit #499:
  Target material: MWNCT, ρ=0,43 g/cm3
  Standard Ta container, cold transfer line, VADIS ion source
  Injection of SF6 into container, leak rate= 0,37*10-4 mbar*l/s, p(SF6)=0.8-1.8 bar
Determination of release of 8B using positron annihilation & ISOLTRAP’s MR-ToF:
  Activity below detection (~7*101 1/uC) limit on masses of 8BFn+ (n=1,2,3) or BOF
  Activity measured on mass 8 originating from 8Li (8He) and a positron emitter
  Positron activity corresponds to 3*102 1/uC
  Proof that activity originates from 8B still pending
Ch. Seiffert, et al.

## Slide 14
Target Concepts

## Slide 15: Molten Salt Target
Beta Beams: proposal of neutrino oscillation physics facility:
Production of pure (anti)-νe beams by storing β emitting ions in a decay ring
Proposal inspired from 18F production for PET imaging:
NaF target loop (23Na(p,X),19F(p,2n)18Ne)
Rates of 1013 18Ne/s are predicted exploiting 1 MW, 160 MeV proton beam
……….
……….
……….
Pump
Heat
Exchanger
Protons
7 mA, 160 MeV
18Ne 1013/s
Transfer line to ion source
Irradiation chamber
Diffusion chamber
NaF:LiF
700ºC
21.6 cm
P. Zuchelli, Phys. Lett B 532 (2002) 166
T. Stora, CERN Yellow Report, CERN-2010-003
T.M. Mendonca et al., NIMB 329 (2014) 1
T. Mendonca, et al.

## Slide 16: Determination of the Diffusion Coefficient of Ne In NaF:LiF
D(Ne) in NaF:LiF ~10-9 m2/s
D(Ne) essential in determination of production rates and dimensioning of the diffusion chamber
Release favoured by smaller sizes
96% release for 100 µm droplet
D(Ne) in NaF:LiF is 8 orders of magnitude higher than oxide targets (CaO, Al2O3 with D~10-17 m2/s)
T. Mendonca, et al.

## Slide 17: LIEBE Project (Liquid Lead-Bismuth Eutectic loop for EURISOL)
LIEBE Project Design Report, June 2014
LIEBE target proposed design
(LIEBE Design Study Report)
Irradiation chamber
Diffusion chamber
Heat exchanger
Fill and drain reservoir
Electromagnetic pump
Compatibility with the ISOLDE Front-end
T. Mendonca, et al.

## Slide 18: Hg Diffusion Study (Liquid Target)
Improvement of diffusion with temperature
177Hg (T1/2= 130 ms) as reference:
  Increasing droplet radius will decrease the released fraction
  Diffusion efficiency of 38% for 100 ms, 44% for 200 ms in the diffusion chamber
T. Mendonca, et al.
Static units
PbBi shower – Offline tests @ ISOLDE, June.2014
Data collection on droplet size, 0.1 mm holes
Metallic grid for material fragmentation in the diffusion chamber

## Slide 19
Ion Source Development

## Slide 20: VADIS and RILIS
Drawbacks of hot-cavity laser ion sources
Surface ionized contamination
- long standing issue but no universal solution has been found
Limited ion capacity (~ 1 uA)
- possible issue for EURISOL, ISOL@MYRRHA etc.
Not currently suitable for liquid targets
Limited scope for non-standard RILIS applications
Modified (2.5 mm diameter entrance aperture) VADIS + Ga mass marker
T.D. Goodacre, et al.

## Slide 21: VADLIS Offline Tests
T.D. Goodacre, et al.

## Slide 22: VADIS + RILIS Online with Liquid Pb Target
These measurements were obtained with a standard VADIS under normal operating conditions
 More optimization possible
T.D. Goodacre, et al.

## Slide 23: Collaboration and Acknowledgement
Thank you for your attention!
The team:
Thierry Stora
Tania Mendonça
João-Pedro Ramos
Christoph Seiffert
Melanie Delonca
EN-STI-RBS
Richard Catherall
Tim Giles
Stefano Marzari
Ana-Paula Bernardes
Recent Collaborators:
Peter Kunz (TRIUMF)
Friedhelm Ames (TRIUMF)
Aurelia Laxdal (TRIUMF)
Pierre Bricault (SCK CEN)
Antonio Gonçalves (CTN)
Ulli Köster (ILL)
Hans Fynbo (Aarhus)
Adam Stevenson (Saint-Gobain)
Christophe Lau (IPNO)
Sandrine Tusseau (IPNO)
Brigitte Roussiere (IPNO)
RILIS:
Valentin Fedosseev
Bruce Marsh
Sebastian Rothe
Tom Goodacre
Daniel Fink
Daniel Grolimund
Matthias Martin
Claude Degueldre
Alberto Andrighetto (INFN)
Stefano Coradetti (INFN)
Hanna Frånberg (GANIL)
Pierre Delahaye (GANIL)
Johanna Grinyer (GANIL)
Ana Senos (University Aveiro)
Susanne Kreim (CERN)
Alexandre Dorsival (CERN-RP)
… and many more
Machine shop:
Bernard Crepieux
Micheal Owen
Ermanno Barbero