## Slide 1: Development of a new technology for the next generation of 3D Pixel Sensors for HL-LHC within the INFN (ATLAS-CMS) R&D program in collaboration with FBK
Sabina Ronchin
S. Ronchin TREDI 2015

## Slide 2
  A lot of experiments require thin detectors, but are thin 3D feasible?
  Key point:
    Too thin (or thinned) 6-inch wafers are not suitable to process
    from double sided process to single side process
    on “special” wafers...
Introduction
S. Ronchin TREDI 2015

## Slide 3
Are thin 3D feasible ?
G. Pellegrini et al., NIMA 604 (2009) 115
  Local thinning
  Single side
  Processing thicker wafers with local thinning of sensor active areas by DRIE (1) or TMAH (2) could be done
  Back end process:
  thinning the processed wafers
  Single side
  “special” wafers: Epi, SOI, Si-Si…
  After bump
1.
2.
S. Ronchin TREDI 2015
Two possible technological approaches

## Slide 4
FBK past experience on back end process: edgless technology
Trench filled with polisilicon
S. Ronchin TREDI 2015
SOI (200um Fz) ATLAS
Epi
PANDA
ALICE
Device separation along the trenches
thin n+ epi-layer
Substrate
thinning (by IZM)

## Slide 5
Thin Si3D: proposed fabrication approach
Thin silicon HR-p-type active layer (100-150 m)
Ohmic columns depth > device wafers
Junction columns depth < device wafers
Compatible with edgless
p++ LR Si
p+ HR Si
S. Ronchin TREDI 2015
Single side process with support wafer

## Slide 6
S. Ronchin TREDI 2015
Most critical issues
  Identify the “best” row material
    We need a “processable” thin silicon substrate (100-150 m)
  Controls of the hole depth
    Optimization of DRIE process
  Doped Polysilicon Filling
    Hole must be filled or partially filled
  Two DRIE on the same wafer side
  Deep SiO2 etching

## Slide 7
  Identify the “best” row material
Two possibilities:
  Epi or Si-Si
  SOI
Under bump metallization
Support wafer thinning (removal)
back-side metal deposition
p++ low Wcm wafer
200 nm Silicon oxide
p+ high Wcm wafer
p++ low Wcm buried region
p++ low Wcm wafer
p+ high Wcm wafer
100-150m
100-150m
S. Ronchin TREDI 2015
Thin silicon with support wafer

## Slide 8
Thin Si3D: the two technological options
p++ LR wafer
p+ HR wafer
p++ LR wafer
p+ HR wafer
S. Ronchin TREDI 2015
Epi or Si-Si wafer
SOI wafer
Ohmic columns must be passing through the bonding oxide

## Slide 9
Planar test run on Si-Si to test available wafers
Wafers
Si-Si Icemos silicon wafers, 100±2m and 130±2m active material with a ρ>3000 Ωcm
Process
n-on-p planar process
three p-spray doses
Layout
Many test structures
10 ATLAS & 30 CMS pixel design
ATLAS
CMS
Test Devices
S. Ronchin TREDI 2015

## Slide 10
FBK test diode IV measurements
Circular 4mm2 diode with two GR
Jleak distributions on 135 diodes
Guar Ring I rev on 3 wafers
3 p-spray dose
Low Medium High
S. Ronchin TREDI 2015
J leak [nA/cm2]

## Slide 11: Test diode: CV measurements
Concentration profile from CV
Doping 1 – 3 E12
Thickness about 10micron less than the nominal value
Vdep 16V and 20V
S. Ronchin TREDI 2015

## Slide 12
ATLAS FEI4
CMS
CMS without Bias Grid
Pixel detectors: IV measurements on W81
Comments:
40 devices (10Atlas + 30CMS)
Some defective devices
V BK > 100V
I leak decrease if detectors area decrease
only a small part of the detectors is depleted
S. Ronchin TREDI 2015

## Slide 13
Pixel detectors: statistics
“good” detectors if
ATLAS Ileak < 1E-7 @ 50V
CMS Ileak < 5E-8 @ 50V
V depl 20V
ATLAS 70/100
(70%)
CMS 257/270 (95%)
S. Ronchin TREDI 2015

## Slide 14
S. Ronchin TREDI 2015
Most critical issues
  Identify the “best” row material
    We need a “processable” thin silicon substrate (100-150 m)
✓
p++ LR wafer
p+ HR wafer
  Doped Polysilicon Filling
    Hole must be filled or partially filled
  Two DRIE on the same wafer side
  Deep SiO2 etching
  Controls of the hole depth
    Optimization of DRIE process

## Slide 15
155 m
4.7m
3.4 m
TSV deeper than 130 m
Holes with =5 m
S. Ronchin TREDI 2015
  Controls of the hole depth (1)
    Optimization of DRIE process

## Slide 16
S. Ronchin TREDI 2015
5.3 m
5.3  m
117 m
Not TSV shallower than 130 m
Holes with =5 m
  Controls of the hole depth (2)
    Optimization of DRIE process

## Slide 17
S. Ronchin TREDI 2015
5.3 m
5.5  m
88 m
Not TSV shallower than 100 m
Holes with =5 m
  Controls of the hole depth (3)
    Optimization of DRIE process

## Slide 18
S. Ronchin TREDI 2015
Most critical issues
  Identify the “best” row material
    We need a “processable” thin silicon substrate (100-150 m)
  Controls of the hole depth
    Optimization of DRIE process
  Doped Polysilicon Filling
    Hole must be filled or partially filled
  Two DRIE on the same wafer side
  Deep SiO2 etching
✓
✓

## Slide 19
S. Ronchin TREDI 2015
4m Poly-Si
5.3m
1m
Poly-Si filling of a 5 m hole
  Doped Polysilicon Filling (1)
    Hole must be filled or partially filled

## Slide 20
S. Ronchin TREDI 2015
4m Poly-Si
12.5m
4.5m
The photoresist
closes the hole
Poly-Si filling of a 12 m hole
  Doped Polysilicon Filling (2)
    Hole must be filled or partially filled

## Slide 21
S. Ronchin TREDI 2015
Most critical issues
  Identify the “best” row material
    We need a “processable” thin silicon substrate (100-150 m)
  Controls of the hole depth
    Optimization of DRIE process
  Doped Polysilicon Filling
    Hole must be filled or partially filled
  Two DRIE on the same wafer side
  Deep SiO2 etching
✓
✓
✓

## Slide 22
14µm
Reducing the hole diameter with a polysilicon deposition
S. Ronchin TREDI 2015
Picture from the surface
with photresist after second DRIE
SEM image
  Two DRIE on the same wafer side
First holes
partially filled
with poly-Si

## Slide 23
S. Ronchin TREDI 2015
Most critical issues
  Identify the “best” row material
    We need a “processable” thin silicon substrate (100-150 m)
  Controls of the hole depth
    Optimization of DRIE process
  Doped Polysilicon Filling
    Hole must be filled or partially filled
  Two DRIE on the same wafer side
  Deep SiO2 etching
✓
✓
✓
✓

## Slide 24
200 µm Si
200 nm SiO2
2 m poly
Photoresist
2 m poly-Si
200 nm etched SiO2
S. Ronchin TREDI 2015
  Deep SiO2 etching

## Slide 25
S. Ronchin TREDI 2015
Most critical issues
  Identify the “best” row material
    We need a “processable” thin silicon substrate (100-150 m)
  Controls of the hole depth
    Optimization of DRIE process
  Doped Polysilicon Filling
    Hole must be filled or partially filled
  Two DRIE on the same wafer side
  Deep SiO2 etching
✓
✓
✓
✓
✓

## Slide 26
Conclusions
Designed a new technology for 3D single side detectors on thin material
Settled most process critical issues
Validation of acquired Si-Si material
Ready to start a new 3D batch!!!

## Slide 27: Thanks for your attention
S. Ronchin TREDI 2015