## Slide 1
Photocathode Research using Facilities at Daresbury Laboratory:
Progress Report
Sonal Mistry
Loughborough University, STFC ASTeC

## Slide 2
Motivations for Research
Research Equipment
Results & Discussion
Future Plans
Overview

## Slide 3
VELA
Photoinjector consists of 2.5 cell S-band RF gun
Cu photocathode:
Quantum Efficiency = 1 x 10-5
Motivations
CLARA
1.5 cell high repetition rate gun
Interchangeable photocathode
Interest in investigating alternative metal to copper
Investigate applicability of metals to deliver ultra high brightness beams

## Slide 4: Photocathode Research Equipment
SAPI - Surface Analysis/Preparation Installation
ESCALAB-II – Surface analysis facility
TESS – Transverse Electron Energy Spread spectrometer

## Slide 5: Photocathode Research Techniques
Photoelectron
1s
2s
2p
X-ray
XPS
Kelvin Probe
Sample
Probe
Vs
+++++++++++++++
- - - - - - - - -
QE
hν
e-
e-
e-
e-
e-

## Slide 6: Photocathode Research Techniques
Argon Ion Sputtering
Plasma Cleaning
Annealing

## Slide 7: Experimental Procedure
11
1st Experiment Aim:
To identify metal photocathodes with reasonable QE
A survey of a 10 bulk metals, chosen because:
Widely used in photoinjectors
Low work function
Vacuum compatibility
Zirconium
Vanadium
Titanium
Lead
Niobium
Magnesium
Aluminium
Silver
XPS survey spectra for cleaned metal photocathodes
Notes: Preparation procedure
Took metals and cleaned and took xps analysis

## Slide 8: Results: Ar+ sputter
Metal | QE (%) | XPS for sample surface(%) O 1s C 1s | Work Function (eV)
Al Received Ar+ sputter | 9.5E-6 2.2E-5 | 36.8 38.3 13.4 17.4 | 4.0 4.9
Ag Received Ar+ sputter | 8.5E-6 5.1E-5 | 0 59.4 0 0 | 5.1 5.1
Cu Received Ar+ sputter | 5.0E-6 1.1E-5 | 32.9 66.2 0 0 | 5.4 5.3
Mg Received Ar+ sputter | 6.0E-6 1.7E-3 | 35.2 52.3 40.0 0 | 3.4 3.4
Mo Received Ar+ sputter | 1.47E-7 2.48E-6 | 24.2 64.9 7.8 17.8 | 5.1 5.2
Metal | QE (%) | XPS for sample surface (%) O 1s C 1s | Work Function (eV)
Nb Received Ar+ sputter | 3.9E-7 1.9E-4 | 47.8 48.6 16.2 21.0 | 5.3 4.7
Pb Received Ar+ sputter | 2.9E-5 2.4E-4 | 43.9 34.8 0 0 | 4.6 4.7
Ti Received Ar+ sputter | 0 3.3E-4 | 39.2 53.6 14.6 16.8 | 4.7 4.5
V Received Ar+ sputter | 1.4E-6 2.2E-5 | 45.7 45.9 25.0 0 | 5.5 5.0
Zr Received Ar+ sputter | 3.88E-6 2.89E-4 | 48.4 44.1 14.4 0 | 4.4 4.3
12
Notes: Discuss results. BUT how long does it last for??

## Slide 9: O2 plasma cleaning and post annealing
VELA Cu photocathode prepared by:
O2 plasma cleaning
  Removes carbon
  Leaves thin oxygen layer
Annealing
  Oxygen dissolves into bulk
Second experiment applies this cleaning procedure to the metals identified in the first experiment.

## Slide 10: Results: O2 plasma cleaning
Metal | QE (%) | XPS for sample surfaces (%) O 1s C 1s | Work Function (eV)
Ti O2 plasma Anneal 250°C (0.5 hr) Anneal 250C (24 hr) | 0 6.32E-5 1.16E-4 | 87.1 5.1 88.3 4.5 79.9 9.0 | 5.8 4.5 4.3
Zr O2 plasma Anneal 250°C (0.5 hr) Anneal 250°C (24 hr) | 3.82E-7 6.94E-5 1.35E-4 | 78.4 12.4 83.5 3.9 74.6 9.8 | 4.9 4.3 4.8
Mg O2 plasma Anneal 200°C (0.5 hr) Anneal 200°C (4 hr) Anneal 200°C (24 hr) | 3.82E-7 2.40E-5 4.90E-5 7.09E-5 | 83.5 3.2 76.8 3.5 67.8 9.4 66.7 3.8 | 4.4 3.9 3.7 3.6
Metal | QE | XPS for sample surfaces (%) O 1s C 1s | Work Function (eV)
Cu O2 plasma Anneal 250°C (0.5 hr) | 0 1.6E-4 | 80.1 3.1 76.7 6.5 | 5.7 5.7
Nb O2 plasma Anneal 300°C (0.5 hr) | 5.21E-7 1.34E-4 | 87.5 5.7 80.2 6.3 | 5.7 4.5
Pb O2 plasma Anneal 160°C (0.5 hr) Anneal 200°C (0.5 hr) | 3.47E-7 6.94E-6 1.67E-5 | 82.1 7.1 77.9 10.9 77.8 9.9 | 5.6 4.3 4.5
Measurements for Ti, Zr, Mg, Cu, Nb, Pb:
O2 Plasma Cleaned for 20 minutes
Annealed
13

## Slide 11: Results: O2 plasma cleaning
x 10
3
0
10
20
30
40
50
60
CPS
970
965
960
955
950
945
940
935
930
925
Binding Energy (eV)
x 10
4
0
2
4
6
8
10
12
14
CPS
970
965
960
955
950
945
940
935
930
925
Binding Energy (eV)
x 10
2
0
10
20
30
40
50
60
CPS
970
965
960
955
950
945
940
935
930
925
Binding Energy (eV)
Cu 2p3/2
Cu 2p1/2
Satellite
Satellite
Metal | QE | XPS (%) O 1s C 1s
Cu Received O2 plasma Anneal 250°C | 4.2E-6 0 1.6E-4 | 40.4 59.0 80.1 3.1 76.7 6.5
14
CuO
Cu2O
Cu region as received
CuO
Cu 2p3/2
Cu 2p1/2
Satellite
Satellite
Cu 2p3/2
Cu 2p1/2
Cu region oxygen plasma cleaned
Cu region oxygen plasma cleaned and post annealed

## Slide 12: Results: Ar plasma cleaned
Argon plasma treatment is just as effective in removing C 1s from the sample surfaces
QE obtained for oxygen plasma treatment and post anneal is greater than that obtained with argon plasma treatment for all samples
15

## Slide 13: Thin Films Photocathodes
Metal thin film | QE (%) | XPS for sample surfaces (%) O 1s C 1s | Measured  (eV)
Cu Received Heated 250°C Repeat | 1.47E-6 1.14E-4 1.17E-4 | 23.5 67.8 20.2 61.7 17.9 62.0 | 5.1 4.9 4.7
Nb Received Heated 250°C Heated 300°C Ar+ sputter | 7.75E-7 2.45E-5 5.66E-6 2.64E-4 | 63.1 25.3 61.5 4.3 55.8 15.9 9.6 0 | 4.4 4.9 5.1 4.8
Metal thin films deposited on silicon substrate by magnetron sputtering
So far only Cu and Nb thin films have been produced (µm)
Along with polycrystalline metals, can consider also using film deposition
Notes: Silicon is not a proper material for RF gun, we are planning to use cu/moly

## Slide 14: Cu thin film compared with bulk
 | Work function (eV) | QE
Bulk | 5.234 | 1.70E-5
Thin Film | 4.68 | 1.17E-4
17
970
965
960
955
950
945
940
935
930
925
Binding Energy (eV)
x 10
4
0
2
4
6
8
10
CPS
Satellite
Cu 2p3/2
Cu 2p1/2
Satellite
Bulk Cu as received
Thin film Cu as received
Bulk Cu Ar+ sputter and post annealed 250°C
Thin film Cu annealed 250°C
Cu 2p3/2
Cu 2p1/2
Satellite
Satellite
Cu 2p3/2
Cu 2p1/2
Cu 2p1/2
Cu 2p3/2
CuO
CuO
Cu
Cu2O
XPS | Bulk (%) | Thin film(%)
O 1s | 6.1 | 17.943
C 1s | none | 62.03
Cu 2p | 93.9 | 20.027

## Slide 15: Nb thin film compared with bulk
 | Work function (eV) | QE (%)
Bulk | 4.7 | 1.9E-4
Thin Film | 4.8 | 2.64E-4
18
x 10
3
5
10
15
20
25
CPS
214
212
210
208
206
204
202
200
198
196
Binding Energy (eV)
Nb2O5
Bulk Nb as received
Thin film Nb as received
Bulk Nb Ar+ sputter
Thin film Nb annealed 250°C
Thin film Nb annealed 300°C
Thin film Nb Ar+ sputter
Nb2O5
NbO
NbO and NbO2
Nb
NbO and NbO2
XPS | Bulk (%) | Thin film(%)
O 1s | 16.24 | 9.57
C 1s | 20.98 | none
Nb 3p | 62.78 | 90.43

## Slide 16: Future Plans
Short Term Plan
Deposit metal thin films onto Cu/Mo substrate
Investigate single crystal cu (and others) photocathodes
Medium Term Plan
Carry out transverse longitudinal energy measurements from metal photocathodes
Long Term Plan
Modify ESCALAB-II to accept INFN style pucks
Produce and investigate metal thin film photocathodes
Investigate single crystal photocathodes (Cu and others)
Modify ESCALAB-II to accept DESY/INFN plug based photocathodes
Transverse and longitudinal energy spread measurements from metal photocathodes
Test metal photocathodes in VELA/CLARA

## Slide 17: Future Plans
Short Term Plan
Deposit metal thin films onto Cu/Mo substrate
Investigate single crystal cu (and others) photocathodes
Medium Term Plan
Carry out transverse longitudinal energy measurements from metal photocathodes
Long Term Plan
Modify ESCALAB-II to accept INFN style pucks
DESY / INFN puck design
ESCALAB upgrade later this year
High repetition rate gun with photocathode transfer facility to be commissioned 2016

## Slide 18: Conclusions
Short Term Plan
Deposit metal thin films onto Cu/Mo substrate
Investigate single crystal cu (and others) photocathodes
Medium Term Plan
Carry out transverse longitudinal energy measurements from metal photocathodes
Long Term Plan
Modify ESCALAB-II to accept INFN style pucks
New results for O2 and Ar plasma cleaned photocathodes
Preliminary results for Cu and Nb thin film photocathodes
Progress with design work for ESCALAB upgrade
For Further Information: -
DELIVERABLE REPORT: 12.4, ‘SCIENTIFIC REPORT ON PHOTOCATHODE R&D’
MILESTONE REPORT: MS75, ‘INVESTIGATION OF QUANTUM YIELD AND ENERGY SPECTRUM OF THE ELECTRONS, EMITTED FROM THE METAL PHOTOCATHODE’
Commissioning of High Repetition Rate gun in February 2016

## Slide 19
STFC ASTeC
Deepa Angal-Kalinin, Boris Militsyn, Lee Jones, Joe Herbert, Tim Noakes, Reza Valizadeh, Keith Middleman, Mark Surman
Daresbury Technology Department
Ryan Cash and Barry Fell
Loughborough University
Mike Cropper
Acknowledgements
Thank you for listening!

## Slide 20
1s
2s
2p
X-ray
Photoelectron
XPS process:
Sample surface illuminated with X-Rays
X-Rays absorbed within 10 nm of sample
Core level electrons are emitted
Measure Ek of photoelectrons
Corresponding Eb is deduced:
Eb for core level electrons are unique for each chemical species
Therefore spectrum represents surface composition
Ek = hν – Eb – ɸs
Kinetic Energy
X-Ray Energy
Binding Energy
Spectrometer work function
9
XPS
Notes: This is of high significance, because the binding energies for core level electrons are unique for each chemical species. Thus, by recording the number of photoelectrons emitted as a function of Eb, it is possible to obtain a spectrum representing surface composition.

## Slide 21
eVCPD= φprobe - φsample
Result is a periodic flow of charge around the circuit, and thus a varying voltage
Output signal is periodic (Vs)
Sample
Probe set to vibrate upon close contact with sample surface
As d varies, so does C
Probe
Vs
+++++++++++++++
- - - - - - - - -
Vb is set to a range of potentials and a plot of Vptp verses Vb is made.
When Vptp = 0 the VCPD of the surface is equal and opposite to Vb.
Peak to peak voltgae
Externally applied backing potential
21
Kelvin Probe
Notes: Measure the local contact potential difference (CPD) between the conducting probe and the sample
The probe is brought in close to the sample surface
An electrical force is experienced between them as a result of the difference in Fermi energies.
If this force can be matched, and cancelled out with an opposing force of equal magnitude, then the difference in work functions can be obtained.

## Slide 22
QE is the average photoelectric yield per incident photon.
QE measurements comprise
  a LED source giving 265 nm (4.65 eV) light and a pico-ammeter to measure drain current.
  a UV LASER source which offers higher intensity at 266 nm
  Photodiode used to measure LED power
QE suggests how much current can be extracted from a cathode and as such is an indication of the potential beam current.
hν
e-
e-
e-
e-
e-
This property is unique to each photocathode material and is a function of the laser wavelength and the photocurrent produced.
11
QE
Notes: For a metal, providing that the incident photon has energy greater than or equal to the work function, the electrons in the conduction band will be excited above the vacuum level, and are then free to escape.
There is a high density of free electrons in the conduction band, therefore when photoelectrons are transported up to vacuum level, there is a large amount of electron-electron scattering dominates and redistributes energy distribution very quickly