## Slide 1: Magnet challenges for FCC-hh
Gijs de Rijk
CERN
Workshop "Accelerators Revealing the QCD Secrets”
Thessaloniki
4 September 2016

## Slide 2: Contents
Very short intro on superconductors and SC magnets
The early High Field Magnet epoch (1986-2004)
Conductor development
Basic magnet technology development for HILUMI and beyond (2004-2013)
The HILUMI magnet development (2013-2016)
FCC magnet development (2014 - ... )

## Slide 3: FCC-hh requested B field levels
FCC-hh
  Ecm=100 TeV , 100 km ring: B = 16 T Project Baseline
  Ecm=100 TeV , 80 km ring: B = 20 T
What would this mean in the LHC ring for a potential HE-LHC ?
  Ecm=25 TeV , 27 km ring: B = 16 T
  Ecm=33 TeV , 27 km ring: B = 20 T

## Slide 4: Magnets for Accelerators
Dipoles
  Design for B field which is the highest feasible and economic, to reduce the bending radius (NB. bending radius LHC = 2803.95m)
Quadrupoles
  Design for the largest feasible integrated gradient to reduce the magnet bore size, and gradient to increase the dipole filling factor
Beam energy
Dipole field
Bending radius
Beam size
Emittance
Beta function
FODO cell length
Integrated quadrupole gradient
Lorentz factor
High field (SC) accelerator magnets !

## Slide 5: What is specific about accelerator magnets ?
Cylindrical volume with perpendicular field
Dipoles, quadrupoles, etc
Field quality:
Field quality formulated and measured in a multipole expansion,
Long magnets: dipoles from 6 m (Tevatron) to 15 m (LHC)
Often magnets are bent (9.14 mm sagitta for the LHC dipoles)
Artist view of a dipole, from M. N. Wilson « Superconducting Magnets »
CosQ coil : J = J0 cosQ

## Slide 6: The state of the art: Comparison between dipoles and solenoids
We can see roughly a factor 2 due to Coil «efficiency» and to force-stress management
Courtesy L. Rossi

## Slide 7: High Field accelerators magnets, the state of the art
NB. HFM is a imprecisely defined term: It is mostly used to indicate magnets at a field level we do not yet have
Maximum attainable field slowly approaches 16 T
  20% margin needed (80% on the load line):
  for a 16 T nominal field we need to design for 20 T

## Slide 8: Superconductors
Below a the critical surface the material is “superconducting”. Above the surface it is “normal conducting”
Qc Critical Temperature (at zero field and current density)
Bc2 Critical Field (at zero temperature and current density)
Jc Critical Current Density ( at zero temperature and field)
The Critical surface depends on the material type Nb-Ti, Nb3Sn, etc) and the processing
Superconductivity is a macroscopic quantum effect. Resistance = 0
J: few x 103 A/mm2 inside the superconductor
Critical surface
for Nb-Ti
Courtesy M. Wilson

## Slide 9: Available Superconductors
Nb-Ti: the workhorse for 4 to 10 T
  Up to ~2500 A/mm2 at 6 T and 4.2K or at 9 T and 1.9 K
  Well known industrial process, good mechanical properties
  Thousands of accelerator magnets have been built
  10 T field in the coil is the practical limit at 1.9 K
Nb3Sn: towards 20 T
  Up to ~3000 A/mm2 at 12 T and 4.2 K
  Complex industrial process, higher cost, brittle and strain sensitive
  25+ short models for accelerator magnets have been built
  ~20 T field in the coil is the practical limit at 1.9 K, but above 16 T coils will get very large
HTS materials: dreaming 40 T (Bi-2212, YBCO)
Current density is low, but very little dependence on the magnetic field
Used in solenoids (20T range), used in power lines – no accelerator magnets have been
built (only 1 model) – small racetracks have been built

## Slide 10: Forces
Scaling of force on coil quadrant vs. Field
Plot for recent production and R&D dipoles
The electromagnetic loads in a 20 T dipole would be a factor 5 to 8 larger than in the LHC dipoles

## Slide 11: Stored Energy
Scaling of the energy per unit length of magnet vs. Field
Plot for recent production and R&D dipoles
Scaling of the energy per unit length of magnet in recent production vs. R&D dipoles
x10

## Slide 12: Using Nb3Sn conductor in magnets
Nb3Sn has to be reacted after winding for ~100 hours at 650°C (wind and react)
Cables have to be insulated with a non-organic woven insulation: glass or ceramic fibres
After reaction the coils has to be impregnated to prevent any movements and to take care that stresses are distributed, instrumentation connections are moulded in
Reacted Nb3Sn is brittle and stress sensitive

## Slide 13: The early High Field Magnet epoch, I LHC options: 1988-1995
CERN
In 1986 Nb3Sn was still considered an option for the 10T LHC magnets.
The magnet by A. Asner & R. Perin in 1989 went up to 9.5 T at 4.3 K.
It used a 17 mm cable an a wind and react technology.
A single coil in a mirror reached 10.1 T.
Many problems though remained in the fabrication
S. Wenger, A. Asner, F. Zerobin, IEEE Trans. Mag, 25(2) 1989
Twente
In 1995 Twente constructed the MSUT that was powered up to 11.3 T.
It had a 50 mm bore, graded, 33 PIT strand PIT cables with 192 filaments.
This magnet showed that fields above 10T are feasible.
A. den Ouden, H. H. J. ten Kate et al., in Proc. of 15th International Conference on Magnet Technology, Eds. Beijing, China: Science Press, pp. 137-140, 1998.

## Slide 14: The early High Field Magnet epoch, II Mixed results (1995-2004)
CEA quadrupole
A 210T/m @ 4.2K Nb3Sn quadrupole as alternative to the Nb-Ti @ 1.9K design
A very difficult construction with collars done like for the Nb-Ti version
Lots was learned, only one was built, it did not reach nominal field.
FNAL 10T program for VLHC (HFDA)
Several magnets were built, reaching after long training 10T at 4.2K Rediscovery of conductor instabilities
Tough to fabricate !

## Slide 15: The early High Field Magnet epoch, III Some achievements at LBNL (1995-2004)
Since 20 years LBNL is running a high field dipole development program
Some achievements:
D20, 50 mm aperture, cosQ 4 layer dipole, reached 13.5 T@1.9K
HD1, flat block coil, 8 mm aperture, reached 16 T
HD2, flared end block coil, 36 mm aperture, reached 13.8 T
These pose a clear breakthrough above 10 T with a new coil layout (block coil) and a mechanical structure aimed (shell-bladder and keys) at high fields
A.D. McInturff, et al., Proc. of PAC 1997, 3212

## Slide 16: The early High Field Magnet epoch, IV New geometry: Block coils
LBNL block coil designs
When used with wide coils the field quality is naturally homogeneous
Not yet used in accelerators
  Is less efficient (~10%) wrt to cos(Q) for quantity of superconductor used
  The EM forces cause a stress buildup at the outside edge of the coil where the fields are lower
  The straight part is very easy : rectangular cable and wedges (field quality)
  ‘flared ends’ look easy but there is little experience making them
HD2
Courtesy LBNL

## Slide 17: The early High Field Magnet epoch, V Realizing what the challenges are
=== It should in principle be possible to go up to 16T with Nb3Sn===
But: it will be hard to get there in a reliable way and good enough for an accelerator.
A number of issues were identified:
High Jc (Jc>1500 A/mm2) conductor is a must to reach high fields
Conductor instabilities can occur at high current and low fields with certain types of Nb3Sn strands (high Jc, thick strands, big sub-elements, low RRR of the Cu stabiliser)
Insulation is tricky (650ºC reaction cycle)
Nb3Sn stress sensitivity can be an issue and is poorly understood
Construction tooling are critical items, as important as the magnet itself
Putting a Nb3Sn coil in a pure Nb-Ti structure does not work
The coils are very sensitive and fragile
To get up to high fields other coil geometries and force containment / pre-stress structures will be needed

## Slide 18: Conductor development (1998-2008)
after 10 years of development the US and EU development gave us the Nb3Sn conductor for HILUMI.
ITER
US-CDP
CARE-NED
EuCARD
HL-LHC
HL-LHC specs
FCC
FCC specs

## Slide 19: Nb3Sn Conductor specification for HEP
Courtesy L. Bottura, B. Bordini
0.7 mm, 108/127 stack
RRP from Oxford OST
1 mm, 192 tubes
PIT from Bruker EAS
Between HL-LHC and FCC the Jc target shifts from 12 T to 16 T !

## Slide 20: Basic magnet technology development for HILUMI and beyond (2004-2013) ; Europe
European programs
2004-2008 FP7-CARE-NED project (Next European dipole)
  European accelerator grade Nb3Sn conductor  Powder In Tube (PIT) conductor now available from Brucker
  Various studies on design options and materials
2009-2013 PF7-EuCARD-HFM project (High Field Magnets)
  100mm aperture 13 – 15 T Nb3Sn dipole “Fresca2”
  HTS insert with DB = 6 T (inside Fresca2)
  HTS current link
  Nb3Sn helical undulator
2008 – 2014 CERN High Field Magnet project
  Development of Nb3Sn technology magnets for LHC upgrades and new projects (conductor, small models, materials, etc)

## Slide 21: CERN-European development evolution
RMC (Racetrack Model Coil)
Laminated Yoke
Vertical Pad
Aluminium Shell
Longitudinal Rods
Horizontal Pad
Nb3Sn Coil
Electrical connexion box
SMC (Short Model Coil)
Short Model Coil
FReSCa2
Nb3Sn Dipole
Race-track
Model Coil
FReSCa2
11 T dipole
(CERN)

## Slide 22: RMC3 16T: first milestone for FCC 16T !
RMC reached 16.2 T (on coil) end summer 2015 at CERN
Joining LBNL at the 16T record level
.

## Slide 23: EuCARD high field dipole (FRESCA2)
Diameter Aperture = 100 mm
L coils = 1.5 m
L straight section = 700 mm
L yoke = 1.6 m
Diameter magnet = 1.03 m
156 turns per pole
Iron post
Bcenter = 13.0 T
I13T = 10.7 kA
Bpeak = 13.2 T
Emag = 3.6 MJ/m
L = 47mH/m
Courtesy Attilio Milanese, Pierre Manil
42
42
36
36
FRESCA2 : CERN, CEA construction phase
First tests end 2015
13 T bore field (“nominal”)
  ~79% of Iss at 4.2 K
  ~72% of Iss at 1.9 K
15 T bore field (“ultimate”)
  86% of 1.9 K Iss

## Slide 24: Fabrication of Fresca2 coils
Straightforward technology to wind block coils with flared ends:
This is a lesson for FCC magnets !

## Slide 25: Fresca2 : the 15T FCC milestone by end 2016 ?
First test: 13T loading,
then warm up and loading for 15T,
Second test: go up to 15T
Magnet assembly in September, to be tested end this year

## Slide 26: Basic magnet technology development for HILUMI and beyond (2004-2013) ; US development evolution
By courtesy of D. Dietderich, LBNL

## Slide 27: Basic magnet technology development for HILUMI and beyond: Results
This phase of development gave us
  Conductor pre-FCC grade in both US and EU
  Basic coil manufacturing technology close to FCC standard
  New coil and structure geometries
2 milestones
  HD1 & RMC 16T on the coil (no aperture) Achieved mid 2015
  Fresca2 13T15T in a large aperture end 2016 !

## Slide 28: :HILUMI magnet development (2013-2016)
HILUMI means new magnets in ~1 km of the the LHC main ring
The ultimate test-bed for the feasibility of Nb3Sn magnets in accelerators!

## Slide 29: New triplet for HHILUMI
Present triplets
NC D1
SC D1
Corrector
Package
Q1
Q2a
Q2b
Q3
D2
Q4
CC
Lower b value in the interaction points : larger apertures needed in the triplet of the machine (from 70 mm to 150 mm)

## Slide 30: HILUMI IT magnet zoo
Courtesy E. Todesco

## Slide 31: LHC IP Quadrupole design and technology evolution
70
90
120
150
Aperture (optics)
Courtesy L. Bottura

## Slide 32: HL-LHC: MQXF low beta Nb3Sn quadrupole
A CERN LARP collaboration.
Nominal Gradient 132.6 T/m
Aperture diameter 150 mm
Peak Field 12.1 T
Current 17.5 A
Loadline Margin 20% @ 1.9 K
Stored Energy 1.32 MJ/m
Spring 2016 the first model achieved the nominal and ultimate field at FNAL !
By courtesy of G. Ambrosio (FNAL), P. Ferracin (CERN et al)

## Slide 33: HILUMI: The 11T Dipole Two-in-One for DS
Create space in the dispersion suppressor regions of LHC, i.e. a room temperature beam vacuum sector, to install additional collimators (TCLD), (needed to cope with beam intensities that are larger than nominal, such as in the HL LHC)
Replace a standard MB by a pair of 11T dipoles (the 11T dipole is also called MBH)
Interconnect
Space for Collimator
11 T dipole cold mass
By-pass cryostat
15660 mm

## Slide 34: HL-LHC: 11 T Dispersion suppressor magnet
First Nb3Sn magnet to go into an accelerator (2019) !
Present model program (CERN and FNAL)
  demonstrated the required performance (11.25 T at 11850 A) and Achieved accelerator field quality
Nominal Field 11 T
Aperture diameter 60 mm
Peak Field 11.35 T
Current 11.85 kA
Loadline Margin 19.7% @ 1.9 K
Stored Energy 0.96 MJ/m

## Slide 35: conclusion from previous and running programs
We now have all the elements in hand to develop 16T magnets
  11 T dipoles: we have working models (at CERN and FNAL)
  12 T quadrupoles: we have working models (made together by LARP and CERN)
  We showed 16T is feasible on flat coils (at LBNL and CERN)

## Slide 36: FCC development (2014 - ... )
LHC
27 km, 8.33 T
14 TeV (c.o.m.)
FCC-hh
80 km, 20 T
100 TeV (c.o.m.)
FCC-hh
100 km, 16 T
100 TeV (c.o.m.)i
HE-LHC
27 km, 20 T
33 TeV (c.o.m.)
Geneva
PS
SPS
LHC

## Slide 37: FCC: Magnet design for 16 T dipoles, LTS Nb3Sn
P. McIntyre, 2005
E. Todesco, 2013
GL. Sabbi, 2014
Blocks
E. Todesco 2013
D. Schoerling 2015
Cos-q
S. Caspi, 2014
Canted Cos-q
R. Gupta, 1997
J.M. Van Oort, R. Scanlan, 1994
Common coils

## Slide 38: US program lines
5T Nb-Ti
2014-2015
10T Nb3Sn
2015-2016
2016
canted-cos-q
cos-q
2017
common coils
2018

## Slide 39: FCC plan for 16T baseline
Real estate
Pinning
16 T models
Conductor R&D
Opportunity for prototypes built in industry
ERMC
RMM

## Slide 40: EuroCirCol Program for FCC 16 T dipole
Complete conceptual design and select a baseline for the FCC accelerator dipole
Engineering design of the FCC accelerator dipole (assuming high-performance wire)
Engineering design of 16T dipole model for the following R&D program (assuming existing wire performance)(*)
Manufacturing folder for 16 T dipole model
Manufacturing folder for the 16 T dipole model construction tooling(*)
Japan
KEK
Finland
TUT
France
CEA
Italy
INFN
Netherlands
UT
Spain
CIEMAT
CERN&UNIGE
WP 5

## Slide 41: FCC Nb3Sn performance targets
Ultimate Nb3Sn ? Pursue the idea of improved high field pinning
(D. Dietrich and R. Scanlan, A. Godeke)
All single parameters are in reach, their combination is the challenge !
Dstrand: 0.5…1 mm
JC (16 T, 4.2 K) > 1500 A/mm2
m0DM (1 T,4.2 K) <150 mT (Dfil < 20 m)
RRR > 150
UL > 5 km
Cost(16 T, 4.2 K) < 5 USD/kAm
Large cables, cabling !
Field quality
Stability, protection
ITER material cost per kg

## Slide 42: FCC Conductor R&D Program
Four year’s program (2016-2019) focused on the increase of JC(16 T, 4.2 K) ≥ 1500 A/mm2 with high RRR ≥ 150
At this stage all “expedients” are considered: maximize Nb3Sn fraction, grain refinement, APC
Worldwide R&D, coordinated by national institutes:
  EU – CERN: BEAS (partly in preparation)
  JA – KEK: SH Copper, Furukawa, JASTEC; Tohoku University, NIMS
  RU – Bochvar: TVEL
  KO – KAT: Kiswire
Material characterization and advanced analysis
  EU – Technisce Universitaet Wien (Atominstitut)
  US – ASC at NHMFL

## Slide 43: FCC: 16T dipole options
Common coils
F. Toral (CIEMAT)
Cos-theta coil
S. Farinon, P. Fabbricatore (INFN)
Block coil
C. Lorin, M. Durante (CEA)

## Slide 44: FCC 20T option: HTS program
Early phase: EuCARD HTS insert magnet (2009 – 2016)
First step to an HTS accelerator magnet: EuCARD2 (2013 – )
  10kA rated ReBCO cable (Roeble cable)
  5T stand alone accelerator quality ReBCO magnet
We are now starting a long term HTS magnet development program at CERN and collaborating institutes (2016 – 2024)

## Slide 45: FCC 20T option: HTS program
Preliminary HTS magnet development program
Courtesy , J. van Nugteren, CERN

## Slide 46: EuCARD2 5T accelerator quality ReBCO magnet
5 Tesla stand alone, (18 T–20 T in 13 T background or other), @ 4.5K, 40 mm aperture, 10 kA class cable, Accelerator Field quality
http://eucard2.web.cern.ch/

## Slide 47: Feather0 - Feather-M2.0
Feather0: First coil in the test station
Feather2: winding of first coil with dummy cable in progress

## Slide 48: Synergy programs
30 T (NMR) to 60 T (user facilities) HTS solenoids
ISBN: 978-0-309-28634-3
16 T LTS and 20 T HTS accelerator dipoles and associated technologies
By courtesy of S. Gourlay (LBNL)

## Slide 49: Conclusions
FCC CDR (EuroCirCol) propose a new energy frontier accelerator
16 T magnet model(s)
2016
2017
2018
2019
2020
2025
2030
2035
2040
2015
End of LHC useful life
20 T magnet model(s)
LHC Run-II provides results to define future HEP roadmap (European Strategy 2018)
HL-LHC demonstrates large-scale use of Nb3Sn
FCC construction decision
Accelerator-grade HTS 5 T demo
12 T accelerator technology
16 T accelerator technology

## Slide 51: FCC-hh magnet parameters
 | B / G (T) / (T/m) | Bpeak (T) | Bore (mm) | Length (units x m)
MB | 16 | 16.4 | 50 | ≈4500 x 14.3
MQ | 450 (> 350) | 13 | 50 | ≈800 x 6
MQX | 225 | 13 | 100 (<150) | 
MQY | 300 | 13 | 70 | 
MBX | 12 | 12.5 | 60 | (4x2) x 12
MBR | 10 | 10.5 | 60 | (4x3) x 10
Inter-aperture distance ≈ 250 mm
Yoke diameter ≤ 700 mm
Stray field ≤ 100 mT