## Slide 1: RRP conductor quench analysis in SMC-11T & DS-11T
H. Bajas, M. Bajko, Gerard Willering,
S. Izquierdo Bermudez, J. C. Perez

## Slide 3
Nb3Sn RRP strand
40-strand cable
Number of strands | 40 | -
Strand diameter | 0.7 | mm
Copper non-copper ratio | 1.25 | -
Cable width | 14.85 | mm
Bare Cable Thickness | 1.202 | mm
Insulation thickness | 0.1 | mm
Copper surface | 8.55 | mm2
Total surface | 21.10 | mm2
Volume ratio Copper | 0.41 | -
Volume ratio Superconductor | 0.32 | -
Volume ratio insulation & impregnation | 0.27 | -
SMC-11T coil
MBHSP101 coil

## Slide 5
SMC 11T 1 & 2
Dipole 11T CERN & FNAL (mirror, double coil)
Compared to 4.3 K, the performances at 1.9 K are limited and less stable.

## Slide 6
CERN SMC-11T quench analysis

## Slide 7
Delayed extraction
MIITs > 7.5
Training
MIITS < 7
Extraction
Maximum Current= 15.9 kA
(13.5T)
Current decays
SMC-11T-1

## Slide 8
Maximum MIITs = 11.3
Delayed extraction
MIITs > 7.5
Training
MIITS < 7

## Slide 9
SMC11T: Typical quench pattern (longitudinal velocity along the pole turn)

## Slide 10
Three independent methods to derive the temperature of the segments during the quenches from:
the experimental voltage and current signals
theoretical temperature dependences for the material (Copper, Nb3Sn, G10 ) properties (resistivity and heat capacity)

## Slide 11
Resistivity r [W.m]
Segment length l [m]
Copper area Scu [m2]
Transport Current I [A]
Measured voltage u [V]
Segment inductance L [H]
Fully propagated
Resistive voltage
Resistivity:

## Slide 12
Training quenches
High MIITs
tests
Resistivity as function of time for all the quenches (segment U4-U5)
Delayed extraction

## Slide 13
Symmetric quench (upper/lower)
Segment fully quenched
Extremely similar behavior for the 4 segments.
High MIITs case (11 MA2.s) in SMC-11T-1

## Slide 14
Residual Resistivity Ratio RRR
Magnetic field B [T]
Temperature T [K]
Method 1: Copper as thermometers for segment temperature estimates
mr= 0.005 W.m/T
C0= 1.7 W.m

## Slide 15
Temperature as function of time for all the quenches (segment U4-U5)
Training quenches
High MIITs
tests
Maximum Temperature 220 K

## Slide 16
Generated Energy:
Two ways..
Copper area Scu [m2]
Theoretic resistivity rth
Stored Energy:
Volumetric Heat capacity [J.m-3.K-1]
Composite total area St [m2]
Adiabatic assumption and integration:
Two HST estimates

## Slide 17
Temperature as function of time for all the quenches (segment U4-U5)
Effect of the insulation+ impregnation (G10 on the HST)

## Slide 18
Temperature as function of time for all the quenches (segment U4-U5)

## Slide 19
Maximum temperature as function of the maximum MIITs for
all quenches
all location
3 methods
Purely theoretical approach:
Relevant set of material properties as proved by the coherence of the 3 methods.
MIITs see by the segments
Good agreement with theory.

## Slide 20
CERN MBHSP01 quench analysis

## Slide 21
Training
Quench

## Slide 22
Training
Quench

## Slide 23
Training
Quench

## Slide 25
Quench Heater test (10 kA)

## Slide 26
Quench Heater test (10 kA)

## Slide 27
Quench Heater test (10 kA)

## Slide 28
Good agreement with SMC11T behavior

## Slide 29
Quench performance limited at 1.9 K as compared to 4.3 K.
With the present set of material properties, the Hot Spot Temperature can be computed from the 0D adiabatic model with good agreement with temperature estimates from experimental signals.
Good coherence between both SMC-11T and with 11T-dipole.

## Slide 32
80-µm-thick C-shaped Mica film and a braided sleeve made of S2-glass fibers (total thickness = 100-µm[2])

## Slide 33
HCMBHSP0001-101
SMC11T-1
SMC11T-2

## Slide 35
Splicing using MOB 39 as flux and solder 96/4 Tin/Silver