## Slide 1: Electromagnetic design
Susana Izquierdo Bermudez
B. Auchmann, L. Fiscarelli, M. Karppinen, A. Zlobin
International Review of the HL-LHC 11 T Dipole for DS collimation
December 2014

## Slide 2: Outline
Introduction
Magnet parameters at operation conditions
Coil cross section
Peak field
Load line and margin
Transfer function
Iron saturation
Fringe field
Persistent currents
Eddy currents
3D effects
Manufacturing tolerances
Summary

## Slide 3: 1. Introduction
  DS-11 T magnet must be 100 % compatible with the LHC lattice and main systems
  This has important consequences, as it is setting (many) important constrains in the design:
  Integrated field (pair of DS-11T dipoles): 118.8 Tm
  Operational point
  Yoke dimension/geometry
  Aperture
  Length
  …
Collimator
Collimator
Challenges: high field, forces, stored energy!

## Slide 4: 1. Introduction
Before getting to a full length operational magnet, FNAL-CERN R&D Program:
FNAL
MBHSM01
CERN
MBHSM101
Mirror/Single coil assembly:
validate coil technology/assembly process
One aperture short models:
mechanics, quench protection, field quality (persistent current effects, eddy current effects)
CERN 2in1
Two aperture magnets
field quality (cross talk),iron saturation, mechanics (2D&3D), alignment
FNAL
MBHSP01/02/03
CERN
MBHSP101
FNAL 2in1

## Slide 5: 2. Magnet parameters
 | CERN 1in1 | CERN 2in1
Aperture, mm | 60 | 
Nominal current, kA | 11.85 | 
Yoke outer diameter, mm | 510 | 550
Central field at Inom, T | 11.20 | 11.21
Peak field in the conductor at Inom without strand self field, T | 11.53 | 11.59
Peak field in the conductor at Inom with strand self field, T | 11.72 | 11.75
Horizontal EM-force Fx per side at Inom, MN/m | 6.22 | 6.23
Vertical EM-force Fy per coil at Inom, MN/m | 3.18 | 3.15
Longitudinal EM-force Fz per coil at Inom, kN | 472 | 474
Differential inductance at Inom, mH/m | 5.7 | 11.7
Stored energy at Inom, kJ/m | 445 | 897
Magnetic length, m | 1.69 | 1.69/5.3
We will focus in the CERN 2 in 1 design
Details on FNAL design will be addressed by A. Zlobin

## Slide 6: 3. Coil cross section
 | Before reaction | After reaction
Number of strands | 40 | 
Core | Stainless Steel 11 mm x 0.025 mm | 
Bare cable width [mm] | 14.7 | 14.847
Bare cable mid-thickness [mm] | 1.269 | 1.307
Key-stone angle [degrees] | 0.79 | 0.81
Insulation Thickness | 0.155 | 0.100
COIL:
Same design FNAL/CERN
6 Blocks, 56 turns
Aperture = 60 mm, which avoids bending the Nb3Sn coils in order to accommodate the LHC beam sagitta.
CABLE: 40 strands cored cable. Assumptions on cable dimensional changes during heat treatment[1]:
Thickness increase: 3%
Width increase: 1%
[1] Andreev 2001, Volume expansion of Nb3Sn strands and cables during heat treatment
[2] Actual insulation thickness ~ 110 µm
INSULATION:
FNAL: 75-µm-thick E-glass tape. Double wrap (total thickness = 100-µm)
CERN: 80-µm-thick C-shaped Mica film and a braided sleeve made of S2-glass fibers (total thickness = 100-µm[2])

## Slide 7: 4. Peak field
Pole tip
Straight part
Arc length of the conductor
Peak field is in the inner layer pole turn, before the pole tip
Pole tip
Straight part
Chart: Arc length of the conductor (mm)
0.16 T peak field enhancement
Peak field at Inom = 11.85 kA in the straight part is 11.75 T (including strand self field).
Magnetic iron laminations covering the entire length  0.16 T peak field enhancement at the ends.

## Slide 8: 4. Peak field
No cut-back
cut-back
Pros of reducing the magnetic iron extension (cut-back):
Suppression of the peak field enhancement at the ends  ~ 1.5 % additional margin in the load line
Cons of reducing the magnetic iron extension (cut-back):
For the same integrated field, the coil should be 20 mm longer.
Additional complication in the procurement and manufacturing process (“Kawasaki steel” needed to have similar thermal contraction)
2 additional units of b2. The impact in the rest of the harmonics is less than 0.05 units
The only way to reduce the peak field in the ends is to reduce the extension of the magnetic iron yoke
 | 2D | Integrated (no cut-back) | Integrated (cut-back)
b2 | -14.4 | -13.2 | -15.3
Pole tip
Straight part
Chart: Arc length of the conductor (mm)

## Slide 9: 5. Load line and margin
Chart: Bp [T]
| 16 | 15 | 14 | 13 | 12.26 | 11 | 9
Critical Current Density 1.9 K | 10.0754 | 12.6904 | 15.7351 | 19.2698 | 22.245 | 28.1359 | 40.2213
Magnet Load Line (yoke cut-back) | 0.001185 | 1.7786 | 3.5559 | 5.3333 | 7.1107 | 8.8881 | 10.665 | 12.443 | 14.22 | 15.998 | 17.775
Magnet Load Line (full iron coverage) | 0.001185 | 1.7786 | 3.5559 | 5.3333 | 7.1107 | 8.8881 | 10.665 | 12.443 | 14.22 | 15.998 | 17.775
Operational Point | 11.85
Operational Point | 11.85
Operational Conditions:
  Iop = 11.85 kA
  Bpeak = 11.75 T
Margin in the load line
      80.6 % of Iss at 1.9 K for the “yoke cut-back solution”
      81.9 % of Iss at 1.9 K for the “full iron coverage solution”
Temperature margin 4.4 K – 14.3 K
I = 11.85 kA, T = 1.9 K
zoom
Chart: Bp [T]
| 16 | 15 | 14 | 13 | 12.26 | 11 | 9
Critical Current Density 1.9 K | 10.0754 | 12.6904 | 15.7351 | 19.2698 | 22.245 | 28.1359 | 40.2213
Magnet Load Line (yoke cut-back) | 0.001185 | 1.7786 | 3.5559 | 5.3333 | 7.1107 | 8.8881 | 10.665 | 12.443 | 14.22 | 15.998 | 17.775
Magnet Load Line (full iron coverage) | 0.001185 | 1.7786 | 3.5559 | 5.3333 | 7.1107 | 8.8881 | 10.665 | 12.443 | 14.22 | 15.998 | 17.775
Operational Point | 11.85
Operational Point | 11.85

## Slide 10: 6. Transfer function
A discrepancy between MB and 11 T is inevitable:
  More turns than MB (56 vs. 40)  11 T dipole is stronger low field.
  More saturation  reduction of transfer function at high field.
MB
11 T
Remedy:
  Option 1: Correct the orbit using MCBH corrector
    See talk [M. GIOVANNOZZI], beam specifications
  Option 2: Use a 300 A trim converter to compensate the effect
    Baseline solution
Chart: I [A]
| 1185 | 2370 | 3555 | 4740 | 5925 | 7110 | 8295 | 9480 | 10665 | 11850
 | 0.52333 | 1.045 | 1.5667 | 2.0717 | 2.4164 | 2.4114 | 1.9826 | 1.3423 | 0.61673 | -0.01134
Chart: Imagnet [A]
| 1185 | 2370 | 3555 | 4740 | 5925 | 7110 | 8295 | 9480 | 10665 | 11850
 | -52.2311 | -104.2992 | -156.3615 | -206.7681 | -241.1679 | -240.6658 | -197.8764 | -133.9713 | -61.5528 | 1.1318

## Slide 11: 7. Iron saturation
Chart: DS-11T Dipole: MBHSP101
measured | 1985.7464 | 53.0736 | -43.0304 | -34.7658 | -42.5924 | -40.7692 | -28.8462 | -17.6129 | -10.197 | -6.1776 | 0 | -0.38536 | -17.1292 | -59.6204 | -122.2446 | -196.0211 | -274.1616 | -353.0663 | -373.3222
Further investigation on the magnetic properties of the iron needed to understand the discrepancy between measured and expected values.
[P. Hagen]
MBHSP101 (CERN first aperture)
Chart: I (A)
| 1000 | 2000 | 3000 | 4000 | 5000 | 6000 | 7000 | 8000 | 9000 | 10000 | 11000 | 12000
 | 0 | 0 | 0 | 0.25085 | 1.0034 | 4.0135 | 7.8838 | 10.7864 | 12.1521 | 13.6461 | 14.5947 | 15.887
Iron saturation effect in the transfer function is strong.
For the first aperture measured at CERN, the difference with respect to the model is ~ 55 units.
(LHC-MB Dipole, iron saturation effect is 70 units, and agreement with the model ~ 5 units)
The difference can be partly explained by the 100 % packing factor of the iron laminations observed during magnet assembly
[C. Loffler]
Difference in computed transfer function for 98.5% and 100% packing factor

## Slide 12: 7. Iron saturation
Coil geometry optimized to have all harmonics below 1 units at Rref = 17 mm
Yoke design
  The cut-outs on top of the aperture reduce the b3 variation by 4.7 units as compared to a circular shape.
  The holes in the yoke reduce the b3 variation by 2.4 units.
  The two holes in the yoke insert reduce the b2 variation from 16 to 12 units.
  Iron gives 7.38 units of b3  coil re-optimization
Chart: I [kA]
| 1.1850000000000001E-3 | 0.59362999999999999 | 1.1860999999999999 | 1.7785 | 2.3709000000000002 | 2.9634 | 3.5558000000000001 | 4.1482999999999999 | 4.7407000000000004 | 5.3331999999999997 | 5.9256000000000002 | 6.5179999999999998 | 7.1105 | 7.7028999999999996 | 8.295399999999999 | 8.8877999999999986 | 9.4802000000000017 | 10.073 | 10.665000000000001 | 11.258000000000001 | 11.85
b2 | -0.080619 | -0.080619 | -0.08059 | -0.079036 | -0.074935 | -0.065963 | -0.065008 | -0.13382 | -0.41819 | -1.0504 | -2.615 | -4.0729 | -5.1286 | -5.6263 | -6.1072 | -6.7986 | -7.8991 | -9.4336 | -11.087 | -12.804 | -14.602
b3 | 7.356 | 7.356 | 7.356 | 7.3555 | 7.3543 | 7.3518 | 7.3517 | 7.3583 | 7.3782 | 7.4089 | 7.3942 | 7.2712 | 7.0638 | 6.9642 | 6.9192 | 6.933 | 6.9751 | 7.0381 | 7.1374 | 7.2575 | 7.3787
b9 | 0.89045 | 0.89045 | 0.89045 | 0.89045 | 0.89045 | 0.89046 | 0.89049 | 0.89057 | 0.89087 | 0.89171 | 0.89352 | 0.89617 | 0.89969 | 0.9041 | 0.90889 | 0.91371 | 0.91853 | 0.92328 | 0.92785 | 0.93221 | 0.93635
b4 | 0.00010541 | 0.00010541 | 0.00010697 | 0.00019004 | 0.00034 | 0.00044263 | 0.00068203 | 0.004084 | 0.011821 | 0.023016 | 0.054361 | 0.062875 | 0.033376 | -0.023867 | -0.098385 | -0.17344 | -0.24639 | -0.31393 | -0.37294 | -0.42464 | -0.47234
b5 | 0.017356 | 0.017356 | 0.017356 | 0.017362 | 0.017374 | 0.017476 | 0.017757 | 0.019368 | 0.025301 | 0.039057 | 0.071638 | 0.11392 | 0.15954 | 0.19908 | 0.23251 | 0.26162 | 0.28767 | 0.31096 | 0.33234 | 0.35207 | 0.37019
b6 | -1.1335e-05 | -1.1336e-05 | -1.1344e-05 | -1.0977e-05 | -9.6812e-06 | -8.779e-06 | 7.1318e-07 | 0.00012529 | 0.00056579 | 0.0011894 | 0.0030067 | 0.0047581 | 0.0045748 | 0.0024024 | -0.00080194 | -0.0039864 | -0.0068732 | -0.0092894 | -0.011275 | -0.012847 | -0.014068
b7 | -0.087022 | -0.087022 | -0.087022 | -0.087021 | -0.087021 | -0.08702 | -0.087033 | -0.087123 | -0.087401 | -0.088132 | -0.08949 | -0.091006 | -0.092361 | -0.093409 | -0.094314 | -0.095113 | -0.095827 | -0.096485 | -0.097088 | -0.097645 | -0.098167
b8 | -3.1618e-07 | -3.1103e-07 | -3.2167e-07 | -4.3491e-07 | -7.5283e-07 | -1.1889e-06 | -2.0261e-06 | -7.0379e-06 | -1.8354e-05 | -5.0157e-05 | -0.00012158 | -0.00016401 | -0.00020039 | -0.00026157 | -0.0003368 | -0.00040032 | -0.0004487 | -0.00048177 | -0.00050359 | -0.00051621 | -0.00052003
[M. Karppinen]

## Slide 13: 8. Fringe field
The cryostat has the standard dimensions of the LHC Dipole, i.e., 915 mm outer diameter, 12 mm thickness and it is 80 mm off centred.
The main contribution to the harmonics is 3 units of a1
x-axis
y-axis
Chart: Distance from the centre of the magnet (mm)

## Slide 14: 9. Persistent Currents Effects
Chart: I (A)
Injection | -30 | 50
  Dynamic aperture simulations accept b3 up to 20 units at injection, and a variation +-20 units from injection to nominal
  Value at injection can be adjusted using current reset level during pre-cycle
Present value of magnetization are compatible with field quality requirements
For future study: assessment of the variability in wire magnetization and resulting uncertainty
Ireset = 100 A
Ireset = 350 A
Ireset = 500 A
Chart: Current (A)
| 2250 | 1942.9 | 1635.8 | 1328.6 | 1021.5 | 714.38 | 407.25 | 100.12 | 253.69 | 407.25 | 560.80999999999995 | 714.38 | 867.94 | 1021.5 | 1175.0999999999999 | 1328.6 | 1482.2 | 1635.8 | 1789.3 | 1942.9 | 2096.4 | 2250 | 3000 | 3750 | 4500 | 5250 | 6000 | 6750 | 7500 | 8250 | 9000 | 9750 | 10500 | 11250 | 9964.2999999999993 | 8678.6 | 7392.9 | 6107.1 | 4821.3999999999996 | 3535.7 | 2250 | 1978.6 | 1707.1 | 1435.7 | 1164.2 | 892.77 | 621.32000000000005 | 349.88
Model | 28.312 | 33.526 | 41.118 | 52.929 | 73.155 | 113.55 | 221.91 | 955.73 | 327.11 | 152.12 | 74.333 | 33.549 | 10.818 | -1.8575 | -8.5301 | -11.552 | -12.446 | -12.263 | -11.602 | -10.741 | -9.8115 | -8.874 | -4.8045 | -1.8172 | 0.24733 | 1.6306 | 2.4719 | 2.9698 | 3.7211 | 4.4637 | 5.0552 | 5.3765 | 5.4014 | 5.1494 | 9.0999 | 9.6518 | 9.8665 | 11.026 | 13.364 | 17.597 | 28.311 | 32.82 | 39.067 | 48.149 | 62.257 | 86.378 | 134.53 | 264.15
Injection | -30 | 50
  RRP150/169
  RRP108/127
Ireset = 100 A

## Slide 15: 10. Eddy current effects
Core dimensions: 11 mm x 0.025 mm (~80 % coverage)
Both measurements at FERMILAB and CERN show that Eddy Current effects is small.
Details will be addressed by [A. Zlobin] and [L. Fiscarelli]
Pros:
Suppression of ramp-rate dependence of field quality
Increased reproducibility
Stainless Steel Core to control the cross-over resistance Rc
Cons:
Less quench back for protection
Stability (current sharing among layers)
MBHSP01 (no core)
MBHSP02 (core)
[A. Zlobin]
[A. Zlobin]

## Slide 16: 11. 3D effects
Measured data in MBHSP101 showed very consistent results for b3. The agreement is not good for a3
Reported values correspond to the solution with no-cutback
Meas.
coil
 | 2D | 3D | Δ
b2 | -14.42 | -13.15 | 1.27
b3 | 7.48 | 8.67 | 1.19
a1 | 0.00 | 1.25 | 1.25
a3 | 0.00 | -0.16 | -0.16
Meas.
coil

## Slide 17: 12. Manufacturing tolerances
Chart: Multipole Order
| 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11
Skew | 2.87 | 1.66 | 1 | 0.64 | 0.38 | 0.2 | 0.06 | 0.05 | 0.03 | 0.02
Normal | 1.93 | 1.24 | 0.6 | 0.31 | 0.18 | 0.11 | 0.06 | 0.03 | 0.01
Order | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
Normal | 1.93 | 1.24 | 0.6 | 0.31 | 0.18 | 0.11 | 0.06 | 0.03 | 0.01 | 0.01 | 0.00 | 0.00 | 0.00 | 0.00
Skew | 2.87 | 1.66 | 1 | 0.64 | 0.38 | 0.2 | 0.06 | 0.05 | 0.03 | 0.02 | 0.01 | 0.00 | 0.00 | 0.00
Random component for the harmonic content defined by applying:
Radial and azimuthal shift applied independently to each block
+-10 µm variation on the thickness of conductor and insulation
Block | Radial shift (µm) |  | Azimuthal shift(µm) | 
1 | -100 | 10 | 0 | 15
2 | -100 | 20 | -10 | 10
3 | -100 | 20 | -14 | 6
4 | -100 | 20 | -16 | 4
5 | -100 | 20 | 0 | 15
6 | -100 | 20 | -14 | 6
[M. Karppinen]

## Slide 18: 12. Manufacturing tolerances
CERN experience (MBHSP101)
Coils were oversized  Reduction of the S2 glass wrap around the coil
Cross section of coil 104 [X. Sarasola]
(discarded because it is too much oversized)
 | Inner radius [mm] | Outer radius [mm]
Nominal [mm] | 0.100 | 0.200
Coil 106 [mm] | 0.000 | 0.000
Coil 107 [mm] | 0.100 | 0.100
0.2  0.0 mm
0.1  0.0 mm
0.1 mm
0.2  0.1 mm
300 K | Measured |  | ROXIE | 
n | bn | an | bn | an
2 | -0.13 | 3.73 | 0.00 | 0.00
3 | 7.00 | -0.11 | 6.71 | 0.00
4 | 0.16 | -2.60 | 0.00 | 0.00
5 | 0.14 | 0.00 | 0.14 | 0.00
1.9 K | Measured |  | ROXIE | 
n | bn | an | bn | an
2 | 0.86 | 5.47 | 0.00 | 0.00
3 | 6.35 | -1.21 | 6.22 | 0.00
4 | 0.30 | 1.72 | 0.00 | 0.00
5 | 1.49 | 0.01 | 0.38 | 0.00
Large a2 and a4 measured both at warm and cold. They are “compatible” with coil asymmetries
Very good agreement in b3,both at warm and cold
It remains to be understood the large b5 measured at cold
 | RANDOM | 
n | bn | an
2 | 1.93 | 2.87
3 | 1.24 | 1.66
4 | 0.6 | 1
5 | 0.31 | 0.64
Based on the defined manufacturing tolerances:

## Slide 19: 12. Manufacturing tolerances
 | Warm Mag. Meas. |  | ROXIE Original |  | ROXIE Shifted | 
n | bn | an | bn | an | bn | an
2 | -0.13 | 3.73 | 0.00 | 0.00 | 0.00 | 3.48
3 | 7.00 | -0.11 | 6.71 | 0.00 | 6.70 | 0.00
4 | 0.16 | -2.60 | 0.00 | 0.00 | 0.00 | -2.09
5 | -0.76 | 0.03 | 0.14 | 0.00 | 0.24 | 0.00
6 | -0.03 | 0.66 | -0.03 | 0.25 | 0.00 | 0.22
Radial displacements is giving a positive contribution to a2 and a4.
In combination with a rotation of the blocks close to the mid-plane, we get the negative contribution to a4.
At cold, measured a4 varies from 0-2 units depending on the longitudinal segment.
The good news are that for nominal coil dimensions, we should be able to stay within the stablished manufacturing tolerance limits.
Radial displacement coil106 = 350 µm
0.69° Rotation
coil 106
coil 107
Radial displacement coil107 = -350 µm
Total offset mid-plane =
500 µm

## Slide 20: Summary
Field quality is in line with limits set by AP-studies
Main topics to be addressed:
  Impact of iron saturation in the transfer function
  Assessment of the variability in wire magnetization and resulting uncertainty on b3 at injection

## Slide 21: Additional slides

## Slide 22: Margin
Chart: Bp [T]
| 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16
Ic (1.9K) coil 105 | 57.5603 | 47.7399 | 39.6017 | 32.7674 | 26.9768 | 22.0439 | 17.831 | 14.2335 | 11.17 | 8.5759
Ic (1.9K) coil 106 | 58.0088 | 48.5001 | 40.5986 | 33.9398 | 28.2736 | 23.4212 | 19.2505 | 15.661 | 12.5749 | 9.9303
Ic (1.9K) coil 107 | 61.7083 | 51.169 | 42.4359 | 35.1026 | 28.8899 | 23.5983 | 19.0798 | 15.2223 | 11.9382 | 9.1582
Extracted strand coil 105 | 31.216 | 25.988 | 21.46 | 30.408 | 25.36 | 20.872
Extracted strand coil 106 | 26.592 | 22.192 | 32.036 | 26.768 | 22.256
Magnet Load Line | 0.001185 | 1.7786 | 3.5559 | 5.3333 | 7.1107 | 8.8881 | 10.665 | 12.443 | 14.22 | 15.998 | 17.775
Operational Point | 11.85
Reference critical surface | 10.0754 | 12.6904 | 15.7351 | 19.2698 | 22.245 | 28.1359 | 40.2213

## Slide 23: Magnet Design and Parameters (FNAL)
A. Zlobin
0.7 mm Nb3Sn RRP strand
40-strand cable
Stainless steel collar
2-layer coil

## Slide 24: Field in the coil
Without strand self field correction
With strand self field correction

## Slide 25: MB-Transfer Function

## Slide 26: Difference in the transfer function
Chart: I [A]
| 1185 | 2370 | 3555 | 4740 | 5925 | 7110 | 8295 | 9480 | 10665 | 11850
Baseline | 0.52333 | 1.045 | 1.5667 | 2.0717 | 2.4164 | 2.4114 | 1.9826 | 1.3423 | 0.61673 | -0.01134
Aleternative design | 0.35799 | 0.71436 | 1.0707 | 1.4107 | 1.5924 | 1.4292 | 0.84822 | 0.059356 | -0.81225 | -1.5848
11T-DS dipole designed to match LHC-MB transfer function at nominal current
An alternative solution is to minimize the difference in TF with respect to the LHC_MB dipole
  In case of operate without trim, less corrector strength required
  In case of using a trim, it should be bipolar (difficult for protection!!)

## Slide 27: Magnetic and Physical lengths
Chart: z [mm]
magnetic length starts | -200 | 200
magnetic length ends | -200 | 200
Yoke starts | -200 | 200
Yoke ends | -200 | 200
Pad starts | -200 | 200
Pad ends | -200 | 200
Conductors starts | -200 | 200
Conductor ends | -200 | 200
Magnetic Yoke
Magnetic Length
Coil Length
Total Yoke Length
250 mm non magnetic
(43 laminations)
150 mm non magnetic
(26 laminations)

## Slide 28: Eddy currents
Chart: Multipole order
| B1 | B2 | B3 | B4 | A2 | A3 | A4
Rc effect without core | 0.010544 | 0.0016817 | 0.0012994 | 0.00069716 | 0.0014761 | 0.0014585 | 0.0014827
Ra effect | 0.00013491 | 1.8977e-05 | 9.435e-06 | 5.5365e-06 | 1.697e-05 | 1.9327e-05 | 1.9327e-05
Rc effect with core | 0.0012437 | 0 | 7.5148e-05 | 0 | 0 | 0 | 0
Assuming:
Uncored cable
Ra = Rc = 1-4 µΩ
(distribution defined to fit MBHSP01 data)
Cored cable
Ra = 1-4 µΩ
Rc = 30 µΩ (homogeneus)
According to ROXIE:
Impact of Ra is 100 times smaller than the impact of Rc
With an homogeneous Rc = 30 µΩ, we can only produce allowed harmonics B1 and B3 that are one order of magnitude smaller than in the uncored case.
Analysis based on MBHSP01
[B. Auchmann]

## Slide 29: EM forces
Singe Coil
One aperture
Single coil |  |  |  |  | 
I(kA) | 14.24 | (80% Iss 2D) | Bp Coil (2D) (T) | 10.4 | 
Block | FORCE -X- | FORCE -Y- | FORCE ¦¦ | FORCE ¦- | FORCE ¦-/w
 | (N/m) | (N/m) | (N/m) | (N/m) | (MPa)
1 | 6.57E+05 | 4.88E+05 | 6.79E+05 | 4.44E+05 | 30
2 | 7.79E+05 | 8.53E+04 | 7.05E+05 | -3.32E+05 | -22
3 | 3.70E+05 | -2.96E+04 | 1.58E+05 | -3.36E+05 | -22
4 | 2.63E+05 | -2.86E+04 | 5.92E+04 | -2.58E+05 | -17
5 | -8.15E+04 | 4.09E+05 | -6.81E+04 | 4.17E+05 | 28
6 | 7.91E+05 | -7.95E+05 | 4.94E+04 | -1.13E+06 | -75
 |  |  |  |  | -40
Aperture |  |  |  |  | 
I(kA) | 11.85 | (80% Iss 2D) | Bp Coil (2D) (T) | 11.5 | 
Block | FORCE -X- | FORCE -Y- | FORCE ¦¦ | FORCE ¦- | FORCE ¦-/w
 | (N/m) | (N/m) | (N/m) | (N/m) | 
1 | 7.66E+05 | -9.39E+04 | 7.55E+05 | -1.42E+05 | -9
2 | 7.85E+05 | -1.39E+05 | 5.96E+05 | -5.26E+05 | -35
3 | 3.46E+05 | -5.70E+04 | 1.22E+05 | -3.29E+05 | -22
4 | 2.42E+05 | -3.34E+04 | 4.79E+04 | -2.39E+05 | -16
5 | 7.36E+04 | -3.85E+05 | 1.52E+04 | -3.95E+05 | -26
6 | 8.98E+05 | -8.82E+05 | 9.02E+04 | -1.27E+06 | -84
 |  |  |  |  | -97

## Slide 30: Inverse analysis
 | R17 |  | R22 | 
n | bn | an | bn | an
2 | 0.37 | 10.02 | -0.13 | 3.73
3 | 11.99 | -0.15 | 7.00 | -0.11
4 | 0.39 | -5.23 | 0.16 | -2.60
5 | -0.76 | 0.03 | 0.14 | 0.00
6 | -0.03 | 0.66 | -0.03 | 0.25
Right/left symmetric
Top/bottom anti-symmetric
a2, a4
Right/left symmetric
Top/bottom symmetry
b3
Right/left anti-symmetric
Top/bottom anti-symmetric
a1, a3
Right/left anti-symmetric
Top/bottom symmetry
b2,b4
As we are looking for high a2 and a4, but b1, b3, a1 and a3 are small…let’s look for the right/left symmetric tom/bottom anti-symmetric deformation model

## Slide 31: Mitigating the persistent-current induced sextupole
Passive compensation: ferromagnetic, passive strands
  Superconducting strands between cold bore and coil. Might reduce aperture by as much as 4 mm in diam.
However, the model cannot be used to predict effectiveness.
Design and construction should start now for test in the next magnet.
ferromagnetic shims
passive strands
B3 from PC
B5 from PC
Notes: check aperture requirements with B. Holzer