## Slide 1: Quench protection
Susana Izquierdo Bermudez
International Review of the HL-LHC 11 T Dipole for DS collimation
December 2014
Many thanks to H. Bajas, G. Chlachidze, J. Feuvrier, M. Karppinen, J. Rysti, G. Willering, A. Zlobin, and all the rest of the team that design, built and tested the magnets.

## Slide 2: Why protection is a critical issue?
1. Dramatically lower Cu/SC ratio  much lower margin in the cable
 | MB LHC inner layer | MB LHC outer layer | DS-11T
Total cable area, mm2 | 33.52 | 27.04 | 22.67
Cu area, mm2 | 15.53 | 13.43 | 8.23
SC area, mm2 | 9.41 | 6.89 | 6.84
Insulation area, mm2 | 4.83 | 4.70 | 3.25
Void area, mm2 | 3.75 | 2.03 | 4.00
 | MB | DS-11T dipole
Peak field in the conductor at Inom (Bp), T | 8.6 | 11.6
Differential inductance at Inom, mH/m | 6.9 | 11.7
Stored energy at Inom, mH/m | 484 | 897
Magnetic length, m | 14.312 | 2 x 5.3
Temperature margin, K | 1.8-6.5 | 4.4-14.3
2. More stored energy and substantially larger temperature margins
Comparing to the MB-LHC dipoles, in the case of DS-11 T we have:
We need to detect fast, and quench in a fast and efficient way!!

## Slide 3: The quench event
Quench initiation
Quench detection
Validation and power supply off
Quench heater effective
Quench heater provoked quench
10 ms
5 ms
Quench propagation within the coil
Quench heater delay and effectiveness
Initial propagation of the quench zone
Chart: time

## Slide 4: Quench initiation and detection
Quench initiation
Quench detection
Validation and power supply off
Quench heater effective
Quench heater provoked quench
10 ms
5 ms
Quench propagation within the coil
Quench heater delay and effectiveness
Initial propagation of the quench zone
Chart: time

## Slide 5: Longitudinal quench propagation
Chart: I [kA]
| 5 | 7 | 9 | 12 | 13
OL mid-plane (model) | 1.5 | 2.4 | 3.6 | 6.5 | 8
IL pole (model) | 1.9546 | 3.5 | 5.8 | 10.2 | 13.426 | 17.5
OL mid-plane 4.2 K (measured) | 1.2 | 2.2 | 3.8 | 6.2
IL pole 4.2 K (measured) | 5.4 | 8.1 | 9.5 | 12.5 | 13.8 | 15 | 18.3
Longitudinal propagation velocity was measured at different current levels, in cable stacks, SMC-11T and 11T dipoles at FNAL/CERN.
(details for CERN-11T measurements will by addressed by [G. Willering])
In all the cases, measured propagation velocity is close to the expected values.
Important to keep on mind  propagation is very slow at low current levels
SMC 11T. Experimental data from H. Bajas
MBHSM01. Experimental data from G. Chlachidze
Chart: I [kA]
| 2 | 4 | 6 | 8 | 10 | 11 | 12 | 13 | 14 | 15
Only conductor (4.2 K) | 1.0535 | 2.002 | 3.8043 | 7.2292 | 14.1295 | 18.941 | 25.508 | 34.871 | 48.7015 | 71.22
Only conductor (1.9 K) | 1.9929 | 3.75 | 7.1894 | 13.799 | 18.412 | 24.6235 | 33.1095 | 44.655 | 64.05
Conductor + Insulation (4.2 K) | 0.61692 | 1.1747 | 2.2367 | 4.2588 | 8.4495 | 11.1995 | 15.0095 | 20.5205 | 28.8745 | 42.8355
Conductor + Insulation (1.9 K) | 1.0989 | 2.1877 | 4.1891 | 8.2825 | 10.939 | 14.5325 | 19.656 | 26.432 | 38.6655
SMC11T (4.2 K) | 6.1905 | 21.6667 | 23.6364 | 25.4902 | 26.5306 | 24.0741 | 26.694 | 24.1187 | 25.2918 | 30.445 | 15.7767 | 19.0337 | 19.1176 | 20.0308 | 21.6667 | 16.25 | 24.1636 | 24.952 | 14.2857 | 26.6393 | 23.0496 | 31.401 | 17.0828 | 34.7594 | 34.2105 | 30.9524 | 33.3333 | 34.0314 | 36.5169
SMC11T (1.9 K) | 33.0789 | 26.3692 | 20.3125 | 21.0016 | 24.7619 | 17.7596 | 20.5047 | 17.2185 | 15.4762 | 31.7073 | 23.766 | 30.7329 | 24.5283 | 25.1451 | 25.4403 | 29.8165 | 30.2326 | 28.8889 | 32.9114 | 26.5306 | 33.5052
High field region
(natural quench)
Low field region
(spot heater quench)
Natural quenches in the high field region
model
Measu.
Remark: model considers conductor + insulation

## Slide 6: Voltage Threshold & Detection time
Chart: Time (s)
Expected resistive voltage growth for a quench initiated in the high field area
At high current, the quench propagates fast, so a threshold voltage of 100 mV – 400 mV is not having a great impact on the detection delay.
It becomes critical for protecting the magnet at low current 
it should be kept as low as possible.
Design value: 100 mV threshold and 10 ms validation delay.

## Slide 7: Quench heater delay and effectiveness
Quench initiation
Quench detection
Validation and power supply off
Quench heater effective
Quench heater provoked quench
10 ms
5 ms
Quench propagation within the coil
Quench heater delay and effectiveness
Initial propagation of the quench zone, longitudinal quench propagation
Chart: time

## Slide 8: Heater design
 | Low field heater strip | High field heater strip
Coverage (mm) (Stainless steel part) | 50 | 
Distance Between Stations (mm) (Copper plating) | 90 | 130
Width (mm) | 19 | 24
Stainless steel thickness (mm) | 0.025 | 
Copper plating thickness (mm) | 0.005 | 
SS
SS
Copper
Copper
Copper
Coverage
Distance between stations
width
Chart: I0 (A)
| 40 | 50 | 60 | 70 | 84 | 100 | 110 | 120 | 130 | 140 | 150
Low Field Region | 10.3196 | 16.1244 | 23.2191 | 31.6038 | 45.5094 | 64.4975 | 78.0419 | 92.8763 | 109.0007 | 126.415 | 145.1193
High Field Region | 6.4677 | 10.1057 | 14.5522 | 19.8072 | 28.5224 | 40.4229 | 48.9117 | 58.209 | 68.3147 | 79.2289 | 90.9515
Heaters are only present in the outer layer.
Heaters are copper plated to reduce the overall strip resistance (max. voltage across the heaters +-450 V).
Width of the heaters and distance between heater stations has been optimized to quench the coil in an uniform way.
4 heater circuits per aperture for redundancy (could be increased up to 8 per aperture).

## Slide 9: Heater delay
Chart: I/Iss (%)
| 28 | 34 | 39 | 45 | 51 | 56 | 62 | 67 | 73 | 79 | 84
Coil 105 (0.1 + 0.2 mm G10, MBHSM101) | 66.55 | 62.35 | 58.234 | 54.522 | 50.665 | 46.065 | 42.265 | 38.665 | 35.465 | 32.265 | 28.782
Coil 105 (0.1 + 0.1 mm G10, MBHSM101) | 42.15 | 39.35 | 36.92 | 34.506 | 32.411 | 30.411 | 28.611 | 26.811 | 25.211 | 23.706 | 22.306
Coil 106 (0.1 mm G10 MBHSP101) | 22.14 | 20.74 | 19.32 | 17.23 | 15.38 | 13.6 | 12 | 10.55 | 9.2 | 7.95
Coil 107 (0.1+0.1mm G10,MBHSP101) | 39.36 | 36.94 | 34.23 | 30.63 | 27.43 | 24.5 | 21.75 | 19.2 | 16.7 | 13.58
Experimental Coil 105 | 48 | 38.5 | 32 | 28.5
Experimental Coil 106 | 17 | 14.4 | 12.76
Experimental Coil 107 | 33 | 27.9 | 26.26
Heaters are glued on top of the coil after impregnation
The amount of insulation between heater and coil is the critical parameter
Iheater = 150 A
PdLF = 145 W/cm2
PdHF = 90 W/cm2
S2 glass (nominal = 0.2 mm)
0.025+ mm glue + 0.050 mm kapton
QUENCH HEATERS
4x0.5 mm kapton (ground insulation)
Minimizing the S2 glass between heater and coil, expected heaters delays in nominal operation conditions ~ 12 ms
Model [J. Rysti]
Experimental data [J. Feuvrier, G. Willering]
Quench heater onset
Thickness S2 glass between heater and coil | 
Coil 105 | 0.2 mm
Coil 106 | 0.0 mm
Coil 107 | 0.1 mm
[Coil 107: Preliminary data]
Only conductor insulation
Conductor insulation + 0.2 mm S2 glass
Conductor insulation + 0.1 mm S2 glass
Conductor insulation + 0.1 mm S2 glass

## Slide 10: Heater efficiency
18 ms
21ms
28 ms
35 ms
2 times to look at:
Quench heater onset (QO): start of the quench
Quench heater efficient (QE): time where slope of the resistive voltage cross the “time” axis
1.9 K, MBHSM101
Remarks:
At high current, the difference between QO-QE is very small, but at lower current there is an important offset to keep into account.
The difference between quench onset and quench efficient increases for low heater power density.
Experimental data from G. Willering

## Slide 11: Heater efficiency
Quench heaters are covering ~ 1/3 of the magnet in the longitudinal direction, but resistance growth is well reproduced by the model assuming that the entire magnet length is covered my heaters
Copper
Stainless steel
Heater pattern
Imagnet = 8 kA
Imagnet = 10 kA
Imagnet = 12 kA
Experimental data corresponds to MBHSM101
(CERN single coil assembly)
A decrease of the distance between the heater stations will not significantly improve the quench heater performance.
[G. Willering]

## Slide 12: Can we further optimize the outer layer heaters?
Chart: Quench heater current (A)
| 50 | 62.5 | 75 | 87.5 | 100 | 125 | 150 | 175 | 200 | 225 | 250
I/Iss = 50 % | 68.42 | 48.697 | 38.37 | 32.064 | 27.56 | 22.02 | 18.67 | 16.37 | 14.88 | 13.65 | 12.76
I/Iss = 80 % | 27.52 | 22.507 | 19.31 | 16.641 | 14.81 | 12.35 | 10.84 | 9.78 | 9 | 8.42 | 7.95
Operation Point | 0 | 80
Quench heaters are already covering most of the conductors in the outer layer. Two additional turns can potentially be covered if some voltage taps are removed, but the overall heater performance will not change significantly.
If the insulation between heater and coil is only the conductor insulation + 50 µm of kapton, further increase of the heater power density is not going to improve the heater performance.
The dominant parameters is the amount of insulation between heater and coil.
Not a lot of room for optimizing the outer layer heaters
(except further reduction of the insulation thickness between heater and coil)
Additional turns that can be potentially covered
QH cover 16.5 turns (out of 18)
QH cover: 14 turns (out of 16)

## Slide 13: Quench propagation within the coil
Quench initiation
Quench detection
Validation and power supply off
Quench heater effective
Quench heater provoked quench
10 ms
5 ms
Quench propagation within the coil
Quench heater delay and effectiveness
Initial propagation of the quench zone, longitudinal quench propagation
Chart: time

## Slide 14: Quench propagation within the coil
Chart: I/Iss (%)
| 44.943820224719097 | 56.179775280898873 | 67.415730337078642 | 78.651685393258418
B5 to B1 | 73 | 45 | 29 | 13
B6 to B2 | 84 | 51 | 33 | 28
B6 to B3 | 72 | 45 | 29
Measurements at FNAL and CERN show quench propagation from outer to inner layer in the order of 15 ms for 80 % Iss.
Experimental data from G. Chlachidze
1.9 K, MBHSM101
Experimental data from G. Willering
Agreement with the model is reasonable, given the uncertainties in the thermal conductivity properties of the material in the interlayer
Chart: I/Iss (%)
| 44.943820224719097 | 56.179775280898873 | 67.415730337078642 | 78.651685393258418
MEASURED | 73 | 45 | 29 | 13
Model (IL2OL insulation thickness = 0.2 mm G10) | 38 | 26 | 18.5 | 11
Model (IL2OL insulation thickness = 0.7mm G10) | 66.5 | 43 | 26.5
1.9 K, MBHSM101

## Slide 15: Quench Back & Dynamic Effects
Fast energy extraction tests were performed in the dipole mirror MBHSM01 shows that the “quench-back” effect is not present
If present, it will help to spread the magnet stored energy, but as there is not clear evidence of it, it is not being consider for the model
Chart: time [ms]
Reduction of apparent inductance due to the IFCC does not seem to play an dominant role at the expected range of dI/dt: current decay is pretty well reproduced neglecting dynamic effects
For higher dI/dt, this effect can have an important impact on the decay.
Measured
(MBHSM101)
Model
Experimental data from [G. Willering]
Extraction (dump), greater impact IFCC effect
Decay due to coil resistance growth, moderate dI/dt, small impact of IFCC
Experimental data from [G. Chlachidze]

## Slide 16: Quench Integral Studies
Measured difference = 1.2
According to the model = 1.4
Chart: Quench integral all QH fired 1.9 K
| 53.125 | 63.75 | 74.0625
QI (from heaters effective) | 9.6 | 10.3 | 10.75
Model (from heaters effective) | 8.877 | 9.625 | 10.1 | 10.483 | 10.7
QI (from heaters fired) | 12.93 | 13.8 | 14.45
Long heater delays (27 ms) compared to what we expect if the insulation between heater and coil is minimized (~15ms)
Chart: Quench Integral from QH effective 4.5K
| 17.502100252030242 | 35.004200504060485 | 49.005880705684682 | 63.007560907308878 | 71.408569028283395
Half of the heaters fired | 2.44 | 7.85 | 10.1 | 11.12 | 11.36
All heaters fired | 2.65 | 8.68 | 10.16
MBHSP02
Data from G. Chlachidze
MBHSP02
Data from G. Chlachidze
Quench integral studies performed at FNAL (MBHSP02):
Provoke heater discharge manually at the desired current
No energy extraction system  magnet protection rely only on the heaters
Equivalent studies on-going at CERN in MBHSP101. See talk [G. Willering].

## Slide 17: Hot spot temperature
 | MIITs detection & validation [MA2s] | MIITs from heaters fired to effective [MA2s] | MIITs decay [MA2s] | TOTAL MIITs [MA2s] | Tmax [K]
All the outer layer heaters fired | 2.5 | 2.5 | 11.0 | 16.0 | 335
Redundant configuration (only half of the heaters fired) | 2.5 | 2.5 | 12.5 | 17.5 | 400
Rdump = 150 mΩ
Cold diode
Uthr=6V, Rdiff=0.1 µΩ
L = 15.9 H
Quenching magnet
Quench under “accelerator conditions”:
Vthreshold = 100 mV
tvalidation = 10 ms
Quench starts in the high field region at the nominal operating current (11.85 kA)
Heater firing delay = 5 ms
Outer layer heaters can protect the magnet, but it is not a redundant system
Remarks:
MIITs vs. Tmax validated SMC-11T. Details will be addressed by [H. Bajas]
HQ02 high MIITs tests: 380+ K hot spot temperature without significant degradation

## Slide 18: How to improve the situation?
Action: Quench faster the Inner Layer.
Options:
  CLIQ (Coupling Loss Induced Quench): careful study needed to understand the interaction with the rest of the circuit. We cannot count on it for LS2.
  Inter layer heaters: as the temperature margin in the inner layer is lower, they will be efficient even with low power density and they will provide the needed redundancy to the system.
Chart: I/Iss (%)
| 34.106412005457024 | 40.927694406548433 | 47.748976807639835 | 54.570259208731244 | 61.391541609822639 | 68.212824010914048 | 75.034106412005457 | 81.855388813096866 | 88.676671214188261 | 95.49795361527967
OL delay with OL+IL heaters | 19.95 | 18.75 | 17.15 | 15.5 | 13.99 | 12.49 | 11.09 | 9.7 | 8.06 | 6.48
IL delay with OL+IL heaters | 60.75 | 51.6 | 43.15 | 35.5 | 28.99 | 23.19 | 17.89 | 12.93 | 8.1 | 3.65
OL delay with OL heater | 21.74 | 20.34 | 18.92 | 16.98 | 15.18 | 13.5 | 11.95 | 10.5 | 9.15 | 7.92
IL delay with OL heaters | 84.1094 | 59.7169 | 41.5745 | 26.9321
[J. Rysti]

## Slide 19: Inter layer Heaters
Inter layer heater under development.
Main concern: electrical integrity.
Design guideline: maximum voltage across the heaters ~ 150 V.
According to computations, at nominal magnet current, inter layer heaters are effective even if the power in the heater is low.
At lower magnet current, they will be also able to quench the magnet providing redundancy to the system.
Great technical challenge!
Chart: Interlayer heater power (W/cm2)
| 1 | 5 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Outer layer | 10.511 | 10.311 | 10.21 | 10.11 | 10.02 | 10 | 9.95 | 9.82 | 9.72 | 9.66 | 9.57 | 9.5
Inner layer | 43.574 | 24.736 | 19.25 | 16.1 | 14.8 | 14.12 | 13.6 | 13.27 | 12.99 | 12.8 | 12.54 | 12.38
[J. Rysti]
Nominal quench heater operation point
[J. Mazet]
But…if they don’t work, inter layer propagation might gets slower!
Inner layer heaters are not considered at the moment, but they are also a potential solution.

## Slide 20: Hot spot temperature
 | MIITs detection & validation [MA2s] | MIITs from heaters fired to effective [MA2s] | MIITs decay [MA2s] | TOTAL MIITs [MA2s] | Tmax [K]
All the outer layer heaters | 2.5 | 2.5 | 11.0 | 16.0 | 335
Outer layer in redundant configuration (only half of the heaters fired) | 2.5 | 2.5 | 12.5 | 17.5 | 400
Outer layer + Inter layer heaters | 2.5 | 1.7 | 10.5 | 14.6 | 290
Rdump = 150 mΩ
Cold diode
Uthr=6V, Rdiff=0.1 µΩ
L = 15.9 H
Quenching magnet
Quench under “accelerator conditions”:
Vthreshold = 100 mV
tvalidation = 10 ms
Quench starts in the high field region at the nominal operating current (11.85 kA)
Heater firing delay = 5 ms

## Slide 21: Summary
The low Cu/SC ratio combined with the large stored energy and temperature margins make the protection of the 11T dipole a non-trivial problem
Efficient heat transfer from quench heaters to coil is a must:
  Minimize insulation thickness assuring electrical integrity.
  Current design of outer layer heaters in terms of coverage/power density demonstrated good results in MBHSM101 and MBHSP101.
Outer layer heaters can protect the magnet, but not in a redundant configuration.
In order to provide redundancy to the system, inter layer heaters are being explored.

## Slide 22: Additional slides

## Slide 23: MBHSP101
Chart: Magnetic field [T]
| 11.360357881219903 | 12.30073187800963
VAMAS 1 -106, 1.9 K | 26.592 | 22.192
VAMAS 2 -106, 1.9 K | 32.036 | 26.768 | 22.256
Param.Godeke, 1.9 K | 60.9127 | 58.6355 | 56.4556 | 54.367 | 52.364 | 50.4413 | 48.5943 | 46.8188 | 45.1106 | 43.4663 | 41.8824 | 40.3558 | 38.8836 | 37.4633 | 36.0923 | 34.7684 | 32.6197 | 32.0714 | 31.0582 | 29.9024 | 28.7843 | 27.7023 | 26.655 | 25.6411 | 24.6593 | 23.7084 | 22.6967 | 22.3375 | 21.0301 | 20.192 | 19.3799 | 18.5927 | 17.8298 | 17.0902 | 16.3734 | 15.6785 | 15.005 | 14.3523 | 13.7196 | 13.1066 | 12.5125 | 11.937 | 11.3795 | 10.8396 | 10.3167 | 9.8106
VAMAS 1 - 106, 4.3 K | 24.328 | 19.748 | 15.86
VAMAS 2 - 106, 4.3 K | 24.288 | 19.7 | 15.872
VAMAS 3 - 106, 4.3 K | 24.472 | 19.892 | 15.928
Param. Godeke, 4.3 K | 48.7586 | 46.7619 | 44.8525 | 43.0249 | 41.2741 | 39.5955 | 37.985 | 36.4388 | 34.9533 | 33.5253 | 32.1519 | 30.8303 | 29.558 | 28.3325 | 27.1518 | 26.0137 | 24.1716 | 23.7027 | 22.8372 | 21.8521 | 20.9013 | 19.9836 | 19.0975 | 18.242 | 17.4159 | 16.6182 | 15.7722 | 15.4725 | 14.3852 | 13.6914 | 13.0214 | 12.3745 | 11.7501 | 11.1473 | 10.5657 | 10.0045 | 9.4631 | 8.9412 | 8.438 | 7.9532 | 7.4862 | 7.0366 | 6.6039 | 6.1878 | 5.7879 | 5.4037
Loadline Roxie 2D w SF | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
Loadline Roxie 3D w SF | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15

## Slide 24: MBHSM101
Chart: Magnetic field [T]
| 10.423019390048154 | 11.352172857142858 | 12.290812279293739
VAMAS 1 - XS, 1.9 K | 31.216 | 25.988 | 21.46
VAMAS 2 - XS, 1.9 K | 30.408 | 25.36 | 20.872
Param. XS, 1.9 K | 58.2681 | 56.1056 | 54.0288 | 52.0327 | 50.1127 | 48.2646 | 46.4846 | 44.7691 | 43.1149 | 41.519 | 39.9786 | 38.491 | 37.0539 | 35.6651 | 34.3224 | 33.024 | 30.9131 | 30.3739 | 29.3766 | 28.2381 | 27.1358 | 26.0684 | 25.0347 | 24.0335 | 23.0636 | 22.1241 | 21.1245 | 20.7695 | 19.4778 | 18.6502 | 17.8485 | 17.0718 | 16.3196 | 15.591 | 14.8854 | 14.2022 | 13.5409 | 12.9007 | 12.2812 | 11.6819 | 11.1023 | 10.5418 | 10 | 9.4765 | 8.9708 | 8.4826
VAMAS 1 - XS, 4.3 K | 23.908 | 19.36 | 15.4
Param. XS, 4.3 K | 47.2108 | 45.2782 | 43.4246 | 41.6454 | 39.9365 | 38.294 | 36.7146 | 35.1949 | 33.732 | 32.3233 | 30.9661 | 29.6581 | 28.3971 | 27.1811 | 26.0083 | 24.8767 | 23.0433 | 22.5763 | 21.7141 | 20.7324 | 19.7847 | 18.8699 | 17.9867 | 17.1342 | 16.3112 | 15.517 | 14.6753 | 14.3773 | 13.2972 | 12.6088 | 11.9451 | 11.3052 | 10.6885 | 10.0943 | 9.5221 | 8.9713 | 8.4413 | 7.9316 | 7.4416 | 6.971 | 6.5192 | 6.0858 | 5.6705 | 5.2726 | 4.892 | 4.5282
VAMAS 2 - XS, 4.3 K | 23.172 | 18.636 | 14.74
Loadline Roxie 2D w SF | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12 | 12.5 | 13 | 13.5 | 14 | 14.5 | 15 | 15.5 | 16 | 16.5 | 17 | 17.5 | 18 | 18.5 | 19 | 19.5 | 20
Loadline Roxie 2D wo SF | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12 | 12.5 | 13 | 13.5 | 14 | 14.5 | 15 | 15.5 | 16 | 16.5 | 17 | 17.5 | 18 | 18.5 | 19 | 19.5 | 20
Loadline Roxie 3D w SF | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12 | 12.5 | 13 | 13.5 | 14 | 14.5 | 15 | 15.5 | 16 | 16.5 | 17 | 17.5 | 18 | 18.5 | 19 | 19.5 | 20
Loadline Roxie 3D wo SF | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12 | 12.5 | 13 | 13.5 | 14 | 14.5 | 15 | 15.5 | 16 | 16.5 | 17 | 17.5 | 18 | 18.5 | 19 | 19.5 | 20

## Slide 25: MIITs vs. Tmax
H. Bajas

## Slide 26: Model validation SMC-11T

## Slide 27: “Time budget” for detectio
Resistive voltage growth for a quench initiated in the high field area
Chart: Imagnet (kA)
| 12 | 10 | 8 | 6 | 4 | 2
Vth= 100 mV | 18.6333 | 24.4 | 34.675 | 58.3333 | 93.5
Vth= 200 mV | 17.2333 | 22.6 | 30.875 | 37.3333 | 1.5
Vth= 300 mV | 16.6333 | 20.4 | 23.475 | 13.3333
Vth= 400 mV | 15.6333 | 17.4 | 16.075 | -7.6667

## Slide 28: Temperature Margin
MB-LHC
DS-11T

## Slide 29: QH Design Guidelines
Design should be suitable for a 5.5 m length magnet
The distance between heating stations should be such that the heat has to propagate between stations in less than 5 ms.
  For longitudinal propagation ≈ 10 m/s, distance ≈ 100 mm
Kapton insulation thickness from heater to coil should be minimized, but guarantee a good electrical insulation from heater to coil.
  50 µm seems to be minimum reliable Kapton thickness
Heat power density in the heating station should be as high as possible, but the temperature in the heater under adiabatic conditions should not increase above 350K.
  Experimental data from LARP magnets and 11T FNAL show that PO ≈ 50-80 W/cm2 heater delay starts saturating, but first short models PO up to 150 W/cm2 to find the optimal power density.
Heat as many turns as possible in the azimuthal direction.
Power density in the low field region should be higher than in the high field region to quench the magnet in a more uniform way.
No sharp edges, keeping the geometry of the heaters as simple and robust as possible.
If possible, use standard LHC QH power supply.
  Total capacitance 7.05 mF , maximum voltage ± 500V.
  Maximum current for continuous operation = 135 A
  Peak current at 25 ˚C for 10 ms =1700 A (it will probably destroy the PCB of the power supply)
  Can be safely operated up to 300 A
At least two independent circuits per aperture (for redundancy)

## Slide 30: Overview QH design
More details can be found in https://indico.cern.ch/event/311824/
  Main features:
  Stainless steel 25 µm thick, partially plated with 5 µm thick layer of copper to reduce their overall resistance (design suitable for 5.5 m length)
  Heating stations are 19 mm wide in the mid-plane (LF) and 24 mm wide in pole area (HF)
  The distance in between non-plated sections is 90 mm in the LF and 130 mm in the HF where quench propagation is faster in the longitudinal direction.
  The heaters are embedded in between two layers of polyimide insulation foils. The thickness of the insulation between the heater and the coil is composed of 0.050 mm of polyimide, about 0.025 mm of Epoxy glue plus the additions S2 glass added to the coil outer radius during impregnation.
  The trace is then glued to the coil and compressed radially during collaring to about 40 MPa.
Coverage
Distance between stations
width
0.2 mm S2 glass
0.025+ mm glue + 0.050 mm kapton
QUENCH HEATERS
4x0.5 mm kapton (ground insulation)
Chart: Heater Current (A)
| 40 | 50 | 60 | 70 | 80 | 100 | 110 | 120 | 130 | 140 | 150
Low Field Region | 13.8283 | 21.6066 | 31.1136 | 42.349 | 55.313 | 86.4266 | 104.5762 | 124.4543 | 146.0609 | 169.3961 | 194.4598
High Field Region | 8.6667 | 13.5417 | 19.5 | 26.5417 | 34.6667 | 54.1667 | 65.5417 | 78 | 91.5417 | 106.1667 | 121.875

## Slide 31: Trace manufacturing and characterization
Resistance measurements at RT and 77 K
  Stainless steel stations: Measured resistance close to expected values
    3% difference at RT
    8 % difference at 77K
  Copper regions: Measured resistance higher
  than expected value
    20% difference at RT
    25 % difference at 77K
High current test
  No degradation was observed in the bonding
Temperature cycling at 77 K
  No degradation
Chart: Resistance @ RT
HF_Copper | 24.8 | 23.1 | 25.5 | 23.8 | 23.8
HF_Stainless Steel | 61.3 | 60.9 | 61.1 | 61.4 | 59.2
LF_Copper | 20.9 | 18.9 | 21.3 | 20.7 | 19.8
LF_Stainless Steel | 78 | 78 | 76 | 75.9 | 77.5 | 74.7 | 73.4
HF_Copper Expected | 19.4783 | 19.4783
LF_Copper Expected | 17.0337 | 17.0337
HF_Stainless Steel Expected | 60.4583 | 60.4583
LF_Stainless Steel Expected | 76.3684 | 76.3684
LF_Copper Expected if 4 um | 21.3 | 21.3
HF_Copeer Expected if 4 um | 24.3 | 24.3
Kapton (50 µm)
Glue (<25 µm)
Stainless Steel (25 µm)
Copper (5 µm)
Glue (50 µm)
Kapton (25 µm)
Trace stack for 11T
ρss=7.3·10-7Ωm, RRRSS=1.34
ρss=1.8·10-8Ωm, RRRSS=30

## Slide 32: Trace QA
Before trace installation
Resistance measurements at RT
High voltage test to ground under 20-30 MPa pressure (2kV).
After trace installation, every step of the manufacturing process
Expected value: R1=R2=1.65 Ω
Measured value ≈ 1.7 Ω
Resistance
QH to ground and QH to coil (1 kV)
Discharge test (pulse). Low thermal load to the heaters (under adiabatic conditions and assuming constant material properties, peak current defined to limit the temperature increase to 50 K) (only in the manufacturing steps after collaring)

## Slide 33: Impact of insulation material/thickness

## Slide 34: Quench Heater Delay
Large difference between “Quench Onset (QO)” and “Quench heater efficient (QE)” at low currents.
From now on, if not specified, heater delays plotted correspond to the “Quench Onset” and not “Quench Efficient”

## Slide 35: Comparison to FNAL 11T dipoles
MBHSM101
FNAL MBHSM% insulation between heater and coil:
  0.125 mm of glass on the outer, impregnated with the coil
  0.125 mm of kapton between heater and coil
CERN MBHSM101insulation between heater and coil:
  0.200-0.250 mm of glass on the outer, impregnated with the coil
  0.050 mm of kapton between heater and coil + about 0.025 mm glue
FNAL data from https://indico.cern.ch/event/311824/
Slides from Guram Chlachidze
Heater delays are very close to delays measured in FNAL

## Slide 36: Comparison to HQ
HQ data data from https://indico.cern.ch/event/311824/
Slides from Tiina Slami
Significant longer delays than in HQ.
Main difference: in the case of 11T, heaters are glued on top of the coil after impregnation

## Slide 37: Quench Heater Temperature
IQH= 150 A

## Slide 38
Cu
Cu
Stainless steel
60 % variation in current density (160 % in )
Less than 0.1 % variation in current density (~ 0.1 % in )
[J. Rysti]
Scalar magneto-resistance

## Slide 39
Cu
Cu
Stainless steel
5 % variation in current density (8 % in )
[J. Rysti]
Hall effect

## Slide 40: Inter layer heaters
Pd IL heaters = 50 W/cm2
Pd IL heaters = 100 W/cm2

## Slide 41: Inter layer heaters
Chart: U (V)
| 50 | 100 | 150 | 200 | 250 | 300 | 350 | 400
real coil | 6.833 | 27.3322 | 61.4974 | 109.3288 | 170.8262 | 245.9897 | 334.8193 | 437.315

## Slide 42: STANDARD LHC HEATER POWER SUPPLIES
Supply based on the thyristor-triggered discharge of aluminium electrolytic capacitors.
Each power supply contains a bank with 6 capacitors (4.7 mF/500V) where two sets of 3 parallel capacitors are connected in series  total capacitance 7.05 mF
Nominal operating voltage 450 V (90 % of the maximum voltage)
OPERATION: Peak current about 85 A, giving a maximum stored energy of 2.86 kJ
Actual limitations in terms of current
Power supply equipped with two SKT80/18E type thyristors rated for 80 A at 85 ˚C.
Maximum current for continuous operation = 135 A
Peak current at 25 ˚C for 10 ms =1700 A (it will probably destroy the PCB of the power supply)
Can be safely operated up to 300 A (resistive load in LHC from 12Ω in most of the circuits to 3.1 Ω in some systems such as D1 protection )
QUENCH HEATER EXPERIMENTS ON THE LHC MAIN SUPERCONDUCTING MAGNETS
F. Rodriguez-Mateos, P. Pugnat,S. Sanfilippo, R. Schmidt, A. Siemko, F. Sonnemann

## Slide 43: Protection System LHC Magnets
The Protection System for the Superconducting Elements of the Large Hadron Collider at CERN
K. Dahlerup-Petersen1, R. Denz1, J.L. Gomez-Costa1, D. Hagedorn1, P. Proudlock1, F. Rodriguez-Mateos1, R. Schmidt1 and F. Sonnemann2

## Slide 44: Modelling heat propagation within the coil
Two principal directions:
1. Longitudinal
Length scale is hundreds of m
2. Transverse
Length scale is tenths of mm
Power exchanged between components in the conductor
Joule heating
External heat perturbation
The conductor is a continuum solved with accurate (high order) and adaptive (front tracking) methods
Longitudinal
Transverse
Power exchange between adjacent conductors
2nd order thermal network explicitly coupling with the 1D longitudinal model: