Modification of field emitters by electromigration
Stefan Parviainen, Flyura Djurabekova

---
Contents
- Background
- What is electromigration?
- Modeling electromigration in HELMOD
- Results
- Conclusions

---
Background
- Field emission is measured prior to vacuum breakdown in CLIC structures
- Measured current is “suspiciously” high, corresponds to a surface feature with high aspect ratio (β = ~50-100)
  - Not 100% clear if β is from geometry or not
- These features have not been definitely identified with SEM. Where are they???
  - See the presentation by P. Serbun

---
Where are the field emitters
- Our theory:
  - Field emitters may grow spontaneously under an electric field
  - Some emitters are destroyed during the field emission process
    - Partial melting due to resistive heating?
    - Field evaporation due to high field?
    - High internal forces from the field emission current? (this work)
  - Remaining emitters flatten once the field is removed
    - See talk by V. Jansson
E

---
Current densities in an emitter
Breakdowns occur about here

---
Temperature reached in emitter

---
Electromigration
Impurity
Linear77/Wikipedia
Electron wind force:
bold{F} = bold{E}_"int" (Z_"d" + Z_"w")
P. Zörner

---
Effective charge
bold{F} = bold{E}_"int" (Z_d + Z_w) = bold{E}_"int" Z^"*"
Effective valence
Direct Ion valence
Wind valence
- Both Zd and Zw are difficult to determine precisly
- Zd is affected by screening in a metal
- Zw depends on the electron transport corss section
  - Difficult to calculate (Possible project coming)

---
“Electromigration” in HELMOD
- We want to include this effect in our HELMOD code
  - Classical electromigration is a diffusion process: not suitable for study with MD
  - But other interesting effects appear
  - Electromigration proper will be probably be included in the KMC model by V. Jansson et al.

---
JFN
HELMOD quick recap
- Hybrid electrodynamics - molecular dynamics code with support for various electronic effects, e.g.
  - Dynamic field calculation
  - Induced surface charge and Lorentz force on atoms
  - Calculation of field emission current and resulting resistive heating

---
“Electromigration” in HELMOD
- Implemented as additional ”electron wind force” acting on atoms in protrusion
- Force proportional to the internal electric field and effective valence of surface copper atoms as seen by current
bold{E}_{"int"} = bold{J_{FN}}/%sigma
bold{F} = bold{E}_"int" Z^"*"
Z^"*" approx 10..100
- Assume current (and force) is going straight upwards
  - actually follows surface geometry
- Apply on surface atoms (impurities), assume effective charge Z* is constant

---
Stretching of emitter
- Whole emitter is stretched out by the electron wind force
- Large strain is seen at the base of the structure
No wind
Large strain at the base
(Color indicates strain)

---
Reduction in critical field
  - Protrusion with height 6.5nm, diameter 2nm, 300K

---
Conclusions
- We have large current densities in our field emitters
  - Electromigration should become an issue
  - MD is too slow to handle proper electromigration (diffusion process)
  - Electron wind force implemented into HELMOD
  - The wind force is sufficient to stretch emitters, reducing the critical field for their destruction

---
My current work contract is ending this year ...